Electronic Supplementary Information (ESI)  (02/7/22)

Synthesis and pH-variable ultracentrifugation molecular weight measurements of the dimeric, Ti-O-Ti bridged anhydride form of novel di-TiIV-1,2-substituted -Keggin polyoxotungstate.  Molecular Structure of [(-1,2-PW10Ti2O39)2]10- polyoxoanion†

Kenji Nomiya, *a Mizuto Takahashi, a Jason A. Widegren, b Takao Aizawa, a Yoshitaka Sakai a and Noriko C. Kasuga a

a Department of Materials Science, Faculty of Science, Kanagawa University, Hiratsuka, Kanagawa 259-1293, Japan.  E-mail: nomiya@chem.kanagawa-u.ac.jp

b Department of Chemistry, Colorado State University, Fort Collins, CO 80523, USA

Bond lengths and angles of compound 1, which are not listed in Table 2, are deposited in Table S1.

# Table S1.  Bond lengths (Å) and angles (o) for polyoxoanion 1

Distances(Å)

atom	atom	distance		atom	atom	distance

W(1)	O(3)	1.71(2)		W(1)	O(4)	1.84(1)

W(1)	O(6)	1.83(2)		W(1)	O(11)	2.00(2)

W(1)	O(12)	1.98(1)		W(1)	O(37)	2.45(2)

W(2)	O(12)	1.87(2)		W(2)	O(13)	1.88(1)

W(2)	O(18)	1.92(2)		W(2)	O(19)	1.93(2)

W(2)	O(28)	1.68(2)		W(2)	O(37)	2.46(1)

W(3)	O(7)	1.83(2)		W(3)	O(13)	1.94(1)

W(3)	O(14)	1.88(2)		W(3)	O(20)	1.98(2)

W(3)	O(29)	1.72(2)		W(3)	O(38)	2.43(1)

W(4)	O(8)	1.81(2)		W(4)	O(14)	1.96(1)

W(4)	O(15)	1.95(1)		W(4)	O(21)	1.97(2)

W(4)	O(30)	1.74(2)		W(4)	O(38)	2.46(1)

W(5)	O(9)	1.85(1)		W(5)	O(15)	1.89(1)

atom	atom	distance		atom	atom	distance

W(5)	O(16)	1.91(2)		W(5)	O(22)	1.96(2)

W(5)	O(31)	1.75(2)		W(5)	O(39)	2.43(1)

W(6)	O(10)	1.86(2)		W(6)	O(16)	1.94(2)

W(6)	O(17)	1.91(2)		W(6)	O(23)	1.95(2)

W(6)	O(32)	1.72(2)		W(6)	O(39)	2.43(1)

W(7)	O(11)	1.86(2)		W(7)	O(17)	1.91(2)

W(7)	O(18)	1.91(1)		W(7)	O(24)	1.91(2)

W(7)	O(33)	1.74(2)		W(7)	O(37)	2.42(2)

W(8)	O(19)	1.90(2)		W(8)	O(20)	1.86(2)

W(8)	O(25)	1.92(2)		W(8)	O(27)	1.92(2)

W(8)	O(34)	1.71(2)		W(8)	O(40)	2.43(1)

W(9)	O(21)	1.86(2)		W(9)	O(22)	1.86(2)

W(9)	O(25)	1.93(2)		W(9)	O(26)	1.94(2)

W(9)	O(35)	1.75(2)		W(9)	O(40)	2.45(1)

W(10)	O(23)	1.92(2)		W(10)	O(24)	1.91(2)

W(10)	O(26)	1.90(2)		W(10)	O(27)	1.93(1)

atom	atom	distance		atom	atom	distance

W(10)	O(36)	1.77(2)		W(10)	O(40)	2.44(2)

W(11)	O(41)	1.71(2)		W(11)	O(42)	1.82(1)

W(11)	O(44)	1.84(1)		W(11)	O(49)	2.02(2)

W(11)	O(50)	2.02(2)		W(11)	O(75)	2.45(2)

W(12)	O(49)	1.83(2)		W(12)	O(55)	1.91(1)

W(12)	O(56)	1.93(1)		W(12)	O(62)	1.94(2)

W(12)	O(71)	1.71(2)		W(12)	O(75)	2.42(2)

W(13)	O(48)	1.82(2)		W(13)	O(54)	1.93(2)

W(13)	O(55)	1.94(2)		W(13)	O(61)	1.93(2)

W(13)	O(70)	1.72(2)		W(13)	O(77)	2.42(1)

W(14)	O(47)	1.85(2)		W(14)	O(53)	1.92(1)

W(14)	O(54)	1.94(2)		W(14)	O(60)	1.94(2)

W(14)	O(69)	1.73(2)		W(14)	O(77)	2.43(1)

W(15)	O(46)	1.83(2)		W(15)	O(52)	1.91(1)

W(15)	O(53)	1.93(1)		W(15)	O(59)	1.94(2)

W(15)	O(68)	1.71(2)		W(15)	O(76)	2.41(1)

atom	atom	distance		atom	atom	distance

W(16)	O(45)	1.84(2)		W(16)	O(51)	1.95(2)

W(16)	O(52)	1.93(2)		W(16)	O(58)	1.97(2)

W(16)	O(67)	1.72(2)		W(16)	O(76)	2.44(1)

W(17)	O(50)	1.86(2)		W(17)	O(51)	1.89(2)

W(17)	O(56)	1.88(1)		W(17)	O(57)	1.89(2)

W(17)	O(66)	1.72(2)		W(17)	O(75)	2.45(1)

W(18)	O(61)	1.90(2)		W(18)	O(62)	1.90(2)

W(18)	O(64)	1.93(2)		W(18)	O(65)	1.90(1)

W(18)	O(74)	1.72(2)		W(18)	O(78)	2.47(2)

W(19)	O(59)	1.89(2)		W(19)	O(60)	1.92(1)

W(19)	O(63)	1.94(2)		W(19)	O(64)	1.94(2)

W(19)	O(73)	1.70(2)		W(19)	O(78)	2.46(1)

W(20)	O(57)	1.95(2)		W(20)	O(58)	1.89(2)

W(20)	O(63)	1.89(2)		W(20)	O(65)	1.93(1)

W(20)	O(72)	1.71(2)		W(20)	O(78)	2.45(1)

Ti(1)	O(1)	1.81(2)		Ti(1)	O(4)	1.93(2)

atom	atom	distance		atom	atom	distance

Ti(1)	O(5)	1.81(1)		Ti(1)	O(7)	2.00(2)

Ti(1)	O(8)	1.96(2)		Ti(1)	O(38)	2.37(2)

Ti(2)	O(2)	1.80(2)		Ti(2)	O(5)	1.83(1)

Ti(2)	O(6)	1.92(2)		Ti(2)	O(9)	2.02(1)

Ti(2)	O(10)	2.01(2)		Ti(2)	O(39)	2.35(2)

Ti(3)	O(1)	1.83(2)		Ti(3)	O(43)	1.82(1)

Ti(3)	O(44)	1.94(2)		Ti(3)	O(47)	1.98(2)

Ti(3)	O(48)	2.04(2)		Ti(3)	O(77)	2.31(2)

Ti(4)	O(2)	1.84(2)		Ti(4)	O(42)	1.95(2)

Ti(4)	O(43)	1.84(1)		Ti(4)	O(45)	2.00(1)

Ti(4)	O(46)	2.00(1)		Ti(4)	O(76)	2.34(2)

K(4)	K(5)	2.59(5)		K(6)	K(7)	2.68(6)

P(1)	O(37)	1.55(2)		P(1)	O(38)	1.51(2)

P(1)	O(39)	1.54(1)		P(1)	O(40)	1.53(2)

P(2)	O(75)	1.54(2)		P(2)	O(76)	1.57(2)

P(2)	O(77)	1.56(1)		P(2)	O(78)	1.50(2)

Angles(°)

atom	atom	atom	angle		atom	atom	atom	angle

O(3)	W(1)	O(4)	104.5(8)		O(3)	W(1)	O(6)	103.7(7)

O(3)	W(1)	O(11)	99.5(8)		O(3)	W(1)	O(12)	101.6(7)

O(3)	W(1)	O(37)	166.8(7)		O(4)	W(1)	O(6)	91.0(7)

O(4)	W(1)	O(11)	155.4(7)		O(4)	W(1)	O(12)	89.5(6)

O(4)	W(1)	O(37)	85.9(6)		O(6)	W(1)	O(11)	88.4(7)

O(6)	W(1)	O(12)	153.7(7)		O(6)	W(1)	O(37)	83.8(6)

O(11)	W(1)	O(12)	80.4(7)		O(11)	W(1)	O(37)	69.5(6)

O(12)	W(1)	O(37)	70.0(6)		O(12)	W(2)	O(13)	91.3(7)

O(12)	W(2)	O(18)	87.4(7)		O(12)	W(2)	O(19)	153.7(6)

O(12)	W(2)	O(28)	104.1(8)		O(12)	W(2)	O(37)	71.4(6)

O(13)	W(2)	O(18)	155.8(6)		O(13)	W(2)	O(19)	85.1(7)

O(13)	W(2)	O(28)	100.7(7)		O(13)	W(2)	O(37)	84.7(6)

O(18)	W(2)	O(19)	85.5(7)		O(18)	W(2)	O(28)	103.0(7)

O(18)	W(2)	O(37)	72.0(6)		O(19)	W(2)	O(28)	102.1(8)

atom	atom	atom	angle		atom	atom	atom	angle

O(19)	W(2)	O(37)	82.4(6)		O(28)	W(2)	O(37)	173.2(7)

O(7)	W(3)	O(13)	92.1(7)		O(7)	W(3)	O(14)	90.9(7)

O(7)	W(3)	O(20)	154.7(6)		O(7)	W(3)	O(29)	104.3(8)

O(7)	W(3)	O(38)	73.8(6)		O(13)	W(3)	O(14)	155.6(6)

O(13)	W(3)	O(20)	80.3(6)		O(13)	W(3)	O(29)	101.7(7)

O(13)	W(3)	O(38)	83.8(5)		O(14)	W(3)	O(20)	86.7(7)

O(14)	W(3)	O(29)	101.0(7)		O(14)	W(3)	O(38)	73.8(6)

O(20)	W(3)	O(29)	100.9(7)		O(20)	W(3)	O(38)	81.3(5)

O(29)	W(3)	O(38)	174.2(7)		O(8)	W(4)	O(14)	89.2(7)

O(8)	W(4)	O(15)	90.6(6)		O(8)	W(4)	O(21)	155.7(7)

O(8)	W(4)	O(30)	102.1(8)		O(8)	W(4)	O(38)	73.8(6)

O(14)	W(4)	O(15)	155.2(6)		O(14)	W(4)	O(21)	85.6(7)

O(14)	W(4)	O(30)	101.5(7)		O(14)	W(4)	O(38)	72.1(5)

O(15)	W(4)	O(21)	84.4(6)		O(15)	W(4)	O(30)	102.8(7)

O(15)	W(4)	O(38)	84.0(5)		O(21)	W(4)	O(30)	102.2(8)

O(21)	W(4)	O(38)	82.1(6)		O(30)	W(4)	O(38)	172.2(7)

atom	atom	atom	angle		atom	atom	atom	angle

O(9)	W(5)	O(15)	89.9(6)		O(9)	W(5)	O(16)	90.6(7)

O(9)	W(5)	O(22)	157.4(6)		O(9)	W(5)	O(31)	101.6(7)

O(9)	W(5)	O(39)	75.7(6)		O(15)	W(5)	O(16)	155.8(7)

O(15)	W(5)	O(22)	84.1(7)		O(15)	W(5)	O(31)	104.2(7)

O(15)	W(5)	O(39)	84.3(5)		O(16)	W(5)	O(22)	86.2(7)

O(16)	W(5)	O(31)	99.4(7)		O(16)	W(5)	O(39)	72.4(6)

O(22)	W(5)	O(31)	101.0(7)		O(22)	W(5)	O(39)	82.0(6)

O(31)	W(5)	O(39)	171.2(6)		O(10)	W(6)	O(16)	90.2(7)

O(10)	W(6)	O(17)	91.2(7)		O(10)	W(6)	O(23)	158.2(6)

O(10)	W(6)	O(32)	102.2(8)		O(10)	W(6)	O(39)	74.9(5)

O(16)	W(6)	O(17)	154.9(7)		O(16)	W(6)	O(23)	84.6(7)

O(16)	W(6)	O(32)	101.0(8)		O(16)	W(6)	O(39)	72.0(6)

O(17)	W(6)	O(23)	84.8(7)		O(17)	W(6)	O(32)	103.2(8)

O(17)	W(6)	O(39)	84.2(6)		O(23)	W(6)	O(32)	99.6(8)

O(23)	W(6)	O(39)	83.4(6)		O(32)	W(6)	O(39)	172.2(7)

O(11)	W(7)	O(17)	91.8(8)		O(11)	W(7)	O(18)	87.5(7)

atom	atom	atom	angle		atom	atom	atom	angle

O(11)	W(7)	O(24)	154.8(7)		O(11)	W(7)	O(33)	102.1(9)

O(11)	W(7)	O(37)	72.4(7)		O(17)	W(7)	O(18)	155.9(7)

O(17)	W(7)	O(24)	83.9(7)		O(17)	W(7)	O(33)	103.0(8)

O(17)	W(7)	O(37)	83.5(6)		O(18)	W(7)	O(24)	86.7(6)

O(18)	W(7)	O(33)	100.7(8)		O(18)	W(7)	O(37)	73.3(6)

O(24)	W(7)	O(33)	103.1(8)		O(24)	W(7)	O(37)	82.5(6)

O(33)	W(7)	O(37)	171.7(8)		O(19)	W(8)	O(20)	85.7(7)

O(19)	W(8)	O(25)	155.6(7)		O(19)	W(8)	O(27)	87.0(7)

O(19)	W(8)	O(34)	104.2(8)		O(19)	W(8)	O(40)	82.7(6)

O(20)	W(8)	O(25)	90.7(7)		O(20)	W(8)	O(27)	154.4(7)

O(20)	W(8)	O(34)	104.0(7)		O(20)	W(8)	O(40)	82.8(6)

O(25)	W(8)	O(27)	85.9(7)		O(25)	W(8)	O(34)	100.1(7)

O(25)	W(8)	O(40)	72.8(6)		O(27)	W(8)	O(34)	101.5(8)

O(27)	W(8)	O(40)	72.0(6)		O(34)	W(8)	O(40)	170.5(7)

O(21)	W(9)	O(22)	86.9(7)		O(21)	W(9)	O(25)	88.9(7)

O(21)	W(9)	O(26)	154.9(7)		O(21)	W(9)	O(35)	104.0(8)

atom	atom	atom	angle		atom	atom	atom	angle

O(21)	W(9)	O(40)	83.5(6)		O(22)	W(9)	O(25)	155.7(7)

O(22)	W(9)	O(26)	89.1(7)		O(22)	W(9)	O(35)	102.8(8)

O(22)	W(9)	O(40)	83.6(6)		O(25)	W(9)	O(26)	84.6(7)

O(25)	W(9)	O(35)	101.4(8)		O(25)	W(9)	O(40)	72.2(6)

O(26)	W(9)	O(35)	101.0(9)		O(26)	W(9)	O(40)	71.5(6)

O(35)	W(9)	O(40)	170.3(8)		O(23)	W(10)	O(24)	87.2(7)

O(23)	W(10)	O(26)	88.8(7)		O(23)	W(10)	O(27)	156.3(8)

O(23)	W(10)	O(36)	101.7(8)		O(23)	W(10)	O(40)	84.7(6)

O(24)	W(10)	O(26)	154.9(7)		O(24)	W(10)	O(27)	87.9(6)

O(24)	W(10)	O(36)	105.8(8)		O(24)	W(10)	O(40)	82.5(6)

O(26)	W(10)	O(27)	85.8(7)		O(26)	W(10)	O(36)	99.3(8)

O(26)	W(10)	O(40)	72.4(6)		O(27)	W(10)	O(36)	102.0(8)

O(27)	W(10)	O(40)	71.7(6)		O(36)	W(10)	O(40)	169.6(7)

O(41)	W(11)	O(42)	105.4(8)		O(41)	W(11)	O(44)	104.0(7)

O(41)	W(11)	O(49)	99.6(7)		O(41)	W(11)	O(50)	100.1(7)

O(41)	W(11)	O(75)	165.9(7)		O(42)	W(11)	O(44)	93.0(7)

atom	atom	atom	angle		atom	atom	atom	angle

O(42)	W(11)	O(49)	154.3(7)		O(42)	W(11)	O(50)	87.8(7)

O(42)	W(11)	O(75)	85.0(6)		O(44)	W(11)	O(49)	86.8(7)

O(44)	W(11)	O(50)	154.7(7)		O(44)	W(11)	O(75)	84.6(6)

O(49)	W(11)	O(50)	81.8(6)		O(49)	W(11)	O(75)	69.3(6)

O(50)	W(11)	O(75)	70.3(6)		O(49)	W(12)	O(55)	90.3(7)

O(49)	W(12)	O(56)	88.7(6)		O(49)	W(12)	O(62)	156.0(7)

O(49)	W(12)	O(71)	102.1(8)		O(49)	W(12)	O(75)	72.8(6)

O(55)	W(12)	O(56)	155.1(6)		O(55)	W(12)	O(62)	84.7(7)

O(55)	W(12)	O(71)	103.2(8)		O(55)	W(12)	O(75)	84.4(6)

O(56)	W(12)	O(62)	86.2(7)		O(56)	W(12)	O(71)	101.4(7)

O(56)	W(12)	O(75)	71.5(6)		O(62)	W(12)	O(71)	101.9(8)

O(62)	W(12)	O(75)	83.4(6)		O(71)	W(12)	O(75)	171.1(7)

O(48)	W(13)	O(54)	91.1(7)		O(48)	W(13)	O(55)	91.2(7)

O(48)	W(13)	O(61)	156.1(6)		O(48)	W(13)	O(70)	103.4(7)

O(48)	W(13)	O(77)	73.8(6)		O(54)	W(13)	O(55)	157.1(6)

O(54)	W(13)	O(61)	85.0(7)		O(54)	W(13)	O(70)	100.1(7)

atom	atom	atom	angle		atom	atom	atom	angle

O(54)	W(13)	O(77)	73.7(6)		O(55)	W(13)	O(61)	83.7(7)

O(55)	W(13)	O(70)	101.5(7)		O(55)	W(13)	O(77)	85.1(6)

O(61)	W(13)	O(70)	100.5(7)		O(61)	W(13)	O(77)	82.4(6)

O(70)	W(13)	O(77)	173.0(6)		O(47)	W(14)	O(53)	90.0(6)

O(47)	W(14)	O(54)	90.2(7)		O(47)	W(14)	O(60)	156.9(7)

O(47)	W(14)	O(69)	101.5(7)		O(47)	W(14)	O(77)	72.8(6)

O(53)	W(14)	O(54)	156.6(6)		O(53)	W(14)	O(60)	86.3(6)

O(53)	W(14)	O(69)	101.5(7)		O(53)	W(14)	O(77)	84.5(5)

O(54)	W(14)	O(60)	84.4(7)		O(54)	W(14)	O(69)	101.4(7)

O(54)	W(14)	O(77)	73.2(6)		O(60)	W(14)	O(69)	101.6(7)

O(60)	W(14)	O(77)	84.1(6)		O(69)	W(14)	O(77)	171.9(6)

O(46)	W(15)	O(52)	90.1(6)		O(46)	W(15)	O(53)	89.7(6)

O(46)	W(15)	O(59)	157.0(6)		O(46)	W(15)	O(68)	102.0(7)

O(46)	W(15)	O(76)	75.0(6)		O(52)	W(15)	O(53)	157.0(6)

O(52)	W(15)	O(59)	85.6(6)		O(52)	W(15)	O(68)	100.0(7)

O(52)	W(15)	O(76)	73.2(6)		O(53)	W(15)	O(59)	85.6(6)

atom	atom	atom	angle		atom	atom	atom	angle

O(53)	W(15)	O(68)	102.6(6)		O(53)	W(15)	O(76)	84.6(5)

O(59)	W(15)	O(68)	101.0(7)		O(59)	W(15)	O(76)	82.1(6)

O(68)	W(15)	O(76)	172.3(6)		O(45)	W(16)	O(51)	90.5(7)

O(45)	W(16)	O(52)	90.6(7)		O(45)	W(16)	O(58)	156.2(6)

O(45)	W(16)	O(67)	104.0(8)		O(45)	W(16)	O(76)	74.2(6)

O(51)	W(16)	O(52)	155.3(6)		O(51)	W(16)	O(58)	83.3(7)

O(51)	W(16)	O(67)	101.9(7)		O(51)	W(16)	O(76)	84.4(5)

O(52)	W(16)	O(58)	85.7(7)		O(52)	W(16)	O(67)	101.7(7)

O(52)	W(16)	O(76)	72.2(5)		O(58)	W(16)	O(67)	99.8(7)

O(58)	W(16)	O(76)	82.3(6)		O(67)	W(16)	O(76)	173.5(7)

O(50)	W(17)	O(51)	90.3(7)		O(50)	W(17)	O(56)	88.0(7)

O(50)	W(17)	O(57)	156.0(7)		O(50)	W(17)	O(66)	102.8(8)

O(50)	W(17)	O(75)	72.7(6)		O(51)	W(17)	O(56)	155.8(6)

O(51)	W(17)	O(57)	85.9(7)		O(51)	W(17)	O(66)	102.1(7)

O(51)	W(17)	O(75)	84.6(6)		O(56)	W(17)	O(57)	85.9(7)

O(56)	W(17)	O(66)	101.8(7)		O(56)	W(17)	O(75)	71.8(6)

atom	atom	atom	angle		atom	atom	atom	angle

O(57)	W(17)	O(66)	101.2(8)		O(57)	W(17)	O(75)	83.3(6)

O(66)	W(17)	O(75)	172.1(6)		O(61)	W(18)	O(62)	86.8(7)

O(61)	W(18)	O(64)	88.9(6)		O(61)	W(18)	O(65)	153.6(7)

O(61)	W(18)	O(74)	106.0(7)		O(61)	W(18)	O(78)	82.0(6)

O(62)	W(18)	O(64)	157.5(7)		O(62)	W(18)	O(65)	87.9(6)

O(62)	W(18)	O(74)	102.0(8)		O(62)	W(18)	O(78)	84.0(6)

O(64)	W(18)	O(65)	86.1(6)		O(64)	W(18)	O(74)	100.4(8)

O(64)	W(18)	O(78)	73.6(6)		O(65)	W(18)	O(74)	100.4(7)

O(65)	W(18)	O(78)	71.7(6)		O(74)	W(18)	O(78)	170.2(6)

O(59)	W(19)	O(60)	88.9(7)		O(59)	W(19)	O(63)	88.7(7)

O(59)	W(19)	O(64)	155.8(7)		O(59)	W(19)	O(73)	104.8(7)

O(59)	W(19)	O(78)	81.9(6)		O(60)	W(19)	O(63)	155.5(7)

O(60)	W(19)	O(64)	88.2(7)		O(60)	W(19)	O(73)	105.1(7)

O(60)	W(19)	O(78)	84.0(6)		O(63)	W(19)	O(64)	84.0(7)

O(63)	W(19)	O(73)	99.2(8)		O(63)	W(19)	O(78)	71.5(6)

O(64)	W(19)	O(73)	99.2(8)		O(64)	W(19)	O(78)	73.9(6)

atom	atom	atom	angle		atom	atom	atom	angle

O(73)	W(19)	O(78)	168.6(7)		O(57)	W(20)	O(58)	86.4(7)

O(57)	W(20)	O(63)	155.0(7)		O(57)	W(20)	O(65)	87.1(7)

O(57)	W(20)	O(72)	102.8(8)		O(57)	W(20)	O(78)	82.6(6)

O(58)	W(20)	O(63)	90.4(7)		O(58)	W(20)	O(65)	154.2(6)

O(58)	W(20)	O(72)	103.4(8)		O(58)	W(20)	O(78)	82.5(6)

O(63)	W(20)	O(65)	85.1(7)		O(63)	W(20)	O(72)	102.0(8)

O(63)	W(20)	O(78)	72.4(6)		O(65)	W(20)	O(72)	102.5(8)

O(65)	W(20)	O(78)	71.9(6)		O(72)	W(20)	O(78)	172.2(7)

O(1)	Ti(1)	O(4)	101.3(7)		O(1)	Ti(1)	O(5)	102.1(7)

O(1)	Ti(1)	O(7)	100.8(7)		O(1)	Ti(1)	O(8)	98.5(7)

O(1)	Ti(1)	O(38)	170.0(6)		O(4)	Ti(1)	O(5)	87.9(6)

O(4)	Ti(1)	O(7)	87.3(6)		O(4)	Ti(1)	O(8)	159.7(7)

O(4)	Ti(1)	O(38)	86.2(6)		O(5)	Ti(1)	O(7)	157.1(8)

O(5)	Ti(1)	O(8)	92.2(6)		O(5)	Ti(1)	O(38)	84.7(6)

O(7)	Ti(1)	O(8)	84.8(6)		O(7)	Ti(1)	O(38)	72.6(6)

O(8)	Ti(1)	O(38)	73.6(6)		O(2)	Ti(2)	O(5)	103.3(7)

atom	atom	atom	angle		atom	atom	atom	angle

O(2)	Ti(2)	O(6)	100.2(7)		O(2)	Ti(2)	O(9)	97.8(6)

O(2)	Ti(2)	O(10)	97.3(6)		O(2)	Ti(2)	O(39)	169.0(6)

O(5)	Ti(2)	O(6)	88.4(7)		O(5)	Ti(2)	O(9)	91.0(6)

O(5)	Ti(2)	O(10)	159.4(7)		O(5)	Ti(2)	O(39)	85.1(6)

O(6)	Ti(2)	O(9)	161.7(7)		O(6)	Ti(2)	O(10)	88.2(7)

O(6)	Ti(2)	O(39)	86.9(6)		O(9)	Ti(2)	O(10)	85.9(6)

O(9)	Ti(2)	O(39)	74.8(6)		O(10)	Ti(2)	O(39)	74.4(6)

O(1)	Ti(3)	O(43)	102.8(7)		O(1)	Ti(3)	O(44)	100.7(7)

O(1)	Ti(3)	O(47)	98.4(7)		O(1)	Ti(3)	O(48)	99.8(6)

O(1)	Ti(3)	O(77)	169.6(6)		O(43)	Ti(3)	O(44)	91.2(6)

O(43)	Ti(3)	O(47)	89.5(6)		O(43)	Ti(3)	O(48)	157.3(7)

O(43)	Ti(3)	O(77)	84.3(6)		O(44)	Ti(3)	O(47)	160.3(7)

O(44)	Ti(3)	O(48)	86.7(7)		O(44)	Ti(3)	O(77)	86.6(6)

O(47)	Ti(3)	O(48)	85.1(6)		O(47)	Ti(3)	O(77)	73.8(6)

O(48)	Ti(3)	O(77)	73.0(6)		O(2)	Ti(4)	O(42)	100.2(7)

O(2)	Ti(4)	O(43)	102.1(6)		O(2)	Ti(4)	O(45)	99.2(7)

atom	atom	atom	angle		atom	atom	atom	angle

O(2)	Ti(4)	O(46)	98.0(7)		O(2)	Ti(4)	O(76)	169.8(6)

O(42)	Ti(4)	O(43)	90.0(6)		O(42)	Ti(4)	O(45)	87.7(6)

O(42)	Ti(4)	O(46)	161.4(7)		O(42)	Ti(4)	O(76)	87.4(6)

O(43)	Ti(4)	O(45)	158.7(7)		O(43)	Ti(4)	O(46)	89.5(6)

O(43)	Ti(4)	O(76)	84.6(6)		O(45)	Ti(4)	O(46)	86.1(6)

O(45)	Ti(4)	O(76)	74.1(6)		O(46)	Ti(4)	O(76)	74.1(6)

O(37)	P(1)	O(38)	109.6(9)		O(37)	P(1)	O(39)	108.8(8)

O(37)	P(1)	O(40)	108.2(9)		O(38)	P(1)	O(39)	110.6(9)

O(38)	P(1)	O(40)	110.1(8)		O(39)	P(1)	O(40)	109.5(9)

O(75)	P(2)	O(76)	110.0(9)		O(75)	P(2)	O(77)	109.6(8)

O(75)	P(2)	O(78)	109.1(9)		O(76)	P(2)	O(77)	108.5(9)

O(76)	P(2)	O(78)	107.2(8)		O(77)	P(2)	O(78)	112.4(9)

Ti(1)	O(1)	Ti(3)	136.4(8)		Ti(2)	O(2)	Ti(4)	136.3(8)

W(1)	O(4)	Ti(1)	145.7(9)		Ti(1)	O(5)	Ti(2)	153(1)

W(1)	O(6)	Ti(2)	145.5(9)		W(3)	O(7)	Ti(1)	123.9(9)

W(4)	O(8)	Ti(1)	124.8(9)		W(5)	O(9)	Ti(2)	120.3(8)

atom	atom	atom	angle		atom	atom	atom	angle

W(6)	O(10)	Ti(2)	120.9(7)		W(1)	O(11)	W(7)	127.6(9)

W(1)	O(12)	W(2)	128.9(8)		W(2)	O(13)	W(3)	154.6(9)

W(3)	O(14)	W(4)	125.0(8)		W(4)	O(15)	W(5)	152.4(9)

W(5)	O(16)	W(6)	125.4(9)		W(6)	O(17)	W(7)	154(1)

W(2)	O(18)	W(7)	125.5(8)		W(2)	O(19)	W(8)	150(1)

W(3)	O(20)	W(8)	155.2(8)		W(4)	O(21)	W(9)	151.3(9)

W(5)	O(22)	W(9)	153(1)		W(6)	O(23)	W(10)	149(1)

W(7)	O(24)	W(10)	152.2(9)		W(8)	O(25)	W(9)	125.7(8)

W(9)	O(26)	W(10)	127(1)		W(8)	O(27)	W(10)	126.6(9)

W(1)	O(37)	W(2)	89.7(5)		W(1)	O(37)	W(7)	90.5(5)

W(1)	O(37)	P(1)	123.7(9)		W(2)	O(37)	W(7)	88.7(5)

W(2)	O(37)	P(1)	125.1(8)		W(7)	O(37)	P(1)	127.7(9)

W(3)	O(38)	W(4)	88.3(4)		W(3)	O(38)	Ti(1)	89.6(5)

W(3)	O(38)	P(1)	128.0(8)		W(4)	O(38)	Ti(1)	87.8(5)

W(4)	O(38)	P(1)	125.8(8)		Ti(1)	O(38)	P(1)	125.0(8)

W(5)	O(39)	W(6)	89.4(5)		W(5)	O(39)	Ti(2)	89.3(5)

atom	atom	atom	angle		atom	atom	atom	angle

W(5)	O(39)	P(1)	126.4(8)		W(6)	O(39)	Ti(2)	89.8(5)

W(6)	O(39)	P(1)	126.8(9)		Ti(2)	O(39)	P(1)	123.7(9)

W(8)	O(40)	W(9)	89.3(5)		W(8)	O(40)	W(10)	89.7(5)

W(8)	O(40)	P(1)	126.5(8)		W(9)	O(40)	W(10)	89.2(5)

W(9)	O(40)	P(1)	124.3(8)		W(10)	O(40)	P(1)	126.3(8)

W(11)	O(42)	Ti(4)	145.0(8)		Ti(3)	O(43)	Ti(4)	149.8(9)

W(11)	O(44)	Ti(3)	143.7(9)		W(16)	O(45)	Ti(4)	122.2(8)

W(15)	O(46)	Ti(4)	121.4(8)		W(14)	O(47)	Ti(3)	123.0(8)

W(13)	O(48)	Ti(3)	122.1(7)		W(11)	O(49)	W(12)	127.8(8)

W(11)	O(50)	W(17)	126.9(9)		W(16)	O(51)	W(17)	152.9(9)

W(15)	O(52)	W(16)	124.8(8)		W(14)	O(53)	W(15)	151.5(9)

W(13)	O(54)	W(14)	123.3(8)		W(12)	O(55)	W(13)	152.5(9)

W(12)	O(56)	W(17)	127.2(8)		W(17)	O(57)	W(20)	151(1)

W(16)	O(58)	W(20)	152.0(8)		W(15)	O(59)	W(19)	150.8(8)

W(14)	O(60)	W(19)	148.7(9)		W(13)	O(61)	W(18)	152.7(9)

W(12)	O(62)	W(18)	150(1)		W(19)	O(63)	W(20)	127.4(9)

atom	atom	atom	angle		atom	atom	atom	angle

W(18)	O(64)	W(19)	124.5(9)		W(18)	O(65)	W(20)	127.8(9)

W(11)	O(75)	W(12)	90.1(5)		W(11)	O(75)	W(17)	90.0(5)

W(11)	O(75)	P(2)	123.6(9)		W(12)	O(75)	W(17)	89.0(5)

W(12)	O(75)	P(2)	126.6(9)		W(17)	O(75)	P(2)	126.2(8)

W(15)	O(76)	W(16)	89.1(5)		W(15)	O(76)	Ti(4)	89.5(5)

W(15)	O(76)	P(2)	126.9(8)		W(16)	O(76)	Ti(4)	89.4(5)

W(16)	O(76)	P(2)	126.7(8)		Ti(4)	O(76)	P(2)	123.5(8)

W(13)	O(77)	W(14)	89.1(4)		W(13)	O(77)	Ti(3)	91.1(5)

W(13)	O(77)	P(2)	124.5(9)		W(14)	O(77)	Ti(3)	90.3(5)

W(14)	O(77)	P(2)	125.4(8)		Ti(3)	O(77)	P(2)	125.5(8)

W(18)	O(78)	W(19)	88.1(5)		W(18)	O(78)	W(20)	88.4(5)

W(18)	O(78)	P(2)	124.4(8)		W(19)	O(78)	W(20)	88.7(5)

W(19)	  O(78)    P(2)	  126.3(8)	   W(20)	O(78)	    P(2)	 128.4(8)

atom	atom	distance	        atom     atom	     distance

K(1)     O(73)     2.79(2)               K(1)      O(91)     2.81(3)

K(2)     O(41)     2.87(2)               K(2)      O(3)      2.94(2)

K(2)     O(41)i     2.81(2)               K(2)      O(3) i      2.81(2)

K(3)     O(79)     2.89(2)               K(3)      O(9)       3.06(2)

K(3)     O(47)     3.06(2)               K(3)      O(43)      3.07(2)

K(3)     O(5)      3.09(2)               K(3)      O(8)       3.09(2)

K(3)     O(15)     3.10(2)               K(3)      O(53)      3.17(2)

K(3)     O(46)     3.17(2)               K(4)      O(10)      2.72(2)

K(4)     O(86)     3.06(3)               K(4)      O(32)      3.25(3)

K(5)     O(10)     3.11(5)               K(5)      O(16)      3.19(5)

K(5)     O(9)      3.19(5)               K(5)      O(93)      3.28(6)

K(6)     O(32)     2.73(2)               K(6)      O(87)      2.85(3)

K(6)     O(88)     3.45(4)               K(7)      O(32)      3.22(6)

Symmetry  operation i; 1-x, -y, -z