Investigation of the Solid State Reaction of FeSO47H2O with 1,10-Phenanthroline

Lixu Leia, Su Jingb, Richard I Waltona, Xinquan Xinb and Dermot O’Hare*a

a Inorganic Chemistry Laboratory, University of Oxford, Oxford OX1 3QR, UK.

b State Key Lab of Coordination Chemistry, Nanjing University, Nanjing 210093, China

Email: dermot.ohare@chem.ox.ac.uk

Powder XRD pattern of Fe(phen)SO43H2O

CRYSFIRE Solution Nb   1

Cell:   13.7070   10.0750   11.9140    90.000   111.630    90.000

Space group:P21/A

Wavelength:    1.54056

Angular Tolerance:    0.150

Nb of calculated lines:  210

Nb of observed lines  :   39

Nb of indexed lines   :   39

N    h   k   l    ThObs     Thcalc     Dif

1   0   0   1     8.010     7.976     0.034

2   1   1   0    11.239    11.187     0.052

3   0   1   1    11.914    11.865     0.049

4  -2   0   1    13.271    13.223     0.048

5  -2   0   0    13.935    13.889     0.046

6   1   1   1    15.219    15.176     0.043

7   0   0   2    15.943    15.992    -0.049

8   0   0   2    16.042    15.992     0.050

9   2   1   0    16.494    16.449     0.045

10  -2   0   2    16.938    16.890     0.048

11  -1   1   2    17.355    17.312     0.043

12   0   2   0    17.636    17.591     0.045

13   0   1   2    18.321    18.266     0.055

14   2   0   1    18.483    18.434     0.049

15  -1   2   0    18.899    18.928    -0.029

16  -2   1   2    19.096    19.061     0.035

17   0   2   1    19.387    19.341     0.046

18  -1   2   1    19.580    19.532     0.048

19   2   1   1    20.493    20.446     0.047

20  -3   1   1    21.380    21.338     0.042

21   1   1   2    21.629    21.580     0.049

22  -2   2   1    22.122    22.070     0.052

23   2   2   0    22.532    22.482     0.050

24   3   1   0    22.754    22.702     0.052

25  -2   0   3    22.993    22.944     0.049

26   0   2   2    23.904    23.860     0.044

27  -1   1   3    24.136    24.143    -0.007

28  -2   1   3    24.657    24.605     0.052

29   2   0   2    24.917    24.870     0.047

30   0   1   3    25.636    25.679    -0.043

31  -4   0   1    26.131    26.081     0.050

32  -3   2   1    26.365    26.314     0.051

33  -4   0   2    26.635    26.626     0.009

34   3   2   0    27.499    27.445     0.054

35   2   3   0    30.100    30.055     0.045

36   2   2   2    30.673    30.627     0.046

37   4   2   0    33.302    33.249     0.053

38   1   1   4    36.734    36.735    -0.001

39  -2   1   5    38.860    38.813     0.047