New pentanuclear mixed valence Co(II)-Co(III) complexes of “short” salen homologues.

Brunetto Chiari,a Antonio Cinti,a Ornella Crispu,b Francesco Demartin,c Alessandro Pasinib and Olivo Piovesana.a

a Dipartimento di Chimica, via Elce di Sotto 8, 06100 Perugia, Italy

b Dipartimento di Chimica Inorganica Metallorganica e Analitica, via Venezian 21, 20133 Milano, Italy

c Dipartimento di Chimica Strutturale e Stereochimica Inorganica, via Venezian 21 20133 Milano, Italy.

Supplementary information

Table 3

- Selected interatomic distances (Å) and angles (°) for

[Co5(3-OH)2(salNO2ben)4]I. 2(CH3)2O

and   [Co5(3-OH)2(salClben)4]I. 2(CH3)2NCHO.CH2Cl2

|  | SalNO2ben | SalClben |
| --- | --- | --- |
| Co(1) - O(1) | 1.917(3) | 1.901(2) |
| Co(1) - O(2) | 1.914(3) | 1.913(2) |
| Co(1) - O(1d) | 1.888(3) | 1.895(2) |
| Co(1) - O(25a) | 1.899(2) | 1.905(2) |
| Co(1) - N(9d) | 1.952(3) | 1.944(3) |
| Co(1) - N(17a) | 1.959(3) | 1.964(3) |
| Co(2) - O(1a) | 1.891(3) | 1.894(3) |
| Co(2) - O(25d) | 1.907(4) | 1.906(3) |
| Co(2) - N(9a) | 1.989(3) | 1.998(3) |
| Co(2) - N(17d) | 2.002(3) | 2.001(3) |
| Co(3) - O(2) | 2.002(2) | 1.994(2) |
| Co(3) - O(1b) | 1.988(3) | 1.999(2) |
| Co(3) - O(1c) | 1.907(3) | 1.904(3) |
| Co(3) - O(25a) | 2.291(3) | 2.269(2) |
| Co(3) - N(9c) | 2.044(4) | 2.045(3) |
| Co(4) - O(1) | 2.217(3) | 2.202(2) |
| Co(4) - O(2) | 2.190(3) | 2.179(2) |
| Co(4) - O(1b) | 2.038(2) | 2.037(2) |
| Co(4) - O(25c) | 2.031(2) | 2.036(2) |
| Co(4) - N(9b) | 2.115(3) | 2.117(3) |
| Co(4) - N(17c) | 2.119(3) | 2.116(3) |
| Co(5) - O(1) | 1.989(2) | 1.995(2) |
| Co(5) - O(1d) | 2.266(3) | 2.255(2) |
| Co(5) - O(25b) | 1.896(3) | 1.900(2) |
| Co(5) - O(25c) | 1.999(3) | 1.994(2) |
| Co(5) - N(17b) | 2.046(3) | 2.037(3) |

| O(25a) - Co(1) - O(1) | 91.2(1) | 91.7(1) |
| --- | --- | --- |
| O(25a) - Co(1) - O(1d) | 170.4(1) | 170.9(1) |
| O(25a) - Co(1) - O(2) | 80.9(1) | 80.4(1) |
| O(25a) - Co(1) - N(9d) | 93.7(1) | 93.2(1) |
| O(25a) - Co(1) - N(17a) | 94.0(1) | 93.4(1) |
| O(1) - Co(1) - O(1d) | 80.8(1) | 80.7(1) |
| O(1) - Co(1) - O(2) | 83.9(1) | 83.5(1) |
| O(1) - Co(1) - N(9d) | 171.2(1) | 170.3(1) |
| O(1) - Co(1) - N(17a) | 91.5(1) | 92.0(1) |
| O(1d) - Co(1) - O(2) | 92.9(1) | 93.7(1) |
| O(1d) - Co(1) - N(9d) | 94.1(1) | 93.7(1) |
| O(1d) - Co(1) - N(17a) | 91.6(1) | 91.8(1) |
| O(2) - Co(1) - N(9d) | 89.3(1) | 89.0(1) |
| O(2) - Co(1) - N(17a) | 173.0(1) | 172.2(1) |
| N(9d) - Co(1) - N(17a) | 95.8(1) | 96.2(1) |
| O(1a) - Co(2) - O(25d) | 121.8(1) | 121.7(1) |
| O(1a) - Co(2) - N(9a) | 95.6(1) | 95.6(1) |
| O(1a) - Co(2) - N(17d) | 111.4(1) | 114.7(1) |
| O(25d) - Co(2) - N(9a) | 117.2(1) | 113.4(1) |
| O(25d) - Co(2) - N(17d) | 95.1(1) | 94.7(1) |
| N(9a) - Co(2) - N(17d) | 117.2(1) | 118.6(1) |
| O(25a) - Co(3) - O(1c) | 91.5(1) | 91.7(1) |
| O(25a) - Co(3) - O(1b) | 88.2(1) | 87.6(1) |
| O(25a) - Co(3) - O(2) | 70.0(1) | 70.3(1) |
| O(25a) - Co(3) - N(9c) | 169.1(1) | 169.4(1) |
| O(1c) - Co(3) - O(1b) | 138.6(1) | 139.2(1) |
| O(1c) - Co(3) - O(2) | 127.9(1) | 127.9(1) |
| O(1c) - Co(3) - N(9c) | 94.8(1) | 94.6(1) |
| O(1b) - Co(3) - O(2) | 90.6(1) | 90.0(1) |
| O(1b) - Co(3) - N(9c) | 93.0(1) | 93.1(1) |
| O(2) - Co(3) - N(9c) | 99.1(1) | 99.1(1) |
| O(1) - Co(4) - O(1b) | 90.4(1) | 91.2(1) |
| O(1) - Co(4) - O(25c) | 84.0(1) | 83.6(1) |
| O(1) - Co(4) - O(2) | 71.0(1) | 70.8(1) |
| O(1) - Co(4) - N(9b) | 87.9(1) | 87.6(1) |
| O(1) - Co(4) - N(17c) | 153.6(1) | 153.7(1) |
| O(1b) - Co(4) - O(25c) | 174.1(1) | 174.2(1) |
| O(1b) - Co(4) - O(2) | 84.2(1) | 84.1(1) |
| O(1b) - Co(4) - N(9b) | 88.0(1) | 88.6(1) |
| O(1b) - Co(4) - N(17c) | 95.2(1) | 94.3(1) |
| O(25c) - Co(4) - O(2) | 92.3(1) | 91.7(1) |
| O(25c) - Co(4) - N(9b) | 93.6(1) | 93.8(1) |
| O(25c) - Co(4) - N(17c) | 89.1(1) | 89.2(1) |
| O(2) - Co(4) - N(9b) | 157.4(1) | 157.0(1) |
| O(2) - Co(4) - N(17c) | 83.8(1) | 84.2(1) |
| N(9b) - Co(4) - N(17c) | 118.0(1) | 118.2(1) |
| O(1) - Co(5) - O(25c) | 91.1(1) | 90.3(1) |
| O(1) - Co(5) - O(25b) | 128.3(1) | 128.3(1) |
| O(1) - Co(5) - O(1d) | 70.5(1) | 70.34(1) |
| O(1) - Co(5) - N(17b) | 96.8(1) | 95.6(1) |
| O(25c) - Co(5) - O(25b) | 138.7(1) | 139.6(1) |
| O(25c) - Co(5) - O(1d) | 87.1(1) | 88.1(1) |
| O(25c) - Co(5) - N(17b) | 93.5(1) | 94.3(1) |
| O(25b) - Co(5) - O(1d) | 94.5(1) | 94.1(1) |
| O(25b) - Co(5) - N(17b) | 93.4(1) | 93.1(1) |
| O(1d) - Co(5) - N(17b) | 167.3(1) | 165.7(1) |

b) Selected interatomic distances (Å) and angles (°) for   H2salNO2ben

|  | H2SalNO2ben |
| --- | --- |
| O(1) - C(2) | 1.356(4) |
| O(25) - C(24) | 1.356(4) |
| O(27) - N(26) | 1.211(6) |
| O(28) - N(26) | 1.204(6) |
| N(9) - C(8) | 1.264(4) |
| N(9) - C(10) | 1.461(4) |
| N(17) - C(10) | 1.456(4) |
| N(17) - C(18) | 1.279(4) |
| N(26) - C(14) | 1.468(5) |
| C(2) - C(7) | 1.400(4) |
| C(7) - C(8) | 1.460(4) |
| C(10) - C(11) | 1.510(4) |
| C(18) - C(19) | 1.438(4) |
| C(19) - C(24) | 1.385(4) |
| C(8) - N(9) - C(10) | 121.8(2) |
| C(10) - N(17) - C(18) | 117.8(2) |
| O(27) - N(26) - O(28) | 123.1(4) |
| O(27) - N(26) - C(14) | 119.0(3) |
| O(28) - N(26) - C(14) | 117.8(3) |
| O(1) - C(2) - C(3) | 119.2(3) |
| O(1) - C(2) - C(7) | 121.0(3) |
| C(3) - C(2) - C(7) | 119.8(3) |
| C(2) - C(7) - C(6) | 118.4(3) |
| C(2) - C(7) - C(8) | 121.9(2) |
| C(6) - C(7) - C(8) | 119.7(3) |
| N(9) - C(8) - C(7) | 122.1(3) |
| N(9) - C(10) - N(17) | 112.7(2) |
| N(9) - C(10) - C(11) | 108.6(2) |
| N(17) - C(10) - C(11) | 109.9(2) |
| N(17) - C(18) - C(19) | 122.7(3) |
| C(18) - C(19) - C(20) | 119.3(3) |
| C(18) - C(19) - C(24) | 121.9(3) |
| C(20) - C(19) - C(24) | 118.7(3) |
| O(25) - C(24) - C(19) | 122.1(3) |
| O(25) - C(24) - C(23) | 117.8(3) |
| C(19) - C(24) - C(23) | 120.0(3) |
| C(10) - C(11) - C(12) | 120.7(3) |
| C(10) - C(11) - C(16) | 120.2(3) |
| N(26) - C(14) - C(13) | 119.0(3) |
| N(26) - C(14) - C(15) | 118.4(3) |

Expression for the magnetic susceptibility

The eigenvalues of  the Htet Hamiltonian are E(S) = -JAB S(S+1), where S varies from |SA – SB| = 6/2 to (SA + SB)=12/2  in integral steps.

The van Vleck  formalism then gives the  expression:

 = (N2g2/3kT)S(S+1)(2S+1)exp-E(S)/kT /  (2S+1)exp- E(S)/(kT)

Taking the E(S=6/2) as the energy origin,  defining X = JAB/(kT) and with JAB in cm-1, we obtain:

= (.1251/T) g2 84 + 180 X8 + 330 X18 + 546 X30) / (63 X8  + 11 X18 + 13 X30)

The best fit to the experimental data for T  25 K was obtained with  g=2.04, JAB=-0.3 cm-1.

The eigenvalues of H1  in Htr are easily found to be:

E(S,S’) = -J S(S+1) + (J-J’)S’(S’+1), where   S’ = S3 + S5  and S = S’ + S4. S’ varies by an integer value from 0 to 6/2,  and for each S’ value, S varies by an integer value from |S’ – 3/2| to S’ +3/2.

The g value for each E(S,S’) state, assuming g3 = g5  g4 is expressed as:

g(S,S’) = [g3S2 +(S’)2 – S42 + g4S2 – (S’)2 + S42] / 2S(S + 1)

Taking  E(9/2,6/2) as the energy origin,  the zero-field relative energies and g values of the 12 E(S,S’) states are:

E(1)  =  E(9/2, 6/2)   =    0                                     g(1) = g(9/2, 6/2) =  0.66 g3 + 0.33 g4

E(2)  =  E(7/2, 6/2)   =    9 J                                   g(2) = g(7/2, 6/2) = 0.76 g3 + 0.24 g4

E(3)  =  E(5/2, 6/2)   =    16 J                                 g(3) = g(5/2, 6/2) = 0.97 g3 + 0.03 g4

E(4)  =  E(3/2, 6/2)   =    21 J                                 g(4) = g(3/2, 6/2) = 1.60 g3 – 0.60 g4

E(5)  =  E(7/2, 4/2)   =    3 J + 6 J’                         g(5) = g(7/2, 4/2) = 0.57 g3 + 0.43 g4

E(6)  =  E(5/2, 4/2)   =    10 J + 6 J’                       g(6) = g(5/2, 4/2) = 0.63 g3  + 0.37 g4

E(7)  =  E(3/2, 4/2)   =    15 J + 6 J’                       g(7) = g(3/2, 4/2) = 0.80 g3  + 0.20 g4

E(8)  =  E(1/2, 4/2)   =    18 J + 6 J’                       g(8) = g(1/2, 4/2) = 2.00 g3  - 1.00 g4

E(9)  =  E(5/2, 2/2)   =    6 J + 10 J’                       g(9) = g(5/2, 2/2) = 0.40 g3 + 0.60 g4

E(10)  =  E(3/2, 2/2)   =    11 J + 10 J’                   g(10) = g(3/2, 2/2) = 0.27 g3 + 0.73 g4

E(11)  =  E(1/2, 2/2)   =    14 J + 10 J’                   g(11) = g(1/2, 2/2) =  -0.67 g3 +1.67 g4

E(12)  =  E(3/2, 0)      =      9 J + 12 J’                    g(12) = g(3/2, 0) = 0.00 g3 + 1.00 g4

The 1 contribution from the H1  Hamiltonian to the total susceptbibility above 25 K is then:

1  = (.1251/T)[ì g(i)2 S(i)S(i) + 1 2 S(i) +1Exp -E(i)/kT] / [i2 S(i) + 1 Exp -E(i)/kT]

As described in Ref. 8, the <2 >contribution from the H2 Hamiltonian is:

<2>  = (0.3753/T) [1 + 9 Exp (2x)/3 + 4 + (3/x)1 – Exp(2x)2/3 ] / [4 1 + 2 Exp(-2x)]

where x = D/kT.

The total average susceptibility ,  , is then equal to  1  +  <2>

The best fit to the experimental data was obtained with J = 40.0 cm-1, J’ = -15.0 cm-1, g3 = 2.03 and g4 =  2.01.