Table S1 Crystal and structure refinement data for complexes 4a, 4b and 5a.

Complex                      		[Fe2(CO)5{MeSCH2C(Me)(CH2S)2}] 	[Fe2(CO)5{PhCH2SCH2C(Me)(CH2S)2}]	[NEt4][Fe2(CO)4(CN){MeSCH2C(Me)(CH2S)2}]

Code                                                  	4a					4b					5a

Elemental formula                		C11 H12 Fe2 O5 S3   			C17 H16 Fe2 O5 S3    			C8 H20 N, C11 H12 Fe2 N O4 S3

Formula weight                    		432.1       				508.2    					560.3

Crystal system                    		Monoclinic       				Triclinic    				Triclinic

Space group                       		P21/n (equiv. to no. 14)       		P-1  (no. 2)    				P-1  (no. 2)

Unit cell dimensions 	a, Å		18.4670(16)    				  9.8755(11)   				  8.2990(14)

b  		10.9622(12)     				11.3853(13)     				  9.357(4)

c  		16.9055(18)    				10.3912(13)    				16.534(3)

α, 		  90 					110.555(10) 				  85.87(2)

β 		105.267(8) 				  92.983(9)  				  78.327(13)

γ		  90 					104.374(9) 				  77.90(2)

Cell volume, V, Å3                     	3301.6(6)       				1047.2(2)    				1228.8(6)

No. of formula units/cell, Z    		8      					2    					2

Density (calculated), Mg/m3                	1.739       				1.612    					1.514

F(000)                             		1744       				516    					584

Absorption coefficient, mm-1           	2.15        				1.71     					1.46

Temperature, K                      		293(1)        				293(1)     				140(1)

Crystal colour, shape              		deep red, diamond-shaped plates       	red-brown, elongated plates   		orange rhombs

Crystal size, mm                        	0.29 x 0.17 x 0.14      			0.64 x 0.27 x 0.02   			ca 0.5 x 0.5 x 0.5

Crystal mounting                    		in a capillary      				on a glass fibre   				coated in silicone grease, in a capilliary

On the diffractometer:

θ range for data collection,       	1.9 - 21.0         				2.0 - 25.0      				1.5 - 30.0

Index ranges for h, k, l         	 	-18/18, 0/11, 0/17         			-11/11, -1/13, -12/12      			-11/11, -13/13, -1/23

Crystal degradation, %               	5.3 	       				0    					4.4

Max. and min. transmission  		0.997 and 0.976       			0.30 and 0.25    				0.999 and 0.920

Total no. of reflections measured

(not including absences)		3678       				4297    					7586

Rint for equivalents 			0.021       				0.025   					0.027

Total no. of unique reflections 	3528       				3686    					7138

No. of 'observed' reflections (I > 2σI)  	2614      					2715    					5512

Structure determined by: 		direct methods, in SHELXS       		direct methods, in SHELXS    		direct methods, in SHELXS

Refinement:             (by full-matrix least-squares methods, on F2, in SHELXL-97)

Data / restraints / parameters 	3528 / 0 / 392         			3686 / 0 / 245      			7138 / 0 / 303

Goodness-of-fit on F2, S     		1.048        				1.033      				1.247

Final R indices ('observed' data)	R1 = 0.028, wR2 = 0.054         		R1 = 0.037, wR2 = 0.090      		R1 = 0.051, wR2 = 0.132

Final R indices (all data)        	R1 = 0.046, wR2 = 0.061         		R1 = 0.053, wR2 = 0.105      		R1 = 0.067, wR2 = 0.138

Reflections weighted # :    w = 	[σ2(Fo2)]-1            				[σ2(Fo2)+(0.0579P)2]-1 #            		[σ2(Fo2)+4.639P]-1 #

Largest diff. peak and hole, e.Å-3         	0.24 and -0.22       			0.44 and -0.37    				0.69 and -0.82

Location of largest difference peak 	near a carbonyl ligand      			all within core of cluster   		close to S(1)

# - where P=(Fo2+2Fc2)/3