Supporting Information:

Preparation of Mn[NC5H3(COO)2]·H2O: A mixture of Mn(CH3COO)2·4H2O (0.061g, 0.25mmol), pyridine-3,4-dicarboxylic acid (0.167g, 1mmol), triethylamine (0.1ml) and distilled water (15ml) (pH ≈ 8.0) was sealed in a Teflon-lined stainless steel autoclave and heated at 160 °C for 72 hours under autogenous pressure to give pink rhombohedral crystals of the polymer. The resulting colorless crystals were collected by filtration, washed with distilled water and dried in air at ambient temperature. All chemicals used are as purchased without purification. Anal. Calcd for C7H5MnNO5: C, 35.29; H, 2.10; N, 5.88. Found: C, 35.09; H, 2.04; N, 5.29.

Analyses: Elemental analyses were conducted on a Perkin-Elmer 240C element analyzer. Thermogravimetric analyses (TGA) were performed on a NETZSCH STA 449C thermogravimetric analyzer under an atmospheric environment at a heating rate of 20 °C/min. Magnetic susceptibility data were collected in the temperature range 4.0-298K in an applied field of 5000 Oe with the use of a Quantum Design Model MPMS SQUID magnetometer.

Crystallographic analyses: Crystallographic data for Mn[NC5H3(COO)2]·H2O were recorded at room temperature on a Bruker-AXS Smart CCD diffractometer equipped with a normal-focus, 2.4 kW sealed tube X-ray source (graphite-monochromated Mo-Kα radiation with λ=0.71073 Å) operating at 50 kV and 40 mA. Intensity data were collected in 1271 frames with increasing ω (width of 0.3° and exposure time 30 s per frame). The structures were solved by direct methods and refined by full-matrix least-squares techniques against F2 using the SHELXTL-NT5.1 package1. Non-hydrogen atoms were refined anisotropically. All the hydrogen atoms were found in the electron density map and refined isotropically.

1. G. M. Sheldrick, SHELXTL-NT, Version 5.1, Brucker Axs Inc., Madison, WI, 1997.

Table S1. Selected bond lengths [Å] and angles [°].

| Mn(1)-O(1) | 2.1593(16) |
| --- | --- |
| Mn(1)-O(2)#1 | 2.1667(15) |
| Mn(1)-O(3)#3 | 2.1980(16) |
| Mn(1)-O(4)#2 | 2.1770(16) |
| Mn(1)-N(1)#4 | 2.2845(18) |
| Mn(1)-O(5) | 2.3087(17) |
| O(1)-Mn(1)-O(2)#1 | 87.60(6) |
| O(1)-Mn(1)-O(3)#3 | 172.94(6) |
| O(1)-Mn(1)-O(4)#2 | 90.41(6) |
| O(1)-Mn(1)-N(1)#4 | 89.53(6) |
| O(1)-Mn(1)-O(5) | 82.91(6) |
| O(2)#1-Mn(1)-O(3)#3 | 99.34(6) |
| O(2)#1-Mn(1)-O(4)#2 | 87.65(7) |
| O(2)#1-Mn(1)-N(1)#4 | 100.84(7) |
| O(2)#1-Mn(1)-O(5) | 166.08(6) |
| O(3)#3-Mn(1)-O(5) | 90.49(6) |
| O(3)#3-Mn(1)-N(1)#4 | 87.87(6) |
| O(4)#2-Mn(1)-O(3)#3 | 91.19(6) |
| O(4)#2-Mn(1)-N(1)#4 | 171.50(7) |
| O(4)#2-Mn(1)-O(5) | 82.29(6) |
| N(1)#4-Mn(1)-O(5) | 89.27(6) |

Symmetry transformations used to generate equivalent atoms:

#1 x-1/2,-y+3/2,z-1/2   #2 x-1/2,-y+3/2,z+1/2    #3 x-1,y,z   #4 -x+1,-y+2,-z+1

#5 x+1/2,-y+3/2,z+1/2       #6 x+1,y,z         #7 x+1/2,-y+3/2,z-1/2

Figure S1. TGA and DSC curves for Mn[NC5H3(COO)2]·H2O

Table S2. Experimental magnetic data.

| Temperature (K) | Long Moment (emu) |
| --- | --- |
| 297.9886 | 0.04388 |
| 258.3277 | 0.04906 |
| 218.8433 | 0.0554 |
| 179.2357 | 0.06386 |
| 139.6033 | 0.07697 |
| 100.0333 | 0.09941 |
| 95.9276 | 0.10215 |
| 92.08303 | 0.10559 |
| 88.25326 | 0.1092 |
| 84.43048 | 0.11318 |
| 80.61344 | 0.11743 |
| 76.78488 | 0.12207 |
| 72.95277 | 0.12717 |
| 69.13428 | 0.13281 |
| 65.32059 | 0.13904 |
| 61.49396 | 0.1459 |
| 57.65604 | 0.15377 |
| 53.84149 | 0.16246 |
| 50.01968 | 0.17239 |
| 48.97639 | 0.17536 |
| 47.99002 | 0.17845 |
| 46.98693 | 0.18147 |
| 45.98529 | 0.18466 |
| 44.99667 | 0.18805 |
| 43.99489 | 0.19154 |
| 43.01339 | 0.19519 |
| 41.9947 | 0.19884 |
| 40.99357 | 0.20266 |
| 39.99958 | 0.20673 |
| 39.00017 | 0.21091 |
| 37.99656 | 0.21541 |
| 37.00535 | 0.22011 |
| 36.00718 | 0.22502 |
| 35.00558 | 0.23007 |
| 34.0008 | 0.23534 |
| 33.00173 | 0.24088 |
| 32.00139 | 0.24686 |
| 30.99856 | 0.25311 |
| 29.99964 | 0.25961 |
| 29.00117 | 0.26649 |
| 28.00845 | 0.27371 |
| 27.00112 | 0.28141 |
| 25.99729 | 0.28963 |
| 25.00092 | 0.29815 |
| 24.01299 | 0.30731 |
| 23.01375 | 0.31712 |
| 22.00844 | 0.32775 |
| 20.99894 | 0.33907 |
| 20.00131 | 0.35106 |
| 19.00151 | 0.36404 |
| 18.00033 | 0.37807 |
| 17.00335 | 0.39308 |
| 15.99887 | 0.4095 |
| 14.99952 | 0.42719 |
| 14.00238 | 0.44551 |
| 13.00253 | 0.46576 |
| 12.00294 | 0.48765 |
| 11.00058 | 0.51291 |
| 9.99798 | 0.53956 |
| 8.99934 | 0.5682 |
| 8.00029 | 0.59888 |
| 6.99812 | 0.63099 |
| 6.00126 | 0.66329 |
| 4.99805 | 0.69262 |
| 3.99762 | 0.71021 |