Supporting Materials:

Dihalo(diphosphane)metal(II) complexes (metal = Co, Ni, Pd) as pre-catalysts for the vinyl-polymerization of norbornene – elucidation of the activation process with B(C6F5)3/AlEt3 or Ag[closo-1-CB11H12] and evidence for the in situ formation of "naked" Pd2+ as highly active species

Paul-Gerhard Lassahn,a Vasile Lozan,a Biao Wu,a Andrew Wellerb and Christoph Janiak*a

a Institut für Anorganische und Analytische Chemie, Universität Freiburg, Albertstr. 21, 79104 Freiburg, Germany. E-mail: janiak@uni-freiburg.de; Fax: +49(0)761-2036147

b Department of Chemistry, University of Bath, Bath, UK BA2 7AY. E-mail: a.s.weller@bath.ac.uk; Fax: +44(0)1225-386231

Scheme 1

Table 1. 1H NMR data of the phosphine ligands dppe and dppp and the palladium complexes 5 and 6 in combination with different amounts of B(C6F5)3

| Compound a | 1H-NMR |
| --- | --- |
| [µmol] (molar ratio) | [ppm (Hz)] |
| dppe [7] | 2.02 (d, 6.6, 4H, CH2), 7.22 (d, 1.4, 20H, Harom.) |
| dppe/B(C6F5)3 [7/63] (1:9) | 2.52 (s, br, 4H, CH2), 7.28 and 7.52 (s, br, 16H, Harom.), 7.71 (d, br, 7.2, Harom.) |
| 5 [7] b | 2.65 ("d", 24.4, 4H, CH2), 7.61-7.49 (m, 12H, Harom.), 7.87-7.80 (m, 8H, Harom.) |
| 5/B(C6F5)3 [7/7] (1:1) | not soluble |
| 5/B(C6F5)3 [7/14] (1:2) | 2.49 (m, br, CH2), 7.04 (d, 6.2, Harom.), 7.31 (t, 7.5, Harom.), 7.50 (t, 7.3, Harom.), 7.5-7.8 (m, br, Harom.) |
| 5/B(C6F5)3 [7/35] (1:5) | 2.48 (m, br, CH2), 7.05 (d, 6.0, Harom.), 7.31 (t, 7.6, Harom.), 7.50 (t, 7.4, Harom.), 7.60 (s, br, Harom.) |
| 5/B(C6F5)3 [7/63] (1:9) | no changes compared to the 1:5-spectrum |
| dppp [7] | 1.49 (m, 2H, C-CH2-C), 2.11 (t, 7.8, 4H, P-CH2), 7.1-7.4 (m, 20H, Harom.) |
| dppp/B(C6F5)3 [7/63] (1:9) | 1.44 (m, br, 2H, C-CH2-C),2.46 (t, br, 70.1, P-CH2), 6.9-8.1 (m, 20H, Harom.) |
| 6 [7] b | 1.69 (tquint, 2H, C-CH2-C, 3JPH  23 Hz, 3JHH  4 Hz), 2.65 ("quint", 4H, P-CH2), 7.51-7.40 (m, 12H, Harom.), 7.80-7.73 (m, 8H, Harom.) |
| 6/B(C6F5)3 [7/7] (1:1) | 2.00 (t, br, 2H, C-CH2-C), 2.38 (s, br, 4H, P-CH2), 7.4 und 7.6 (s, br, 20H, Harom.) |
| 6/B(C6F5)3 [7/14] (1:2) | 2.09 (t, br, 2H, C-CH2-C), 2.56 (s, br, 4H, P-CH2), 7.1-7.7 (m, 20H, Harom.) |
| 6/B(C6F5)3 [7/35] (1:5) | no changes compared to the 1:2-spectrum |
| 6/B(C6F5)3 [7/63] (1:9) | no changes compared to the 1:2-spectrum |
| a solvent: CD2Cl2 (0.5 mL) except where noted otherwise; b solvent: DMSO-d6 (0.5 mL) |  |

Scheme 2 31P NMR data of the interaction between dppe, dppp, dppb, 5 and 6 with B(C6F5)3 – see Table 2

Scheme 3 19F NMR data of the interaction between dppe, dppp and Cl– (from 5, 6 or Et4NCl) and B(C6F5)3 – see Table 2

Table 2. 19F NMR and 31P NMR data of the phosphine ligands dppe and dppp, the palladium(II) complexes 5 and 6 and Et4N+Cl- in combination with different amounts of B(C6F5)3 (measured in CD2Cl2 at room temperature).

| Compound a [µmol] (molar ratio) | 31P-NMR | 19F NMR [ppm (JFF Hz)] |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | [ppm] | o-F |  | p-F | m-F |  |
| B(C6F5)3 A | n. s. | -129.27 (s, br) A |  | -145.28 (s, br) A | -161.76 (tdd, 20.7, 7.5, 2.8) A |  |
| dppe [7] | –12.9 | n. s. |  |  |  |  |
| dppe/B(C6F5)3 [7/63] (1:9) | +12.6 | -128.88 (d, 8.8) A -133.87 (s, br) B |  | -145.64 (s, br) A -160.15 (t, 20.2) B | -161.79 (“td”, 7.1, 20.5) A -166.24 (t, 19.1) B |  |
| 5 [7] b | +66.5 | n. S. |  |  |  |  |
| 5/B(C6F5)3 [7/7] (1:1) | not soluble |  |  |  |  |  |
| 5/B(C6F5)3 [7/14] (1:2) | +56.9 |  | -130.91 (s, br) C -133.91 (s, br) D | -150.3 (s, br) C -160.13 (t, 20.2) D |  | -163.48 (s, br) C -166.21 (t, 19.0) D |
| 5/B(C6F5)3 [7/35] (1:5) | +56.9 |  | -129.53 (s, br) C -133.88 (s, br) D | -146.81 (s, br) C -160.15 (t, 20.3) D |  | -162.27 (s, br) C -166.22 (t, 19.0) D |
| 5/B(C6F5)3 [7/63] (1:9) | +56.9 |  | -129.35 (s, br) C -133.89 (s, br) D | -145.98 (s, br) C -160.16 (t, 20.2) D |  | -161.96 (s, br) C -166.23 (t, 19.2) D |
| dppp [7] | –17.6 |  | n. s. |  |  |  |
| dppp/B(C6F5)3 [7/63] (1:9) | +13.5, +7.9 |  | -128.62 (d, 8.8) A -133.89 (s, br) B | -145.6 (s, br) A -160.10 (t, 20.3) B |  | -161.89 (s, br) A -166.19 (t, 19.2) B |
| 6 [7] b | +12.5 |  | n. s. |  |  |  |
| 6/B(C6F5)3 [7/7] (1:1) | +14.1, 12.8 |  | -132.80 (d, 17.7) C -133.93 (s, br) -134.88 (s, br) D | -162.30 (t, 20.3) C -160.21 (t, 20.2) D -159.11 (s, br) |  | -167.26 (t, 18.4) C -166.25 (t, 19.7) D -165.50 (s, br) |
| 6/B(C6F5)3 [7/14] (1:2) | +16.0 |  | -132.54 (s, br) C -133.89 (s, br) D | -155.2 (s, br) C -160.13 (t, 20.3) D |  | -164.00 (s, br) C -166.20 (t, 18.6) D |
| 6/B(C6F5)3 [7/35] (1:5) | +16.0 |  | -129.83 (s, br) C -133.88 (s, br) D | -146.69 (s, br) C -160.15 (t, 20.2) D |  | -162.27 (s, br) C -166.22 (t, 19.4) D |
| 6/B(C6F5)3 [7/63] (1:9) | +16.0 |  | -129.38 (s, br) C -133.90 (s, br) D | -146.08 (s, br) C -160.18 (t, 20.2) D |  | -162.06 (s, br) C -166.25 (t, 19.0) D |
| dppb c [7] | -16.1 |  | n. s. |  |  |  |
| dppbc/B(C6F5)3 [7/63] (1:9) | 14.5, 13.9, 9.6 |  | -128.53(s, br) -133.91 (s, br) | -144.57 (s, br) -160.15 (t, 20.2) |  | -161.78 (s, br) -166.23 (t, 18.8) |
| Et4NCl/B(C6F5)3 (1:1) | n. s. |  | -133.23 (dd, 7.7, 23.3) C -135.85 (d, br, 20.9) D | -162.54 (t, 20.3) C -160.62 (t, 20.2) D |  | -167.52 (m) C -166.27 (td, 21.8, 6.7) D |
| Et4NCl/B(C6F5)3 (1:9) | n. s. |  | -129.47 (s, br) C -133.95 (s, br) D | -146.30 (s, br) C -160.24 (t, 20.2) D |  | -162.03 (s, br) C -166.31 (t, 18.7) D |
| Et4NCl/B(C6F5)3/Al (1:1:10) | n. s. |  | -121.97 (d, br, 18.1) -122.25 (dd, 12.5, 29.8) -123.52 (m) | -156.6 (s, br) -160.18 (t, 19.0) -154.90 (t, 18.8) |  | -163.86 (s, br) -165.39 (m) -162.69 (m) |
| Et4NCl/B(C6F5)3/Al (1:9:10) | n. s. |  | -122.16 (dd, 10.7, 24.3) -123.45 (m, br) | -153.93 (m, br) -158.94 (t, 19.3) |  | -162.53 (m, br) -165.09 (m) |
| n. s. = no signal; a solvent: CD2Cl2 (0.5 mL); b solvent: DMSO-d6 (0.5 mL); c dppb = bis(1,4-diphenylphosphino)butane |  |  |  |  |  |  |

Scheme 4 31P NMR data of the interaction between dppe, dppp, 5 and 6 with AlEt3 and different amounts of B(C6F5)3. Al(C6F5)3 is derived from the nearly equimolar (9:10) reaction of B(C6F5)3 and AlEt3 (resulting chemical shifts given in italics) – see Table 3.

Table 3. 31P NMR data of the phosphine ligands dppe and dppp and the palladium complexes 5 and 6 in combination with different amounts of B(C6F5)3/AlEt3 (measured in CD2Cl2 at room temperature).

| molar ratio mixture a | 1:0:0 | 1:0:10 | 1:2:10 | 1:5:10 | 1:9:10 |
| --- | --- | --- | --- | --- | --- |
| dppe/B(C6F5)3/AlEt3 | -12.9 | -12.0 | n. m. | n. m. | -10.4 |
| 5/B(C6F5)3/AlEt3 | 66.5 b | n. m. | 56.9 | 56.9 | 56.9 |
| dppp/B(C6F5)3/AlEt3 | -17.6 | -15.2 | n. m. | n. m. | +8.2, -13.4, -18.8 |
| 6/B(C6F5)3/AlEt3 | 12.5 b | n. m. | n. s. | n. s. | n. s. |
| dppb c | -16.1 | n. m. | n. m. | n. m. | n. m. |
| n. s. = no signal; n. m. = not measured; a solvent: CD2Cl2 (0.5 mL); b solvent: DMSO-d6 (0.5 mL); c dppb = bis(1,4-diphenylphosphino)butane |  |  |  |  |  |