Supplementary data for the publication:

In-situ X-ray powder diffraction studies of hydrothermal and thermal decomposition reactions of basic bismuth(III) nitrates in the temperature range 20-650oC

J. Chem. Soc., Dalton Trans, 2003,

Axel Nørlund Christensen,a Torben René Jensen,b Nicola V. Y. Scarlett,c Ian C. Madsen,c Jonathan C. Hanson,d and Angela Altomaree

# Graphical content entry

In-situ X-ray powder diffraction studies of hydrothermal and thermal decomposition reactions of basic bismuth(III) nitrates in the temperature range 20-650oC

Axel Nørlund Christensen, Torben René Jensen, Nicola V. Y. Scarlett, Ian C. Madsen, Jonathan C. Hanson, and Angela Altomare

# Abstract

The syntheses of basic bismuth(III) nitrates under hydrothermal conditions and their dry decomposition to -Bi2O3 in solid state reactions was investigated by in-situ synchrotron X-ray radiation powder diffraction. Three basic bismuth(III) nitrates with known structures are: [Bi6O4(OH)4](NO3)6(4H2O, C, [Bi6O4(OH)4](NO3)6(H2O, D, and [Bi6O5(OH)3](NO3)5(3H2O, A. They contain the complex ions [Bi6O4(OH)4]6+ and{[Bi6O5(OH)3]5+}2, respectively. A fourth basic bismuth(III) nitrate, X, apparently has the composition [Bi6O4.5(OH)3.5](NO3)5.5(H2O according to chemical analysis. The transformation of C via D to X, or of C directly to X was established in the in-situ hydrothermal synthesis. Similarities in the decomposition paths of C, D and X in the solid state in-situ investigations support the above composition indicated for X. The compound A has a decomposition path different from those of C, D and X. This is consistent with the complex ion {[Bi6O5(OH)3]5+}2 in A, being different from the complex ion [Bi6O4(OH)4]6+ in the other two basic bismuth(III) nitrates. All four compounds have -Bi2O3 as the final decomposition product.

Fig. S1. TGA-DTA diagrams for the compound D.

Fig. S2. X-Ray powder patterns of D and the decomposition products X1, X2, X3, X4, and -Bi2O3.

Fig. S3. TGA-DTA diagrams for the compound X.

Fig. S4. X-Ray powder pattern of X and the decomposition products X1, X2, X3, X4, and -Bi2O3.

Fig. S5. TGA-DTA diagrams for the compound B.

Fig. S6. X-Ray powder patterns of the compounds B, B, B1, X3, X4 (with impurity of X3), and -Bi2O3.

Fig. S7. TGA-DTA diagrams of the compound A.

Fig. S8. X-Ray powder patterns of A and the decomposition products A1, A2, X2, X3, X4, and -Bi2O3.