S1. Powder XRD profiles for 1 and 2

S2. Calculated oxidation states, Vi, for atoms in the structure of Co2.59Zn0.41(PO4)2H2O 1, using ref. 26. The contribution from H is not included in the calculations.

|  | Vi | Coord. number |
| --- | --- | --- |
| Co(1) | 1.91 | 6 |
| Co(2) | 1.94 | 6 |
| Co(3) | 1.97 | 5 |
| Zn(3) | 2.03 | 5 |
| P(1) | 4.92 | 4 |
| P(2) | 4.90 | 4 |
| O(1) | 1.93 | 3 |
| O(2) | 2.00 | 3 |
| O(3) | 1.75 | 2 |
| O(4) | 1.77 | 3 |
| O(5) | 2.02 | 3 |
| O(6) | 1.90 | 3 |
| O(7) | 1.86 | 3 |
| O(8) | 1.88 | 3 |
| O(9) | 0.55 | 2 |

S3. Calculated oxidation states, Vi, for atoms in the structure of Co0.72Zn2.28(PO4)2H2O 2, using ref. 26. The contribution from H is not included in the calculations.

|  | Vi | Coord. number |
| --- | --- | --- |
| Zn(1) | 1.99 | 4 |
| Zn(2) | 2.03 | 4 |
| Zn(3) | 2.06 | 6 |
| Co(1) | 1.92 | 4 |
| Co(2) | 1.96 | 4 |
| Co(3) | 1.97 | 6 |
| P(1) | 4.95 | 4 |
| P(2) | 4.92 | 4 |
| O(1) | 1.77 | 2 |
| O(2) | 1.95 | 3 |
| O(3) | 1.96 | 3 |
| O(4) | 2.03 | 3 |
| O(5) | 1.78 | 2 |
| O(6) | 2.07 | 3 |
| O(7) | 1.76 | 2 |
| O(8) O(9) | 1.94 0.36 | 3 1 |

S4

Fig. 1 Phase fractions of the materials in the solid products from Series A (amine present) as a function of the relative amount of Co, n, in the reaction mixtures: [CH3NH3][(CoxZn1-x)4(PO4)3], blue square; hopeite, (CoxZn1-x)3(PO4)24H2O, green star; Co2.59Zn0.41(PO4)2H2O 1, red triangle; amorphous powder, orange diamond; Co3(HPO4)2(OH)2, black circle. The lines are sketched as a guide to the eye.

Fig. 2 Phase fractions of the materials in the solid products from Series B (amine absent) as a function of the relative amount of Co, n, in the reaction mixtures: Co0.72Zn2.28(PO4)2(H2O 2, blue diamonds and Co7(HPO4)4(PO4)2, red circles. The lines are sketched as a guide to the eye.