Manuscript: B414229B

The synthesis, structure and ethene polymerisation catalysis of mono(salicylaldiminato) titanium and zirconium complexes

Dale A. Pennington, William Clegg, Simon J. Coles, Ross W. Harrington, Michael B. Hursthouse, David L. Hughes, Mark E. Light, Mark Schormann, Manfred Bochmann and Simon J. Lancaster*

Electronic supplementary information.

Ligand syntheses

3-But-2-(OSiMe3)C6H3CH=N(2,6-Pri2C6H3) (2b)

Following a similar procedure to that for 2a, 1b (7.2 g, 25 mmol) was deprotonated with n-BuLi (15.6 cm3 of a 1.6 M hexane solution, 25 mmol) and treated with excess SiClMe3 (20 cm3).  The volatiles were removed under reduced pressure and the resulting product crystallised from ethanol (50 cm3) at 20 °C to give yellow blocks (9.8 g, 24 mmol, 95%). 1H NMR (293 MHz, 293 K, CDCl3): δ 8.55 (s, 1H, CH=N), 8.13 (dd, 1H, J = 5.9, 1.8 Hz, Ar-H), 7.52 (dd, 1H, J = 5.9, 1.8 Hz, Ar-H), 7.19-7.09 (m, 4H, Ar-H), 3.03 (m, 2H, J = 6.9 Hz, CH(CH3)2), 1.47 (s, 9H, But), 1.19 (d, 6H, J = 6.9 Hz, CH(CH3)2), 0.28 (s, 9H, Si(CH3)3). 13C NMR (75.5 MHz, 293 K, CDCl3): δ 159.8 (C-O), 155.5 (C=N), 137.9, 131.0, 128.4, 126.4, 124.3, 123.3, 122.0 (Ar), 35.3 (C(CH3)3), 30.8 (CH3), 28.2 (CH(CH3)2), 23.9 (CH(CH3)2), 2.2 (Si(CH3)3).

3-But-2-(OSiMe3)C6H3CH=N(2,4,6-Me3C6H2) (2c)

Following a similar procedure to that for 2a, 1c (9.20 g, 30 mmol) was deprotonated with n-BuLi (18.8 cm3 of a 1.6 M hexane solution, 30 mmol) and treated with excess SiClMe3 (20 cm3).  The volatiles were removed under reduced pressure and the resulting product crystallised from ethanol (50 cm3) at 20 °C to give orange blocks (8.2 g, 27 mmol, 89%). 1H NMR (300 MHz, 293 K, CDCl3): δ 8.50 (s, 1H, CH=N), 7.99 (d, 1H, J = 7.5 Hz, Ar-H), 7.47 (d, 1H, J = 7.5 Hz, Ar-H), 7.05 (t, 1H, J = 7.6 Hz, Ar-H), 6.87 (s, 2H, Ar-H), 2.29 (s, 3H, p-Me), 2.12 (s, 6H, o-Me), 1.43 (s, 9H, But), 0.24 (s, 9H, Si(CH3)3). 13C NMR (75.5 MHz, 293 K, CDCl3): δ 161.6 (C-O), 155.5 (C=N), 149.3, 141.6, 133.1, 130.9, 129.2, 128.9, 127.3, 126.4, 122.0 (Ar), 35.3 (C(CH3)3), 30.8 (C(CH3)3), 21.2 (p-CH3), 18.8 (o-CH3), 2.1 (Si(CH3)3). Anal. Found: C, 75.36; H, 8.93; N, 3.74.  Calc. for :C23H33N: C, 75.15; H, 9.05; N 3.81.

3-But-2-(OSiMe3)C6H3CH=N(2-C6H5C6H4) (2d)

Following a similar procedure to that for 2a, 1d (13.4 g, 41 mmol) was deprotonated with n-BuLi (25.6 cm3 of a 1.6 M hexane solution, 41 mmol) and treated with excess SiClMe3 (20 cm3).   The volatiles were removed under reduced pressure and the resulting product crystallised from ethanol (50 cm3) at 20 °C to give yellow blocks (13.3 g, 36.9 mmol, 90%).  1H NMR (300 MHz, 293 K, CDCl3): δ 8.78 (s, 1H, CH=N), 7.80-6.55 (m, 11H, Ar), 1.47 (s, 9H, But), 0.32 (s, 9H, Si(CH3)3). 13C NMR (75.5 MHz, 293 K, CDCl3): δ 158.8 (C-O), 155.7 (C=N), 150.8, 144.6 (Ar), 140.1, 135.0, 130.8, 130.6, 130.4, 129.9, 129.3, 128.9, 128.7, 128.1, 127.7, 127.2, 127.0, 126.1, 122.1, 122.0, 119.5, 116.9, 112.1 (Ar), 35.3 (C(CH3)3), 30.9 (C(CH3)3), 2.3 (Si(CH3)3).

3-But-2-(OSiMe3)C6H3CH=N(C6F5) (2e)

Following a similar procedure to that for 2a, 1e (14.8 g, 43 mmol) was deprotonated with n-BuLi (26.9 cm3 of a 1.6 M hexane solution, 43 mmol) and treated with excess SiClMe3 (20 cm3).    The volatiles were removed under reduced pressure and the resulting product crystallised from light petroleum (40 cm3) at –30 °C to give bright yellow needle-shaped crystals (17 g, 41 mmol, 95%).  1H NMR (300 MHz, 293 K, CDCl3): δ 8.85 (s, 1H, CH=N), 7.97 (dd, 1H, J = 7.7, 1.8 Hz, Ar-H), 7.55 (dd, 1H, J = 7.7, 1.8 Hz, Ar-H), 7.05 (t, 1H, J = 7.7 Hz, Ar-H), 1.43 (s, 9H, But), 0.28 (s, 9H, Si(CH3)3).  13C NMR (75.5 MHz, 293 K, CDCl3): δ 167.6 (C-O), 156.6 (C=N), 141.9, 140.0, 136.6, 132.7, 128.0, 127.8, 126.7, 122.3 (Ar), 35.3 (C(CH3)3), 30.8 (C(CH3)3), 2.1 (Si(CH3)3).  19F (282.4 MHz, 293 K, CDCl3): δ –149.7 (s, 2F, o-F), -157.2 (s, 1F, p-F), -159.2 (s, 2F, m-F). Anal. Found: C, 58.20 ; H, 5.43; N, 3.40.  Calc. for C20H22N: C, 57.82; H, 5.34; N, 3.37.

3-But-2-(OSiMe3)C6H3CH=O (2f)

Following a similar procedure to that for 2a, 3-But-2-(OH)C6H3CH=O (4.1 g, 15 mmol) was deprotonated with n-BuLi (9.4 cm3 of a 1.6 M hexane solution, 15 mmol) and treated with excess SiClMe3 (10 cm3).    The volatiles were removed under reduced pressure and the resulting product crystallised from light petroleum (40 cm3) at –30 °C to give yellow plate-like crystals (3.2 g, 13 mmol, 85%). 1H NMR (293 MHz, 293 K, CDCl3): δ 8.77 (s, 1H, CH=N), 8.57 (d, 1H, J = 6.9 Hz, Ar-H), 7.67-6.96 (m, 7H, Ar-H), 3.41 (s, 2H, N-CH2), 1.41 (s, 9H, C(CH3)3), 0.32 (s, 9H, Si(CH3)). 13C NMR (75.5 MHz, 293 K, CDCl3): δ 191.5 (C=O), 158.1 (C-O), 142.3, 134.2, 129.4, 127.2, 121.9 (Ar), 35.3 (C(CH3)3), 30.8 (C(CH3)3),  2.1 (Si(CH3)).

Complex syntheses

[Ti{3-But-2-(O)C6H3CH=N(2,6-Pri2C6H3)}Cl(µ-Cl3)TiCl3] (3b)

TiCl4 (1.54 cm3, 14 mmol) was treated with 2b (2.79 g, 7 mmol) following a similar procedure to that for 3a.  The volatiles were removed under reduced pressure and the resulting red solid was washed with light petroleum (2 x 40 cm3).  The crude product was recrystallised from toluene at -30 °C, affording dark red blocks (suitable for X-ray diffraction) (4.24 g, 6.23 mmol, 89%).  1H NMR (300 MHz, 293 K, CDCl3): δ 8.54 (s, 1H, CH=N), 7.89-7.24 (m, 6H, Ar-H), 2.80 (m, 2H, CH(CH3)2), 1.65 (s, 9H, C(CH3)3), 1.36-1.34 (d, 6H, J = 6.7 Hz, CH(CH3)2), 1.09-1.11 (d, 6H, J = 6.8 Hz, CH(CH3)2).  13C NMR (75.5 MHz, 293 K, CDCl3): δ 170.9 (C-O), 167.0 (C=N), 140.6 (Ar), 139.2 (Ar), 136.6 (Ar), 133.6 (Ar), 128.7 (Ar), 124.7 (Ar), 124.4 (Ar), 124.1 (Ar), 35.7 (C(CH3)3), 30.4 (C(CH3)3), 29.6 (CH(CH3)2), 25.5 (CH(CH3)2), 23.1 (CH(CH3)2).  Anal. Found: C, 40.36; H, 4.33; N, 1.82; Cl, 37.33.  Calc. for C23H30NOCl7Ti2: C, 40.60; H, 4.44; N, 2.06; Cl, 36.47.

[Ti{3-But-2-(O)C6H3CH=N(2,4,6-Me3C6H2)}Cl(µ-Cl3)TiCl3] (3c)

TiCl4 (1.10 cm3, 10 mmol) was treated with 2c (1.84 g, 5 mmol) following a similar procedure to that for 3a.  The volatiles were removed under reduced pressure and the resulting red solid was washed with light petroleum (2 x 40 cm3).  Cooling a dichloromethane / petroleum solution to -30 °C overnight precipitated a dark red microcrystalline solid (2.55 g, 4.0 mmol, 80%)  1H NMR (300 MHz, 293 K, CDCl3): δ 8.49 (s, 1H, CH=N), 7.84 (d, 1H, J = 6.7Hz, Ar-H), 7.50 (dd, 1H, J = 6.2, 1.5 Hz, Ar-H), 7.30-6.97 (m, 3H, Ar-H), 2.34 (s, 3H, p-CH3), 2.17 (s, 6H, o-CH3), 1.62 (s, 9H, C(CH3)3). 13C NMR (75.5 MHz, 293 K, CDCl3): δ 171.9 (C-O), 163.6 (C=N), 139.9, 138.9, 136.4, 133.6, 132.7, 132.7, 130.9, 129.5, 124.7 (Ar), 35.6 (C(CH3)3), 30.3 (C(CH3)3), 21.3 (p-CH3), 19.8 (o-CH3).  Anal. Found: C, 37.69; H, 4.01; N, 1.98; Cl, 38.50.  Calc. for C20H24NOCl7Ti2: C, 37.63; H, 3.79; N, 2.19; Cl, 38.87.

Ti{3-But-2-(O)C6H3CH=N(2,4,6-Me3C6H2)}Cl3 (4c)

Repeated recrystallisation of 3c from a dichloromethane / light petroleum mixture afforded very small dark red plate-shaped crystals of the title compound (suitable for X-ray diffraction).

Ti{3-But-2-(O)C6H3CH=N(2,6-Pri2C6H3)}Cl3(THF) (5b)

2b (1.99 g, 5 mmol) was treated with TiCl4(THF)2 (1.67 g, 5 mmol) following a similar procedure to that for 5a.  The product was isolated in a similar fashion to 5a giving a dark red microcrystalline solid (2.50 g, 4.45 mmol, 89%).  1H NMR (300 MHz, 293 K, CDCl3): δ 8.37 (s, 1H, CH=N), 7.71-7.08 (m, 6H, Ar-H), 4.35 (m, 4H, THF), 2.39 (m, 2H, CH(CH3)3), 2.03 (m, 4H, THF), 1.58 (s, 9H, But), 1.34 (d, 6H, J = 4.1 Hz, CH(CH3)3), 1.06 (d, 6H, J = 4.1 Hz, CH(CH3)3).  13C NMR (75.5 MHz, 293 K, CDCl3): δ 169.9 (C-O), 142.0 (C=N), 138.4, 135.1, 133.9, 128.2, 124.4, 124.3 (Ar), 76.8 (THF), 35.7 (C(CH3)3), 30.3 (C(CH3)3), 26.4 (CH(CH3)3), 25.8 (THF), 23.4 (CH(CH3)3).  Anal. Found: C, 57.03; H, 6.79; N, 2.26; Cl, 19.17. Calc. for C27H38NO2Cl3Ti: C, 57.62; H, 6.81; N, 2.49; Cl, 18.90.

Ti{3-But-2-(O)C6H3CH=N(2,4,6-Me3C6H3)}Cl3(THF) (5c)

2c (2.60 g, 5 mmol) was treated with TiCl4(THF)2 (1.67 g, 5 mmol) following a similar procedure to that for 5a.  The product was isolated in a similar fashion to 5a giving dark red needle-shaped crystals (suitable for X-ray diffraction) (2.21 g, 4.25 mmol, 85%).  1H NMR (300 MHz, 293 K, CDCl3): δ 8.27 (s, 1H, CH=N), 7.73-7.16 (m, 5H, Ar-H), 4.25 (m, 4H, THF), 2.31 (s, 3H, p-CH3), 2.28 (s, 6H, o-CH3), 1.93 (m, 4H, THF), 1.59 (s, 9H, C(CH3)3).  13C NMR (75.5 MHz, 293 K, CDCl3): δ 170.4 (C-O), 138.3, 137.0, 134.9, 133.7, 131.3, 129.6, 124.4 (Ar), 35.7 (C(CH3)3), 30.3 (C(CH3)3), 25.7 (THF), 21.2 (p-CH3), 19.8 (o-CH3).  Anal. Found: C, 54.54; H, 6.11; N, 2.58; Cl, 20.06.  Calc. for C24H32NO2Cl3Ti: C, 55.35; H, 6.19; N, 2.69; Cl, 20.42.

Ti{3-But-2-(O)C6H3CH=N(2-C6H5C6H4)}Cl3(THF) (5d)

2d (2.4 g, 5.7 mmol) was treated with TiCl4(THF)2 (1.90 g, 5.7 mmol) following a similar procedure to that for 5a.  The product was isolated in a similar fashion to 5a giving dark red blocks (2.22 g, 4.0 mmol, 70%).  1H NMR (300 MHz, 293 K, CDCl3): δ 8.27 (s, 1H, CH=N), 7.61-7.03 (m, 12H, Ar-H), 4.17 (m, 4H, THF), 1.85 (m, 4H, THF), 1.53 (s, 9H, C(CH3)3). 13C NMR (75.5 MHz, 293 K, CDCl3): δ 170.3 (C-O), 161.9 (C=N), 139.0, 138.4, 135.7, 134.6, 133.6, 132.3, 130.5, 128.8, 127.8, 127.6, 126.8, 126.6, 124.4 (Ar), 75.7 (THF), 35.6 (C(CH3)3), 30.1 (C(CH3)3), 25.8 (THF).  Anal. Found: C, 57.53; H, 5.46; N, 2.30; Cl, 19.83.  Calc. For C27H30NO2Cl3Ti: C, 58.45; H, 5.45; N, 2.52; Cl, 19.17.

Ti{3-But-2-(O)C6H3CH=N(C6F5)}Cl3(THF) (5e)

2e (1.6 g, 5 mmol) was treated with TiCl4(THF)2 (1.67 g, 5 mmol) following a similar procedure to that for 5a.  The product was isolated in a similar fashion to 5a giving dark red blocks (suitable for X-ray diffraction) (3.05 g, 5.36 mmol, 85%).  1H NMR (300 MHz, 293 K, CDCl3): δ 8.51 (s, 1H, CH=N), 7.79 (dd, 1H, J = 7.5, 1.4 Hz, Ar-H), 7.48 (dd, 1H, J = 7.6, 1.4 Hz, Ar-H),  7.20 (t, 1H, J = 7.8 Hz, Ar-H), 4.22 (m, 4H, THF), 2.00 (m, 4H, THF), 1.58 (s, 9H, C(CH3)3).  13C NMR (75.5 MHz, 293 K, CDCl3): δ 173.8 (C-O), 162.4 (C=N), 139.1, 136.8, 135.1, 125.2, 124.2 (Ar), 75.5 (THF), 35.6 (C(CH3)3), 30.0 (C(CH3)3), 25.8 (THF).  19F (282.4 MHz, 293 K, CDCl3): δ –148.5 (br, 2F, o-F), -146.5 (t, 1F, p-F), -162.2 (br, 2F, m-F).  Anal. Found: C, 43.90; H, 3.70; N, 2.35; Cl, 19.56.  Calc. For C21H21NO2Cl3F5Ti: C, 44.36; H, 3.72; N, 2.46; Cl, 18.70.

Zr{3-But-2-(O)C6H3CH=N(2,4,6-Me3C6H2)}Cl3(THF) (6c)

2c (1.32 g, 4.5 mmol) was treated with ZrCl4(THF)2 (1.63 g, 4.5 mmol) following a similar procedure to that for 5a.  The product was isolated in a similar fashion to 5a giving a yellow microcrystalline solid (2.36 g, 4.11 mmol, 93%). 1H NMR (300 MHz, 293 K, CDCl3): δ 8.31 (s, 1H, CH=N), 7.68 (dd, 1H, J = 7.8, 1.6 Hz, Ar-H), 7.30 (dd, 1H, J = 7.7, 1.6 Hz, Ar-H), 7.05 (t, 1H, J = 7.7 Hz, Ar-H), 6.93 (s, 2H, Ar-H), 4.31 (m, 4H, THF), 2.28 (s, 6H, o-CH3), 2.24 (s, 3H, p-CH3), 1.98 (m, 4H, THF), 1.55 (s, 9H, C(CH3)3). 13C NMR (75.5 MHz, 293 K, CDCl3): δ 173.2 (C-O), 168.7 (C=N), 140.2, 138.9, 133.6, 133.2, 130.2, 122.1, 119.9 (Ar), 76.6 (THF), 35.9 (C(CH3)3), 31.3 (C(CH3)3), 26.0 (THF), 21.6 (p-CH3), 18.6 (o-CH3).  Anal. Found: C, 51.26; H, 6.02; N, 2.18; Cl, 17.41.  Calc. For C24H32NO2Cl3Zr: C, 51.10; H, 5.72; N, 2.48; Cl, 18.85.

Zr{3-But-2-(O)C6H3CH=N(2-C6H5C6H4)}Cl3(THF) (6d)

2d (2.4 g, 5.7 mmol) was treated with ZrCl4(THF)2 (2.1 g, 5.7 mmol) following a similar procedure to that for 5a.  The product was isolated in a similar fashion to 5a giving yellow block crystals suitable for X-ray crystallography (3.00 g, 5.02 mmol, 88%). 1H NMR (300 MHz, 293 K, CDCl3): δ 8.45 (s, 1H, CH=N), 7.67-6.91 (m, 12H, Ar-H), 4.79 (m, 4H, THF), 2.13 (m, 4H, THF), 1.61 (s, 12H, C(CH3)3). 13C NMR (75.5 MHz, 293 K, CDCl3): δ 173.9 (C=N), 139.8, 135.4, 134.5, 132.8, 130.8, 130.4, 130.0, 128.3, 128.2, 127.7, 127.5, 126.1, 122.0 (Ar), 75.7 (THF), 35.4 5 (C(CH3)3), 29.8 (C(CH3)3), 26.1 (THF). Anal. Found: C, 54.00; H, 2.04; N, 2.04; Cl, 18.10.  Calc. For C27H30NO2Cl3Zr: C, 54.22; H, 5.06; N, 2.34; Cl, 17.78.

Zr{3-But-2-(O)C6H3CH=N(C6F5)}Cl3(THF) (6e)

2e (2.08 g, 5 mmol) was treated with ZrCl4(THF)2 (1.81 g, 5 mmol) following a similar procedure to that for 5a. The product was isolated in a similar fashion to 5a giving yellow needle-shaped crystals (suitable for X-ray diffraction). 1H NMR (300 MHz, 293 K, CDCl3): δ 8.51 (s, 1H, CH=N), 7.76 (dd, 1H, J = 6.4, 1.3 Hz, Ar-H), 7.43 (dd, 1H, J = 6.4, 1.3 Hz, Ar-H), 7.10 (t, 1H, J = 7.7 Hz, Ar-H), 4.23 (m, 4H, THF), 2.03 (m, 4H, THF), 1.51 (s, 9H, C(CH3)3).  13C NMR (75.5 MHz, 293 K, CDCl3): δ 177.4 (C-O), 162.7 (C=N), 160.2, 143.2, 140.5, 139.9, 137.6, 135.6, 122.9, 122.5 (Ar), 75.8 (THF), 35.5 (C(CH3)3), 29.8 (C(CH3)3), 25.8 (THF).  19F NMR (282.4 MHz, 293 K, CDCl3): δ –147.3 (br, 1F, m-F), -151.0 (br, 1F, m-F), -156.5 (t, 1F, p-F), -161.0 (br, 1F, o-F), -162.7 (br, 1F, o-F).  Anal. Found: C, 41.32; H, 3.33; N, 2.26; Cl, 17.20.  Calc. For C21H21NO2Cl3F5Zr: C, 41.22; H, 3.46; N, 2.29; Cl, 17.38.