Supporting Information

- Charge-Transfer Guest Interactions in Luminescent MOFs: Implications for Solid-state Temperature and Environmental Sensing

Patrick L. Feng, Kirsty Leong, and Mark D. Allendorf

Sandia National Laboratories, Livermore, CA 94550-0969

E-mail: plfeng@sandia.gov; mdallen@sandia.gov

KEYWORDS:  Metal-Organic Frameworks, charge-transfer complex, ratiometric, fluorescence, sensing

Figure S1. Steady-state photoluminescence spectra for complex 2, highlighting the wavelength-dependent excitation and emission characteristics.

Figure S2. Time-resolved photoluminescence data collected at the monomer emission maximum of 385nm (top) and charge-transfer emission at 532nm (bottom) for complex 1b, both collected at an excitation wavelength of (λex = 341 nm).

Figure S3. Representative Gaussian fit for the photoluminescence spectrum of 1a, collected at λex=340nm.

Table S1. Gaussian fitting parameters corresponding to the fits shown in Figure S3.

Gaussian Fit

R^2	=0.99868

y0		0			±0

362 nm

Center		361.36145		±0.07375

Width		7.78245		±0.14925

Area		5324605.83599		±133884.95693

378 nm

Center		375.75704		±0.10477

Width		12.4626		±0.37759

Area		8692210.7243		±563224.84184

393 nm

Center		392.94668		±0.70019

Width		25.322			±1.05575

Area		11934167.70365	±762781.17073

457 nm

Center		446.23444		±0.54683

Width 		117.25208		±0.81584