Suuplementary Data for:

Journal of Materials Chemistry a907106g

Donor-acceptor complexes of fullerene C60 with organic and organometallic donors.

Dmitri V. Konareva, Rimma  N. Lyubovskaya*a, Natal´ya  V. Drichkob, Evgeniya  I. Yudanovaa, Yury M. Shul`gaa, Aleksey  L. Litvinova, Viktor  N. Semkinb, and Boris P. Tarasova

aInstitute of Problems of Chemical Physics RAS, Chernogolovka, Moscow region 142432, Russia. E-mail:  lyurn@icp.ac.ru

bA.F. Ioffe Physical-Technical Institute, St.-Petersburg 194021, Russia

Table  C60 complexes and their characteristics: elemental analysis, the a.b. of solvents in the IR spectrum, and the content of a solvent according to TG analysis.

| N | Complex | Elemental analysis (Found/Calculated) C H S N |  |  |  | Solvent1, cm-1 | Solv.,% |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | (BA)2C60 | 94.39 93.44 | 1.95 1.90 |  |  | Absent | 0 |
| 2 | (BXA)2C60 | 91.84 93.13 | 2.90 2.47 |  |  | Absent | 0 |
| 3 | TMT(C60)3C6H6 | 93.27 93.56 | 1.37 0.94 | 2.64 2.75 |  | 676, 1478, 3030 | 2.7 |
| 4 | (TMT)2C60(C7H8)0.5 | 78.44 79.75 | 2.65 2.49 | 8.69 8.88 |  | 465, 730, 1494, 2922, 3028 | 2.7 |
| 5 | (BEDT-TTF)2C60 (C5H5N)2 | 66.24 65.76 | 1.36 1.57 | 31.00 30.97 | 1.72 1.70 | 702, 745, 1030, 1440, 3022 | - |
| 6 | OMTTFC60C5H5N | 86.64 85.44 | 1.64 1.87 | 10.68 11.44 | 1.44 1.25 | 701, 745, 1029, 1442, 3022 | - |
| 7 | (BEDO-TTF)2C60 | 70.56 70.76 | 1.64 1.17 | 19.89 18.74 |  | Absent | - |
| 8 | BEDO-TTFC60C6H6 | 79.41 81.68 | 1.55 1.24 | 10.07 11.38 |  | 680, 1482, 3025 | 5.5 |
| 9 | DP-TTFC60C6H6 | 86.51 87.43 | 1.48 1.55 | 11.65 11.02 |  | 679, 1480, 3032 | - |
| 10 | (DMDP-TTF)2C60C6H6 | 82.24 81.35 | 2.31 2.41 | 14.91 16.24 |  | 680, 1478, 3030 | - |
| 11 | OOT-TTF C60C7H8 | 74.86 75.41 | 1.24 1.29 | 22.10 20.71 |  | 730, 1490, 2922, 3028 | 5.1 |
| 12 | TBT-TTF(C60)2 | 84.84 84.56 | 1.22 0.90 | 11.13 11.61 |  | Absent | - |
| 13 | EDY-BEDT-DTC60C6H6 | - / 77.7 | - / 1.3 | 19.9 /21.0 |  | 674, 1477, 3024 | - |
| 14 | BNDYC60 | 85.10 87.62 | 1.12 1.06 | 12.04 11.32 |  | Absent | 0 |
| 15 | DADTF(C60)2CS2 | 84.78 85.17 | 1.26 1.06 | 8.80 9.34 | 1.20 1.35 | 1508 | - |
| 16 | TBMA(C60)2 | 95.48 95.89 | 1.55 1.61 |  | 1.43 1.50 | Absent | - |
| 17 | LCVC60C6H5Cl | 91.29 91.07 | 2.45 2.55 | 2.52 (Cl) 2.92 (Cl) | 2.48 3.46 | 680, 736, 918, 1475 | 5.1 |
| 18 | BMPPC60 | 92.65 92.64 | 1.84 1.40 | 2.58 2.78 |  | Absent | 0 |
| 19 | (TP)2C60 | 95.99 97.98 | 1.65 2.02 |  |  | Absent | 0 |
| 21 | TPBC60 | 98.67 97.98 | 1.76 2.02 |  |  | Absent | 0 |
| 22 | TPEC60(C6H5Cl)0.5 | 96.31 96.41 | 1.64 2.01 | 1.42 (Cl) 1.58 (Cl) |  | 735, 1476 | 2.0 |
| 23 | DPAC60 | 98.30 96.26 | 2.05 1.70 |  |  | Absent | 0 |
| 24 | DBAC60C6H6 | 98.2 98.16 | 2.04 1.84 |  |  | 674, 1476, 3028 | - |
| 25 | (Cp*2Fe)2C60 | 86.52 87.56 | 4.27 4.34 |  |  | Absent | 0 |
| 26 | (Cp2Ni)xC60(CS2)2 x < 0.2 | 86.00 85.97 | Absent 0.02 | 11.65 12.79 |  | 1510 | 10.6 |
| 27 | C60 (I2)0.9 | I, (%) 24.52 25.91 |  |  |  | Absent | 0 |

1- The table lists only a.b. of the solvent which did not coincide with a.b. of the donors.