Electronic Supplementary Information

X1[K+]. Anal. calc. for C23H26Si2O9KSN : C, 47.02, K, 6.64, Si, 9.54 %. Found : C, 45.39, K, 5.50, Si, 8.10 %.

X1[Na+]. Anal. calc. for C23H26Si2O9NaSN : C, 48.33 , Na, 4.03 , Si, 9.81. Found : C, 48.7, Na, 3.65, Si, 8.90 %.

X2[K+]. 13C NMR (, ppm) 20, 68, 112-122, 131, 147. Anal. calc. for C25H26Si2O9KSN : C, 49.10, K, 6.38, Si, 9.16 %. Found : C, 47.95, K, 5.9, Si, 8.54 %.

X3[K+]. Anal. calc. for C29H28Si4O12KSN : C, 45.49 , H, 3.69, K, 5.00, Si, 14.63 %. Found : C, 48.38, H, 5.06, K, 4.30 , Si, 12.30 %.

Complexation of Na+ by the xerogel X1 at reflux

29Si NMR (, ppm) -63, -69. Anal. calc. for C23H26Si2O9NaSN : C, 48.33, Na, 4.03, Si, 9.81 %. Found C, 51.31, Na, 1.80, Si, 10.10 %.

Complexation of K+ by the xerogel X1 at room temperature

29Si NMR (, ppm) -62, -70. Anal. calc. for C23H26Si2O9KSN : C, 47.02, K, 6.64, Si, 9.54 %. Found C, 51.85, K, 4.99, Si, 9.95 %.

Complexation of K+ by the xerogel X1 at reflux

29Si NMR (, ppm) -62, -67. Specific surface area <10 m2.g-1. Anal. calc. for C23H26Si2O9KSN : C, 47.02, K, 6.64, Si, 9.54 %. Found C, 47.92, K, 4.85, Si, 9.00 %.

Complexation of the 1/1 Na+/K+ mixture by the xerogel X1 at room temperature

Anal. calc. for C23H26Si2O9NaSN : C, 48.33, H, 4.55, Na, 4.03, N, 2.45,Si, 9.81 %. Anal.calc. for C23H26Si2O9KSN : C, 47.02, H, 4.43, K, 6.64, N, 2.39, Si, 9.54 %. Found C, 47.31, H, 4.94, K, 4.80, Na, 0.40, N, 1.98, Si, 8.30 %.

Complexation of Na+ and K+ by the xerogel X1 at reflux

Anal. calc. for C23H26Si2O9NaSN : C, 48.33, H, 4.55, Na, 4.03, N, 2.45, Si, 9.81 %. Anal. calc. for C23H26Si2O9KSN : C, 47.02, K, 6.64, N, 2.39, Si, 9.54 %. Found C, 47.65, H, 5.18, K, 4.80, Na, 0.40, N, 1.93, Si, 9.30 %.

Complexation of Na+ by the xerogel X2A at room temperature

Anal. calc. for C25H26Si2O9NaSN : Si, 9.41, N, 2.35, Na, 3.87 %. Found Si, 8.80, Na, 1.14 %.

Complexation of K+ by the xerogel X2A at room temperature

Anal. calc. for C25H26Si2O9KSN : Si, 9.16, K, 6.38 % . Found Si, 8.40, K, 3.06 %.

Complexation of the 1/1 Na+/K+ mixture by the xerogel X2A at room temperature

Anal. calc. for C25H26Si2O9NaSN : Si, 9.41, Na, 3.87 %. Anal. calc. for C25H26Si2O9KSN : Si, 9.16, K, 6.38 %. Found Si, 8.40, K, 3.10, Na, 0.85%.

Complexation of Na+ by the xerogel X2B at room temperature

Anal. calc. for C25H26Si2O9NaSN : Si, 9.41, Na, 3.87 %. Found Si, 9.00, Na, 1.36 %.

Complexation of K+ by the xerogel X2B at room temperature

Anal. calc. for C25H26Si2O9KSN : Si, 9.16, K, 6.38 %. Found Si, 8.50, K, 3.27 %.

Complexation of the 1/1 Na+/K+ mixture by the xerogel X2B at room temperature

Anal. calc. for C25H26Si2O9NaSN : Si, 9.41, Na, 3.87 %. Anal. calc. for C25H26Si2O9KSN : Si, 9.16, K, 6.38 %. Found Si, 8.05, K, 3.40, Na, 0.85 %.

Complexation of Na+ by the xerogel X2C at room temperature

Anal. calc. for C25H26Si2O9NaSN : Si, 9.41, Na, 3.87 %. Found Si, 9.01, Na, 1.22 %.

Complexation of K+ by the xerogel X2C at room temperature

Anal. calc. for C25H26Si2O9KSN : Si, 9.16, K, 6.38 %. Found Si, 8.40, K, 3.30 %.

Complexation of the 1/1 Na+/K+ mixture by the xerogel X2C at room temperature

Anal. calc. for C25H26Si2O9NaSN : Si, 9.41, Na, 3.87 %. Anal. calc. for C25H26Si2O9KSN : Si, 9.16, K, 6.38 %. Found : Si, 8.25, K, 3.25, Na, 0.60 %.

Complexation of Na+ by the xerogel X3A at room temperature

Anal. calc. for C29H28Si4O12NaSN : Si, 14.95, Na, 3.07 %. Found Si, 12.60, Na, 0.31 %.

Complexation of K+ by the xerogel X3A at room temperature

Anal. calc. for C29H28Si4O12KSN : Si, 14.63, K, 5.00 %. Found Si, 12.65, K, 1.62 %.

Complexation of the 1/1 Na+/K+ mixture by the xerogel X3A at room temperature

Anal. calc. for C29H28Si4O12NaSN : Si, 14.95, Na, 3.07 %. Anal. calc. for C29H28Si4O12KSN : Si, 14.63, K, 5.00 %. Found Si, 12.70, K, 1.50, Na, 0.40 %.

Complexation of Na+ by the xerogel X3B at room temperature

Anal. calc. for C29H28Si4O12NaSN : Si, 14.95, Na, 3.07 %. Found Si, 12.90, Na, 0.64 %.

Complexation of K+ by the xerogel X3B at room temperature

Anal. calc. for C29H28Si4O12KSN : Si, 14.63, K, 5.00 %. Found Si, 12.44, K, 1.92 %.

Complexation of the 1/1 Na+/K+ mixture by the xerogel X3B at room temperature

Anal. calc. for C29H28Si4O12NaSN : Si, 14.95, Na, 3.07 %. Anal. calc. for C29H28Si4O12KSN : Si, 14.63, K, 5.00 %. Found Si, 13.05, Na, 0.45, K,1.95 %.

Complexation of Na+ by the xerogel X3C at room temperature

Anal. calc. for C29H28Si4O12NaSN : Si 14.95, Na, 3.07 %. Found Si, 12.79, Na, 0.91 %.

Complexation of K+ by the xerogel X3C at room temperature

Anal. calc. for C29H28Si4O12KSN : Si, 14.63, K, 5.00 %. Found Si, 12.57, K, 2.07 %.

Complexation of the 1/1 Na+/K+ mixture by the xerogel X3C at room temperature

Anal. calc. for C29H28Si4O12NaSN : Si 14.95, Na, 3.07 %. Anal. calc. for C29H28Si4O12KSN : Si, 14.63, K, 5.00 %. Found Si, 13.45, K, 2.15, Na, 0.35 %.