Mass loss and temperatures transition of the protonated phases H2[A0.5nBnO3n+1].xH2O observed from the TG-DT analysis

| Composition | Mass loss (%) Observed Calculated |  | Temperature (°C) and characteristics of transformations |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| H2Sr1.5Nb3O10.0.22H2O | 3.80 | 3.80 |  | 242-NR-En | 470-NR-Ex | 680-NR-Ex |  |  |  |  |  |
| H2SrNb2O7 | 4.69 | 4.64 |  | 301- NR- En | 329-NR-En | 725-NR-Ex |  |  |  |  |  |
| H2SrTa2O7 | 3.14 | 3.19 |  | 116-R-En | 280-R-En | 434- NR-En |  |  | 942-NR-Ex |  |  |
| H2Ca1.5Nb3O10 | 3.80 | 3.81 |  | 171-NR-En | 251-NR-Ex | 383-NR-Ex |  | 665-NR-Ex |  |  |  |

R : Reversible transformation - NR : Non Reversible transformation

En : Endotherm transformation - Ex : Exotherm transformation