Electronic Supplementary materials

Spin Density of a Ferromagnetic Tempo Derivative:

Polarized Neutron Investigation and Ab Initio Calculation1

Yves Pontillon a, André Grand b, Takayuki Ishida c, Eddy Lelièvre-Berna d, Takashi Nogami c, Eric Ressouche a and Jacques Schweizer a *.

a Commissariat à l'Energie Atomique, MDN/SPSMS/DRFMC, CEN-Grenoble, 17 rue des Martyrs, 38054 Grenoble Cedex 9, France.

b Commissariat à l'Energie Atomique, SCIB/DRFMC, CEN-Grenoble, 17 rue des Martyrs, 38054 Grenoble Cedex 9, France.

c Department of Applied Physics and Chemistry, University of Electro-Communications, Chofu, Tokyo 182-8585, Japan

d Institut Laue Langevin, 6 rue J. Horowitz, 156X, 38042 Grenoble Cedex 9, France

Atoms x y z Beq (Å2)

CL1 4406( 4) 5053( 1) 1719( 1) 0.77 O 1 -2162( 7) 7172( 1) 10057( 2) 0.80 N 1 -1036( 4) 6953( 1) 9332( 1) 0.54 N 2 1921( 4) 6171( 1) 6734( 1) 0.64 C 1 1879( 6) 6492( 1) 7824( 2) 0.48 C 2 235( 6) 6993( 1) 7401( 2) 0.59 C 3 -419( 6) 7333( 1) 8417( 2) 0.55 C 4 311( 6) 6426( 1) 9751( 2) 0.55 C 5 789( 6) 6124( 1) 8648( 2) 0.69 C 6 -2650( 6) 7682( 1) 7869( 2) 0.80 C 7 1629( 6) 7725( 1) 9047( 2) 0.74 C 8 -1273( 6) 6059( 1) 10341( 2) 0.89 C 9 2653( 6) 6560( 1) 10708( 2) 0.77 C 10 3791( 6) 6191( 1) 6320( 2) 0.61 C 11 3966( 6) 5905( 1) 5207( 2) 0.53 C 12 2203( 6) 5523( 1) 4641( 2) 0.68 C 13 2297( 6) 5259( 1) 3567( 2) 0.75 C 14 4226( 6) 5385( 1) 3057( 2) 0.61 C 15 5984( 6) 5765( 1) 3588( 2) 0.68 C 16 5852( 6) 6019( 1) 4672( 2) 0.75 H 11 3711( 12) 6624( 2) 8300( 5) 1.60 H 21 -1459( 12) 6841( 2) 6772( 5) 1.77 H 22 1054( 13) 7276( 2) 6871( 5) 1.93 H 51 -942( 12) 5965( 2) 8094( 4) 1.65 H 52 1928( 14) 5762( 2) 8958( 4) 1.97 H 61 -2341( 14) 7931( 2) 7115( 5) 2.28 H 62 -3088( 14) 7960( 2) 8538( 5) 2.38 H 63 -4215( 14) 7418( 3) 7499( 6) 2.54 H 71 1850( 14) 8060( 2) 8420( 5) 2.03 H 72 3393( 13) 7528( 2) 9333( 6) 2.34 H 73 1188( 15) 7925( 2) 9826( 5) 2.51 H 81 -428( 15) 5648( 2) 10535( 5) 2.50 H 82 -1555( 14) 6245( 2) 11158( 5) 2.44 H 83 -3043( 13) 6000( 2) 9711( 5) 2.09 H 91 2236( 14) 6820( 3) 11417( 5) 2.48 H 92 3460( 14) 6170( 2) 11106( 5) 2.34 H 93 3984( 14) 6777( 2) 10335( 5) 2.02 H 10 5404( 13) 6431( 3) 6810( 5) 2.42 H 12 711( 13) 5438( 3) 5059( 5) 2.19 H 13 956( 14) 4952( 2) 3141( 5) 2.62 H 15 7469( 13) 5858( 2) 3181( 5) 1.95 H 16 7264( 13) 6311( 2) 5119( 5) 2.30

Table S1: Positions and isotropic thermal parameters at T=4.5 K

| 4.5 K | 298 K |
| --- | --- |
| N 1 C 3 1.486 ( 3) N 1 C 4 1.494 ( 3) N 2 C 1 1.459 ( 3) N 2 C 10 1.272 ( 3) CL1 C 14 1.736 ( 3) O 1 N 1 1.276 ( 4) C 1 C 2 1.528 ( 3) C 1 C 5 1.525 ( 4) C 2 C 3 1.530 ( 3) C 3 C 6 1.524 ( 4) C 3 C 7 1.533 ( 4) C 4 C 5 1.525 ( 3) C 4 C 8 1.529 ( 4) C 4 C 9 1.536 ( 4) C 10 C 11 1.459 ( 3) C 11 C 12 1.396 ( 3) C 11 C 16 1.389 ( 4) C 12 C 13 1.384 ( 3) C 13 C 14 1.399 ( 4) C 14 C 15 1.380 ( 4) C 15 C 16 1.389 ( 4) C 1 H 11 1.101 ( 7) C 2 H 21 1.114 ( 6) C 2 H 22 1.085 ( 7) C 5 H 51 1.102 ( 6) C 5 H 52 1.090 ( 6) C 6 H 61 1.090 ( 7) C 6 H 62 1.084 ( 7) C 6 H 63 1.092 ( 8) C 7 H 71 1.100 ( 6) C 7 H 72 1.089 ( 8) C 7 H 73 1.087 ( 7) C 8 H 81 1.094 ( 6) C 8 H 82 1.074 ( 7) C 8 H 83 1.095 ( 7) C 9 H 91 1.088 ( 7) C 9 H 92 1.089 ( 6) C 9 H 93 1.089 ( 8) C 10 H 10 1.113 ( 7) C 12 H 12 1.093 ( 8) C 13 H 13 1.087 ( 7) C 15 H 15 1.086 ( 8) C 16 H 16 1.094 ( 7) | N 1 C 3 1.487 N 1 C 4 1.484 N 2 C 1 1.463 N 2 C 10 1.259 CL1 C 14 1.749 O 1 N 1 1.284 C 1 C 2 1.526 C 1 C 5 1.530 C 2 C 3 1.534 C 3 C 6 1.532 C 3 C 7 1.547 C 4 C 5 1.525 C 4 C 8 1.546 C 4 C 9 1.534 C 10 C 11 1.470 C 11 C 12 1.389 C 11 C 16 1.369 C 12 C 13 1.372 C 13 C 14 1.366 C 14 C 15 1.354 C 15 C 16 1.387 |

Table S2: Comparison of the bond lengths at T=298K and T=4.5K

| 4.5 K | 298 K |
| --- | --- |
| O 1 N 1 C 3 116.2 (0.2) O 1 N 1 C 4 116.5 (0.2) C 3 N 1 C 4 123.2 (0.2) C 1 N 2 C 10 118.9 (0.2) N 2 C 1 C 2 106.7 (0.2) N 2 C 1 C 5 107.9 (0.2) N 2 C 1 H 11 110.7 (0.4) C 2 C 1 C 5 109.4 (0.3) C 2 C 1 H 11 111.5 (0.3) C 5 C 1 H 11 110.5 (0.3) C 1 C 2 C 3 115.4 (0.2) C 1 C 2 H 21 108.4 (0.4) C 1 C 2 H 22 110.3 (0.4) C 3 C 2 H 21 108.6 (0.4) C 3 C 2 H 22 107.6 (0.4) H 21 C 2 H 22 106.1 (0.5) N 1 C 3 C 2 110.0 (0.2) N 1 C 3 C 6 107.5 (0.3) N 1 C 3 C 7 109.7 (0.2) C 2 C 3 C 6 108.7 (0.2) C 2 C 3 C 7 112.0 (0.3) C 6 C 3 C 7 108.9 (0.2) N 1 C 4 C 5 108.8 (0.2) N 1 C 4 C 8 108.0 (0.2) N 1 C 4 C 9 109.9 (0.2) C 5 C 4 C 8 109.3 (0.2) C 5 C 4 C 9 112.0 (0.3) C 8 C 4 C 9 108.8 (0.2) C 1 C 5 C 4 114.2 (0.2) C 1 C 5 H 51 107.3 (0.4) C 1 C 5 H 52 110.8 (0.5) C 4 C 5 H 51 108.2 (0.4) C 4 C 5 H 52 109.1 (0.3) H 51 C 5 H 52 107.0 (0.5) C 3 C 6 H 61 109.7 (0.5) C 3 C 6 H 62 111.5 (0.4) C 3 C 6 H 63 111.5 (0.4) H 61 C 6 H 62 108.7 (0.5) H 61 C 6 H 63 107.0 (0.5) H 62 C 6 H 63 108.3 (0.7) C 3 C 7 H 71 110.0 (0.4) C 3 C 7 H 72 114.9 (0.4) C 3 C 7 H 73 110.1 (0.5) H 71 C 7 H 72 105.2 (0.6) H 71 C 7 H 73 106.7 (0.5) H 72 C 7 H 73 109.5 (0.5) | O 1 N 1 C 3 115.8 O 1 N 1 C 4 117.4 C 3 N 1 C 4 123.9 C 1 N 2 C 10 117.9 N 2 C 1 C 2 107.3 N 2 C 1 C 5 107.8 C 2 C 1 C 5 108.4 C 1 C 2 C 3 115.5 N 1 C 3 C 2 109.8 N 1 C 3 C 6 108.3 N 1 C 3 C 7 108.8 C 2 C 3 C 6 108.4 C 2 C 3 C 7 111.6 C 6 C 3 C 7 109.9 N 1 C 4 C 5 109.4 N 1 C 4 C 8 108.2 N 1 C 4 C 9 109.0 C 5 C 4 C 8 109.0 C 5 C 4 C 9 111.9 C 8 C 4 C 9 109.3 C 1 C 5 C 4 114.5 |

Table S3a: Comparison of the bond angles at T=298K and T=4.5K

| 4.5 K | 298 K |
| --- | --- |
| C 4 C 8 H 81 108.8 (0.5) C 4 C 8 H 82 111.7 (0.4) C 4 C 8 H 83 110.1 (0.4) H 81 C 8 H 82 110.6 (0.5) H 81 C 8 H 83 108.0 (0.5) H 82 C 8 H 83 107.6 (0.6) C 4 C 9 H 91 109.1 (0.5) C 4 C 9 H 92 108.7 (0.4) C 4 C 9 H 93 113.6 (0.4) H 91 C 9 H 92 109.4 (0.5) H 91 C 9 H 93 108.4 (0.5) H 92 C 9 H 93 107.6 (0.6) N 2 C 10 C 11 123.0 (0.3) N 2 C 10 H 10 120.5 (0.4) C 11 C 10 H 10 116.6 (0.5) C 10 C 11 C 12 120.5 (0.3) C 10 C 11 C 16 120.7 (0.2) C 12 C 11 C 16 118.7 (0.2) C 11 C 12 C 13 121.5 (0.3) C 11 C 12 H 12 118.6 (0.3) C 13 C 12 H 12 119.9 (0.4) C 12 C 13 C 14 118.0 (0.3) C 12 C 13 H 13 121.5 (0.5) C 14 C 13 H 13 120.4 (0.4) CL1 C 14 C 13 119.0 (0.2) CL1 C 14 C 15 119.2 (0.3) C 13 C 14 C 15 121.8 (0.2) C 14 C 15 C 16 118.8 (0.3) C 14 C 15 H 15 120.9 (0.3) C 16 C 15 H 15 120.3 (0.4) C 11 C 16 C 15 121.1 (0.3) C 11 C 16 H 16 119.3 (0.4) C 15 C 16 H 16 119.6 (0.5) | N 2 C 10 C 11 122.7 C 10 C 11 C 12 121.7 C 10 C 11 C 16 121.3 C 12 C 11 C 16 117.1 C 11 C 12 C 13 121.4 C 12 C 13 C 14 119.5 CL1 C 14 C 13 119.6 CL1 C 14 C 15 119.3 C 13 C 14 C 15 121.0 C 14 C 15 C 16 118.8 C 11 C 16 C 15 122.2 |

Table S3b: Comparison of the bond angles at T=298K and T=4.5K

Thermal parameters beta(i,j)

CL1 0.0081( 7) 0.0002( 0) 0.0014( 1) 0.0002( 1) 0.0015( 2)-0.0001( 0) O 1 0.0089( 13) 0.0003( 0) 0.0012( 2)-0.0001( 2) 0.0020( 4) 0.0000( 1) N 1 0.0056( 7) 0.0002( 0) 0.0009( 1) 0.0002( 1) 0.0009( 2) 0.0000( 1) N 2 0.0062( 7) 0.0003( 0) 0.0010( 1)-0.0001( 2) 0.0015( 2)-0.0002( 1) C 1 0.0044( 9) 0.0002( 0) 0.0009( 2)-0.0001( 2) 0.0009( 4) 0.0000( 1) C 2 0.0060( 10) 0.0002( 0) 0.0009( 2)-0.0004( 2) 0.0004( 4)-0.0001( 1) C 3 0.0060( 9) 0.0002( 0) 0.0010( 2) 0.0001( 2) 0.0015( 3) 0.0001( 1) C 4 0.0045( 9) 0.0002( 0) 0.0013( 2)-0.0004( 2) 0.0015( 3) 0.0000( 1) C 5 0.0074( 11) 0.0002( 0) 0.0013( 2) 0.0000( 2) 0.0010( 4) 0.0000( 1) C 6 0.0089( 11) 0.0002( 0) 0.0014( 2) 0.0004( 2) 0.0011( 4) 0.0000( 1) C 7 0.0076( 10) 0.0002( 0) 0.0014( 2)-0.0006( 2) 0.0014( 4) 0.0002( 1) C 8 0.0103( 13) 0.0002( 0) 0.0017( 2)-0.0004( 2) 0.0023( 4) 0.0001( 1) C 9 0.0076( 11) 0.0003( 0) 0.0014( 2)-0.0001( 3) 0.0012( 4) 0.0000( 1) C 10 0.0057( 10) 0.0003( 0) 0.0009( 2)-0.0001( 3) 0.0016( 4)-0.0001( 1) C 11 0.0060( 9) 0.0002( 0) 0.0007( 1) 0.0006( 2) 0.0016( 3) 0.0001( 1) C 12 0.0055( 10) 0.0003( 0) 0.0014( 2)-0.0004( 2) 0.0012( 4)-0.0001( 1) C 13 0.0062( 10) 0.0003( 0) 0.0013( 2)-0.0001( 2) 0.0019( 4)-0.0003( 1) C 14 0.0064( 10) 0.0002( 0) 0.0011( 2) 0.0004( 2) 0.0013( 4) 0.0000( 1) C 15 0.0055( 9) 0.0003( 0) 0.0012( 2) 0.0002( 2) 0.0010( 4) 0.0000( 1) C 16 0.0075( 10) 0.0003( 0) 0.0011( 2) 0.0001( 2) 0.0014( 4)-0.0003( 1) H 11 0.0110( 22) 0.0007( 1) 0.0034( 4)-0.0006( 5) 0.0012( 8) 0.0001( 2) H 21 0.0103( 22) 0.0008( 1) 0.0043( 4)-0.0004( 5)-0.0021( 9)-0.0002( 2) H 22 0.0185( 25) 0.0005( 1) 0.0042( 4) 0.0001( 5) 0.0046( 9) 0.0003( 2) H 51 0.0113( 22) 0.0007( 1) 0.0038( 4)-0.0010( 5) 0.0004( 9)-0.0002( 2) H 52 0.0193( 26) 0.0005( 1) 0.0043( 4) 0.0013( 5) 0.0026( 9) 0.0003( 2) H 61 0.0234( 27) 0.0009( 1) 0.0036( 4) 0.0005( 5) 0.0050( 9) 0.0008( 2) H 62 0.0209( 28) 0.0008( 1) 0.0048( 5) 0.0009( 6) 0.0030( 10)-0.0005( 2) H 63 0.0142( 25) 0.0010( 1) 0.0069( 5)-0.0013( 6) 0.0000( 11)-0.0002( 2) H 71 0.0180( 26) 0.0006( 1) 0.0046( 4)-0.0009( 5) 0.0026( 10) 0.0008( 2) H 72 0.0149( 25) 0.0007( 1) 0.0065( 5)-0.0001( 5) 0.0044( 10)-0.0001( 2) H 73 0.0246( 29) 0.0009( 1) 0.0041( 4)-0.0018( 5) 0.0038( 10)-0.0006( 2) H 81 0.0226( 32) 0.0006( 1) 0.0064( 5) 0.0003( 5) 0.0054( 11) 0.0004( 2) H 82 0.0227( 27) 0.0009( 1) 0.0042( 5)-0.0011( 6) 0.0063( 9)-0.0001( 2) H 83 0.0121( 23) 0.0011( 1) 0.0043( 4)-0.0018( 5) 0.0003( 9) 0.0004( 2) H 91 0.0200( 27) 0.0012( 1) 0.0037( 4)-0.0002( 6) 0.0041( 9)-0.0009( 2) H 92 0.0190( 29) 0.0007( 1) 0.0060( 5) 0.0008( 5)-0.0014( 10) 0.0007( 2) H 93 0.0144( 22) 0.0008( 1) 0.0045( 4)-0.0008( 5) 0.0028( 9) 0.0004( 2) H 10 0.0128( 24) 0.0013( 1) 0.0047( 4)-0.0024( 6) 0.0033( 9)-0.0012( 2) H 12 0.0135( 20) 0.0012( 1) 0.0040( 4)-0.0018( 5) 0.0054( 8)-0.0005( 2) H 13 0.0237( 27) 0.0009( 1) 0.0049( 4)-0.0031( 6) 0.0071( 10)-0.0008( 2) H 15 0.0143( 22) 0.0009( 1) 0.0035( 4)-0.0016( 5) 0.0042( 8)-0.0002( 2) H 16 0.0174( 25) 0.0010( 1) 0.0046( 4)-0.0027( 5) 0.0033( 9)-0.0006( 2)

Table S4: Anisotropic vibration parameters at T=4.5K (neutron diffraction)

Identification code               CL-TEMPO

Empirical formula                 Cl C16 N2 O H22

Molecular weight                  293.5

Temperature                       4.5 K

Wavelength                        1.17400 A

Monochromator                     Cu (3 3 1)

Crystal system, space group       Monoclinic, P21/c

Unit cell dimensions              a =  5.736(9)  A  alpha = 90 deg.

b = 23.946(11) A  beta  = 104.36(9) deg.

c = 11.322(10) A  gamma = 90 deg.

Volume                            1507 (11) A^3

Z                                 4

Absorption coefficient            0.234 mm^-1

Crystal size (1)                  6.0 x 2.0 x 2.0 (mm)

Crystal size (2)                  3.5 x 2.5 x 1.0 (mm)

Reflections collected/unique (1)  1944 / 1209

Reflections collected/unique (2)  1135 / 897

sin(/)  (1)                     0.65 A-1

sin(/)  (1)                     0.74 A-1

Refinement method                 Full-matrix least-squares on F^2

R indices (all data)              R1 = 0.0550

Parameters ref. / constraints     297 / 0

Diffractometer                    D15,ILL

Diffraction geometry              Normal beam geometry

Data collection                   -scan

Programs used:

* The calculation of integrated intensities was done by the COLL5 program (M. S. Lehmann, F. K. Larsen, Acta. Crystallogr. 1970, B26, 1198),

* The data were sorted and averaged with the program ARRNGE based on the Cambridge Crystallographic Library (J. Brown, J. C. Matthewman, The Cambridge Crystallographic Library RL-81-063),

* The structure was refined using the program ORXFLS (W. R. Busing; K. O. Martin; H. A. Levy ORNL   Report 59-37, Oak Ridge National Laboratory: Oak Ridge, TN, 1991)

* The extinction was modeled in the approximation of the Gaussian mosaic crystal with scattered intensities corresponding to a secondary extinction of type II.

Table S5: Crystal data and structure refinement for Cl-TEMPO (neutron diffraction).