Supplementary Data for:

Journal of Materials Chemistry B001376P.

Synthesis of model organosiloxanes containing perfluoroether side-chains.

###### James A S Smitha, Brian J Brisdon*a, Stuart A Brewerb and Colin R Willisb

###### aDepartment of Chemistry, University of Bath, Bath, BA2 7AY, UK. E-mail: b.j.brisdon@bath.ac.uk

bDERA, CBD Porton Down, Salisbury, Wiltshire, SP4 0JQ, UK

Fragments in the mass spectrum of Me3SiOSiMe(R)OSiMe3

|  |  | (M)+ | (M-Me)+ | (M-R)+ | (R)+ | (Me3SiOSiMe2)+ | (Me3Si)+ | (Me3SiOSi(H)OSiMe3)+ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| T3 | E.I | - | 62 | 100 | 25 | 9 | 46 | 16 |
|  | C.I | - | 45 | 100 | - | - | - | - |
| T5 | E.I | - | 7 | 100 | - | 26 | 61 | 17 |
|  | C.I | 13 | - | 100 | - | - | - | 6 |
| T7 | E.I | - | 25 | 100 | - | 17 | 58 | 36 |
|  | C.I | - | 49 | 100 | 8 | 6 | 13 | 7 |
| T8 | E.I | - | 3 | 100 | 18 | 46 | 92 | 22 |
|  | C.I | 70 | 19 | 100 | 32 | 26 | 35 | 24 |
| T9 | E.I | - | - | 16 | 12 | 22 | 100 | 95 |
|  | C.I | - | - | 100 | 22 | 16 | 37 | 44 |