Supplementary Crystallographic Data

Including:

Table 1 Crystallographic data and details of the room temperature data collection and structure refinement of [Cu(pyr)2]2+ containing siliceous ferrierite.

Table 2 Final atomic coordinates, equalized temperature factors and occupancy factors of [Cu(pyr)2]2+ containing siliceous ferrierite.

Table 3 Anisotropic temperature factors (Å2) for [Cu(pyr)2]2+ containing siliceous ferrierite.

Table 4 Selected bond distances (Å) for [Cu(pyr)2]2+ containing siliceous ferrierite.

Table 5 Selected bond angles (°) in [Cu(pyr)2]2+ containing siliceous ferrierite.

Table 1 Crystallographic data and details of the room temperature data collection and structure refinement of [Cu(pyr)2]2+ containing siliceous ferrierite.

_________________________________________________________________

| Formula | Cu0.964F1.2(Si36O72).4C5H5N |
| --- | --- |
| Molecular weight | 2563.52 |
| Crystal system | Orthorhombic |
| Space-group | Pmnn (#58) |
| F(000) | 1297.37 |
| Unit cell determination | Determined from 25 reflections found using a ‘spiral search’ method |
| a | 18.775(1) Å |
| b | 14.086(1) Å |
| c | 7.4296(6) Å |
| V | 1964.9(4) Å3 |
| Z | 1 |
| Dc | 2.17 g cm-3 |
|  | 70.91 cm-1 |
| Habit and colour | Rectangular plate, colourless |
| Dimensions | 0.15 x 0.05 x 0.01 mm |
| Diffractometer and radiation source | CAD4-MACH (kappa geometry) with a Rigaku rotating anode |
| Radiation | Cu K (= 1.54180 Å) |
| Monochromator | Graphite |
| Absorption correction type | Psi scan |
| Absorption correction T min/ T max | 0.76/ 1.00 |
| Scanning mode | -2 |
|  range | 0, 72 ° |
| hkl range | -1 to 23; -1 to 17; -9 to 9 |
| No. of reflections | 4780 |
| No. of independent reflections | 1993 |
| No. of observed reflections | 1096 |
| Criterion for reflection observation | I > 3(I) |
| Rint | 3.16 % |
| Structure solution and development | Structure from a known model and completed using Fourier difference techniques |
| No. of refined parameters | 182 |
|  min/ max | -0.751/ 0.378 e Å-3 |
| R(F) (I > 3(I)) | 3.88 % |
| Rw(F) (I > 3(I)) | 4.31 % |
| S, goodness of fit | 0.9322 |
| Average shift/ error | 0.0028 |
| Extinction parameter | 31(4) |
| Weighting scheme | 3 term Chebyshev, 6.74, -0.069, 4.88 |
| Data reduction program | RC85 (P. D. Baird, Chemical Crystallography Laboratory, Oxford, 1987.) |
| Structure refinement program | CRYSTALS (D. J. Watkin, J. R. Carruthers and P. W. Betteridge, Chemical Crystallography Laboratory, Oxford, 1990.) |

Table 2 Final atomic coordinates, equalized temperature factors and occupancy factors of [Cu(pyr)2]2+ containing siliceous ferrierite.

_________________________________________________________________

| Atom | x | y | z | U(eq)(Å2) | Occupancy |
| --- | --- | --- | --- | --- | --- |
| Si(1) | 0.15393(7) | 0.0000 | 0.0000 | 0.0127 | 1.000 |
| Si(2) | 0.27373(5) | -0.00196(9) | 0.2931(1) | 0.0137 | 1.000 |
| Si(3) | 0.08396(5) | -0.20054(7) | -0.0095(1) | 0.0145 | 1.000 |
| Si(4) | 0.17249(5) | -0.30161(7) | 0.2837(1) | 0.0140 | 1.000 |
| Si(5) | 0.17921(5) | -0.29441(8) | -0.3055(1) | 0.0149 | 1.000 |
| O(1) | 0.2498(2) | 0.0000 | 0.5000 | 0.0221 | 1.000 |
| O(2) | 0.2026(2) | 0.0035(3) | 0.1759(4) | 0.0294 | 1.000 |
| O(3) | 0.1038(2) | -0.0909(2) | 0.0074(5) | 0.0278 | 1.000 |
| O(4) | 0.1540(2) | -0.2803(2) | 0.4896(4) | 0.0215 | 1.000 |
| O(5) | 0.0000 | -0.2117(3) | -0.0243(6) | 0.0250 | 1.000 |
| O(6) | 0.2463(2) | -0.2555(3) | 0.2298(6) | 0.0369 | 1.000 |
| O(7) | 0.1191(2) | -0.2448(3) | -0.1862(4) | 0.0287 | 1.000 |
| O(8) | 0.1100(2) | -0.2568(2) | 0.1660(4) | 0.0256 | 1.000 |
| O(9) | 0.3247(1) | 0.0865(2) | 0.2507(4) | 0.0255 | 1.000 |
| O(10) | 0.3178(2) | -0.0963(2) | 0.2508(5) | 0.0282 | 1.000 |
| Cu(1) | 0.5000 | 0.7474(4) | 0.0146(9) | 0.0639 | 0.241(6) |
| F(1) | 0.259(1) | -0.337(1) | -0.460(2) | 0.0333 | 0.15(1) |
| N(1) | 0.5000 | 0.6000(8) | -0.001(1) | 0.0801 | 1.000 |
| C(11) | 0.5624(4) | 0.5477(5) | 0.001(1) | 0.0636 | 1.000 |
| N(2) | 0.5000 | 0.903(2) | -0.009(8) | 0.1176 | 1.000 |
| C(21) | 0.5000 | 0.957(4) | -0.164(6) | 0.1382 | 1.000 |
| C(22) | 0.5000 | 0.954(3) | 0.151(6) | 0.1251 | 1.000 |
| H(11) | 0.605(4) | 0.581(4) | -0.027(8) | 0.0500 | 1.000 |
| H(21) | 0.5000 | 0.925(7) | -0.32(1) | 0.0500 | 1.000 |
| H(22) | 0.5000 | 0.914(3) | 0.262(6) | 0.0500 | 1.000 |

__________________________________________________________________

Table 3 Anisotropic temperature factors (Å2) for [Cu(pyr)2]2+ containing siliceous ferrierite.

_________________________________________________________________

| Atom | U(11) | U(22) | U(33) | U(23) | U(13) | U(12) |
| --- | --- | --- | --- | --- | --- | --- |
| Si(1) | 0.0112(6) | 0.0159(6) | 0.0114(6) | -0.0004(6) | 0.0000 | 0.0000 |
| Si(2) | 0.0153(4) | 0.0175(5) | 0.0097(5) | -0.0003(5) | -0.0012(3) | -0.0014(4) |
| Si(3) | 0.0131(5) | 0.0163(5) | 0.0145(5) | 0.0015(5) | -0.0010(4) | 0.0001(3) |
| Si(4) | 0.0139(5) | 0.0173(5) | 0.0116(5) | -0.0014(4) | 0.0008(4) | -0.0003(4) |
| Si(5) | 0.0179(6) | 0.0164(5) | 0.0132(5) | -0.0007(4) | -0.0057(4) | -0.0013(4) |
| O(1) | 0.024(2) | 0.046(2) | 0.010(2) | 0.000(2) | 0.0000 | 0.0000 |
| O(2) | 0.024(1) | 0.068(2) | 0.019(1) | 0.000(2) | -0.009(1) | -0.003(2) |
| O(3) | 0.028(2) | 0.017(1) | 0.049(2) | 0.001(2) | -0.003(2) | -0.006(1) |
| O(4) | 0.029(1) | 0.038(2) | 0.010(1) | -0.005(1) | -0.003(1) | 0.005(1) |
| O(5) | 0.013(2) | 0.033(2) | 0.037(2) | 0.000(2) | 0.0000 | 0.0000 |
| O(6) | 0.028(2) | 0.057(2) | 0.062(2) | -0.022(2) | 0.019(2) | -0.024(2) |
| O(7) | 0.031(2) | 0.042(2) | 0.021(1) | -0.004(2) | 0.006(1) | 0.008(1) |
| O(8) | 0.030(2) | 0.033(2) | 0.021(2) | 0.008(1) | -0.005(1) | 0.006(1) |
| O(9) | 0.025(2) | 0.021(1) | 0.034(1) | 0.006(1) | 0.003(2) | -0.003(1) |
| O(10) | 0.033(2) | 0.019(1) | 0.040(2) | -0.008(1) | 0.004(2) | 0.002(1) |
| Cu(1) | 0.132(7) | 0.029(3) | 0.068(4) | 0.003(3) | 0.0000 | 0.0000 |
| F(1) | 0.05(1) | 0.03(1) | 0.03(1) | 0.000(7) | 0.000(8) | 0.002(8) |
| N(1) | 0.072(6) | 0.095(7) | 0.075(5) | 0.005(6) | 0.0000 | 0.0000 |
| C(11) | 0.044(4) | 0.079(4) | 0.076(4) | 0.009(5) | 0.005(4) | -0.007(3) |
| N(2) | 0.030(6) | 0.16(2) | 0.37(4) | -0.08(3) | 0.0000 | 0.0000 |
| C(21) | 0.06(1) | 0.18(4) | 0.29(5) | -0.07(3) | 0.0000 | 0.0000 |
| C(22) | 0.048(9) | 0.14(2) | 0.29(5) | 0.01(3) | 0.0000 | 0.0000 |

_________________________________________________________________

Table 4 Selected bond distances (Å) for [Cu(pyr)2]2+ containing siliceous ferrierite.

_________________________________________________________________

| Si(1)—O(2) | 1.595(3) | Si(1)—O(2) | 1.595(3) |  |
| --- | --- | --- | --- | --- |
| Si(1)—O(3) | 1.589(3) | Si(1)—O(3) | 1.589(3) |  |
| Si(2)—O(1) | 1.602(1) | Si(2)—O(2) | 1.597(3) |  |
| Si(2)—O(9) | 1.603(3) | Si(2)—O(10) | 1.596(3) |  |
| Si(3)—O(3) | 1.594(3) | Si(3)—O(5) | 1.588(1) |  |
| Si(3)—O(7) | 1.596(3) | Si(3)—O(8) | 1.602(3) |  |
| Si(4)—O(4) | 1.597(3) | Si(4)—O(6) | 1.582(4) |  |
| Si(4)—O(8) | 1.594(3) | Si(4)—O(9) | 1.597(3) |  |
| Si(5)—O(4) | 1.606(3) | Si(5)—O(6) | 1.587(4) |  |
| Si(5)—O(7) | 1.597(3) | Si(5)—O(10) | 1.597(3) |  |
| Si(5)—F(1) | 1.99(2) |  |  |  |
| Weighted average Si—O bond length 1.596 |  |  |  |  |  |  |  |
| F(1)—O(4) | 2.17(2) | F(1)—O(6) | 1.92(2) |  |
| F(1)—O(10) | 2.33(2) |  |  |  |
| Cu(1)—N(1) | 2.08(1) | Cu(1)—N(2) | 2.20(2) |  |
| Cu(1)—O(4) x 2 | 2.934(4) |  |  |  |
| N(1)—C(11) | 1.384(9) | C(11)—C(11) | 1.34(1) |  |
| C(11)—H(11) | 0.95(6) |  |  |  |
| N(2)—C(21) | 1.38(4) | N(2)—C(22) | 1.39(4) |  |
| C(21)—C(22) | 1.26(3) | C(21)—H(21) | 1.24(9) |  |
| C(22)—H(22) | 1.00 |  |  |  |

_________________________________________________________________

Table 5 Selected bond angles (°) in [Cu(pyr)2]2+ containing siliceous ferrierite.

_________________________________________________________________

| O(2)—Si(1)—O(2) | 110.1(2) | O(2)—Si(1)—O(3) | 109.6(2) |
| --- | --- | --- | --- |
| O(2)—Si(1)—O(3) | 110.0(2) | O(2)—Si(1)—O(3) | 110.0(2) |
| O(2)—Si(1)—O(3) | 109.6(2) | O(3)—Si(1)—O(3) | 107.4(2) |
| O(1)—Si(2)—O(2) | 106.7(2) | O(1)—Si(2)—O(9) | 110.0(2) |
| O(2)—Si(2)—O(9) | 110.8(2) | O(1)—Si(2)—O(10) | 110.4(2) |
| O(2)—Si(2)—O(10) | 111.5(2) | O(9)—Si(2)—O(10) | 107.4(2) |
| O(3)—Si(3)—O(5) | 109.5(2) | O(3)—Si(3)—O(7) | 110.3(2) |
| O(5)—Si(3)—O(7) | 108.3(2) | O(3)—Si(3)—O(8) | 110.1(2) |
| O(5)—Si(3)—O(8) | 108.1(2) | O(7)—Si(3)—O(8) | 110.5(2) |
| O(4)—Si(4)—O(6) | 110.8(2) | O(4)—Si(4)—O(8) | 106.9(2) |
| O(6)—Si(4)—O(8) | 110.1(2) | O(4)—Si(4)—O(9) | 110.2(2) |
| O(6)—Si(4)—O(9) | 109.6(2) | O(8)—Si(4)—O(9) | 109.1(2) |
| O(4)—Si(5)—O(6) | 111.2(2) | O(4)—Si(5)—O(7) | 105.3(2) |
| O(6)—Si(5)—O(7) | 109.7(2) | O(4)—Si(5)—O(10) | 112.2(2) |
| O(6)—Si(5)—O(10) | 110.6(2) | O(7)—Si(5)—O(10) | 107.6(2) |
| O(4)—Si(5)—F(1) | 73.3(5) | O(6)—Si(5)—F(1) | 64.0(6) |
| O(7)—Si(5)—F(1) | 171.6(6) | O(10)—Si(5)—F(1) | 80.4(5) |
| Si(1)—O(1)—Si(2) | 147.4(3) | Si(1)—O(2)—Si(2) | 157.6(2) |
| Si(1)—O(3)—Si(3) | 156.4(2) | Si(4)—O(4)—Si(5) | 145.1(2) |
| Si(3)—O(5)—Si(3) | 166.1(3) | Si(4)—O(6)—Si(5) | 174.7(3) |
| Si(3)—O(7)—Si(5) | 156.9(2) | Si(3)—O(8)—Si(4) | 150.1(3) |
| Si(2)—O(9)—Si(4) | 144.9(2) | Si(2)—O(10)—Si(5) | 150.8(2) |
| N(1)-Cu(1)-N(2) | 172.3(16) | O(4)-Cu(1)-O(4) | 160.4(2) |
| N(1)-Cu(1)-O(4) x 2 | 98.9(1) | N(2)-Cu(1)-O(4) x 2 | 80.6(1) |
| C(11)-N(1)-C(11) | 115.7(9) | N(1)-C(11)-C(11) | 122.2(5) |
| N(1)-C(11)-H(11) | 116.4(39) | C(11)-C(11)-H(11) | 119.6(39) |
| C(21)-N(2)-C(22) | 115.2(28) | N(2)-C(21)-C(22) | 119.2(40) |
| N(2)-C(22)-C(21) | 125.6(35) | N(2)-C(21)-H(21) | 124.8(73) |
| C(22)-C(21)-H(21) | 116.0(77) | N(2)-C(22)-H(22) | 114.3(28) |
| C(21)-C(22)-H(22) | 120.1(37) |  |  |

_________________________________________________________________