ESI 1:	“Hypothetical” metastable 3-D perovskites A0.5BO3 with exotic ordering of vacancies (n = 2 to n = 3) : small black circles are relative to the A sites, fully occupy for n = 2, and with a vacancy rate of 1/4 for n = 3.

ESI 2:	TGA curve for K2SrTa2O7. xH2O during the rehydration process (humidity rate : 70%).

ESI 3:	Thermal evolution of K2SrTa2O7. xH2O X-ray powder diffraction patterns between 50°C and 570°C.

ESI 4:	X-ray thermodiffractogram of H2SrTa2O7. xH2O between room temperature and 1000°C.

# Text boxes

ESI 1

c = 24,0 Å

n = 3

b)

c ( 16.0 Å

a)

n = 2