Fig. S4 HRTEM image viewed along the <110> direction and an electron diffraction pattern for CuAlO2 single crystal. The insert shows a calculated image demonstrating a two-dimensional layered structure.