Supplementary Information:

Intermolecular organisation of triphenylene-based discotic mesogens by interdigitation of alkyl chains

Matthew T. Allen,a Siegmar Diele,b Kenneth D. M. Harris,a* Torsten Hegmann,c 
Benson M. Kariuki,a Dirk Lose,b Jon A. Preecea* and Carsten Tschierske.c

a School of Chemistry, The University of Birmingham,

Edgbaston, Birmingham, B15 2TT, United Kingdom.

b Institute of Physical Chemistry, Martin-Luther-University Halle,

Mühlpforte 1, D-06118 Halle, Germany.

c Institute of Organic Chemistry, Martin-Luther-University Halle,

Kurt-Mothes-Strasse 2, D-06120 Halle, Germany.

# E-mail: K.D.M.Harris@bham.ac.uk, J.A.Preece@bham.ac.uk

CORRESPONDENCE ADDRESS

Prof. Kenneth D. M. Harris / Dr. Jon A. Preece

School of Chemistry,

University of Birmingham,

Edgbaston,

Birmingham,

B15 2TT,

# United Kingdom.

Supplementary Information:
Figure S1. Examples of variable temperature XRD photographs of (a) C5C5, (b) C5C3.sym, (c) C5C9.sym and (d) C6C4.sym.

Supplementary Information:
Figure S2. Mesophase X-ray diffractogram of C5C3.sym, exhibiting the reflections, d200 and d210.

Supplementary Information:
Table S1. Quantities of reagents used in synthesis of C5Cn materials.

Supplementary Information:
Table S2. Spectroscopic data for compounds C5Cn materials.

# Text boxes

(001)

(100)

(a)

(b)

(c)

(d)

( / °

(001)

(210)

(200)