Supplementary data for III-Bi1.85Zr0.15O3.075 at 298 K

Table 1

Crystal, Data Collection and Structure Refinement Data

| (a) Crystal data |  |
| --- | --- |
| Name | Bizmuth zirconium oxide |
| Empirical formula | Bi1.85Zr0.15O3.075 |
| Formula weight | 449.49 |
| Crystal system | Tetragonal |
| Space group | P42/nmc |
| Unit cell dimensions | a = 7.7206(9), c = 5.6370(6) Å |
| Volume | 336.0(1) Å3 |
| Z | 4 |
| Density (calculated) | 8.889 g cm-3 |
| Absorption coefficient  (Cu radiation) | 190.41 mm-1 |
| F(000) | 736.60 |
| Sample description | Orange powder |
| Synthesis | Solid state synthesis: Bi2O3 + ZrO2 at 850 C for 12 h |
| (b) Data collection |  |
| (i) Neutron diffraction |  |
| Diffractometer | HRPD |
| Temperature | 298 K |
| Radiation | pulsed neutrons |
| Data range collected | 30-130 ms (0.622-2.695 Å) |
| Detector | Back scattering |
| Monochromator/filter | Secondary beam graphite monochromator |
| (ii) X-ray diffraction |  |
| # Diffractometer | Automated Philips PW1050/30 |
| # Scan mode | /2 flat plate |
| # Temperature | 298 K |
| Wavelength | CuK (1.5418 Å) |
| 2 range collected | 5-110 2 |
| Step size | 0.02 2 |
| Scan time | 10s |
| Detector | Proportional counter |
| Monochromator/filter | Ni-filter |
| (c) Refinement |  |
| Refinement software | GSAS (Larson and Von Dreele, 1986) |
| Initial model source | PbF2O |
| # Data range refined | Neutron: 32-120 ms (0.634-2.488 Å) X-ray: 20-110 2 |
| Excluded regions | Neutron: None X-ray: 5-20 2 |
| Data corrections | Neutron: V-can background subtraction X-ray: Flat plate absorption |
| Secondary phases | ZrO2 |
| No. of observations/restraints/parameters | 8904/0/48 |
| Total no. of reflections used | Neutron: 905 X-ray: 604 |
| Independent reflections due to 1 phase | Neutron: 362 X-ray: 260 (130 unique) |
| Peak shape | Neutron: Exponential-Pseudo-Voigt X-ray: Pseudo-Viogt |
| Final R-factors | Neutron: Rp = 0.0701, Rwp = 0.0754 Rex = 0.0216, RF2 = 0.1915 X-ray: Rp = 0.1310, Rwp = 0.1029 Rex = 0.1361, RF2 = 0.1416 Total: Rp = 0.0773, Rwp = 0.0952 2 = 12.26 |

Table 2

Atomic Coordinates and Isotropic Thermal Parameters for

III-Bi1.85Zr0.15O3.075 at 298 K

| Atom | Site | x | y | z | Occupancy | Uiso (Å2) |
| --- | --- | --- | --- | --- | --- | --- |
| Bi | 8g | 0.25 | 0.0025(2) | 0.0097(2) | 0.925a | 0.0214(3) |
| Zr | 8g | 0.25 | 0.026(2) | 0.040(3) | 0.075a | 0.0214(3) |
| O(1) | 4d | 0.25 | 0.25 | -0.1469(2) | 1.00a | 0.0220(4) |
| O(2) | 16h | 0.4611(2) | -0.0630(2) | -0.2227(3) | 0.5a | 0.0258(4) |
| O(3) | 4c | 0.25 | -0.25 | 0.206(6) | 0.075a | 0.059(10) |

aFixed parameters

Table 3

Selected Bond Lengths (Å) and Angles () for

III-Bi1.85Zr0.15O3.075 at 298 K

| Bi-O(1) 2.105(1) | Zr-O(1) 2.03(2) |
| --- | --- |
| Bi-O(2) 2.152(2)  2 | Zr-O(2) 2.31(1)  2 |
| Bi-O(2)’ 2.192(2)  2 | Zr-O(3) 2.33(2) |
|  | Zr-O(2)’ 2.35(1)  2 |
|  | Zr-O(1)’’’ 2.47(2)  2 |
|  | Zr-O(2)’’ 2.472(7)  2 |
|  | Zr-O(3)’ 2.57(2) |

| O(1)-Bi-O(2) 87.59(6)  2 | O(1)-Zr-O(2) 85.4(5)  2 |
| --- | --- |
| O(1)-Bi-O(2)’ 79.79(6)  2 | O(1)-Zr-O(3) 172.3(12) |
| O(2)-Bi-O(2) 98.5(1) | O(1)-Zr-O(2)’ 77.6(5)  2 |
| O(2)-Bi-O(2)’ 90.88(7)  2 | O(1)-Zr-O(1)’’’ 76.9(6) |
| O(2)’-Bi-O(2)’ 82.41(9) | O(1)-Zr-O(2)’’ 96.8(5)  2 |
|  | O(1)-Zr-O(3)’ 177.5(14) |
|  | O(2)-Zr-O(2) 89.9(5) |
|  | O(2)-Zr-O(3) 89.2(7)  2 |
|  | O(2)-Zr-O(2)’ 83.2(5)  2 |
|  | O(2)-Zr-O(1)’’’ 131.8(4)  2 |
|  | O(2)-Zr-O(2)’’ 70.39(9)  2 |
|  | O(2)-Zr-O(3)’ 96.4(7)  2 |
|  | O(3)-Zr-O(2)’ 96.4(8)  2 |
|  | O(3)-Zr-O(1)’’’ 110.8(10) |
|  | O(3)-Zr-O(2)’’ 86.5(5)  2 |
|  | O(3)-Zr-O(3)’ 10.2(15) |
|  | O(2)’-Zr-O(2)’ 75.7(5) |
|  | O(2)’-Zr-O(1)’’’ 133.8(5)  2 |
|  | O(2)’-Zr-O(2)’’ 77.7(1)  2 |
|  | O(2)’-Zr-O(3)’ 104.4(7)  2 |
|  | O(1)’’’-Zr-O(2)’’ 67.8(3)  2 |
|  | O(1)’’’-Zr-O(3)’ 100.6(8) |
|  | O(2)’’-Zr-O(2)’’ 128.9(6) |
|  | O(2)’’-Zr-O(3)’ 82.2(5)  2 |

Symmetry relations: ’ = -y, (x + 0.5) -1, (-z + 0.5) -1; ’’ = -x - 1, -y, -z; ’’’ = y, x, z + 0.5

Table 4

Full List of Contact Distances (Å) for

III-Bi1.85Zr0.15O3.075 at 298 K

Atoms		Distance	Coordinates of second atom

Bi-Zr       0.25(2)       0.2500  0.0259  0.0404

Bi-O(1)     2.105(1)      0.2500  0.2500 -0.1469

Bi-O(1)     2.720(2)      0.2500  0.2500  0.3531

Bi-O(1)     2.105(1)      0.2500  0.2500 -0.1469

Bi-O(2)     2.152(2)      0.4611 -0.0630 -0.2227

Bi-O(2)     2.575(2)      0.5389  0.0630  0.2227

Bi-O(2)     2.862(2)     -0.0630  0.0389  0.2773

Bi-O(2)     2.192(2)      0.0630 -0.0389 -0.2773

Bi-O(2)     2.575(2)     -0.0389  0.0630  0.2227

Bi-O(2)     2.152(2)      0.0389 -0.0630 -0.2227

Bi-O(2)     2.192(2)      0.4370 -0.0389 -0.2773

Bi-O(2)     2.862(2)      0.5630  0.0389  0.2773

Bi-O(3)     2.24(2)       0.2500 -0.2500  0.2059

Bi-O(3)     2.52(2)       0.2500 -0.2500  0.2941

Bi-O(3)     2.52(2)       0.2500 -0.2500  0.2941

Zr-Bi       0.25(2)       0.2500  0.0025  0.0097

Zr-O(1)     2.03(2)       0.2500  0.2500 -0.1469

Zr-O(1)     2.47(2)       0.2500  0.2500  0.3531

Zr-O(2)     2.31(1)       0.4611 -0.0630 -0.2227

Zr-O(2)     2.472(7)      0.5389  0.0630  0.2227

Zr-O(2)     2.762(7)     -0.0630  0.0389  0.2773

Zr-O(2)     2.35(1)       0.0630 -0.0389 -0.2773

Zr-O(2)     2.472(7)     -0.0389  0.0630  0.2227

Zr-O(2)     2.31(1)       0.0389 -0.0630 -0.2227

Zr-O(2)     2.35(1)       0.4370 -0.0389 -0.2773

Zr-O(2)     2.762(7)      0.5630  0.0389  0.2773

Zr-O(3)     2.33(2)       0.2500 -0.2500  0.2059

Zr-O(3)     2.57(2)       0.2500 -0.2500  0.2941

O(1)-Bi     2.105(1)      0.2500  0.0025  0.0097

O(1)-Bi     2.105(1)      0.2500  0.4975  0.0097

O(1)-Bi     2.720(2)      0.4975  0.2500 -0.4903

O(1)-Bi     2.720(2)      0.0025  0.2500 -0.4903

O(1)-Zr     2.03(2)       0.2500  0.0259  0.0404

O(1)-Zr     2.03(2)       0.2500  0.4741  0.0404

O(1)-Zr     2.47(2)       0.4741  0.2500 -0.4596

O(1)-Zr     2.47(2)       0.0259  0.2500 -0.4596

O(1)-O(1)   2.8185(3)     0.2500  0.2500 -0.6469

O(1)-O(1)   2.8185(3)     0.2500  0.2500  0.3531

O(1)-O(2)   2.946(2)      0.4611 -0.0630 -0.2227

O(1)-O(2)   2.946(2)      0.0389  0.5630 -0.2227

O(1)-O(2)   2.757(2)      0.4370  0.5389 -0.2773

O(1)-O(2)   2.757(2)      0.0630 -0.0389 -0.2773

O(1)-O(2)   2.946(2)      0.4611  0.5630 -0.2227

O(1)-O(2)   2.946(2)      0.0389 -0.0630 -0.2227

O(1)-O(2)   2.757(2)      0.4370 -0.0389 -0.2773

O(1)-O(2)   2.757(2)      0.0630  0.5389 -0.2773

O(2)-Bi     2.152(2)      0.2500  0.0025  0.0097

O(2)-Bi     2.575(2)      0.7500 -0.0025 -0.0097

O(2)-Bi     2.862(2)      0.4975  0.2500 -0.4903

O(2)-Bi     2.192(2)      0.5025 -0.2500 -0.5097

Table 4 Continued

Atoms		Distance	Coordinates of second atom

O(2)-Zr     2.31(1)       0.2500  0.0259  0.0404

O(2)-Zr     2.472(7)      0.7500 -0.0259 -0.0404

O(2)-Zr     2.762(7)      0.4741  0.2500 -0.4596

O(2)-Zr     2.35(1)       0.5259 -0.2500 -0.5404

O(2)-O(1)   2.946(2)      0.2500  0.2500 -0.1469

O(2)-O(1)   2.757(2)      0.7500 -0.2500 -0.3531

O(2)-O(2)   2.759(4)      0.5389  0.0630  0.2227

O(2)-O(2)   2.888(3)      0.4611 -0.4370 -0.2227

O(2)-O(2)   0.405(3)      0.4370 -0.0389 -0.2773

O(3)-Bi     2.24(2)       0.2500  0.0025  0.0097

O(3)-Bi     2.24(2)       0.2500 -0.5025  0.0097

O(3)-Bi     2.52(2)       0.5025 -0.2500  0.4903

O(3)-Bi     2.52(2)      -0.0025 -0.2500  0.4903

O(3)-Zr     2.33(2)       0.2500  0.0259  0.0404

O(3)-Zr     2.33(2)       0.2500 -0.5259  0.0404

O(3)-Zr     2.57(2)       0.5259 -0.2500  0.4596

O(3)-Zr     2.57(2)      -0.0259 -0.2500  0.4596

O(3)-O(3)   0.50(7)       0.2500 -0.2500  0.2941

Table 5

Full List of Angles () for III-Bi1.85Zr0.15O3.075 at 298 K

Atoms	      Angle			  Coordinates of bonded atoms

Zr-Bi-O(1)      68.7(3.7)   0.2500  0.0259  0.0404    0.2500  0.2500 -0.1469

Zr-Bi-O(1)       1.5(2.1)   0.2500  0.0259  0.0404    0.2500  0.2500  0.3531

Zr-Bi-O(2)     126.3(1.3)   0.2500  0.0259  0.0404    0.4611 -0.0630 -0.2227

Zr-Bi-O(2)      63.0(9)     0.2500  0.0259  0.0404    0.5389  0.0630  0.2227

Zr-Bi-O(2)      64.2(1.3)   0.2500  0.0259  0.0404   -0.0630  0.0389  0.2773

Zr-Bi-O(2)     128.1(2.0)   0.2500  0.0259  0.0404    0.0630 -0.0389 -0.2773

Zr-Bi-O(2)      63.0(9)     0.2500  0.0259  0.0404   -0.0389  0.0630  0.2227

Zr-Bi-O(2)     126.3(1.3)   0.2500  0.0259  0.0404    0.0389 -0.0630 -0.2227

Zr-Bi-O(2)     128.1(2.0)   0.2500  0.0259  0.0404    0.4370 -0.0389 -0.2773

Zr-Bi-O(2)      64.2(1.3)   0.2500  0.0259  0.0404    0.5630  0.0389  0.2773

Zr-Bi-O(3)     106.6(3.8)   0.2500  0.0259  0.0404    0.2500 -0.2500  0.2059

Zr-Bi-O(3)      96.7(3.8)   0.2500  0.0259  0.0404    0.2500 -0.2500  0.2941

O(1)-Bi-O(1)    70.18(4)    0.2500  0.2500 -0.1469    0.2500  0.2500  0.3531

O(1)-Bi-O(2)    87.59(6)    0.2500  0.2500 -0.1469    0.4611 -0.0630 -0.2227

O(1)-Bi-O(2)    91.78(5)    0.2500  0.2500 -0.1469    0.5389  0.0630  0.2227

O(1)-Bi-O(2)    97.59(5)    0.2500  0.2500 -0.1469   -0.0630  0.0389  0.2773

O(1)-Bi-O(2)    79.79(6)    0.2500  0.2500 -0.1469    0.0630 -0.0389 -0.2773

O(1)-Bi-O(2)    91.78(5)    0.2500  0.2500 -0.1469   -0.0389  0.0630  0.2227

O(1)-Bi-O(2)    87.59(6)    0.2500  0.2500 -0.1469    0.0389 -0.0630 -0.2227

O(1)-Bi-O(2)    79.79(6)    0.2500  0.2500 -0.1469    0.4370 -0.0389 -0.2773

O(1)-Bi-O(2)    97.59(5)    0.2500  0.2500 -0.1469    0.5630  0.0389  0.2773

O(1)-Bi-O(3)   175.2(8)     0.2500  0.2500 -0.1469    0.2500 -0.2500  0.2059

O(1)-Bi-O(3)   165.4(6)     0.2500  0.2500 -0.1469    0.2500 -0.2500  0.2941

O(1)-Bi-O(2)   126.76(5)    0.2500  0.2500  0.3531    0.4611 -0.0630 -0.2227

O(1)-Bi-O(2)    62.68(4)    0.2500  0.2500  0.3531    0.5389  0.0630  0.2227

O(1)-Bi-O(2)    63.65(4)    0.2500  0.2500  0.3531   -0.0630  0.0389  0.2773

O(1)-Bi-O(2)   128.88(5)    0.2500  0.2500  0.3531    0.0630 -0.0389 -0.2773

O(1)-Bi-O(2)    62.68(4)    0.2500  0.2500  0.3531   -0.0389  0.0630  0.2227

O(1)-Bi-O(2)   126.76(5)    0.2500  0.2500  0.3531    0.0389 -0.0630 -0.2227

O(1)-Bi-O(2)   128.88(5)    0.2500  0.2500  0.3531    0.4370 -0.0389 -0.2773

O(1)-Bi-O(2)    63.65(4)    0.2500  0.2500  0.3531    0.5630  0.0389  0.2773

O(1)-Bi-O(3)   105.1(7)     0.2500  0.2500  0.3531    0.2500 -0.2500  0.2059

O(1)-Bi-O(3)    95.2(6)     0.2500  0.2500  0.3531    0.2500 -0.2500  0.2941

O(2)-Bi-O(2)    70.75(7)    0.4611 -0.0630 -0.2227    0.5389  0.0630  0.2227

O(2)-Bi-O(2)   169.58(8)    0.4611 -0.0630 -0.2227   -0.0630  0.0389  0.2773

O(2)-Bi-O(2)    90.88(7)    0.4611 -0.0630 -0.2227    0.0630 -0.0389 -0.2773

O(2)-Bi-O(2)   169.26(6)    0.4611 -0.0630 -0.2227   -0.0389  0.0630  0.2227

O(2)-Bi-O(2)    98.5(1)     0.4611 -0.0630 -0.2227    0.0389 -0.0630 -0.2227

O(2)-Bi-O(2)    10.64(9)    0.4611 -0.0630 -0.2227    0.4370 -0.0389 -0.2773

O(2)-Bi-O(2)    72.80(4)    0.4611 -0.0630 -0.2227    0.5630  0.0389  0.2773

O(2)-Bi-O(3)    95.5(5)     0.4611 -0.0630 -0.2227    0.2500 -0.2500  0.2059

O(2)-Bi-O(3)   101.8(4)     0.4611 -0.0630 -0.2227    0.2500 -0.2500  0.2941

O(2)-Bi-O(2)   117.88(4)    0.5389  0.0630  0.2227   -0.0630  0.0389  0.2773

O(2)-Bi-O(2)   160.21(9)    0.5389  0.0630  0.2227    0.0630 -0.0389 -0.2773

O(2)-Bi-O(2)   119.99(9)    0.5389  0.0630  0.2227   -0.0389  0.0630  0.2227

O(2)-Bi-O(2)   169.26(6)    0.5389  0.0630  0.2227    0.0389 -0.0630 -0.2227

O(2)-Bi-O(2)    78.46(4)    0.5389  0.0630  0.2227    0.4370 -0.0389 -0.2773

O(2)-Bi-O(2)     6.04(5)    0.5389  0.0630  0.2227    0.5630  0.0389  0.2773

O(2)-Bi-O(3)    85.8(4)     0.5389  0.0630  0.2227    0.2500 -0.2500  0.2059

O(2)-Bi-O(3)    81.0(3)     0.5389  0.0630  0.2227    0.2500 -0.2500  0.2941

O(2)-Bi-O(2)    81.20(6)   -0.0630  0.0389  0.2773    0.0630 -0.0389 -0.2773

O(2)-Bi-O(2)     6.04(5)   -0.0630  0.0389  0.2773   -0.0389  0.0630  0.2227

O(2)-Bi-O(2)    72.80(4)   -0.0630  0.0389  0.2773    0.0389 -0.0630 -0.2227

Table 5 Continued

Atoms	      Angle			  Coordinates of bonded atoms

O(2)-Bi-O(2)   163.61(6)   -0.0630  0.0389  0.2773    0.4370 -0.0389 -0.2773

O(2)-Bi-O(2)   115.18(8)   -0.0630  0.0389  0.2773    0.5630  0.0389  0.2773

O(2)-Bi-O(3)    79.9(4)    -0.0630  0.0389  0.2773    0.2500 -0.2500  0.2059

O(2)-Bi-O(3)    75.0(3)    -0.0630  0.0389  0.2773    0.2500 -0.2500  0.2941

O(2)-Bi-O(2)    78.46(4)    0.0630 -0.0389 -0.2773   -0.0389  0.0630  0.2227

O(2)-Bi-O(2)    10.64(9)    0.0630 -0.0389 -0.2773    0.0389 -0.0630 -0.2227

O(2)-Bi-O(2)    82.4(1)     0.0630 -0.0389 -0.2773    0.4370 -0.0389 -0.2773

O(2)-Bi-O(2)   163.61(6)    0.0630 -0.0389 -0.2773    0.5630  0.0389  0.2773

O(2)-Bi-O(3)   103.7(5)     0.0630 -0.0389 -0.2773    0.2500 -0.2500  0.2059

O(2)-Bi-O(3)   110.9(4)     0.0630 -0.0389 -0.2773    0.2500 -0.2500  0.2941

O(2)-Bi-O(2)    70.75(7)   -0.0389  0.0630  0.2227    0.0389 -0.0630 -0.2227

O(2)-Bi-O(2)   160.21(9)   -0.0389  0.0630  0.2227    0.4370 -0.0389 -0.2773

O(2)-Bi-O(2)   117.88(4)   -0.0389  0.0630  0.2227    0.5630  0.0389  0.2773

O(2)-Bi-O(3)    85.8(4)    -0.0389  0.0630  0.2227    0.2500 -0.2500  0.2059

O(2)-Bi-O(3)    81.0(3)    -0.0389  0.0630  0.2227    0.2500 -0.2500  0.2941

O(2)-Bi-O(2)    90.88(7)    0.0389 -0.0630 -0.2227    0.4370 -0.0389 -0.2773

O(2)-Bi-O(2)   169.58(8)    0.0389 -0.0630 -0.2227    0.5630  0.0389  0.2773

O(2)-Bi-O(3)    95.5(5)     0.0389 -0.0630 -0.2227    0.2500 -0.2500  0.2059

O(2)-Bi-O(3)   101.8(4)     0.0389 -0.0630 -0.2227    0.2500 -0.2500  0.2941

O(2)-Bi-O(2)    81.20(6)    0.4370 -0.0389 -0.2773    0.5630  0.0389  0.2773

O(2)-Bi-O(3)   103.7(5)     0.4370 -0.0389 -0.2773    0.2500 -0.2500  0.2059

O(2)-Bi-O(3)   110.9(4)     0.4370 -0.0389 -0.2773    0.2500 -0.2500  0.2941

O(2)-Bi-O(3)    79.9(4)     0.5630  0.0389  0.2773    0.2500 -0.2500  0.2059

O(2)-Bi-O(3)    75.0(3)     0.5630  0.0389  0.2773    0.2500 -0.2500  0.2941

O(3)-Bi-O(3)     9.9(1.4)   0.2500 -0.2500  0.2059    0.2500 -0.2500  0.2941

Bi-Zr-O(1)     104.7(3.8)   0.2500  0.0025  0.0097    0.2500  0.2500 -0.1469

Bi-Zr-O(1)     178.4(2.4)   0.2500  0.0025  0.0097    0.2500  0.2500  0.3531

Bi-Zr-O(2)      48.7(1.2)   0.2500  0.0025  0.0097    0.4611 -0.0630 -0.2227

Bi-Zr-O(2)     111.8(1.0)   0.2500  0.0025  0.0097    0.5389  0.0630  0.2227

Bi-Zr-O(2)     111.2(1.4)   0.2500  0.0025  0.0097   -0.0630  0.0389  0.2773

Bi-Zr-O(2)      47.1(1.9)   0.2500  0.0025  0.0097    0.0630 -0.0389 -0.2773

Bi-Zr-O(2)     111.8(1.0)   0.2500  0.0025  0.0097   -0.0389  0.0630  0.2227

Bi-Zr-O(2)      48.7(1.2)   0.2500  0.0025  0.0097    0.0389 -0.0630 -0.2227

Bi-Zr-O(2)      47.1(1.9)   0.2500  0.0025  0.0097    0.4370 -0.0389 -0.2773

Bi-Zr-O(2)     111.2(1.4)   0.2500  0.0025  0.0097    0.5630  0.0389  0.2773

Bi-Zr-O(3)      67.5(3.7)   0.2500  0.0025  0.0097    0.2500 -0.2500  0.2059

Bi-Zr-O(3)      77.8(3.8)   0.2500  0.0025  0.0097    0.2500 -0.2500  0.2941

O(1)-Zr-O(1)    76.9(6)     0.2500  0.2500 -0.1469    0.2500  0.2500  0.3531

O(1)-Zr-O(2)    85.3(5)     0.2500  0.2500 -0.1469    0.4611 -0.0630 -0.2227

O(1)-Zr-O(2)    96.8(5)     0.2500  0.2500 -0.1469    0.5389  0.0630  0.2227

O(1)-Zr-O(2)   102.8(4)     0.2500  0.2500 -0.1469   -0.0630  0.0389  0.2773

O(1)-Zr-O(2)    77.6(4)     0.2500  0.2500 -0.1469    0.0630 -0.0389 -0.2773

O(1)-Zr-O(2)    96.8(5)     0.2500  0.2500 -0.1469   -0.0389  0.0630  0.2227

O(1)-Zr-O(2)    85.3(5)     0.2500  0.2500 -0.1469    0.0389 -0.0630 -0.2227

O(1)-Zr-O(2)    77.6(4)     0.2500  0.2500 -0.1469    0.4370 -0.0389 -0.2773

O(1)-Zr-O(2)   102.8(4)     0.2500  0.2500 -0.1469    0.5630  0.0389  0.2773

O(1)-Zr-O(3)   172.3(1.2)   0.2500  0.2500 -0.1469    0.2500 -0.2500  0.2059

O(1)-Zr-O(3)   177.5(1.4)   0.2500  0.2500 -0.1469    0.2500 -0.2500  0.2941

O(1)-Zr-O(2)   131.8(4)     0.2500  0.2500  0.3531    0.4611 -0.0630 -0.2227

O(1)-Zr-O(2)    67.8(3)     0.2500  0.2500  0.3531    0.5389  0.0630  0.2227

O(1)-Zr-O(2)    68.3(3)     0.2500  0.2500  0.3531   -0.0630  0.0389  0.2773

O(1)-Zr-O(2)   133.8(5)     0.2500  0.2500  0.3531    0.0630 -0.0389 -0.2773

O(1)-Zr-O(2)    67.8(3)     0.2500  0.2500  0.3531   -0.0389  0.0630  0.2227

O(1)-Zr-O(2)   131.8(4)     0.2500  0.2500  0.3531    0.0389 -0.0630 -0.2227

Table 5 Continued

Atoms	      Angle			  Coordinates of bonded atoms

O(1)-Zr-O(2)   133.8(5)     0.2500  0.2500  0.3531    0.4370 -0.0389 -0.2773

O(1)-Zr-O(2)    68.3(3)     0.2500  0.2500  0.3531    0.5630  0.0389  0.2773

O(1)-Zr-O(3)   110.8(9)     0.2500  0.2500  0.3531    0.2500 -0.2500  0.2059

O(1)-Zr-O(3)   100.6(8)     0.2500  0.2500  0.3531    0.2500 -0.2500  0.2941

O(2)-Zr-O(2)    70.39(9)    0.4611 -0.0630 -0.2227    0.5389  0.0630  0.2227

O(2)-Zr-O(2)   159.9(7)     0.4611 -0.0630 -0.2227   -0.0630  0.0389  0.2773

O(2)-Zr-O(2)    83.2(5)     0.4611 -0.0630 -0.2227    0.0630 -0.0389 -0.2773

O(2)-Zr-O(2)   159.8(6)     0.4611 -0.0630 -0.2227   -0.0389  0.0630  0.2227

O(2)-Zr-O(2)    89.9(5)     0.4611 -0.0630 -0.2227    0.0389 -0.0630 -0.2227

O(2)-Zr-O(2)     9.9(1)     0.4611 -0.0630 -0.2227    0.4370 -0.0389 -0.2773

O(2)-Zr-O(2)    72.76(7)    0.4611 -0.0630 -0.2227    0.5630  0.0389  0.2773

O(2)-Zr-O(3)    89.2(7)     0.4611 -0.0630 -0.2227    0.2500 -0.2500  0.2059

O(2)-Zr-O(3)    96.4(7)     0.4611 -0.0630 -0.2227    0.2500 -0.2500  0.2941

O(2)-Zr-O(2)   125.7(6)     0.5389  0.0630  0.2227   -0.0630  0.0389  0.2773

O(2)-Zr-O(2)   153.4(5)     0.5389  0.0630  0.2227    0.0630 -0.0389 -0.2773

O(2)-Zr-O(2)   128.9(6)     0.5389  0.0630  0.2227   -0.0389  0.0630  0.2227

O(2)-Zr-O(2)   159.8(6)     0.5389  0.0630  0.2227    0.0389 -0.0630 -0.2227

O(2)-Zr-O(2)    77.7(1)     0.5389  0.0630  0.2227    0.4370 -0.0389 -0.2773

O(2)-Zr-O(2)     6.19(7)    0.5389  0.0630  0.2227    0.5630  0.0389  0.2773

O(2)-Zr-O(3)    86.5(5)     0.5389  0.0630  0.2227    0.2500 -0.2500  0.2059

O(2)-Zr-O(3)    82.2(5)     0.5389  0.0630  0.2227    0.2500 -0.2500  0.2941

O(2)-Zr-O(2)    80.73(9)   -0.0630  0.0389  0.2773    0.0630 -0.0389 -0.2773

O(2)-Zr-O(2)     6.19(7)   -0.0630  0.0389  0.2773   -0.0389  0.0630  0.2227

O(2)-Zr-O(2)    72.76(7)   -0.0630  0.0389  0.2773    0.0389 -0.0630 -0.2227

O(2)-Zr-O(2)   155.8(5)    -0.0630  0.0389  0.2773    0.4370 -0.0389 -0.2773

O(2)-Zr-O(2)   122.0(5)    -0.0630  0.0389  0.2773    0.5630  0.0389  0.2773

O(2)-Zr-O(3)    80.8(5)    -0.0630  0.0389  0.2773    0.2500 -0.2500  0.2059

O(2)-Zr-O(3)    76.2(4)    -0.0630  0.0389  0.2773    0.2500 -0.2500  0.2941

O(2)-Zr-O(2)    77.7(1)     0.0630 -0.0389 -0.2773   -0.0389  0.0630  0.2227

O(2)-Zr-O(2)     9.9(1)     0.0630 -0.0389 -0.2773    0.0389 -0.0630 -0.2227

O(2)-Zr-O(2)    75.7(4)     0.0630 -0.0389 -0.2773    0.4370 -0.0389 -0.2773

O(2)-Zr-O(2)   155.8(5)     0.0630 -0.0389 -0.2773    0.5630  0.0389  0.2773

O(2)-Zr-O(3)    96.4(8)     0.0630 -0.0389 -0.2773    0.2500 -0.2500  0.2059

O(2)-Zr-O(3)   104.3(7)     0.0630 -0.0389 -0.2773    0.2500 -0.2500  0.2941

O(2)-Zr-O(2)    70.39(9)   -0.0389  0.0630  0.2227    0.0389 -0.0630 -0.2227

O(2)-Zr-O(2)   153.4(5)    -0.0389  0.0630  0.2227    0.4370 -0.0389 -0.2773

O(2)-Zr-O(2)   125.7(6)    -0.0389  0.0630  0.2227    0.5630  0.0389  0.2773

O(2)-Zr-O(3)    86.5(5)    -0.0389  0.0630  0.2227    0.2500 -0.2500  0.2059

O(2)-Zr-O(3)    82.2(5)    -0.0389  0.0630  0.2227    0.2500 -0.2500  0.2941

O(2)-Zr-O(2)    83.2(5)     0.0389 -0.0630 -0.2227    0.4370 -0.0389 -0.2773

O(2)-Zr-O(2)   159.9(7)     0.0389 -0.0630 -0.2227    0.5630  0.0389  0.2773

O(2)-Zr-O(3)    89.2(7)     0.0389 -0.0630 -0.2227    0.2500 -0.2500  0.2059

O(2)-Zr-O(3)    96.4(7)     0.0389 -0.0630 -0.2227    0.2500 -0.2500  0.2941

O(2)-Zr-O(2)    80.73(9)    0.4370 -0.0389 -0.2773    0.5630  0.0389  0.2773

O(2)-Zr-O(3)    96.4(8)     0.4370 -0.0389 -0.2773    0.2500 -0.2500  0.2059

O(2)-Zr-O(3)   104.3(7)     0.4370 -0.0389 -0.2773    0.2500 -0.2500  0.2941

O(2)-Zr-O(3)    80.8(5)     0.5630  0.0389  0.2773    0.2500 -0.2500  0.2059

O(2)-Zr-O(3)    76.2(4)     0.5630  0.0389  0.2773    0.2500 -0.2500  0.2941

O(3)-Zr-O(3)    10.2(1.5)   0.2500 -0.2500  0.2059    0.2500 -0.2500  0.2941

Bi-O(1)-Bi     130.40(9)    0.2500  0.0025  0.0097    0.2500  0.4975  0.0097

Bi-O(1)-Bi     107.37(3)    0.2500  0.0025  0.0097    0.4975  0.2500 -0.4903

Bi-O(1)-Bi     107.37(3)    0.2500  0.0025  0.0097    0.0025  0.2500 -0.4903

Bi-O(1)-Zr       6.6(4)     0.2500  0.0025  0.0097    0.2500  0.0259  0.0404

Bi-O(1)-Zr     123.8(4)     0.2500  0.0025  0.0097    0.2500  0.4741  0.0404

Table 5 Continued

Atoms	      Angle			  Coordinates of bonded atoms

Bi-O(1)-Zr     107.4(1)     0.2500  0.0025  0.0097    0.4741  0.2500 -0.4596

Bi-O(1)-Zr     107.4(1)     0.2500  0.0025  0.0097    0.0259  0.2500 -0.4596

Bi-O(1)-O(1)   114.80(4)    0.2500  0.0025  0.0097    0.2500  0.2500 -0.6469

Bi-O(1)-O(1)    65.20(4)    0.2500  0.0025  0.0097    0.2500  0.2500  0.3531

Bi-O(1)-O(2)    46.87(4)    0.2500  0.0025  0.0097    0.4611 -0.0630 -0.2227

Bi-O(1)-O(2)   143.65(4)    0.2500  0.0025  0.0097    0.0389  0.5630 -0.2227

Bi-O(1)-O(2)   147.81(4)    0.2500  0.0025  0.0097    0.4370  0.5389 -0.2773

Bi-O(1)-O(2)    51.50(4)    0.2500  0.0025  0.0097    0.0630 -0.0389 -0.2773

Bi-O(1)-O(2)   143.65(4)    0.2500  0.0025  0.0097    0.4611  0.5630 -0.2227

Bi-O(1)-O(2)    46.87(4)    0.2500  0.0025  0.0097    0.0389 -0.0630 -0.2227

Bi-O(1)-O(2)    51.50(4)    0.2500  0.0025  0.0097    0.4370 -0.0389 -0.2773

Bi-O(1)-O(2)   147.81(4)    0.2500  0.0025  0.0097    0.0630  0.5389 -0.2773

Bi-O(1)-Bi     107.37(3)    0.2500  0.4975  0.0097    0.4975  0.2500 -0.4903

Bi-O(1)-Bi     107.37(3)    0.2500  0.4975  0.0097    0.0025  0.2500 -0.4903

Bi-O(1)-Zr     123.8(4)     0.2500  0.4975  0.0097    0.2500  0.0259  0.0404

Bi-O(1)-Zr       6.6(4)     0.2500  0.4975  0.0097    0.2500  0.4741  0.0404

Bi-O(1)-Zr     107.4(1)     0.2500  0.4975  0.0097    0.4741  0.2500 -0.4596

Bi-O(1)-Zr     107.4(1)     0.2500  0.4975  0.0097    0.0259  0.2500 -0.4596

Bi-O(1)-O(1)   114.80(4)    0.2500  0.4975  0.0097    0.2500  0.2500 -0.6469

Bi-O(1)-O(1)    65.20(4)    0.2500  0.4975  0.0097    0.2500  0.2500  0.3531

Bi-O(1)-O(2)   143.65(4)    0.2500  0.4975  0.0097    0.4611 -0.0630 -0.2227

Bi-O(1)-O(2)    46.87(4)    0.2500  0.4975  0.0097    0.0389  0.5630 -0.2227

Bi-O(1)-O(2)    51.50(4)    0.2500  0.4975  0.0097    0.4370  0.5389 -0.2773

Bi-O(1)-O(2)   147.81(4)    0.2500  0.4975  0.0097    0.0630 -0.0389 -0.2773

Bi-O(1)-O(2)    46.87(4)    0.2500  0.4975  0.0097    0.4611  0.5630 -0.2227

Bi-O(1)-O(2)   143.65(4)    0.2500  0.4975  0.0097    0.0389 -0.0630 -0.2227

Bi-O(1)-O(2)   147.81(4)    0.2500  0.4975  0.0097    0.4370 -0.0389 -0.2773

Bi-O(1)-O(2)    51.50(4)    0.2500  0.4975  0.0097    0.0630  0.5389 -0.2773

Bi-O(1)-Bi      89.25(6)    0.4975  0.2500 -0.4903    0.0025  0.2500 -0.4903

Bi-O(1)-Zr     111.8(3)     0.4975  0.2500 -0.4903    0.2500  0.0259  0.0404

Bi-O(1)-Zr     111.8(3)     0.4975  0.2500 -0.4903    0.2500  0.4741  0.0404

Bi-O(1)-Zr       0.2(2)     0.4975  0.2500 -0.4903    0.4741  0.2500 -0.4596

Bi-O(1)-Zr      89.1(4)     0.4975  0.2500 -0.4903    0.0259  0.2500 -0.4596

Bi-O(1)-O(1)    44.63(3)    0.4975  0.2500 -0.4903    0.2500  0.2500 -0.6469

Bi-O(1)-O(1)   135.37(3)    0.4975  0.2500 -0.4903    0.2500  0.2500  0.3531

Bi-O(1)-O(2)    60.53(4)    0.4975  0.2500 -0.4903    0.4611 -0.0630 -0.2227

Bi-O(1)-O(2)   106.59(5)    0.4975  0.2500 -0.4903    0.0389  0.5630 -0.2227

Bi-O(1)-O(2)    56.10(4)    0.4975  0.2500 -0.4903    0.4370  0.5389 -0.2773

Bi-O(1)-O(2)   100.26(5)    0.4975  0.2500 -0.4903    0.0630 -0.0389 -0.2773

Bi-O(1)-O(2)    60.53(4)    0.4975  0.2500 -0.4903    0.4611  0.5630 -0.2227

Bi-O(1)-O(2)   106.59(5)    0.4975  0.2500 -0.4903    0.0389 -0.0630 -0.2227

Bi-O(1)-O(2)    56.10(4)    0.4975  0.2500 -0.4903    0.4370 -0.0389 -0.2773

Bi-O(1)-O(2)   100.26(5)    0.4975  0.2500 -0.4903    0.0630  0.5389 -0.2773

Bi-O(1)-Zr     111.8(3)     0.0025  0.2500 -0.4903    0.2500  0.0259  0.0404

Bi-O(1)-Zr     111.8(3)     0.0025  0.2500 -0.4903    0.2500  0.4741  0.0404

Bi-O(1)-Zr      89.1(4)     0.0025  0.2500 -0.4903    0.4741  0.2500 -0.4596

Bi-O(1)-Zr       0.2(2)     0.0025  0.2500 -0.4903    0.0259  0.2500 -0.4596

Bi-O(1)-O(1)    44.63(3)    0.0025  0.2500 -0.4903    0.2500  0.2500 -0.6469

Bi-O(1)-O(1)   135.37(3)    0.0025  0.2500 -0.4903    0.2500  0.2500  0.3531

Bi-O(1)-O(2)   106.59(5)    0.0025  0.2500 -0.4903    0.4611 -0.0630 -0.2227

Bi-O(1)-O(2)    60.53(4)    0.0025  0.2500 -0.4903    0.0389  0.5630 -0.2227

Bi-O(1)-O(2)   100.26(5)    0.0025  0.2500 -0.4903    0.4370  0.5389 -0.2773

Bi-O(1)-O(2)    56.10(4)    0.0025  0.2500 -0.4903    0.0630 -0.0389 -0.2773

Bi-O(1)-O(2)   106.59(5)    0.0025  0.2500 -0.4903    0.4611  0.5630 -0.2227

Table 5 Continued

Atoms	      Angle			  Coordinates of bonded atoms

Bi-O(1)-O(2)    60.53(4)    0.0025  0.2500 -0.4903    0.0389 -0.0630 -0.2227

Bi-O(1)-O(2)   100.26(5)    0.0025  0.2500 -0.4903    0.4370 -0.0389 -0.2773

Bi-O(1)-O(2)    56.10(4)    0.0025  0.2500 -0.4903    0.0630  0.5389 -0.2773

Zr-O(1)-Zr     117.2(9)     0.2500  0.0259  0.0404    0.2500  0.4741  0.0404

Zr-O(1)-Zr     111.8(3)     0.2500  0.0259  0.0404    0.4741  0.2500 -0.4596

Zr-O(1)-Zr     111.8(3)     0.2500  0.0259  0.0404    0.0259  0.2500 -0.4596

Zr-O(1)-O(1)   121.4(4)     0.2500  0.0259  0.0404    0.2500  0.2500 -0.6469

Zr-O(1)-O(1)    58.6(4)     0.2500  0.0259  0.0404    0.2500  0.2500  0.3531

Zr-O(1)-O(2)    51.3(3)     0.2500  0.0259  0.0404    0.4611 -0.0630 -0.2227

Zr-O(1)-O(2)   140.9(2)     0.2500  0.0259  0.0404    0.0389  0.5630 -0.2227

Zr-O(1)-O(2)   146.1(2)     0.2500  0.0259  0.0404    0.4370  0.5389 -0.2773

Zr-O(1)-O(2)    56.5(3)     0.2500  0.0259  0.0404    0.0630 -0.0389 -0.2773

Zr-O(1)-O(2)   140.9(2)     0.2500  0.0259  0.0404    0.4611  0.5630 -0.2227

Zr-O(1)-O(2)    51.3(3)     0.2500  0.0259  0.0404    0.0389 -0.0630 -0.2227

Zr-O(1)-O(2)    56.5(3)     0.2500  0.0259  0.0404    0.4370 -0.0389 -0.2773

Zr-O(1)-O(2)   146.1(2)     0.2500  0.0259  0.0404    0.0630  0.5389 -0.2773

Zr-O(1)-Zr     111.8(3)     0.2500  0.4741  0.0404    0.4741  0.2500 -0.4596

Zr-O(1)-Zr     111.8(3)     0.2500  0.4741  0.0404    0.0259  0.2500 -0.4596

Zr-O(1)-O(1)   121.4(4)     0.2500  0.4741  0.0404    0.2500  0.2500 -0.6469

Zr-O(1)-O(1)    58.6(4)     0.2500  0.4741  0.0404    0.2500  0.2500  0.3531

Zr-O(1)-O(2)   140.9(2)     0.2500  0.4741  0.0404    0.4611 -0.0630 -0.2227

Zr-O(1)-O(2)    51.3(3)     0.2500  0.4741  0.0404    0.0389  0.5630 -0.2227

Zr-O(1)-O(2)    56.5(3)     0.2500  0.4741  0.0404    0.4370  0.5389 -0.2773

Zr-O(1)-O(2)   146.1(2)     0.2500  0.4741  0.0404    0.0630 -0.0389 -0.2773

Zr-O(1)-O(2)    51.3(3)     0.2500  0.4741  0.0404    0.4611  0.5630 -0.2227

Zr-O(1)-O(2)   140.9(2)     0.2500  0.4741  0.0404    0.0389 -0.0630 -0.2227

Zr-O(1)-O(2)   146.1(2)     0.2500  0.4741  0.0404    0.4370 -0.0389 -0.2773

Zr-O(1)-O(2)    56.5(3)     0.2500  0.4741  0.0404    0.0630  0.5389 -0.2773

Zr-O(1)-Zr      88.9(8)     0.4741  0.2500 -0.4596    0.0259  0.2500 -0.4596

Zr-O(1)-O(1)    44.5(4)     0.4741  0.2500 -0.4596    0.2500  0.2500 -0.6469

Zr-O(1)-O(1)   135.5(4)     0.4741  0.2500 -0.4596    0.2500  0.2500  0.3531

Zr-O(1)-O(2)    60.6(1)     0.4741  0.2500 -0.4596    0.4611 -0.0630 -0.2227

Zr-O(1)-O(2)   106.5(2)     0.4741  0.2500 -0.4596    0.0389  0.5630 -0.2227

Zr-O(1)-O(2)    56.13(9)    0.4741  0.2500 -0.4596    0.4370  0.5389 -0.2773

Zr-O(1)-O(2)   100.2(2)     0.4741  0.2500 -0.4596    0.0630 -0.0389 -0.2773

Zr-O(1)-O(2)    60.6(1)     0.4741  0.2500 -0.4596    0.4611  0.5630 -0.2227

Zr-O(1)-O(2)   106.5(2)     0.4741  0.2500 -0.4596    0.0389 -0.0630 -0.2227

Zr-O(1)-O(2)    56.13(9)    0.4741  0.2500 -0.4596    0.4370 -0.0389 -0.2773

Zr-O(1)-O(2)   100.2(2)     0.4741  0.2500 -0.4596    0.0630  0.5389 -0.2773

Zr-O(1)-O(1)    44.5(4)     0.0259  0.2500 -0.4596    0.2500  0.2500 -0.6469

Zr-O(1)-O(1)   135.5(4)     0.0259  0.2500 -0.4596    0.2500  0.2500  0.3531

Zr-O(1)-O(2)   106.5(2)     0.0259  0.2500 -0.4596    0.4611 -0.0630 -0.2227

Zr-O(1)-O(2)    60.6(1)     0.0259  0.2500 -0.4596    0.0389  0.5630 -0.2227

Zr-O(1)-O(2)   100.2(2)     0.0259  0.2500 -0.4596    0.4370  0.5389 -0.2773

Zr-O(1)-O(2)    56.13(9)    0.0259  0.2500 -0.4596    0.0630 -0.0389 -0.2773

Zr-O(1)-O(2)   106.5(2)     0.0259  0.2500 -0.4596    0.4611  0.5630 -0.2227

Zr-O(1)-O(2)    60.6(1)     0.0259  0.2500 -0.4596    0.0389 -0.0630 -0.2227

Zr-O(1)-O(2)   100.2(2)     0.0259  0.2500 -0.4596    0.4370 -0.0389 -0.2773

Zr-O(1)-O(2)    56.13(9)    0.0259  0.2500 -0.4596    0.0630  0.5389 -0.2773

O(1)-O(1)-O(1) 179.98(0)    0.2500  0.2500 -0.6469    0.2500  0.2500  0.3531

O(1)-O(1)-O(2)  81.66(4)    0.2500  0.2500 -0.6469    0.4611 -0.0630 -0.2227

O(1)-O(1)-O(2)  81.66(4)    0.2500  0.2500 -0.6469    0.0389  0.5630 -0.2227

O(1)-O(1)-O(2)  74.53(4)    0.2500  0.2500 -0.6469    0.4370  0.5389 -0.2773

O(1)-O(1)-O(2)  74.53(4)    0.2500  0.2500 -0.6469    0.0630 -0.0389 -0.2773

Table 5 Continued

Atoms	      Angle			  Coordinates of bonded atoms

O(1)-O(1)-O(2)  81.66(4)    0.2500  0.2500 -0.6469    0.4611  0.5630 -0.2227

O(1)-O(1)-O(2)  81.66(4)    0.2500  0.2500 -0.6469    0.0389 -0.0630 -0.2227

O(1)-O(1)-O(2)  74.53(4)    0.2500  0.2500 -0.6469    0.4370 -0.0389 -0.2773

O(1)-O(1)-O(2)  74.53(4)    0.2500  0.2500 -0.6469    0.0630  0.5389 -0.2773

O(1)-O(1)-O(2)  98.34(4)    0.2500  0.2500  0.3531    0.4611 -0.0630 -0.2227

O(1)-O(1)-O(2)  98.34(4)    0.2500  0.2500  0.3531    0.0389  0.5630 -0.2227

O(1)-O(1)-O(2) 105.47(4)    0.2500  0.2500  0.3531    0.4370  0.5389 -0.2773

O(1)-O(1)-O(2) 105.47(4)    0.2500  0.2500  0.3531    0.0630 -0.0389 -0.2773

O(1)-O(1)-O(2)  98.34(4)    0.2500  0.2500  0.3531    0.4611  0.5630 -0.2227

O(1)-O(1)-O(2)  98.34(4)    0.2500  0.2500  0.3531    0.0389 -0.0630 -0.2227

O(1)-O(1)-O(2) 105.47(4)    0.2500  0.2500  0.3531    0.4370 -0.0389 -0.2773

O(1)-O(1)-O(2) 105.47(4)    0.2500  0.2500  0.3531    0.0630  0.5389 -0.2773

O(2)-O(1)-O(2) 163.32(8)    0.4611 -0.0630 -0.2227    0.0389  0.5630 -0.2227

O(2)-O(1)-O(2) 109.57(6)    0.4611 -0.0630 -0.2227    0.4370  0.5389 -0.2773

O(2)-O(1)-O(2)  65.65(6)    0.4611 -0.0630 -0.2227    0.0630 -0.0389 -0.2773

O(2)-O(1)-O(2) 110.21(6)    0.4611 -0.0630 -0.2227    0.4611  0.5630 -0.2227

O(2)-O(1)-O(2)  67.20(6)    0.4611 -0.0630 -0.2227    0.0389 -0.0630 -0.2227

O(2)-O(1)-O(2)   7.20(7)    0.4611 -0.0630 -0.2227    0.4370 -0.0389 -0.2773

O(2)-O(1)-O(2) 156.17(5)    0.4611 -0.0630 -0.2227    0.0630  0.5389 -0.2773

O(2)-O(1)-O(2)  65.65(6)    0.0389  0.5630 -0.2227    0.4370  0.5389 -0.2773

O(2)-O(1)-O(2) 109.57(6)    0.0389  0.5630 -0.2227    0.0630 -0.0389 -0.2773

O(2)-O(1)-O(2)  67.20(6)    0.0389  0.5630 -0.2227    0.4611  0.5630 -0.2227

O(2)-O(1)-O(2) 110.21(6)    0.0389  0.5630 -0.2227    0.0389 -0.0630 -0.2227

O(2)-O(1)-O(2) 156.17(5)    0.0389  0.5630 -0.2227    0.4370 -0.0389 -0.2773

O(2)-O(1)-O(2)   7.20(7)    0.0389  0.5630 -0.2227    0.0630  0.5389 -0.2773

O(2)-O(1)-O(2) 149.07(9)    0.4370  0.5389 -0.2773    0.0630 -0.0389 -0.2773

O(2)-O(1)-O(2)   7.20(7)    0.4370  0.5389 -0.2773    0.4611  0.5630 -0.2227

O(2)-O(1)-O(2) 156.17(5)    0.4370  0.5389 -0.2773    0.0389 -0.0630 -0.2227

O(2)-O(1)-O(2) 108.00(7)    0.4370  0.5389 -0.2773    0.4370 -0.0389 -0.2773

O(2)-O(1)-O(2)  63.18(7)    0.4370  0.5389 -0.2773    0.0630  0.5389 -0.2773

O(2)-O(1)-O(2) 156.17(5)    0.0630 -0.0389 -0.2773    0.4611  0.5630 -0.2227

O(2)-O(1)-O(2)   7.20(7)    0.0630 -0.0389 -0.2773    0.0389 -0.0630 -0.2227

O(2)-O(1)-O(2)  63.18(7)    0.0630 -0.0389 -0.2773    0.4370 -0.0389 -0.2773

O(2)-O(1)-O(2) 108.00(7)    0.0630 -0.0389 -0.2773    0.0630  0.5389 -0.2773

O(2)-O(1)-O(2) 163.32(8)    0.4611  0.5630 -0.2227    0.0389 -0.0630 -0.2227

O(2)-O(1)-O(2) 109.57(6)    0.4611  0.5630 -0.2227    0.4370 -0.0389 -0.2773

O(2)-O(1)-O(2)  65.65(6)    0.4611  0.5630 -0.2227    0.0630  0.5389 -0.2773

O(2)-O(1)-O(2)  65.65(6)    0.0389 -0.0630 -0.2227    0.4370 -0.0389 -0.2773

O(2)-O(1)-O(2) 109.57(6)    0.0389 -0.0630 -0.2227    0.0630  0.5389 -0.2773

O(2)-O(1)-O(2) 149.07(9)    0.4370 -0.0389 -0.2773    0.0630  0.5389 -0.2773

Bi-O(2)-Bi     109.25(7)    0.2500  0.0025  0.0097    0.7500 -0.0025 -0.0097

Bi-O(2)-Bi     101.34(7)    0.2500  0.0025  0.0097    0.4975  0.2500 -0.4903

Bi-O(2)-Bi     135.62(9)    0.2500  0.0025  0.0097    0.5025 -0.2500 -0.5097

Bi-O(2)-Zr       5.0(3)     0.2500  0.0025  0.0097    0.2500  0.0259  0.0404

Bi-O(2)-Zr     113.8(3)     0.2500  0.0025  0.0097    0.7500 -0.0259 -0.0404

Bi-O(2)-Zr      96.7(3)     0.2500  0.0025  0.0097    0.4741  0.2500 -0.4596

Bi-O(2)-Zr     140.2(4)     0.2500  0.0025  0.0097    0.5259 -0.2500 -0.5404

Bi-O(2)-O(1)    45.54(5)    0.2500  0.0025  0.0097    0.2500  0.2500 -0.1469

Bi-O(2)-O(1)   153.95(9)    0.2500  0.0025  0.0097    0.7500 -0.2500 -0.3531

Bi-O(2)-O(2)    61.82(7)    0.2500  0.0025  0.0097    0.5389  0.0630  0.2227

Bi-O(2)-O(2)   103.59(5)    0.2500  0.0025  0.0097    0.4611 -0.4370 -0.2227

Bi-O(2)-O(2)    90.4(4)     0.2500  0.0025  0.0097    0.4370 -0.0389 -0.2773

Bi-O(2)-Bi      90.45(7)    0.7500 -0.0025 -0.0097    0.4975  0.2500 -0.4903

Bi-O(2)-Bi     109.70(8)    0.7500 -0.0025 -0.0097    0.5025 -0.2500 -0.5097

Table 5 Continued

Atoms	      Angle			  Coordinates of bonded atoms

Bi-O(2)-Zr     105.0(3)     0.7500 -0.0025 -0.0097    0.2500  0.0259  0.0404

Bi-O(2)-Zr       5.2(4)     0.7500 -0.0025 -0.0097    0.7500 -0.0259 -0.0404

Bi-O(2)-Zr      92.0(3)     0.7500 -0.0025 -0.0097    0.4741  0.2500 -0.4596

Bi-O(2)-Zr     106.4(4)     0.7500 -0.0025 -0.0097    0.5259 -0.2500 -0.5404

Bi-O(2)-O(1)   105.25(6)    0.7500 -0.0025 -0.0097    0.2500  0.2500 -0.1469

Bi-O(2)-O(1)    61.22(4)    0.7500 -0.0025 -0.0097    0.7500 -0.2500 -0.3531

Bi-O(2)-O(2)    47.43(5)    0.7500 -0.0025 -0.0097    0.5389  0.0630  0.2227

Bi-O(2)-O(2)   100.43(4)    0.7500 -0.0025 -0.0097    0.4611 -0.4370 -0.2227

Bi-O(2)-O(2)   131.99(6)    0.7500 -0.0025 -0.0097    0.4370 -0.0389 -0.2773

Bi-O(2)-Bi      98.80(6)    0.4975  0.2500 -0.4903    0.5025 -0.2500 -0.5097

Bi-O(2)-Zr      99.0(4)     0.4975  0.2500 -0.4903    0.2500  0.0259  0.0404

Bi-O(2)-Zr      91.9(4)     0.4975  0.2500 -0.4903    0.7500 -0.0259 -0.0404

Bi-O(2)-Zr       4.7(3)     0.4975  0.2500 -0.4903    0.4741  0.2500 -0.4596

Bi-O(2)-Zr      95.5(2)     0.4975  0.2500 -0.4903    0.5259 -0.2500 -0.5404

Bi-O(2)-O(1)    55.82(4)    0.4975  0.2500 -0.4903    0.2500  0.2500 -0.1469

Bi-O(2)-O(1)   102.85(6)    0.4975  0.2500 -0.4903    0.7500 -0.2500 -0.3531

Bi-O(2)-O(2)    99.25(8)    0.4975  0.2500 -0.4903    0.5389  0.0630  0.2227

Bi-O(2)-O(2)   147.59(4)    0.4975  0.2500 -0.4903    0.4611 -0.4370 -0.2227

Bi-O(2)-O(2)    41.97(5)    0.4975  0.2500 -0.4903    0.4370 -0.0389 -0.2773

Bi-O(2)-Zr     140.6(3)     0.5025 -0.2500 -0.5097    0.2500  0.0259  0.0404

Bi-O(2)-Zr     104.6(3)     0.5025 -0.2500 -0.5097    0.7500 -0.0259 -0.0404

Bi-O(2)-Zr     102.4(3)     0.5025 -0.2500 -0.5097    0.4741  0.2500 -0.4596

Bi-O(2)-Zr       4.8(4)     0.5025 -0.2500 -0.5097    0.5259 -0.2500 -0.5404

Bi-O(2)-O(1)    36.73(8)    0.5025 -0.2500 -0.5097    0.2500  0.2500 -0.1469

Bi-O(2)-O(1)    48.71(5)    0.5025 -0.2500 -0.5097    0.7500 -0.2500 -0.3531

Bi-O(2)-O(2)   150.7(1)     0.5025 -0.2500 -0.5097    0.5389  0.0630  0.2227

Bi-O(2)-O(2)    48.79(5)    0.5025 -0.2500 -0.5097    0.4611 -0.4370 -0.2227

Bi-O(2)-O(2)    79.0(4)     0.5025 -0.2500 -0.5097    0.4370 -0.0389 -0.2773

Zr-O(2)-Zr     109.61(9)    0.2500  0.0259  0.0404    0.7500 -0.0259 -0.0404

Zr-O(2)-Zr      94.4(6)     0.2500  0.0259  0.0404    0.4741  0.2500 -0.4596

Zr-O(2)-Zr     145.2(7)     0.2500  0.0259  0.0404    0.5259 -0.2500 -0.5404

Zr-O(2)-O(1)    43.3(4)     0.2500  0.0259  0.0404    0.2500  0.2500 -0.1469

Zr-O(2)-O(1)   153.9(4)     0.2500  0.0259  0.0404    0.7500 -0.2500 -0.3531

Zr-O(2)-O(2)    57.6(3)     0.2500  0.0259  0.0404    0.5389  0.0630  0.2227

Zr-O(2)-O(2)   107.3(4)     0.2500  0.0259  0.0404    0.4611 -0.4370 -0.2227

Zr-O(2)-O(2)    91.6(6)     0.2500  0.0259  0.0404    0.4370 -0.0389 -0.2773

Zr-O(2)-Zr      93.8(7)     0.7500 -0.0259 -0.0404    0.4741  0.2500 -0.4596

Zr-O(2)-Zr     101.3(7)     0.7500 -0.0259 -0.0404    0.5259 -0.2500 -0.5404

Zr-O(2)-O(1)   110.1(4)     0.7500 -0.0259 -0.0404    0.2500  0.2500 -0.1469

Zr-O(2)-O(1)    56.1(3)     0.7500 -0.0259 -0.0404    0.7500 -0.2500 -0.3531

Zr-O(2)-O(2)    52.0(3)     0.7500 -0.0259 -0.0404    0.5389  0.0630  0.2227

Zr-O(2)-O(2)    96.7(4)     0.7500 -0.0259 -0.0404    0.4611 -0.4370 -0.2227

Zr-O(2)-O(2)   132.6(4)     0.7500 -0.0259 -0.0404    0.4370 -0.0389 -0.2773

Zr-O(2)-Zr      99.27(9)    0.4741  0.2500 -0.4596    0.5259 -0.2500 -0.5404

Zr-O(2)-O(1)    51.2(3)     0.4741  0.2500 -0.4596    0.2500  0.2500 -0.1469

Zr-O(2)-O(1)   107.4(3)     0.4741  0.2500 -0.4596    0.7500 -0.2500 -0.3531

Zr-O(2)-O(2)    97.1(3)     0.4741  0.2500 -0.4596    0.5389  0.0630  0.2227

Zr-O(2)-O(2)   151.0(3)     0.4741  0.2500 -0.4596    0.4611 -0.4370 -0.2227

Zr-O(2)-O(2)    41.2(3)     0.4741  0.2500 -0.4596    0.4370 -0.0389 -0.2773

Zr-O(2)-O(1)   137.0(3)     0.5259 -0.2500 -0.5404    0.2500  0.2500 -0.1469

Zr-O(2)-O(1)    45.9(4)     0.5259 -0.2500 -0.5404    0.7500 -0.2500 -0.3531

Zr-O(2)-O(2)   149.6(4)     0.5259 -0.2500 -0.5404    0.5389  0.0630  0.2227

Zr-O(2)-O(2)    52.2(2)     0.5259 -0.2500 -0.5404    0.4611 -0.4370 -0.2227

Zr-O(2)-O(2)    78.5(5)     0.5259 -0.2500 -0.5404    0.4370 -0.0389 -0.2773

Table 5 Continued

Atoms	      Angle			  Coordinates of bonded atoms

O(1)-O(2)-O(1) 156.35(6)    0.2500  0.2500 -0.1469    0.7500 -0.2500 -0.3531

O(1)-O(2)-O(2)  72.50(7)    0.2500  0.2500 -0.1469    0.5389  0.0630  0.2227

O(1)-O(2)-O(2) 145.11(3)    0.2500  0.2500 -0.1469    0.4611 -0.4370 -0.2227

O(1)-O(2)-O(2)  58.6(4)     0.2500  0.2500 -0.1469    0.4370 -0.0389 -0.2773

O(1)-O(2)-O(2) 104.56(8)    0.7500 -0.2500 -0.3531    0.5389  0.0630  0.2227

O(1)-O(2)-O(2)  58.41(3)    0.7500 -0.2500 -0.3531    0.4611 -0.4370 -0.2227

O(1)-O(2)-O(2) 114.2(5)     0.7500 -0.2500 -0.3531    0.4370 -0.0389 -0.2773

O(2)-O(2)-O(2) 110.64(7)    0.5389  0.0630  0.2227    0.4611 -0.4370 -0.2227

O(2)-O(2)-O(2) 129.0(4)     0.5389  0.0630  0.2227    0.4370 -0.0389 -0.2773

O(2)-O(2)-O(2) 117.4(3)     0.4611 -0.4370 -0.2227    0.4370 -0.0389 -0.2773

Bi-O(3)-Bi     120.9(1.5)   0.2500  0.0025  0.0097    0.2500 -0.5025  0.0097

Bi-O(3)-Bi     108.3(2)     0.2500  0.0025  0.0097    0.5025 -0.2500  0.4903

Bi-O(3)-Bi     108.3(2)     0.2500  0.0025  0.0097   -0.0025 -0.2500  0.4903

Bi-O(3)-Zr       5.9(4)     0.2500  0.0025  0.0097    0.2500  0.0259  0.0404

Bi-O(3)-Zr     126.8(1.5)   0.2500  0.0025  0.0097    0.2500 -0.5259  0.0404

Bi-O(3)-Zr     106.0(2)     0.2500  0.0025  0.0097    0.5259 -0.2500  0.4596

Bi-O(3)-Zr     106.0(2)     0.2500  0.0025  0.0097   -0.0259 -0.2500  0.4596

Bi-O(3)-O(3)   119.6(7)     0.2500  0.0025  0.0097    0.2500 -0.2500  0.2941

Bi-O(3)-Bi     108.3(2)     0.2500 -0.5025  0.0097    0.5025 -0.2500  0.4903

Bi-O(3)-Bi     108.3(2)     0.2500 -0.5025  0.0097   -0.0025 -0.2500  0.4903

Bi-O(3)-Zr     126.8(1.5)   0.2500 -0.5025  0.0097    0.2500  0.0259  0.0404

Bi-O(3)-Zr       5.9(4)     0.2500 -0.5025  0.0097    0.2500 -0.5259  0.0404

Bi-O(3)-Zr     106.0(2)     0.2500 -0.5025  0.0097    0.5259 -0.2500  0.4596

Bi-O(3)-Zr     106.0(2)     0.2500 -0.5025  0.0097   -0.0259 -0.2500  0.4596

Bi-O(3)-O(3)   119.6(7)     0.2500 -0.5025  0.0097    0.2500 -0.2500  0.2941

Bi-O(3)-Bi     101.2(1.2)   0.5025 -0.2500  0.4903   -0.0025 -0.2500  0.4903

Bi-O(3)-Zr     104.8(3)     0.5025 -0.2500  0.4903    0.2500  0.0259  0.0404

Bi-O(3)-Zr     104.8(3)     0.5025 -0.2500  0.4903    0.2500 -0.5259  0.0404

Bi-O(3)-Zr       5.6(4)     0.5025 -0.2500  0.4903    0.5259 -0.2500  0.4596

Bi-O(3)-Zr     106.7(1.3)   0.5025 -0.2500  0.4903   -0.0259 -0.2500  0.4596

Bi-O(3)-O(3)    50.6(6)     0.5025 -0.2500  0.4903    0.2500 -0.2500  0.2941

Bi-O(3)-Zr     104.8(3)    -0.0025 -0.2500  0.4903    0.2500  0.0259  0.0404

Bi-O(3)-Zr     104.8(3)    -0.0025 -0.2500  0.4903    0.2500 -0.5259  0.0404

Bi-O(3)-Zr     106.7(1.3)  -0.0025 -0.2500  0.4903    0.5259 -0.2500  0.4596

Bi-O(3)-Zr       5.6(4)    -0.0025 -0.2500  0.4903   -0.0259 -0.2500  0.4596

Bi-O(3)-O(3)    50.6(6)    -0.0025 -0.2500  0.4903    0.2500 -0.2500  0.2941

Zr-O(3)-Zr     132.7(1.7)   0.2500  0.0259  0.0404    0.2500 -0.5259  0.0404

Zr-O(3)-Zr     102.9(4)     0.2500  0.0259  0.0404    0.5259 -0.2500  0.4596

Zr-O(3)-Zr     102.9(4)     0.2500  0.0259  0.0404   -0.0259 -0.2500  0.4596

Zr-O(3)-O(3)   113.7(8)     0.2500  0.0259  0.0404    0.2500 -0.2500  0.2941

Zr-O(3)-Zr     102.9(4)     0.2500 -0.5259  0.0404    0.5259 -0.2500  0.4596

Zr-O(3)-Zr     102.9(4)     0.2500 -0.5259  0.0404   -0.0259 -0.2500  0.4596

Zr-O(3)-O(3)   113.7(8)     0.2500 -0.5259  0.0404    0.2500 -0.2500  0.2941

Zr-O(3)-Zr     112.2(1.4)   0.5259 -0.2500  0.4596   -0.0259 -0.2500  0.4596

Zr-O(3)-O(3)    56.1(7)     0.5259 -0.2500  0.4596    0.2500 -0.2500  0.2941

Zr-O(3)-O(3)    56.1(7)    -0.0259 -0.2500  0.4596    0.2500 -0.2500  0.2941