Supplementary Data for -Bi1.85Zr0.15O3.075 at 1023 K

Table 1

Crystal, Data Collection and Structure Refinement Data

| (a) Crystal data |  |
| --- | --- |
| Name | Bizmuth zirconium oxide |
| Empirical formula | Bi1.85Zr0.15O3.075 |
| Formula weight | 449.49 |
| Crystal system | Cubic |
| Space group | Fm-3m |
| Unit cell dimensions | a = 5.6277(4) Å |
| Volume | 178.24(4) Å3 |
| Z | 2 |
| Density (calculated) | 8.3785 g cm-3 |
| Absorption coefficient  | 179.47 mm-1 |
| F(000) | 368.30 |
| Sample description | Orange powder |
| Synthesis | Solid state synthesis: Bi2O3 + ZrO2 at 850 C for 12 h |
| (b) Data collection |  |
| Diffractometer | Siemens D5000 |
| Scan mode | /2 flat plate |
| Temperature | 1023 K |
| Wavelength | CuK (1.5418 Å) |
| 2 range collected | 10-80 |
| Step size | 0.01431 |
| Scan time | 2s |
| Detector | Linear PSD |
| Monochromator/filter | Secondary beam graphite monochromator |
| (c) Refinement |  |
| Refinement software | GSAS (Larson and Von Dreele, 1986) |
| Initial model source | -Bi2O3 |
| 2 range refined | 20-80 |
| Excluded regions | 10-20 |
| Data corrections | None |
| Secondary phases | None |
| No. of observations/restraints/parameters | 4193/0/22 |
| Total no. of reflections used | 16 |
| Independent reflections due to 1 phase | 8 |
| Peak shape | Pseudo-Voigt |
| Final R-factors | Rp = 0.0413, Rwp = 0.0533 Rex = 0.0427, 2 = 1.568 RB = 0.2163 |

Table 2

Atomic Coordinates and Isotropic Thermal Parameters for

-Bi1.85Zr0.15O3.075 at 1023 K

| Atom | Site | x | y | z | Occ. | Uiso (Å2) |
| --- | --- | --- | --- | --- | --- | --- |
| Bi/Zr | 4a | 0.0(-) | 0.0(-) | 0.0(-) | 0.925/0.075 | 0.013(1) |
| O | 8c | 0.25(-) | 0.25(-) | 0.25(-) | 0.76785 | 0.042(13) |

Table 3

Selected Bond Lengths (Å) and Angles () for

-Bi1.85Zr0.15O3.075 at 1023 K

Bi/Zr-O		   2.4369(1) x 8

O-Bi/Zr-O’	  	  70.529(6)  x 12

O-Bi/Zr-O’’		 109.471(3)  x 12

Bi/Zr-O-Bi/Zr’’’	 109.471(3)  x 6

Symmetry relations: ’ = x, y, -z; ’’ = -x, -y, z; ’’’ = x,y+0.5,z+0.5

Table 4

Full List of Contact Distances (Å) for

-Bi1.85Zr0.15O3.075 at 1023 K

Atoms		  	Distance		Coordinates of second atom

Bi/Zr-O      	2.4369(1)   	(  0.2500  0.2500  0.2500)

Bi/Zr-O      	2.4369(1)   	( -0.2500 -0.2500 -0.2500)

Bi/Zr-O      	2.4369(1)   	( -0.2500 -0.2500  0.2500)

Bi/Zr-O      	2.4369(1)   	(  0.2500  0.2500 -0.2500)

Bi/Zr-O      	2.4369(1)   	( -0.2500  0.2500 -0.2500)

Bi/Zr-O      	2.4369(1)   	(  0.2500 -0.2500  0.2500)

Bi/Zr-O      	2.4369(1)   	(  0.2500 -0.2500 -0.2500)

Bi/Zr-O      	2.4369(1)   	( -0.2500  0.2500  0.2500)

O-O          	2.8138(2)   	(  0.2500  0.2500 -0.2500)

O-O          	2.8138(2)   	(  0.2500  0.2500  0.7500)

O-O          	2.8138(2)   	(  0.2500 -0.2500  0.2500)

O-O          	2.8138(2)   	(  0.2500  0.7500  0.2500)

O-O          	2.8138(2)   	( -0.2500  0.2500  0.2500)

O-O          	2.8138(2)   	(  0.7500  0.2500  0.2500)

Table 5

Full List of Angles () for -Bi1.85Zr0.15O3.075 at 1023 K

Atoms	    Angle			 Coordinates of bonded atoms

O-Bi/Zr-O      180.00(0) (  0.2500  0.2500  0.2500) ( -0.2500 -0.2500 -0.2500)

O-Bi/Zr-O	   109.47(1) (  0.2500  0.2500  0.2500) ( -0.2500 -0.2500  0.2500)

O-Bi/Zr-O	    70.53(1) (  0.2500  0.2500  0.2500) (  0.2500  0.2500 -0.2500)

O-Bi/Zr-O	   109.47(1) (  0.2500  0.2500  0.2500) ( -0.2500  0.2500 -0.2500)

O-Bi/Zr-O	    70.53(1) (  0.2500  0.2500  0.2500) (  0.2500 -0.2500  0.2500)

O-Bi/Zr-O	   109.47(1) (  0.2500  0.2500  0.2500) (  0.2500 -0.2500 -0.2500)

O-Bi/Zr-O	    70.53(1) (  0.2500  0.2500  0.2500) ( -0.2500  0.2500  0.2500)

O-Bi/Zr-O	    70.53(1) ( -0.2500 -0.2500 -0.2500) ( -0.2500 -0.2500  0.2500)

O-Bi/Zr-O	   109.47(1) ( -0.2500 -0.2500 -0.2500) (  0.2500  0.2500 -0.2500)

O-Bi/Zr-O	    70.53(1) ( -0.2500 -0.2500 -0.2500) ( -0.2500  0.2500 -0.2500)

O-Bi/Zr-O	   109.47(1) ( -0.2500 -0.2500 -0.2500) (  0.2500 -0.2500  0.2500)

O-Bi/Zr-O	    70.53(1) ( -0.2500 -0.2500 -0.2500) (  0.2500 -0.2500 -0.2500)

O-Bi/Zr-O	   109.47(1) ( -0.2500 -0.2500 -0.2500) ( -0.2500  0.2500  0.2500)

O-Bi/Zr-O	   180.00(0) ( -0.2500 -0.2500  0.2500) (  0.2500  0.2500 -0.2500)

O-Bi/Zr-O	   109.47(1) ( -0.2500 -0.2500  0.2500) ( -0.2500  0.2500 -0.2500)

O-Bi/Zr-O	    70.53(1) ( -0.2500 -0.2500  0.2500) (  0.2500 -0.2500  0.2500)

O-Bi/Zr-O	   109.47(1) ( -0.2500 -0.2500  0.2500) (  0.2500 -0.2500 -0.2500)

O-Bi/Zr-O	    70.53(1) ( -0.2500 -0.2500  0.2500) ( -0.2500  0.2500  0.2500)

O-Bi/Zr-O	    70.53(1) (  0.2500  0.2500 -0.2500) ( -0.2500  0.2500 -0.2500)

O-Bi/Zr-O	   109.47(1) (  0.2500  0.2500 -0.2500) (  0.2500 -0.2500  0.2500)

O-Bi/Zr-O	    70.53(1) (  0.2500  0.2500 -0.2500) (  0.2500 -0.2500 -0.2500)

O-Bi/Zr-O	   109.47(1) (  0.2500  0.2500 -0.2500) ( -0.2500  0.2500  0.2500)

O-Bi/Zr-O	   180.00(0) ( -0.2500  0.2500 -0.2500) (  0.2500 -0.2500  0.2500)

O-Bi/Zr-O	   109.47(1) ( -0.2500  0.2500 -0.2500) (  0.2500 -0.2500 -0.2500)

O-Bi/Zr-O	    70.53(1) ( -0.2500  0.2500 -0.2500) ( -0.2500  0.2500  0.2500)

O-Bi/Zr-O	    70.53(1) (  0.2500 -0.2500  0.2500) (  0.2500 -0.2500 -0.2500)

O-Bi/Zr-O	   109.47(1) (  0.2500 -0.2500  0.2500) ( -0.2500  0.2500  0.2500)

O-Bi/Zr-O	   180.00(0) (  0.2500 -0.2500 -0.2500) ( -0.2500  0.2500  0.2500)

Bi/Zr-O-Bi/Zr  109.47(1) (  0.0000  0.0000  0.0000) (  0.0000  0.5000  0.5000)

Bi/Zr-O-Bi/Zr  109.47(1) (  0.0000  0.0000  0.0000) (  0.5000  0.0000  0.5000)

Bi/Zr-O-Bi/Zr  109.47(1) (  0.0000  0.0000  0.0000) (  0.5000  0.5000  0.0000)

Bi/Zr-O-Bi/Zr  109.47(1) (  0.0000  0.5000  0.5000) (  0.5000  0.0000  0.5000)

Bi/Zr-O-Bi/Zr  109.47(1) (  0.0000  0.5000  0.5000) (  0.5000  0.5000  0.0000)

Bi/Zr-O-Bi/Zr  109.47(1) (  0.5000  0.0000  0.5000) (  0.5000  0.5000  0.0000)

Bi/Zr-O-O       54.74(0) (  0.0000  0.0000  0.0000) (  0.2500  0.2500 -0.2500)

Bi/Zr-O-O      125.26(0) (  0.0000  0.0000  0.0000) (  0.2500  0.2500  0.7500)

Bi/Zr-O-O       54.74(0) (  0.0000  0.0000  0.0000) (  0.2500 -0.2500  0.2500)

Bi/Zr-O-O      125.26(0) (  0.0000  0.0000  0.0000) (  0.2500  0.7500  0.2500)

Bi/Zr-O-O       54.74(0) (  0.0000  0.0000  0.0000) ( -0.2500  0.2500  0.2500)

Bi/Zr-O-O      125.26(0) (  0.0000  0.0000  0.0000) (  0.7500  0.2500  0.2500)

Bi/Zr-O-O      125.26(0) (  0.0000  0.5000  0.5000) (  0.2500  0.2500 -0.2500)

Bi/Zr-O-O       54.74(0) (  0.0000  0.5000  0.5000) (  0.2500  0.2500  0.7500)

Bi/Zr-O-O      125.26(0) (  0.0000  0.5000  0.5000) (  0.2500 -0.2500  0.2500)

Bi/Zr-O-O       54.74(0) (  0.0000  0.5000  0.5000) (  0.2500  0.7500  0.2500)

Bi/Zr-O-O       54.74(0) (  0.0000  0.5000  0.5000) ( -0.2500  0.2500  0.2500)

Bi/Zr-O-O      125.26(0) (  0.0000  0.5000  0.5000) (  0.7500  0.2500  0.2500)

Bi/Zr-O-O      125.26(0) (  0.5000  0.0000  0.5000) (  0.2500  0.2500 -0.2500)

Bi/Zr-O-O       54.74(0) (  0.5000  0.0000  0.5000) (  0.2500  0.2500  0.7500)

Bi/Zr-O-O       54.74(0) (  0.5000  0.0000  0.5000) (  0.2500 -0.2500  0.2500)

Bi/Zr-O-O      125.26(0) (  0.5000  0.0000  0.5000) (  0.2500  0.7500  0.2500)

Bi/Zr-O-O      125.26(0) (  0.5000  0.0000  0.5000) ( -0.2500  0.2500  0.2500)

Bi/Zr-O-O       54.74(0) (  0.5000  0.0000  0.5000) (  0.7500  0.2500  0.2500)

Table 5 Continued

Atoms	    Angle			 Coordinates of bonded atoms

Bi/Zr-O-O       54.74(0) (  0.5000  0.5000  0.0000) (  0.2500  0.2500 -0.2500)

Bi/Zr-O-O      125.26(0) (  0.5000  0.5000  0.0000) (  0.2500  0.2500  0.7500)

Bi/Zr-O-O      125.26(0) (  0.5000  0.5000  0.0000) (  0.2500 -0.2500  0.2500)

Bi/Zr-O-O       54.74(0) (  0.5000  0.5000  0.0000) (  0.2500  0.7500  0.2500)

Bi/Zr-O-O      125.26(0) (  0.5000  0.5000  0.0000) ( -0.2500  0.2500  0.2500)

Bi/Zr-O-O       54.74(0) (  0.5000  0.5000  0.0000) (  0.7500  0.2500  0.2500)

O-O-O          180.00(0) (  0.2500  0.2500 -0.2500) (  0.2500  0.2500  0.7500)

O-O-O           90.00(0) (  0.2500  0.2500 -0.2500) (  0.2500 -0.2500  0.2500)

O-O-O           90.00(0) (  0.2500  0.2500 -0.2500) (  0.2500  0.7500  0.2500)

O-O-O           90.00(0) (  0.2500  0.2500 -0.2500) ( -0.2500  0.2500  0.2500)

O-O-O           90.00(0) (  0.2500  0.2500 -0.2500) (  0.7500  0.2500  0.2500)

O-O-O           90.00(0) (  0.2500  0.2500  0.7500) (  0.2500 -0.2500  0.2500)

O-O-O           90.00(0) (  0.2500  0.2500  0.7500) (  0.2500  0.7500  0.2500)

O-O-O           90.00(0) (  0.2500  0.2500  0.7500) ( -0.2500  0.2500  0.2500)

O-O-O           90.00(0) (  0.2500  0.2500  0.7500) (  0.7500  0.2500  0.2500)

O-O-O          180.00(0) (  0.2500 -0.2500  0.2500) (  0.2500  0.7500  0.2500)

O-O-O           90.00(0) (  0.2500 -0.2500  0.2500) ( -0.2500  0.2500  0.2500)

O-O-O           90.00(0) (  0.2500 -0.2500  0.2500) (  0.7500  0.2500  0.2500)

O-O-O           90.00(0) (  0.2500  0.7500  0.2500) ( -0.2500  0.2500  0.2500)

O-O-O           90.00(0) (  0.2500  0.7500  0.2500) (  0.7500  0.2500  0.2500)

O-O-O          180.00(0) ( -0.2500  0.2500  0.2500) (  0.7500  0.2500  0.2500)