1Ba3Cu3In2Sc2O12                                                             Version        2000-10-12T13:00:20  Page   1

|----------------------------------------------|

|         Program DISAGL Version MS-DOS        |

| Crystal structure distance and angle program |

|   Distributed on 15/ 7/1999; 0:25:16         |

|----------------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY603 EXPEDT  MS-DOS 2000-10-12T13:00:13                          D  C

Space group I4/mcm

The lattice is centric  I-centered tetragonal    Laue symmetry 4/mmm

Multiplicity of a general site is  32

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)    -Y      X      Z

( 3)    -X     -Y      Z  ( 4)     Y     -X      Z

( 5)    -X      Y  1/2+Z  ( 6)    -Y     -X  1/2+Z

( 7)     X     -Y  1/2+Z  ( 8)     Y      X  1/2+Z

GENLES was run on 2000-10-10T10:25:12     Total cycles run1064

The Current Least-Squares controls are

Maximum number of cycles is    6

I/SigI cut-off is  1.00

The atom type radii are

TYPE     BOND      ANGLE

BA       2.44000   2.24000

CU       1.48000   1.28000

IN       1.86000   1.66000

SC       1.84000   1.64000

O        1.09000    .89000

Lattice constants are   11.99690  11.99690   8.44728  .00000  .00000  .00000

Standard deviations     .00028    .00028    .00022  .00000  .00000  .00000

DMAX is    4.50000 DAGL is     .00000 and IAGL is     0

The atoms read in are

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page   2

BA1       .0000000(0)   .0000000(0)   .0000000(0) 4/M(001)  BA      1 1.000(0)

BA2       .27821(8)     .77821(8)     .0000000(0) MM2(110)  BA      2 1.000(0)

CU3       .5000000(0)   .0000000(0)   .2500000(0) -42M 001  CU      3 1.000(0)

CU4       .10589(17)    .60589(17)    .0000000(0) MM2(110)  CU      4 1.000(0)

IN5       .24165(11)    .0000000(0)   .2500000(0)   2(100)  IN      5  .421(3)

SC6       .24165(11)    .0000000(0)   .2500000(0)   2(100)  SC      6  .579(3)

O7        .1172(6)      .6172(6)      .2261(11)     M(+-0)  O       7 1.000(0)

O8        .1266(7)      .1266(7)      .2500000(0)   2(110)  O       8 1.000(0)

O9        .2361(11)     .5020(6)      .0000000(0)   M(001)  O       9 1.000(0)

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page   3

Vector         Length           Optr Cell        Neighbor atom coordinates

BA1_BA1         4.22364(11)        5 0 0-1      .00000    .00000   -.50000

BA1_BA1         4.22364(11)        5 0 0 0      .00000    .00000    .50000

BA1_BA2         4.26846(18)        1 0-1 0      .27821   -.22179    .00000

BA1_BA2         4.26846(18)        2 1 0 0      .22179    .27821    .00000

BA1_BA2         4.26846(18)        3 0 1 0     -.27821    .22179    .00000

BA1_BA2         4.26846(18)        4-1 0 0     -.22179   -.27821    .00000

BA1_IN5         3.5867(11)         1 0 0 0      .24165    .00000    .25000

BA1_IN5         3.5867(11)         2 0 0 0      .00000    .24165    .25000

BA1_IN5         3.5867(11)         3 0 0 0     -.24165    .00000    .25000

BA1_IN5         3.5867(11)         4 0 0 0      .00000   -.24165    .25000

BA1_IN5         3.5867(11)         5 0 0-1     -.24165    .00000   -.25000

BA1_IN5         3.5867(11)         6 0 0-1      .00000   -.24165   -.25000

BA1_IN5         3.5867(11)         7 0 0-1      .24165    .00000   -.25000

BA1_IN5         3.5867(11)         8 0 0-1      .00000    .24165   -.25000

BA1_SC6         3.5867(11)         1 0 0 0      .24165    .00000    .25000

BA1_SC6         3.5867(11)         2 0 0 0      .00000    .24165    .25000

BA1_SC6         3.5867(11)         3 0 0 0     -.24165    .00000    .25000

BA1_SC6         3.5867(11)         4 0 0 0      .00000   -.24165    .25000

BA1_SC6         3.5867(11)         5 0 0-1     -.24165    .00000   -.25000

BA1_SC6         3.5867(11)         6 0 0-1      .00000   -.24165   -.25000

BA1_SC6         3.5867(11)         7 0 0-1      .24165    .00000   -.25000

BA1_SC6         3.5867(11)         8 0 0-1      .00000    .24165   -.25000

BA1_O8          3.012(8)           1 0 0 0      .12656    .12656    .25000

BA1_O8          3.012(8)           2 0 0 0     -.12656    .12656    .25000

BA1_O8          3.012(8)           3 0 0 0     -.12656   -.12656    .25000

*BA1_O8          3.012(8)           4 0 0 0      .12656   -.12656    .25000

*BA1_O8          3.012(8)           5 0 0-1     -.12656    .12656   -.25000

*BA1_O8          3.012(8)           6 0 0-1     -.12656   -.12656   -.25000

*BA1_O8          3.012(8)           7 0 0-1      .12656   -.12656   -.25000

*BA1_O8          3.012(8)           8 0 0-1      .12656    .12656   -.25000

*BA1_O9          3.167(13)        105 0-1-1      .26394    .00197    .00000

*BA1_O9          3.167(13)        106 0 0-1     -.00197    .26394    .00000

*BA1_O9          3.167(13)        107-1 0-1     -.26394   -.00197    .00000

*BA1_O9          3.167(13)        108-1-1-1      .00197   -.26394    .00000

**** More than 24 Interatomic distances found ****

Angles will be calculated between the first 25

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_BA1_BA1         179.980(0)         5 0 0-1     5 0 0 0

BA1_BA1_BA2          90.000(0)         5 0 0-1     1 0-1 0

BA1_BA1_BA2          90.000(0)         5 0 0-1     2 1 0 0

BA1_BA1_BA2          90.000(0)         5 0 0-1     3 0 1 0

BA1_BA1_BA2          90.000(0)         5 0 0-1     4-1 0 0

BA1_BA1_IN5         126.072(12)        5 0 0-1     1 0 0 0

BA1_BA1_IN5         126.072(12)        5 0 0-1     2 0 0 0

BA1_BA1_IN5         126.072(12)        5 0 0-1     3 0 0 0

BA1_BA1_IN5         126.072(12)        5 0 0-1     4 0 0 0

BA1_BA1_IN5          53.928(12)        5 0 0-1     5 0 0-1

BA1_BA1_IN5          53.928(12)        5 0 0-1     6 0 0-1

BA1_BA1_IN5          53.928(12)        5 0 0-1     7 0 0-1

BA1_BA1_IN5          53.928(12)        5 0 0-1     8 0 0-1

BA1_BA1_SC6         126.072(12)        5 0 0-1     1 0 0 0

BA1_BA1_SC6         126.072(12)        5 0 0-1     2 0 0 0

BA1_BA1_SC6         126.072(12)        5 0 0-1     3 0 0 0

BA1_BA1_SC6         126.072(12)        5 0 0-1     4 0 0 0

BA1_BA1_SC6          53.928(12)        5 0 0-1     5 0 0-1

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page   4

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_BA1_SC6          53.928(12)        5 0 0-1     6 0 0-1

BA1_BA1_SC6          53.928(12)        5 0 0-1     7 0 0-1

BA1_BA1_SC6          53.928(12)        5 0 0-1     8 0 0-1

BA1_BA1_O8          134.52(15)         5 0 0-1     1 0 0 0

BA1_BA1_O8          134.52(15)         5 0 0-1     2 0 0 0

BA1_BA1_O9          134.5(4)           5 0 0-1     3 0 0 0

BA1_BA1_BA2          90.000(0)         5 0 0 0     1 0-1 0

BA1_BA1_BA2          90.000(0)         5 0 0 0     2 1 0 0

BA1_BA1_BA2          90.000(0)         5 0 0 0     3 0 1 0

BA1_BA1_BA2          90.000(0)         5 0 0 0     4-1 0 0

BA1_BA1_IN5          53.928(12)        5 0 0 0     1 0 0 0

BA1_BA1_IN5          53.928(12)        5 0 0 0     2 0 0 0

BA1_BA1_IN5          53.928(12)        5 0 0 0     3 0 0 0

BA1_BA1_IN5          53.928(12)        5 0 0 0     4 0 0 0

BA1_BA1_IN5         126.072(12)        5 0 0 0     5 0 0-1

BA1_BA1_IN5         126.072(12)        5 0 0 0     6 0 0-1

BA1_BA1_IN5         126.072(12)        5 0 0 0     7 0 0-1

BA1_BA1_IN5         126.072(12)        5 0 0 0     8 0 0-1

BA1_BA1_SC6          53.928(12)        5 0 0 0     1 0 0 0

BA1_BA1_SC6          53.928(12)        5 0 0 0     2 0 0 0

BA1_BA1_SC6          53.928(12)        5 0 0 0     3 0 0 0

BA1_BA1_SC6          53.928(12)        5 0 0 0     4 0 0 0

BA1_BA1_SC6         126.072(12)        5 0 0 0     5 0 0-1

BA1_BA1_SC6         126.072(12)        5 0 0 0     6 0 0-1

BA1_BA1_SC6         126.072(12)        5 0 0 0     7 0 0-1

BA1_BA1_SC6         126.072(12)        5 0 0 0     8 0 0-1

BA1_BA1_O8           45.48(15)         5 0 0 0     1 0 0 0

BA1_BA1_O8           45.48(15)         5 0 0 0     2 0 0 0

BA1_BA1_O9           45.48(14)         5 0 0 0     3 0 0 0

BA2_BA1_BA2          90.000(0)         1 0-1 0     2 1 0 0

BA2_BA1_BA2         179.972(0)         1 0-1 0     3 0 1 0

BA2_BA1_BA2          90.000(0)         1 0-1 0     4-1 0 0

BA2_BA1_IN5          50.801(13)        1 0-1 0     1 0 0 0

BA2_BA1_IN5         120.256(14)        1 0-1 0     2 0 0 0

BA2_BA1_IN5         129.199(13)        1 0-1 0     3 0 0 0

BA2_BA1_IN5          59.744(14)        1 0-1 0     4 0 0 0

BA2_BA1_IN5         129.199(13)        1 0-1 0     5 0 0-1

BA2_BA1_IN5          59.744(14)        1 0-1 0     6 0 0-1

BA2_BA1_IN5          50.801(13)        1 0-1 0     7 0 0-1

BA2_BA1_IN5         120.256(14)        1 0-1 0     8 0 0-1

BA2_BA1_SC6          50.801(13)        1 0-1 0     1 0 0 0

BA2_BA1_SC6         120.256(14)        1 0-1 0     2 0 0 0

BA2_BA1_SC6         129.199(13)        1 0-1 0     3 0 0 0

BA2_BA1_SC6          59.744(14)        1 0-1 0     4 0 0 0

BA2_BA1_SC6         129.199(13)        1 0-1 0     5 0 0-1

BA2_BA1_SC6          59.744(14)        1 0-1 0     6 0 0-1

BA2_BA1_SC6          50.801(13)        1 0-1 0     7 0 0-1

BA2_BA1_SC6         120.256(14)        1 0-1 0     8 0 0-1

BA2_BA1_O8           85.415(18)        1 0-1 0     1 0 0 0

BA2_BA1_O8          135.11(15)         1 0-1 0     2 0 0 0

BA2_BA1_O9           94.58(32)         1 0-1 0     3 0 0 0

BA2_BA1_BA2          90.000(0)         2 1 0 0     3 0 1 0

BA2_BA1_BA2         179.972(0)         2 1 0 0     4-1 0 0

BA2_BA1_IN5          59.744(14)        2 1 0 0     1 0 0 0

BA2_BA1_IN5          50.801(13)        2 1 0 0     2 0 0 0

BA2_BA1_IN5         120.256(14)        2 1 0 0     3 0 0 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page   5

Angle             Degrees         atom 1 loc  atom 3 loc

BA2_BA1_IN5         129.199(13)        2 1 0 0     4 0 0 0

BA2_BA1_IN5         120.256(14)        2 1 0 0     5 0 0-1

BA2_BA1_IN5         129.199(13)        2 1 0 0     6 0 0-1

BA2_BA1_IN5          59.744(14)        2 1 0 0     7 0 0-1

BA2_BA1_IN5          50.801(13)        2 1 0 0     8 0 0-1

BA2_BA1_SC6          59.744(14)        2 1 0 0     1 0 0 0

BA2_BA1_SC6          50.801(13)        2 1 0 0     2 0 0 0

BA2_BA1_SC6         120.256(14)        2 1 0 0     3 0 0 0

BA2_BA1_SC6         129.199(13)        2 1 0 0     4 0 0 0

BA2_BA1_SC6         120.256(14)        2 1 0 0     5 0 0-1

BA2_BA1_SC6         129.199(13)        2 1 0 0     6 0 0-1

BA2_BA1_SC6          59.744(14)        2 1 0 0     7 0 0-1

BA2_BA1_SC6          50.801(13)        2 1 0 0     8 0 0-1

BA2_BA1_O8           44.89(15)         2 1 0 0     1 0 0 0

BA2_BA1_O8           85.415(18)        2 1 0 0     2 0 0 0

BA2_BA1_O9          135.11(22)         2 1 0 0     3 0 0 0

BA2_BA1_BA2          90.000(0)         3 0 1 0     4-1 0 0

BA2_BA1_IN5         129.199(13)        3 0 1 0     1 0 0 0

BA2_BA1_IN5          59.744(14)        3 0 1 0     2 0 0 0

BA2_BA1_IN5          50.801(13)        3 0 1 0     3 0 0 0

BA2_BA1_IN5         120.256(14)        3 0 1 0     4 0 0 0

BA2_BA1_IN5          50.801(13)        3 0 1 0     5 0 0-1

BA2_BA1_IN5         120.256(14)        3 0 1 0     6 0 0-1

BA2_BA1_IN5         129.199(13)        3 0 1 0     7 0 0-1

BA2_BA1_IN5          59.744(14)        3 0 1 0     8 0 0-1

BA2_BA1_SC6         129.199(13)        3 0 1 0     1 0 0 0

BA2_BA1_SC6          59.744(14)        3 0 1 0     2 0 0 0

BA2_BA1_SC6          50.801(13)        3 0 1 0     3 0 0 0

BA2_BA1_SC6         120.256(14)        3 0 1 0     4 0 0 0

BA2_BA1_SC6          50.801(13)        3 0 1 0     5 0 0-1

BA2_BA1_SC6         120.256(14)        3 0 1 0     6 0 0-1

BA2_BA1_SC6         129.199(13)        3 0 1 0     7 0 0-1

BA2_BA1_SC6          59.744(14)        3 0 1 0     8 0 0-1

BA2_BA1_O8           94.585(18)        3 0 1 0     1 0 0 0

BA2_BA1_O8           44.89(15)         3 0 1 0     2 0 0 0

BA2_BA1_O9           85.42(11)         3 0 1 0     3 0 0 0

BA2_BA1_IN5         120.256(14)        4-1 0 0     1 0 0 0

BA2_BA1_IN5         129.199(13)        4-1 0 0     2 0 0 0

BA2_BA1_IN5          59.744(14)        4-1 0 0     3 0 0 0

BA2_BA1_IN5          50.801(13)        4-1 0 0     4 0 0 0

BA2_BA1_IN5          59.744(14)        4-1 0 0     5 0 0-1

BA2_BA1_IN5          50.801(13)        4-1 0 0     6 0 0-1

BA2_BA1_IN5         120.256(14)        4-1 0 0     7 0 0-1

BA2_BA1_IN5         129.199(13)        4-1 0 0     8 0 0-1

BA2_BA1_SC6         120.256(14)        4-1 0 0     1 0 0 0

BA2_BA1_SC6         129.199(13)        4-1 0 0     2 0 0 0

BA2_BA1_SC6          59.744(14)        4-1 0 0     3 0 0 0

BA2_BA1_SC6          50.801(13)        4-1 0 0     4 0 0 0

BA2_BA1_SC6          59.744(14)        4-1 0 0     5 0 0-1

BA2_BA1_SC6          50.801(13)        4-1 0 0     6 0 0-1

BA2_BA1_SC6         120.256(14)        4-1 0 0     7 0 0-1

BA2_BA1_SC6         129.199(13)        4-1 0 0     8 0 0-1

BA2_BA1_O8          135.11(15)         4-1 0 0     1 0 0 0

BA2_BA1_O8           94.585(18)        4-1 0 0     2 0 0 0

BA2_BA1_O9           44.89(16)         4-1 0 0     3 0 0 0

IN5_BA1_IN5          69.715(13)        1 0 0 0     2 0 0 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page   6

Angle             Degrees         atom 1 loc  atom 3 loc

IN5_BA1_IN5         107.856(25)        1 0 0 0     3 0 0 0

IN5_BA1_IN5          69.715(13)        1 0 0 0     4 0 0 0

IN5_BA1_IN5         180.000(0)         1 0 0 0     5 0 0-1

IN5_BA1_IN5         110.285(13)        1 0 0 0     6 0 0-1

IN5_BA1_IN5          72.144(25)        1 0 0 0     7 0 0-1

IN5_BA1_IN5         110.285(13)        1 0 0 0     8 0 0-1

IN5_BA1_SC6            .000(0)         1 0 0 0     1 0 0 0

IN5_BA1_SC6          69.715(13)        1 0 0 0     2 0 0 0

IN5_BA1_SC6         107.856(25)        1 0 0 0     3 0 0 0

IN5_BA1_SC6          69.715(13)        1 0 0 0     4 0 0 0

IN5_BA1_SC6         180.000(0)         1 0 0 0     5 0 0-1

IN5_BA1_SC6         110.285(13)        1 0 0 0     6 0 0-1

IN5_BA1_SC6          72.144(25)        1 0 0 0     7 0 0-1

IN5_BA1_SC6         110.285(13)        1 0 0 0     8 0 0-1

IN5_BA1_O8           34.880(8)         1 0 0 0     1 0 0 0

IN5_BA1_O8           89.69(12)         1 0 0 0     2 0 0 0

IN5_BA1_O9           89.69(20)         1 0 0 0     3 0 0 0

IN5_BA1_IN5          69.715(13)        2 0 0 0     3 0 0 0

IN5_BA1_IN5         107.856(25)        2 0 0 0     4 0 0 0

IN5_BA1_IN5         110.285(13)        2 0 0 0     5 0 0-1

IN5_BA1_IN5         180.000(0)         2 0 0 0     6 0 0-1

IN5_BA1_IN5         110.285(13)        2 0 0 0     7 0 0-1

IN5_BA1_IN5          72.144(25)        2 0 0 0     8 0 0-1

IN5_BA1_SC6          69.715(13)        2 0 0 0     1 0 0 0

IN5_BA1_SC6            .000(0)         2 0 0 0     2 0 0 0

IN5_BA1_SC6          69.715(13)        2 0 0 0     3 0 0 0

IN5_BA1_SC6         107.856(25)        2 0 0 0     4 0 0 0

IN5_BA1_SC6         110.285(13)        2 0 0 0     5 0 0-1

IN5_BA1_SC6         180.000(0)         2 0 0 0     6 0 0-1

IN5_BA1_SC6         110.285(13)        2 0 0 0     7 0 0-1

IN5_BA1_SC6          72.144(25)        2 0 0 0     8 0 0-1

IN5_BA1_O8           34.880(8)         2 0 0 0     1 0 0 0

IN5_BA1_O8           34.880(8)         2 0 0 0     2 0 0 0

IN5_BA1_O9           89.69(11)         2 0 0 0     3 0 0 0

IN5_BA1_IN5          69.715(13)        3 0 0 0     4 0 0 0

IN5_BA1_IN5          72.144(25)        3 0 0 0     5 0 0-1

IN5_BA1_IN5         110.285(13)        3 0 0 0     6 0 0-1

IN5_BA1_IN5         179.980(0)         3 0 0 0     7 0 0-1

IN5_BA1_IN5         110.285(13)        3 0 0 0     8 0 0-1

IN5_BA1_SC6         107.856(25)        3 0 0 0     1 0 0 0

IN5_BA1_SC6          69.715(13)        3 0 0 0     2 0 0 0

IN5_BA1_SC6            .000(0)         3 0 0 0     3 0 0 0

IN5_BA1_SC6          69.715(13)        3 0 0 0     4 0 0 0

IN5_BA1_SC6          72.144(25)        3 0 0 0     5 0 0-1

IN5_BA1_SC6         110.285(13)        3 0 0 0     6 0 0-1

IN5_BA1_SC6         179.980(0)         3 0 0 0     7 0 0-1

IN5_BA1_SC6         110.285(13)        3 0 0 0     8 0 0-1

IN5_BA1_O8           89.69(12)         3 0 0 0     1 0 0 0

IN5_BA1_O8           34.880(8)         3 0 0 0     2 0 0 0

IN5_BA1_O9           34.88(21)         3 0 0 0     3 0 0 0

IN5_BA1_IN5         110.285(13)        4 0 0 0     5 0 0-1

IN5_BA1_IN5          72.144(25)        4 0 0 0     6 0 0-1

IN5_BA1_IN5         110.285(13)        4 0 0 0     7 0 0-1

IN5_BA1_IN5         179.980(0)         4 0 0 0     8 0 0-1

IN5_BA1_SC6          69.715(13)        4 0 0 0     1 0 0 0

IN5_BA1_SC6         107.856(25)        4 0 0 0     2 0 0 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page   7

Angle             Degrees         atom 1 loc  atom 3 loc

IN5_BA1_SC6          69.715(13)        4 0 0 0     3 0 0 0

IN5_BA1_SC6            .000(0)         4 0 0 0     4 0 0 0

IN5_BA1_SC6         110.285(13)        4 0 0 0     5 0 0-1

IN5_BA1_SC6          72.144(25)        4 0 0 0     6 0 0-1

IN5_BA1_SC6         110.285(13)        4 0 0 0     7 0 0-1

IN5_BA1_SC6         179.980(0)         4 0 0 0     8 0 0-1

IN5_BA1_O8           89.69(12)         4 0 0 0     1 0 0 0

IN5_BA1_O8           89.69(12)         4 0 0 0     2 0 0 0

IN5_BA1_O9           34.88(21)         4 0 0 0     3 0 0 0

IN5_BA1_IN5          69.715(13)        5 0 0-1     6 0 0-1

IN5_BA1_IN5         107.856(25)        5 0 0-1     7 0 0-1

IN5_BA1_IN5          69.715(13)        5 0 0-1     8 0 0-1

IN5_BA1_SC6         180.000(0)         5 0 0-1     1 0 0 0

IN5_BA1_SC6         110.285(13)        5 0 0-1     2 0 0 0

IN5_BA1_SC6          72.144(25)        5 0 0-1     3 0 0 0

IN5_BA1_SC6         110.285(13)        5 0 0-1     4 0 0 0

IN5_BA1_SC6            .000(0)         5 0 0-1     5 0 0-1

IN5_BA1_SC6          69.715(13)        5 0 0-1     6 0 0-1

IN5_BA1_SC6         107.856(25)        5 0 0-1     7 0 0-1

IN5_BA1_SC6          69.715(13)        5 0 0-1     8 0 0-1

IN5_BA1_O8          145.120(8)         5 0 0-1     1 0 0 0

IN5_BA1_O8           90.31(12)         5 0 0-1     2 0 0 0

IN5_BA1_O9           90.31(12)         5 0 0-1     3 0 0 0

IN5_BA1_IN5          69.715(13)        6 0 0-1     7 0 0-1

IN5_BA1_IN5         107.856(25)        6 0 0-1     8 0 0-1

IN5_BA1_SC6         110.285(13)        6 0 0-1     1 0 0 0

IN5_BA1_SC6         180.000(0)         6 0 0-1     2 0 0 0

IN5_BA1_SC6         110.285(13)        6 0 0-1     3 0 0 0

IN5_BA1_SC6          72.144(25)        6 0 0-1     4 0 0 0

IN5_BA1_SC6          69.715(13)        6 0 0-1     5 0 0-1

IN5_BA1_SC6            .000(0)         6 0 0-1     6 0 0-1

IN5_BA1_SC6          69.715(13)        6 0 0-1     7 0 0-1

IN5_BA1_SC6         107.856(25)        6 0 0-1     8 0 0-1

IN5_BA1_O8          145.120(8)         6 0 0-1     1 0 0 0

IN5_BA1_O8          145.120(8)         6 0 0-1     2 0 0 0

IN5_BA1_O9           90.31(32)         6 0 0-1     3 0 0 0

IN5_BA1_IN5          69.715(13)        7 0 0-1     8 0 0-1

IN5_BA1_SC6          72.144(25)        7 0 0-1     1 0 0 0

IN5_BA1_SC6         110.285(13)        7 0 0-1     2 0 0 0

IN5_BA1_SC6         179.980(0)         7 0 0-1     3 0 0 0

IN5_BA1_SC6         110.285(13)        7 0 0-1     4 0 0 0

IN5_BA1_SC6         107.856(25)        7 0 0-1     5 0 0-1

IN5_BA1_SC6          69.715(13)        7 0 0-1     6 0 0-1

IN5_BA1_SC6            .000(0)         7 0 0-1     7 0 0-1

IN5_BA1_SC6          69.715(13)        7 0 0-1     8 0 0-1

IN5_BA1_O8           90.31(12)         7 0 0-1     1 0 0 0

IN5_BA1_O8          145.120(8)         7 0 0-1     2 0 0 0

IN5_BA1_O9          145.1(6)           7 0 0-1     3 0 0 0

IN5_BA1_SC6         110.285(13)        8 0 0-1     1 0 0 0

IN5_BA1_SC6          72.144(25)        8 0 0-1     2 0 0 0

IN5_BA1_SC6         110.285(13)        8 0 0-1     3 0 0 0

IN5_BA1_SC6         179.980(0)         8 0 0-1     4 0 0 0

IN5_BA1_SC6          69.715(13)        8 0 0-1     5 0 0-1

IN5_BA1_SC6         107.856(25)        8 0 0-1     6 0 0-1

IN5_BA1_SC6          69.715(13)        8 0 0-1     7 0 0-1

IN5_BA1_SC6            .000(0)         8 0 0-1     8 0 0-1

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page   8

Angle             Degrees         atom 1 loc  atom 3 loc

IN5_BA1_O8           90.31(12)         8 0 0-1     1 0 0 0

IN5_BA1_O8           90.31(12)         8 0 0-1     2 0 0 0

IN5_BA1_O9          145.12(22)         8 0 0-1     3 0 0 0

SC6_BA1_SC6          69.715(13)        1 0 0 0     2 0 0 0

SC6_BA1_SC6         107.856(25)        1 0 0 0     3 0 0 0

SC6_BA1_SC6          69.715(13)        1 0 0 0     4 0 0 0

SC6_BA1_SC6         180.000(0)         1 0 0 0     5 0 0-1

SC6_BA1_SC6         110.285(13)        1 0 0 0     6 0 0-1

SC6_BA1_SC6          72.144(25)        1 0 0 0     7 0 0-1

SC6_BA1_SC6         110.285(13)        1 0 0 0     8 0 0-1

SC6_BA1_O8           34.880(8)         1 0 0 0     1 0 0 0

SC6_BA1_O8           89.69(12)         1 0 0 0     2 0 0 0

SC6_BA1_O9           89.69(20)         1 0 0 0     3 0 0 0

SC6_BA1_SC6          69.715(13)        2 0 0 0     3 0 0 0

SC6_BA1_SC6         107.856(25)        2 0 0 0     4 0 0 0

SC6_BA1_SC6         110.285(13)        2 0 0 0     5 0 0-1

SC6_BA1_SC6         180.000(0)         2 0 0 0     6 0 0-1

SC6_BA1_SC6         110.285(13)        2 0 0 0     7 0 0-1

SC6_BA1_SC6          72.144(25)        2 0 0 0     8 0 0-1

SC6_BA1_O8           34.880(8)         2 0 0 0     1 0 0 0

SC6_BA1_O8           34.880(8)         2 0 0 0     2 0 0 0

SC6_BA1_O9           89.69(11)         2 0 0 0     3 0 0 0

SC6_BA1_SC6          69.715(13)        3 0 0 0     4 0 0 0

SC6_BA1_SC6          72.144(25)        3 0 0 0     5 0 0-1

SC6_BA1_SC6         110.285(13)        3 0 0 0     6 0 0-1

SC6_BA1_SC6         179.980(0)         3 0 0 0     7 0 0-1

SC6_BA1_SC6         110.285(13)        3 0 0 0     8 0 0-1

SC6_BA1_O8           89.69(12)         3 0 0 0     1 0 0 0

SC6_BA1_O8           34.880(8)         3 0 0 0     2 0 0 0

SC6_BA1_O9           34.88(21)         3 0 0 0     3 0 0 0

SC6_BA1_SC6         110.285(13)        4 0 0 0     5 0 0-1

SC6_BA1_SC6          72.144(25)        4 0 0 0     6 0 0-1

SC6_BA1_SC6         110.285(13)        4 0 0 0     7 0 0-1

SC6_BA1_SC6         179.980(0)         4 0 0 0     8 0 0-1

SC6_BA1_O8           89.69(12)         4 0 0 0     1 0 0 0

SC6_BA1_O8           89.69(12)         4 0 0 0     2 0 0 0

SC6_BA1_O9           34.88(21)         4 0 0 0     3 0 0 0

SC6_BA1_SC6          69.715(13)        5 0 0-1     6 0 0-1

SC6_BA1_SC6         107.856(25)        5 0 0-1     7 0 0-1

SC6_BA1_SC6          69.715(13)        5 0 0-1     8 0 0-1

SC6_BA1_O8          145.120(8)         5 0 0-1     1 0 0 0

SC6_BA1_O8           90.31(12)         5 0 0-1     2 0 0 0

SC6_BA1_O9           90.31(12)         5 0 0-1     3 0 0 0

SC6_BA1_SC6          69.715(13)        6 0 0-1     7 0 0-1

SC6_BA1_SC6         107.856(25)        6 0 0-1     8 0 0-1

SC6_BA1_O8          145.120(8)         6 0 0-1     1 0 0 0

SC6_BA1_O8          145.120(8)         6 0 0-1     2 0 0 0

SC6_BA1_O9           90.31(32)         6 0 0-1     3 0 0 0

SC6_BA1_SC6          69.715(13)        7 0 0-1     8 0 0-1

SC6_BA1_O8           90.31(12)         7 0 0-1     1 0 0 0

SC6_BA1_O8          145.120(8)         7 0 0-1     2 0 0 0

SC6_BA1_O9          145.1(6)           7 0 0-1     3 0 0 0

SC6_BA1_O8           90.31(12)         8 0 0-1     1 0 0 0

SC6_BA1_O8           90.31(12)         8 0 0-1     2 0 0 0

SC6_BA1_O9          145.12(22)         8 0 0-1     3 0 0 0

O8_BA1_O8           60.55(17)         1 0 0 0     2 0 0 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page   9

Angle             Degrees         atom 1 loc  atom 3 loc

O8_BA1_O9           90.96(21)         1 0 0 0     3 0 0 0

O8_BA1_O9           60.55(12)         2 0 0 0     3 0 0 0

Vector         Length           Optr Cell        Neighbor atom coordinates

BA2_BA1         4.26846(18)        1 0 1 0      .00000   1.00000    .00000

BA2_BA1         4.26846(18)      105 0 0-1      .50000    .50000    .00000

BA2_BA2         4.3307(6)          6 1 1-1      .22179    .72179   -.50000

BA2_BA2         4.3307(6)          6 1 1 0      .22179    .72179    .50000

BA2_CU3         4.3151(12)         1 0 1 0      .50000   1.00000    .25000

BA2_CU3         4.3151(12)         5 1 1-1      .50000   1.00000   -.25000

BA2_CU4         2.9235(31)         1 0 0 0      .10589    .60589    .00000

BA2_CU4         4.1699(17)         2 1 1 0      .39411   1.10590    .00000

BA2_CU4         4.1699(17)         4 0 1 0      .60589    .89411    .00000

BA2_IN5         3.4252(6)          1 0 1 0      .24165   1.00000    .25000

BA2_IN5         3.9568(9)          4 0 1 0      .00000    .75835    .25000

BA2_IN5         3.9568(9)          6 0 1-1      .00000    .75835   -.25000

BA2_IN5         3.4252(6)          7 0 1-1      .24165   1.00000   -.25000

BA2_IN5         3.4252(6)        102 0 0-1      .50000    .74165   -.25000

BA2_IN5         3.9568(9)        103 0 0-1      .25835    .50000   -.25000

BA2_IN5         3.9568(9)        105 0 0-1      .25835    .50000    .25000

BA2_IN5         3.4252(6)        108 0 0-1      .50000    .74165    .25000

BA2_SC6         3.4252(6)          1 0 1 0      .24165   1.00000    .25000

BA2_SC6         3.9568(9)          4 0 1 0      .00000    .75835    .25000

BA2_SC6         3.9568(9)          6 0 1-1      .00000    .75835   -.25000

BA2_SC6         3.4252(6)          7 0 1-1      .24165   1.00000   -.25000

BA2_SC6         3.4252(6)        102 0 0-1      .50000    .74165   -.25000

BA2_SC6         3.9568(9)        103 0 0-1      .25835    .50000   -.25000

BA2_SC6         3.9568(9)        105 0 0-1      .25835    .50000    .25000

BA2_SC6         3.4252(6)        108 0 0-1      .50000    .74165    .25000

BA2_O7          3.333(11)          1 0 0 0      .11717    .61717    .22607

BA2_O7          2.916(8)           6 1 1-1      .38283    .88283   -.27393

BA2_O7          3.333(11)         -3 0 0 0      .11717    .61717   -.22607

BA2_O7          2.916(8)          -8 1 1 1      .38283    .88283    .27393

BA2_O8          3.012(8)           4 0 1 0      .12656    .87344    .25000

BA2_O8          3.012(8)           7 0 1-1      .12656    .87344   -.25000

BA2_O8          3.012(8)         102 0 0-1      .37344    .62656   -.25000

BA2_O8          3.012(8)         105 0 0-1      .37344    .62656    .25000

BA2_O9          3.352(8)           1 0 0 0      .23606    .50197    .00000

BA2_O9          2.690(7)           4 0 1 0      .50197    .76394    .00000

BA2_O9          2.690(7)         105 0 0-1      .26394   1.00197    .00000

BA2_O9          3.352(8)         108-1 0-1      .00197    .73606    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_BA2_BA1         167.13(4)          1 0 1 0   105 0 0-1

BA1_BA2_BA2          88.580(8)         1 0 1 0     6 1 1-1

BA1_BA2_CU3          88.580(13)        1 0 1 0     6 1 1 0

BA1_BA2_CU4          83.56(4)          1 0 1 0     1 0 0 0

BA1_BA2_IN5          54.241(5)         1 0 1 0     1 0 1 0

BA1_BA2_IN5          54.241(19)        1 0 1 0     7 0 1-1

BA1_BA2_IN5         133.41(6)          1 0 1 0   102 0 0-1

BA1_BA2_IN5         133.413(23)        1 0 1 0   108 0 0-1

BA1_BA2_SC6          54.241(5)         1 0 1 0     1 0 1 0

BA1_BA2_SC6          54.241(19)        1 0 1 0     7 0 1-1

BA1_BA2_SC6         133.41(6)          1 0 1 0   102 0 0-1

BA1_BA2_O7          133.4(4)           1 0 1 0   108 0 0-1

BA1_BA2_O7           93.91(23)         1 0 1 0     6 1 1-1

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  10

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_BA2_O7           93.913(21)        1 0 1 0    -8 1 1 1

BA1_BA2_O8           44.88(15)         1 0 1 0     4 0 1 0

BA1_BA2_O8           44.88(15)         1 0 1 0     7 0 1-1

BA1_BA2_O8          132.30(15)         1 0 1 0   102 0 0-1

BA1_BA2_O9          132.3(4)           1 0 1 0   105 0 0-1

BA1_BA2_O9          145.08(29)         1 0 1 0     4 0 1 0

BA1_BA2_O9           47.79(15)         1 0 1 0   105 0 0-1

BA1_BA2_BA2          88.580(8)       105 0 0-1     6 1 1-1

BA1_BA2_CU3          88.580(13)      105 0 0-1     6 1 1 0

BA1_BA2_CU4          83.56(7)        105 0 0-1     1 0 0 0

BA1_BA2_IN5         133.41(6)        105 0 0-1     1 0 1 0

BA1_BA2_IN5         133.413(23)      105 0 0-1     7 0 1-1

BA1_BA2_IN5          54.241(5)       105 0 0-1   102 0 0-1

BA1_BA2_IN5          54.241(19)      105 0 0-1   108 0 0-1

BA1_BA2_SC6         133.41(6)        105 0 0-1     1 0 1 0

BA1_BA2_SC6         133.413(23)      105 0 0-1     7 0 1-1

BA1_BA2_SC6          54.241(5)       105 0 0-1   102 0 0-1

BA1_BA2_O7           54.24(14)       105 0 0-1   108 0 0-1

BA1_BA2_O7           93.91(23)       105 0 0-1     6 1 1-1

BA1_BA2_O7           93.912(21)      105 0 0-1    -8 1 1 1

BA1_BA2_O8          132.30(15)       105 0 0-1     4 0 1 0

BA1_BA2_O8          132.30(15)       105 0 0-1     7 0 1-1

BA1_BA2_O8           44.88(15)       105 0 0-1   102 0 0-1

BA1_BA2_O9           44.88(15)       105 0 0-1   105 0 0-1

BA1_BA2_O9           47.79(28)       105 0 0-1     4 0 1 0

BA1_BA2_O9          145.1(8)         105 0 0-1   105 0 0-1

BA2_BA2_CU3         154.464(34)        6 1 1-1     6 1 1 0

BA2_BA2_CU4          77.232(16)        6 1 1-1     1 0 0 0

BA2_BA2_IN5         134.64(4)          6 1 1-1     1 0 1 0

BA2_BA2_IN5          60.006(12)        6 1 1-1     7 0 1-1

BA2_BA2_IN5          60.006(20)        6 1 1-1   102 0 0-1

BA2_BA2_IN5         134.643(19)        6 1 1-1   108 0 0-1

BA2_BA2_SC6         134.64(4)          6 1 1-1     1 0 1 0

BA2_BA2_SC6          60.006(12)        6 1 1-1     7 0 1-1

BA2_BA2_SC6          60.006(20)        6 1 1-1   102 0 0-1

BA2_BA2_O7          134.6(4)           6 1 1-1   108 0 0-1

BA2_BA2_O7           50.26(23)         6 1 1-1     6 1 1-1

BA2_BA2_O7          155.27(22)         6 1 1-1    -8 1 1 1

BA2_BA2_O8          130.44(12)         6 1 1-1     4 0 1 0

BA2_BA2_O8           44.04(15)         6 1 1-1     7 0 1-1

BA2_BA2_O8           44.04(15)         6 1 1-1   102 0 0-1

BA2_BA2_O9          130.44(28)         6 1 1-1   105 0 0-1

BA2_BA2_O9           98.40(5)          6 1 1-1     4 0 1 0

BA2_BA2_O9           98.40(28)         6 1 1-1   105 0 0-1

CU3_BA2_CU4          77.232(32)        6 1 1 0     1 0 0 0

CU3_BA2_IN5          60.006(22)        6 1 1 0     1 0 1 0

CU3_BA2_IN5         134.64(6)          6 1 1 0     7 0 1-1

CU3_BA2_IN5         134.643(30)        6 1 1 0   102 0 0-1

CU3_BA2_IN5          60.006(17)        6 1 1 0   108 0 0-1

CU3_BA2_SC6          60.006(22)        6 1 1 0     1 0 1 0

CU3_BA2_SC6         134.64(6)          6 1 1 0     7 0 1-1

CU3_BA2_SC6         134.643(30)        6 1 1 0   102 0 0-1

CU3_BA2_O7           60.01(22)         6 1 1 0   108 0 0-1

CU3_BA2_O7          155.3(9)           6 1 1 0     6 1 1-1

CU3_BA2_O7           50.26(22)         6 1 1 0    -8 1 1 1

CU3_BA2_O8           44.04(15)         6 1 1 0     4 0 1 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  11

Angle             Degrees         atom 1 loc  atom 3 loc

CU3_BA2_O8          130.44(13)         6 1 1 0     7 0 1-1

CU3_BA2_O8          130.44(13)         6 1 1 0   102 0 0-1

CU3_BA2_O9           44.04(17)         6 1 1 0   105 0 0-1

CU3_BA2_O9           98.40(6)          6 1 1 0     4 0 1 0

CU3_BA2_O9           98.40(28)         6 1 1 0   105 0 0-1

CU4_BA2_IN5         117.31(4)          1 0 0 0     1 0 1 0

CU4_BA2_IN5         117.31(6)          1 0 0 0     7 0 1-1

CU4_BA2_IN5         117.31(8)          1 0 0 0   102 0 0-1

CU4_BA2_IN5         117.31(9)          1 0 0 0   108 0 0-1

CU4_BA2_SC6         117.31(4)          1 0 0 0     1 0 1 0

CU4_BA2_SC6         117.31(6)          1 0 0 0     7 0 1-1

CU4_BA2_SC6         117.31(8)          1 0 0 0   102 0 0-1

CU4_BA2_O7          117.3(6)           1 0 0 0   108 0 0-1

CU4_BA2_O7          127.5(7)           1 0 0 0     6 1 1-1

CU4_BA2_O7          127.49(24)         1 0 0 0    -8 1 1 1

CU4_BA2_O8           80.859(34)        1 0 0 0     4 0 1 0

CU4_BA2_O8           80.859(34)        1 0 0 0     7 0 1-1

CU4_BA2_O8           80.86(6)          1 0 0 0   102 0 0-1

CU4_BA2_O9           80.86(33)         1 0 0 0   105 0 0-1

CU4_BA2_O9          131.35(31)         1 0 0 0     4 0 1 0

CU4_BA2_O9          131.4(8)           1 0 0 0   105 0 0-1

IN5_BA2_IN5          76.129(4)         1 0 1 0     7 0 1-1

IN5_BA2_IN5         125.39(8)          1 0 1 0   102 0 0-1

IN5_BA2_IN5          79.56(4)          1 0 1 0   108 0 0-1

IN5_BA2_SC6            .000(0)         1 0 1 0     1 0 1 0

IN5_BA2_SC6          76.129(4)         1 0 1 0     7 0 1-1

IN5_BA2_SC6         125.39(8)          1 0 1 0   102 0 0-1

IN5_BA2_O7           79.56(16)         1 0 1 0   108 0 0-1

IN5_BA2_O7          102.12(20)         1 0 1 0     6 1 1-1

IN5_BA2_O7           39.788(18)        1 0 1 0    -8 1 1 1

IN5_BA2_O8           36.470(34)        1 0 1 0     4 0 1 0

IN5_BA2_O8           93.46(14)         1 0 1 0     7 0 1-1

IN5_BA2_O8          161.79(16)         1 0 1 0   102 0 0-1

IN5_BA2_O9           94.90(17)         1 0 1 0   105 0 0-1

IN5_BA2_O9          100.21(23)         1 0 1 0     4 0 1 0

IN5_BA2_O9           38.426(25)        1 0 1 0   105 0 0-1

IN5_BA2_IN5          79.56(4)          7 0 1-1   102 0 0-1

IN5_BA2_IN5         125.39(6)          7 0 1-1   108 0 0-1

IN5_BA2_SC6          76.129(4)         7 0 1-1     1 0 1 0

IN5_BA2_SC6            .000(0)         7 0 1-1     7 0 1-1

IN5_BA2_SC6          79.56(4)          7 0 1-1   102 0 0-1

IN5_BA2_O7          125.39(27)         7 0 1-1   108 0 0-1

IN5_BA2_O7           39.79(5)          7 0 1-1     6 1 1-1

IN5_BA2_O7          102.12(17)         7 0 1-1    -8 1 1 1

IN5_BA2_O8           93.46(15)         7 0 1-1     4 0 1 0

IN5_BA2_O8           36.47(4)          7 0 1-1     7 0 1-1

IN5_BA2_O8           94.90(12)         7 0 1-1   102 0 0-1

IN5_BA2_O9          161.8(6)           7 0 1-1   105 0 0-1

IN5_BA2_O9          100.21(23)         7 0 1-1     4 0 1 0

IN5_BA2_O9           38.426(20)        7 0 1-1   105 0 0-1

IN5_BA2_IN5          76.129(4)       102 0 0-1   108 0 0-1

IN5_BA2_SC6         125.39(8)        102 0 0-1     1 0 1 0

IN5_BA2_SC6          79.56(4)        102 0 0-1     7 0 1-1

IN5_BA2_SC6            .000(0)       102 0 0-1   102 0 0-1

IN5_BA2_O7           76.13(14)       102 0 0-1   108 0 0-1

IN5_BA2_O7           39.79(5)        102 0 0-1     6 1 1-1

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  12

Angle             Degrees         atom 1 loc  atom 3 loc

IN5_BA2_O7          102.12(17)       102 0 0-1    -8 1 1 1

IN5_BA2_O8          161.79(16)       102 0 0-1     4 0 1 0

IN5_BA2_O8           94.90(13)       102 0 0-1     7 0 1-1

IN5_BA2_O8           36.470(34)      102 0 0-1   102 0 0-1

IN5_BA2_O9           93.46(12)       102 0 0-1   105 0 0-1

IN5_BA2_O9           38.43(4)        102 0 0-1     4 0 1 0

IN5_BA2_O9          100.21(31)       102 0 0-1   105 0 0-1

IN5_BA2_SC6          79.56(4)        108 0 0-1     1 0 1 0

IN5_BA2_SC6         125.39(6)        108 0 0-1     7 0 1-1

IN5_BA2_SC6          76.129(4)       108 0 0-1   102 0 0-1

IN5_BA2_O7             .000(0)       108 0 0-1   108 0 0-1

IN5_BA2_O7          102.12(20)       108 0 0-1     6 1 1-1

IN5_BA2_O7           39.788(20)      108 0 0-1    -8 1 1 1

IN5_BA2_O8           94.90(12)       108 0 0-1     4 0 1 0

IN5_BA2_O8          161.79(5)        108 0 0-1     7 0 1-1

IN5_BA2_O8           93.46(15)       108 0 0-1   102 0 0-1

IN5_BA2_O9           36.47(20)       108 0 0-1   105 0 0-1

IN5_BA2_O9           38.426(35)      108 0 0-1     4 0 1 0

IN5_BA2_O9          100.21(31)       108 0 0-1   105 0 0-1

SC6_BA2_SC6          76.129(4)         1 0 1 0     7 0 1-1

SC6_BA2_SC6         125.39(8)          1 0 1 0   102 0 0-1

SC6_BA2_O7           79.56(16)         1 0 1 0   108 0 0-1

SC6_BA2_O7          102.12(20)         1 0 1 0     6 1 1-1

SC6_BA2_O7           39.788(18)        1 0 1 0    -8 1 1 1

SC6_BA2_O8           36.470(34)        1 0 1 0     4 0 1 0

SC6_BA2_O8           93.46(14)         1 0 1 0     7 0 1-1

SC6_BA2_O8          161.79(16)         1 0 1 0   102 0 0-1

SC6_BA2_O9           94.90(17)         1 0 1 0   105 0 0-1

SC6_BA2_O9          100.21(23)         1 0 1 0     4 0 1 0

SC6_BA2_O9           38.426(25)        1 0 1 0   105 0 0-1

SC6_BA2_SC6          79.56(4)          7 0 1-1   102 0 0-1

SC6_BA2_O7          125.39(27)         7 0 1-1   108 0 0-1

SC6_BA2_O7           39.79(5)          7 0 1-1     6 1 1-1

SC6_BA2_O7          102.12(17)         7 0 1-1    -8 1 1 1

SC6_BA2_O8           93.46(15)         7 0 1-1     4 0 1 0

SC6_BA2_O8           36.47(4)          7 0 1-1     7 0 1-1

SC6_BA2_O8           94.90(12)         7 0 1-1   102 0 0-1

SC6_BA2_O9          161.8(6)           7 0 1-1   105 0 0-1

SC6_BA2_O9          100.21(23)         7 0 1-1     4 0 1 0

SC6_BA2_O9           38.426(20)        7 0 1-1   105 0 0-1

SC6_BA2_O7           76.13(14)       102 0 0-1   108 0 0-1

SC6_BA2_O7           39.79(5)        102 0 0-1     6 1 1-1

SC6_BA2_O7          102.12(17)       102 0 0-1    -8 1 1 1

SC6_BA2_O8          161.79(16)       102 0 0-1     4 0 1 0

SC6_BA2_O8           94.90(13)       102 0 0-1     7 0 1-1

SC6_BA2_O8           36.470(34)      102 0 0-1   102 0 0-1

SC6_BA2_O9           93.46(12)       102 0 0-1   105 0 0-1

SC6_BA2_O9           38.43(4)        102 0 0-1     4 0 1 0

SC6_BA2_O9          100.21(31)       102 0 0-1   105 0 0-1

O7_BA2_O7          102.1(4)         108 0 0-1     6 1 1-1

O7_BA2_O7           39.79(11)       108 0 0-1    -8 1 1 1

O7_BA2_O8           94.9(4)         108 0 0-1     4 0 1 0

O7_BA2_O8          161.8(13)        108 0 0-1     7 0 1-1

O7_BA2_O8           93.46(26)       108 0 0-1   102 0 0-1

O7_BA2_O9           36.5(4)         108 0 0-1   105 0 0-1

O7_BA2_O9           38.43(15)       108 0 0-1     4 0 1 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  13

Angle             Degrees         atom 1 loc  atom 3 loc

O7_BA2_O9          100.21(28)       108 0 0-1   105 0 0-1

O7_BA2_O7          105.0(4)           6 1 1-1    -8 1 1 1

O7_BA2_O8          130.8(5)           6 1 1-1     4 0 1 0

O7_BA2_O8           62.64(31)         6 1 1-1     7 0 1-1

O7_BA2_O8           62.64(31)         6 1 1-1   102 0 0-1

O7_BA2_O9          130.8(5)           6 1 1-1   105 0 0-1

O7_BA2_O9           66.29(15)         6 1 1-1     4 0 1 0

O7_BA2_O9           66.29(17)         6 1 1-1   105 0 0-1

O7_BA2_O8           62.64(13)        -8 1 1 1     4 0 1 0

O7_BA2_O8          130.76(13)        -8 1 1 1     7 0 1-1

O7_BA2_O8          130.76(13)        -8 1 1 1   102 0 0-1

O7_BA2_O9           62.64(17)        -8 1 1 1   105 0 0-1

O7_BA2_O9           66.29(16)        -8 1 1 1     4 0 1 0

O7_BA2_O9           66.29(18)        -8 1 1 1   105 0 0-1

O8_BA2_O8           89.02(29)         4 0 1 0     7 0 1-1

O8_BA2_O8          161.72(7)          4 0 1 0   102 0 0-1

O8_BA2_O9           88.09(23)         4 0 1 0   105 0 0-1

O8_BA2_O9          128.82(11)         4 0 1 0     4 0 1 0

O8_BA2_O9           65.36(30)         4 0 1 0   105 0 0-1

O8_BA2_O8           88.09(30)         7 0 1-1   102 0 0-1

O8_BA2_O9          161.7(11)          7 0 1-1   105 0 0-1

O8_BA2_O9          128.82(11)         7 0 1-1     4 0 1 0

O8_BA2_O9           65.36(30)         7 0 1-1   105 0 0-1

O8_BA2_O9           89.02(21)       102 0 0-1   105 0 0-1

O8_BA2_O9           65.36(15)       102 0 0-1     4 0 1 0

O8_BA2_O9          128.8(6)         102 0 0-1   105 0 0-1

O9_BA2_O9           65.36(31)       105 0 0-1     4 0 1 0

O9_BA2_O9          128.8(9)         105 0 0-1   105 0 0-1

O9_BA2_O9           97.3(6)           4 0 1 0   105 0 0-1

Vector         Length           Optr Cell        Neighbor atom coordinates

CU3_BA2         4.3151(12)         1 0-1 0      .27821   -.22179    .00000

CU3_BA2         4.3151(12)         3 1 1 0      .72179    .22179    .00000

CU3_BA2         4.3151(12)         5 1-1 0      .72179   -.22179    .50000

CU3_BA2         4.3151(12)         7 0 1 0      .27821    .22179    .50000

CU3_CU3         4.22364(11)        5 1 0-1      .50000    .00000   -.25000

CU3_CU3         4.22364(11)        5 1 0 0      .50000    .00000    .75000

CU3_CU4         2.7727(18)         2 1 0 0      .39411    .10589    .00000

CU3_CU4         2.7727(18)         4 0 0 0      .60589   -.10589    .00000

CU3_CU4         2.7727(18)         6 1 0 0      .39411   -.10589    .50000

CU3_CU4         2.7727(18)         8 0 0 0      .60589    .10589    .50000

CU3_IN5         3.0994(13)         1 0 0 0      .24165    .00000    .25000

CU3_IN5         3.0994(13)         3 1 0 0      .75835    .00000    .25000

CU3_IN5         3.0994(13)       106 0 0-1      .50000    .25835    .25000

CU3_IN5         3.0994(13)       108 0-1-1      .50000   -.25835    .25000

CU3_SC6         3.0994(13)         1 0 0 0      .24165    .00000    .25000

CU3_SC6         3.0994(13)         3 1 0 0      .75835    .00000    .25000

CU3_SC6         3.0994(13)       106 0 0-1      .50000    .25835    .25000

CU3_SC6         3.0994(13)       108 0-1-1      .50000   -.25835    .25000

CU3_O7          1.998(11)          2 1 0 0      .38283    .11717    .22607

CU3_O7          1.998(11)          4 0 0 0      .61717   -.11717    .22607

CU3_O7          4.486(8)           6 1 0 0      .38283   -.11717    .72607

CU3_O7          4.486(8)           8 0 0 0      .61717    .11717    .72607

CU3_O7          4.486(8)          -2 0 0 0      .61717   -.11717   -.22607

CU3_O7          4.486(8)          -4 1 0 0      .38283    .11717   -.22607

CU3_O7          1.998(11)         -6 0 0 1      .61717    .11717    .27393

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  14

Vector         Length           Optr Cell        Neighbor atom coordinates

CU3_O7          1.998(11)         -8 1 0 1      .38283   -.11717    .27393

CU3_O9          3.533(11)          2 1 0 0      .49803    .23606    .00000

CU3_O9          3.533(11)          4 0 0 0      .50197   -.23606    .00000

CU3_O9          3.533(11)          6 1 0 0      .49803   -.23606    .50000

CU3_O9          3.533(11)          8 0 0 0      .50197    .23606    .50000

CU3_O9          3.533(11)        101 0-1 0      .73606    .00197    .50000

CU3_O9          3.533(11)        103 0 0 0      .26394   -.00197    .50000

CU3_O9          3.533(11)        105 0-1-1      .26394    .00197    .00000

CU3_O9          3.533(11)        107 0 0-1      .73606   -.00197    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

O7_CU3_O7          168.(4)            2 1 0 0     4 0 0 0

O7_CU3_O7           90.59(5)          2 1 0 0    -6 0 0 1

O7_CU3_O9           90.6(4)           2 1 0 0    -8 1 0 1

O7_CU3_O7           90.6(4)           4 0 0 0    -6 0 0 1

O7_CU3_O9           90.6(8)           4 0 0 0    -8 1 0 1

O7_CU3_O9          168.(6)           -6 0 0 1    -8 1 0 1

Vector         Length           Optr Cell        Neighbor atom coordinates

CU4_BA2         2.9235(31)         1 0 0 0      .27821    .77821    .00000

CU4_BA2         4.1699(17)         2 1 0 0      .22179    .27821    .00000

CU4_BA2         4.1699(17)         4-1 1 0     -.22179    .72179    .00000

CU4_CU3         2.7727(18)         2 0 0 0      .00000    .50000    .25000

CU4_CU3         2.7727(18)         6 0 1-1      .00000    .50000   -.25000

CU4_CU4         3.593(6)           3 0 1 0     -.10589    .39411    .00000

CU4_IN5         3.0690(8)          4 0 1 0      .00000    .75835    .25000

CU4_IN5         3.0690(8)          6 0 1-1      .00000    .75835   -.25000

CU4_IN5         3.0690(8)        103 0 0-1      .25835    .50000   -.25000

CU4_IN5         3.0690(8)        105 0 0-1      .25835    .50000    .25000

CU4_SC6         3.0690(8)          4 0 1 0      .00000    .75835    .25000

CU4_SC6         3.0690(8)          6 0 1-1      .00000    .75835   -.25000

CU4_SC6         3.0690(8)        103 0 0-1      .25835    .50000   -.25000

CU4_SC6         3.0690(8)        105 0 0-1      .25835    .50000    .25000

CU4_O7          1.919(9)           1 0 0 0      .11717    .61717    .22607

CU4_O7          4.239(10)          3 0 1 0     -.11717    .38283    .22607

CU4_O7          3.540(10)          5 0 0-1     -.11717    .61717   -.27393

CU4_O7          3.540(10)          7 0 1-1      .11717    .38283   -.27393

CU4_O7          4.239(10)         -1 0 1 0     -.11717    .38283   -.22607

CU4_O7          1.919(9)          -3 0 0 0      .11717    .61717   -.22607

CU4_O7          3.540(10)         -5 0 1 1      .11717    .38283    .27393

CU4_O7          3.540(10)         -7 0 0 1     -.11717    .61717    .27393

CU4_O8          3.850(6)           4 0 1 0      .12656    .87344    .25000

CU4_O8          3.850(6)           7 0 1-1      .12656    .87344   -.25000

CU4_O8          3.850(6)         102 0 0-1      .37344    .62656   -.25000

CU4_O8          3.850(6)         105 0 0-1      .37344    .62656    .25000

CU4_O9          1.998(12)          1 0 0 0      .23606    .50197    .00000

CU4_O9          4.302(13)          3 0 1 0     -.23606    .49803    .00000

CU4_O9          4.302(13)        106 0 0-1     -.00197    .26394    .00000

CU4_O9          1.998(12)        108-1 0-1      .00197    .73606    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

SC6_CU4_O7           84.28(30)         1 0 0 0     1 0 0 0

SC6_CU4_O8           84.28(11)         1 0 0 0    -3 0 0 0

SC6_CU4_O9           83.60(22)         1 0 0 0     1 0 0 0

SC6_CU4_O9           83.60(27)         1 0 0 0   108-1 0-1

O7_CU4_O8          169.(5)            1 0 0 0    -3 0 0 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  15

Angle             Degrees         atom 1 loc  atom 3 loc

O7_CU4_O9           89.4(4)           1 0 0 0     1 0 0 0

O7_CU4_O9           89.4(4)           1 0 0 0   108-1 0-1

O8_CU4_O9           89.4(5)          -3 0 0 0     1 0 0 0

O8_CU4_O9           89.36(18)        -3 0 0 0   108-1 0-1

O9_CU4_O9          167.2(25)          1 0 0 0   108-1 0-1

Vector         Length           Optr Cell        Neighbor atom coordinates

IN5_BA1         3.5867(11)         1 0 0 0      .00000    .00000    .00000

IN5_BA1         3.5867(11)         5 0 0 0      .00000    .00000    .50000

IN5_BA2         3.4252(6)          1 0-1 0      .27821   -.22179    .00000

IN5_BA2         3.9568(9)          2 1 0 0      .22179    .27821    .00000

IN5_BA2         3.9568(9)          6 1 0 0      .22179   -.27821    .50000

IN5_BA2         3.4252(6)          7 0 1 0      .27821    .22179    .50000

IN5_CU3         3.0994(13)         1 0 0 0      .50000    .00000    .25000

IN5_CU4         3.0690(8)          2 1 0 0      .39411    .10589    .00000

IN5_CU4         3.0690(8)          6 1 0 0      .39411   -.10589    .50000

IN5_IN5         4.0998(19)         2 0 0 0      .00000    .24165    .25000

IN5_IN5         4.0998(19)         4 0 0 0      .00000   -.24165    .25000

IN5_IN5         4.22364(11)        7 0 0-1      .24165    .00000   -.25000

IN5_IN5         4.22364(11)        7 0 0 0      .24165    .00000    .75000

IN5_IN5         4.3833(19)       106 0 0-1      .50000    .25835    .25000

IN5_IN5         4.3833(19)       108 0-1-1      .50000   -.25835    .25000

IN5_SC6         4.0998(19)         2 0 0 0      .00000    .24165    .25000

IN5_SC6         4.0998(19)         4 0 0 0      .00000   -.24165    .25000

IN5_SC6         4.22364(11)        7 0 0-1      .24165    .00000   -.25000

IN5_SC6         4.22364(11)        7 0 0 0      .24165    .00000    .75000

IN5_SC6         4.3833(19)       106 0 0-1      .50000    .25835    .25000

IN5_SC6         4.3833(19)       108 0-1-1      .50000   -.25835    .25000

IN5_O7          2.2104(14)         2 1 0 0      .38283    .11717    .22607

IN5_O7          2.2104(14)        -8 1 0 1      .38283   -.11717    .27393

IN5_O8          2.0522(10)         1 0 0 0      .12656    .12656    .25000

IN5_O8          2.0522(10)         4 0 0 0      .12656   -.12656    .25000

IN5_O9          2.1288(16)       103 0 0 0      .26394   -.00197    .50000

IN5_O9          2.1288(16)       105 0-1-1      .26394    .00197    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_IN5_BA1          72.144(25)        1 0 0 0     5 0 0 0

BA1_IN5_BA2          74.958(19)        1 0 0 0     1 0-1 0

BA1_IN5_SC6         117.81(4)          1 0 0 0     7 0 1 0

BA1_IN5_O7          124.44(28)         1 0 0 0     2 1 0 0

BA1_IN5_O7          132.32(21)         1 0 0 0    -8 1 0 1

BA1_IN5_O8           57.06(22)         1 0 0 0     1 0 0 0

BA1_IN5_O8           57.06(22)         1 0 0 0     4 0 0 0

BA1_IN5_O9          133.29(35)         1 0 0 0   103 0 0 0

BA1_IN5_O9           61.15(35)         1 0 0 0   105 0-1-1

BA1_IN5_BA2         117.81(4)          5 0 0 0     1 0-1 0

BA1_IN5_SC6          74.958(25)        5 0 0 0     7 0 1 0

BA1_IN5_O7          132.32(21)         5 0 0 0     2 1 0 0

BA1_IN5_O7          124.44(28)         5 0 0 0    -8 1 0 1

BA1_IN5_O8           57.06(22)         5 0 0 0     1 0 0 0

BA1_IN5_O8           57.06(22)         5 0 0 0     4 0 0 0

BA1_IN5_O9           61.15(35)         5 0 0 0   103 0 0 0

BA1_IN5_O9          133.29(35)         5 0 0 0   105 0-1-1

BA2_IN5_SC6         165.3(4)           1 0-1 0     7 0 1 0

BA2_IN5_O7          109.85(22)         1 0-1 0     2 1 0 0

BA2_IN5_O7           57.60(21)         1 0-1 0    -8 1 0 1

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  16

Angle             Degrees         atom 1 loc  atom 3 loc

BA2_IN5_O8          131.37(18)         1 0-1 0     1 0 0 0

BA2_IN5_O8           60.75(22)         1 0-1 0     4 0 0 0

BA2_IN5_O9          125.94(21)         1 0-1 0   103 0 0 0

BA2_IN5_O9           51.75(19)         1 0-1 0   105 0-1-1

SC6_IN5_O7           57.60(22)         7 0 1 0     2 1 0 0

SC6_IN5_O7          109.85(25)         7 0 1 0    -8 1 0 1

SC6_IN5_O8           60.75(22)         7 0 1 0     1 0 0 0

SC6_IN5_O8          131.37(21)         7 0 1 0     4 0 0 0

SC6_IN5_O9           51.75(21)         7 0 1 0   103 0 0 0

SC6_IN5_O9          125.94(23)         7 0 1 0   105 0-1-1

O7_IN5_O7           80.0(5)           2 1 0 0    -8 1 0 1

O7_IN5_O8           92.58(32)         2 1 0 0     1 0 0 0

O7_IN5_O8          170.4(4)           2 1 0 0     4 0 0 0

O7_IN5_O9           90.1(4)           2 1 0 0   103 0 0 0

O7_IN5_O9           78.8(4)           2 1 0 0   105 0-1-1

O7_IN5_O8          170.4(4)          -8 1 0 1     1 0 0 0

O7_IN5_O8           92.58(32)        -8 1 0 1     4 0 0 0

O7_IN5_O9           78.8(4)          -8 1 0 1   103 0 0 0

O7_IN5_O9           90.1(4)          -8 1 0 1   105 0-1-1

O8_IN5_O8           95.4(6)           1 0 0 0     4 0 0 0

O8_IN5_O9           95.32(29)         1 0 0 0   103 0 0 0

O8_IN5_O9           94.38(28)         1 0 0 0   105 0-1-1

O8_IN5_O9           94.38(28)         4 0 0 0   103 0 0 0

O8_IN5_O9           95.32(29)         4 0 0 0   105 0-1-1

O9_IN5_O9          165.6(7)         103 0 0 0   105 0-1-1

Vector         Length           Optr Cell        Neighbor atom coordinates

SC6_BA1         3.5867(11)         1 0 0 0      .00000    .00000    .00000

SC6_BA1         3.5867(11)         5 0 0 0      .00000    .00000    .50000

SC6_BA2         3.4252(6)          1 0-1 0      .27821   -.22179    .00000

SC6_BA2         3.9568(9)          2 1 0 0      .22179    .27821    .00000

SC6_BA2         3.9568(9)          6 1 0 0      .22179   -.27821    .50000

SC6_BA2         3.4252(6)          7 0 1 0      .27821    .22179    .50000

SC6_CU3         3.0994(13)         1 0 0 0      .50000    .00000    .25000

SC6_CU4         3.0690(8)          2 1 0 0      .39411    .10589    .00000

SC6_CU4         3.0690(8)          6 1 0 0      .39411   -.10589    .50000

SC6_IN5         4.0998(19)         2 0 0 0      .00000    .24165    .25000

SC6_IN5         4.0998(19)         4 0 0 0      .00000   -.24165    .25000

SC6_IN5         4.22364(11)        7 0 0-1      .24165    .00000   -.25000

SC6_IN5         4.22364(11)        7 0 0 0      .24165    .00000    .75000

SC6_IN5         4.3833(19)       106 0 0-1      .50000    .25835    .25000

SC6_IN5         4.3833(19)       108 0-1-1      .50000   -.25835    .25000

SC6_SC6         4.0998(19)         2 0 0 0      .00000    .24165    .25000

SC6_SC6         4.0998(19)         4 0 0 0      .00000   -.24165    .25000

SC6_SC6         4.22364(11)        7 0 0-1      .24165    .00000   -.25000

SC6_SC6         4.22364(11)        7 0 0 0      .24165    .00000    .75000

SC6_SC6         4.3833(19)       106 0 0-1      .50000    .25835    .25000

SC6_SC6         4.3833(19)       108 0-1-1      .50000   -.25835    .25000

SC6_O7          2.2104(14)         2 1 0 0      .38283    .11717    .22607

SC6_O7          2.2104(14)        -8 1 0 1      .38283   -.11717    .27393

SC6_O8          2.0522(10)         1 0 0 0      .12656    .12656    .25000

SC6_O8          2.0522(10)         4 0 0 0      .12656   -.12656    .25000

SC6_O9          2.1288(16)       103 0 0 0      .26394   -.00197    .50000

SC6_O9          2.1288(16)       105 0-1-1      .26394    .00197    .00000

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  17

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_SC6_BA1          72.144(25)        1 0 0 0     5 0 0 0

BA1_SC6_BA2          74.958(19)        1 0 0 0     1 0-1 0

BA1_SC6_SC6         117.81(4)          1 0 0 0     7 0 1 0

BA1_SC6_O7          124.44(28)         1 0 0 0     2 1 0 0

BA1_SC6_O7          132.32(21)         1 0 0 0    -8 1 0 1

BA1_SC6_O8           57.06(22)         1 0 0 0     1 0 0 0

BA1_SC6_O8           57.06(22)         1 0 0 0     4 0 0 0

BA1_SC6_O9          133.29(35)         1 0 0 0   103 0 0 0

BA1_SC6_O9           61.15(35)         1 0 0 0   105 0-1-1

BA1_SC6_BA2         117.81(4)          5 0 0 0     1 0-1 0

BA1_SC6_SC6          74.958(25)        5 0 0 0     7 0 1 0

BA1_SC6_O7          132.32(21)         5 0 0 0     2 1 0 0

BA1_SC6_O7          124.44(28)         5 0 0 0    -8 1 0 1

BA1_SC6_O8           57.06(22)         5 0 0 0     1 0 0 0

BA1_SC6_O8           57.06(22)         5 0 0 0     4 0 0 0

BA1_SC6_O9           61.15(35)         5 0 0 0   103 0 0 0

BA1_SC6_O9          133.29(35)         5 0 0 0   105 0-1-1

BA2_SC6_SC6         165.3(4)           1 0-1 0     7 0 1 0

BA2_SC6_O7          109.85(22)         1 0-1 0     2 1 0 0

BA2_SC6_O7           57.60(21)         1 0-1 0    -8 1 0 1

BA2_SC6_O8          131.37(18)         1 0-1 0     1 0 0 0

BA2_SC6_O8           60.75(22)         1 0-1 0     4 0 0 0

BA2_SC6_O9          125.94(21)         1 0-1 0   103 0 0 0

BA2_SC6_O9           51.75(19)         1 0-1 0   105 0-1-1

SC6_SC6_O7           57.60(22)         7 0 1 0     2 1 0 0

SC6_SC6_O7          109.85(25)         7 0 1 0    -8 1 0 1

SC6_SC6_O8           60.75(22)         7 0 1 0     1 0 0 0

SC6_SC6_O8          131.37(21)         7 0 1 0     4 0 0 0

SC6_SC6_O9           51.75(21)         7 0 1 0   103 0 0 0

SC6_SC6_O9          125.94(23)         7 0 1 0   105 0-1-1

O7_SC6_O7           80.0(5)           2 1 0 0    -8 1 0 1

O7_SC6_O8           92.58(32)         2 1 0 0     1 0 0 0

O7_SC6_O8          170.4(4)           2 1 0 0     4 0 0 0

O7_SC6_O9           90.1(4)           2 1 0 0   103 0 0 0

O7_SC6_O9           78.8(4)           2 1 0 0   105 0-1-1

O7_SC6_O8          170.4(4)          -8 1 0 1     1 0 0 0

O7_SC6_O8           92.58(32)        -8 1 0 1     4 0 0 0

O7_SC6_O9           78.8(4)          -8 1 0 1   103 0 0 0

O7_SC6_O9           90.1(4)          -8 1 0 1   105 0-1-1

O8_SC6_O8           95.4(6)           1 0 0 0     4 0 0 0

O8_SC6_O9           95.32(29)         1 0 0 0   103 0 0 0

O8_SC6_O9           94.38(28)         1 0 0 0   105 0-1-1

O8_SC6_O9           94.38(28)         4 0 0 0   103 0 0 0

O8_SC6_O9           95.32(29)         4 0 0 0   105 0-1-1

O9_SC6_O9          165.6(7)         103 0 0 0   105 0-1-1

Vector         Length           Optr Cell        Neighbor atom coordinates

O7_BA2         3.333(11)          1 0 0 0      .27821    .77821    .00000

O7_BA2         2.916(8)           6 1 1 0      .22179    .72179    .50000

O7_CU3         1.998(11)          2 0 0 0      .00000    .50000    .25000

O7_CU3         4.486(8)           6 0 1-1      .00000    .50000   -.25000

O7_CU4         1.919(9)           1 0 0 0      .10589    .60589    .00000

O7_CU4         4.239(10)          3 0 1 0     -.10589    .39411    .00000

O7_CU4         3.540(10)          5 0 0 0     -.10589    .60589    .50000

O7_CU4         3.540(10)          7 0 1 0      .10589    .39411    .50000

O7_IN5         2.2104(14)         4 0 1 0      .00000    .75835    .25000

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  18

Vector         Length           Optr Cell        Neighbor atom coordinates

O7_IN5         2.2103(14)       105 0 0-1      .25835    .50000    .25000

O7_SC6         2.2104(14)         4 0 1 0      .00000    .75835    .25000

O7_SC6         2.2103(14)       105 0 0-1      .25835    .50000    .25000

O7_O7          3.976(21)          3 0 1 0     -.11717    .38283    .22607

O7_O7          3.819(18)         -3 0 0 0      .11717    .61717   -.22607

O7_O7          2.840(15)         -5 0 1 1      .11717    .38283    .27393

O7_O7          2.840(15)         -7 0 0 1     -.11717    .61717    .27393

O7_O8          4.2477(5)          3 0 1 0     -.12656    .87344    .25000

O7_O8          3.083(8)           4 0 1 0      .12656    .87344    .25000

O7_O8          3.083(8)         105 0 0-1      .37344    .62656    .25000

O7_O8          4.2477(5)        106 0 0-1      .37344    .37344    .25000

O7_O9          2.755(11)          1 0 0 0      .23606    .50197    .00000

O7_O9          3.071(10)          7 0 1 0      .23606    .49803    .50000

O7_O9          3.071(10)        102 0 0 0     -.00197    .73606    .50000

O7_O9          2.755(11)        108-1 0-1      .00197    .73606    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

BA2_O7_CU3          121.69(10)         6 1 1 0     2 0 0 0

BA2_O7_CU4          148.2(12)          6 1 1 0     1 0 0 0

BA2_O7_IN5           82.61(21)         6 1 1 0     4 0 1 0

BA2_O7_IN5           82.61(21)         6 1 1 0   105 0 0-1

BA2_O7_SC6           82.61(21)         6 1 1 0     4 0 1 0

BA2_O7_O9            82.6(5)           6 1 1 0   105 0 0-1

CU3_O7_CU4           90.09(30)         2 0 0 0     1 0 0 0

CU3_O7_IN5           94.73(20)         2 0 0 0     4 0 1 0

CU3_O7_IN5           94.73(20)         2 0 0 0   105 0 0-1

CU3_O7_SC6           94.73(20)         2 0 0 0     4 0 1 0

CU3_O7_O9            94.7(7)           2 0 0 0   105 0 0-1

CU4_O7_IN5           95.75(26)         1 0 0 0     4 0 1 0

CU4_O7_IN5           95.75(33)         1 0 0 0   105 0 0-1

CU4_O7_SC6           95.75(26)         1 0 0 0     4 0 1 0

CU4_O7_O9            95.8(5)           1 0 0 0   105 0 0-1

IN5_O7_IN5          165.1(4)           4 0 1 0   105 0 0-1

IN5_O7_SC6             .000(0)         4 0 1 0     4 0 1 0

IN5_O7_O9           165.(4)            4 0 1 0   105 0 0-1

IN5_O7_SC6          165.1(4)         105 0 0-1     4 0 1 0

IN5_O7_O9              .000(0)       105 0 0-1   105 0 0-1

SC6_O7_O9           165.(4)            4 0 1 0   105 0 0-1

Vector         Length           Optr Cell        Neighbor atom coordinates

O8_BA1         3.012(8)           1 0 0 0      .00000    .00000    .00000

O8_BA1         3.012(8)           5 0 0 0      .00000    .00000    .50000

O8_BA2         3.012(8)           2 1 0 0      .22179    .27821    .00000

O8_BA2         3.012(8)           7 0 1 0      .27821    .22179    .50000

O8_CU4         3.850(6)           2 1 0 0      .39411    .10589    .00000

O8_CU4         3.850(6)           7 0 1 0      .10589    .39411    .50000

O8_IN5         2.0522(10)         1 0 0 0      .24165    .00000    .25000

O8_IN5         2.0522(10)         2 0 0 0      .00000    .24165    .25000

O8_SC6         2.0522(10)         1 0 0 0      .24165    .00000    .25000

O8_SC6         2.0522(10)         2 0 0 0      .00000    .24165    .25000

O8_O7          3.083(8)           2 1 0 0      .38283    .11717    .22607

O8_O7          4.2477(5)          3 0 1 0     -.11717    .38283    .22607

O8_O7          3.083(8)          -5 0 1 1      .11717    .38283    .27393

O8_O7          4.2477(5)         -8 1 0 1      .38283   -.11717    .27393

O8_O8          3.037(16)          2 0 0 0     -.12656    .12656    .25000

O8_O8          4.295(22)          3 0 0 0     -.12656   -.12656    .25000

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  19

Vector         Length           Optr Cell        Neighbor atom coordinates

O8_O8          3.037(16)          4 0 0 0      .12656   -.12656    .25000

O8_O8          4.22364(11)        8 0 0-1      .12656    .12656   -.25000

O8_O8          4.22364(11)        8 0 0 0      .12656    .12656    .75000

O8_O8          4.188(22)        106 0 0-1      .37344    .37344    .25000

O8_O9          3.091(8)         103 0 0 0      .26394   -.00197    .50000

O8_O9          3.068(8)         104-1 0 0      .00197    .26394    .50000

O8_O9          3.068(8)         105 0-1-1      .26394    .00197    .00000

O8_O9          3.091(8)         106 0 0-1     -.00197    .26394    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_O8_BA1           89.04(29)         1 0 0 0     5 0 0 0

BA1_O8_BA2           90.235(4)         1 0 0 0     2 1 0 0

BA1_O8_CU4          170.8(6)           1 0 0 0     7 0 1 0

BA1_O8_IN5           88.06(22)         1 0 0 0     1 0 0 0

BA1_O8_IN5           88.06(22)         1 0 0 0     2 0 0 0

BA1_O8_SC6           88.06(22)         1 0 0 0     1 0 0 0

BA1_O8_O9            88.1(4)           1 0 0 0     2 0 0 0

BA1_O8_BA2          170.83(5)          5 0 0 0     2 1 0 0

BA1_O8_CU4           90.23(6)          5 0 0 0     7 0 1 0

BA1_O8_IN5           88.06(22)         5 0 0 0     1 0 0 0

BA1_O8_IN5           88.06(22)         5 0 0 0     2 0 0 0

BA1_O8_SC6           88.06(22)         5 0 0 0     1 0 0 0

BA1_O8_O9            88.1(4)           5 0 0 0     2 0 0 0

BA2_O8_CU4           91.91(27)         2 1 0 0     7 0 1 0

BA2_O8_IN5          101.05(24)         2 1 0 0     1 0 0 0

BA2_O8_IN5           82.78(19)         2 1 0 0     2 0 0 0

BA2_O8_SC6          101.05(24)         2 1 0 0     1 0 0 0

BA2_O8_O9            82.78(34)         2 1 0 0     2 0 0 0

CU4_O8_IN5           82.78(15)         7 0 1 0     1 0 0 0

CU4_O8_IN5          101.05(22)         7 0 1 0     2 0 0 0

CU4_O8_SC6           82.78(15)         7 0 1 0     1 0 0 0

CU4_O8_O9           101.1(4)           7 0 1 0     2 0 0 0

IN5_O8_IN5          174.6(6)           1 0 0 0     2 0 0 0

IN5_O8_SC6             .000(0)         1 0 0 0     1 0 0 0

IN5_O8_O9           174.6(17)          1 0 0 0     2 0 0 0

IN5_O8_SC6          174.6(6)           2 0 0 0     1 0 0 0

IN5_O8_O9              .000(0)         2 0 0 0     2 0 0 0

SC6_O8_O9           174.6(17)          1 0 0 0     2 0 0 0

Vector         Length           Optr Cell        Neighbor atom coordinates

O9_BA1         3.167(13)        105 0 0-1      .50000    .50000    .00000

O9_BA2         3.352(8)           1 0 0 0      .27821    .77821    .00000

O9_BA2         2.690(7)           2 1 0 0      .22179    .27821    .00000

O9_CU3         3.533(11)          2 0 0 0      .00000    .50000    .25000

O9_CU3         3.533(11)          6 0 1-1      .00000    .50000   -.25000

O9_CU4         1.998(12)          1 0 0 0      .10589    .60589    .00000

O9_CU4         4.302(13)          3 0 1 0     -.10589    .39411    .00000

O9_IN5         2.1288(16)       103 0 0-1      .25835    .50000   -.25000

O9_IN5         2.1288(16)       105 0 0-1      .25835    .50000    .25000

O9_SC6         2.1288(16)       103 0 0-1      .25835    .50000   -.25000

O9_SC6         2.1288(16)       105 0 0-1      .25835    .50000    .25000

O9_O7          2.755(11)          1 0 0 0      .11717    .61717    .22607

O9_O7          3.071(10)          7 0 1-1      .11717    .38283   -.27393

O9_O7          2.755(11)         -3 0 0 0      .11717    .61717   -.22607

O9_O7          3.071(10)         -5 0 1 1      .11717    .38283    .27393

O9_O8          3.068(8)         102 0 0-1      .37344    .62656   -.25000

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  20

Vector         Length           Optr Cell        Neighbor atom coordinates

O9_O8          3.091(8)         103 0 0-1      .37344    .37344   -.25000

O9_O8          3.068(8)         105 0 0-1      .37344    .62656    .25000

O9_O8          3.091(8)         106 0 0-1      .37344    .37344    .25000

O9_O9          4.478(19)          2 1 0 0      .49803    .23606    .00000

O9_O9          4.478(19)          4 0 1 0      .50197    .76394    .00000

O9_O9          4.22391(20)        7 0 1-1      .23606    .49803   -.50000

O9_O9          4.22391(20)        7 0 1 0      .23606    .49803    .50000

O9_O9          4.038(21)        106 0 0-1     -.00197    .26394    .00000

O9_O9          3.971(22)        108-1 0-1      .00197    .73606    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

CU3_O9_CU4          125.0(11)          2 1 0 0     1 0 0 0

CU3_O9_IN5           89.82(25)         2 1 0 0   103 0 0-1

CU3_O9_IN5           89.82(25)         2 1 0 0   105 0 0-1

CU3_O9_SC6           89.82(25)         2 1 0 0   103 0 0-1

CU3_O9_O9            89.8(4)           2 1 0 0   105 0 0-1

CU4_O9_IN5           96.04(34)         1 0 0 0   103 0 0-1

CU4_O9_IN5           96.04(34)         1 0 0 0   105 0 0-1

CU4_O9_SC6           96.04(34)         1 0 0 0   103 0 0-1

CU4_O9_O9            96.0(13)          1 0 0 0   105 0 0-1

IN5_O9_IN5          165.5(7)         103 0 0-1   105 0 0-1

IN5_O9_SC6             .000(0)       103 0 0-1   103 0 0-1

IN5_O9_O9           166.(4)          103 0 0-1   105 0 0-1

IN5_O9_SC6          165.5(7)         105 0 0-1   103 0 0-1

IN5_O9_O9              .000(0)       105 0 0-1   105 0 0-1

SC6_O9_O9           166.(4)          103 0 0-1   105 0 0-1

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  21

Space group I 21 3

The lattice is acentric  I-centered cubic         Laue symmetry m 3

Multiplicity of a general site is  24

The equivalent positions are:

( 1)     X      Y      Z  ( 2)     Z      X      Y  ( 3)     Y      Z      X

( 4) 1/2+X  1/2-Y     -Z  ( 5)    -Z  1/2+X  1/2-Y  ( 6) 1/2-Y     -Z  1/2+X

( 7) 1/2-Z     -X  1/2+Y  ( 8) 1/2+Y  1/2-Z     -X  ( 9)    -Y  1/2+Z  1/2-X

(10) 1/2-X     -Y  1/2+Z  (11) 1/2+Z  1/2-X     -Y  (12)    -X  1/2+Y  1/2-Z

GENLES was run on 2000-10-10T10:25:12     Total cycles run1064

The Current Least-Squares controls are

Maximum number of cycles is    6

I/SigI cut-off is  1.00

The atom type radii are

TYPE     BOND      ANGLE

BA       2.44000   2.24000

CU       1.48000   1.28000

IN       1.86000   1.66000

SC       1.84000   1.64000

O        1.09000    .89000

Lattice constants are   10.11264  10.11264  10.11264  .00000  .00000  .00000

Standard deviations     .00037    .00037    .00037  .00000  .00000  .00000

DMAX is    4.50000 DAGL is    1.78000 and IAGL is     0

The atoms read in are

IN1       .2500000(0)   .2500000(0)   .2500000(0)   3(111)  IN      1 1.000(0)

IN2      -.0215750(0)   .0000000(0)   .2500000(0)   2(100)  IN      2 1.000(0)

IN3       .4998580(0)   .0000000(0)   .2500000(0)   2(100)  IN      3 1.000(0)

O4        .1250000(0)   .1350000(0)   .3950000(0)     1     O       4 1.000(0)

O5        .1000000(0)   .3580000(0)   .3730000(0)     1     O       5 1.000(0)

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  22

Vector         Length           Optr Cell        Neighbor atom coordinates

IN1_IN2         3.42456(9)         7 0 0 0      .25000    .02158    .50000

IN1_IN2         3.42456(9)         8 0 0 0      .50000    .25000    .02158

IN1_IN2         3.42456(13)       12 0 0 0      .02158    .50000    .25000

IN1_IN3         3.57434(13)        1 0 0 0      .49986    .00000    .25000

IN1_IN3         3.57434(9)         2 0 0 0      .25000    .49986    .00000

IN1_IN3         3.57434(9)         3 0 0 0      .00000    .25000    .49986

IN1_IN3         3.57637(9)         7 0 1 0      .25000    .50014    .50000

IN1_IN3         3.57637(9)         8 0 0 1      .50000    .25000    .50014

IN1_IN3         3.57637(13)       12 1 0 0      .50014    .50000    .25000

IN1_O4          2.25843(6)         1 0 0 0      .12500    .13500    .39500

IN1_O4          2.25843(6)         2 0 0 0      .39500    .12500    .13500

IN1_O4          2.25843(6)         3 0 0 0      .13500    .39500    .12500

IN1_O5          2.24521(6)         1 0 0 0      .10000    .35800    .37300

IN1_O5          2.24521(7)         2 0 0 0      .37300    .10000    .35800

IN1_O5          2.24521(6)         3 0 0 0      .35800    .37300    .10000

Angle             Degrees         atom 1 loc  atom 3 loc

O4_IN1_O4          114.175(1)         1 0 0 0     2 0 0 0

O4_IN1_O4          114.175(1)         1 0 0 0     3 0 0 0

O4_IN1_O5           60.833(1)         1 0 0 0     1 0 0 0

O4_IN1_O5           69.289(1)         1 0 0 0     2 0 0 0

O4_IN1_O5          175.007(0)         1 0 0 0     3 0 0 0

O4_IN1_O4          114.175(3)         2 0 0 0     3 0 0 0

O4_IN1_O5          175.007(0)         2 0 0 0     1 0 0 0

O4_IN1_O5           60.833(3)         2 0 0 0     2 0 0 0

O4_IN1_O5           69.289(1)         2 0 0 0     3 0 0 0

O4_IN1_O5           69.289(3)         3 0 0 0     1 0 0 0

O4_IN1_O5          175.007(0)         3 0 0 0     2 0 0 0

O4_IN1_O5           60.833(1)         3 0 0 0     3 0 0 0

O5_IN1_O5          115.687(3)         1 0 0 0     2 0 0 0

O5_IN1_O5          115.687(1)         1 0 0 0     3 0 0 0

O5_IN1_O5          115.687(1)         2 0 0 0     3 0 0 0

Vector         Length           Optr Cell        Neighbor atom coordinates

IN2_IN1         3.42456(13)        5 0-1 0     -.25000   -.25000    .25000

IN2_IN1         3.42456(13)      106-1 0-1     -.25000    .25000    .25000

IN2_IN3         3.58100(9)         3 0 0 0      .00000    .25000    .49986

IN2_IN3         3.42456(9)         5 0-1 0     -.25000   -.00014    .50000

IN2_IN3         3.58100(9)         9 0-1 0      .00000   -.25000    .00014

IN2_IN3         3.42456(9)        11-1 0 0     -.25000    .00014    .00000

IN2_O4          2.49219(7)         1 0 0 0      .12500    .13500    .39500

IN2_O4          2.01024(5)         9 0-1 0     -.13500   -.10500    .37500

IN2_O4          2.49219(7)       104-1-1 0      .12500   -.13500    .10500

IN2_O4          2.01023(5)       106-1 0-1     -.13500    .10500    .12500

IN2_O5          2.05870(6)        12 0-1 0     -.10000   -.14200    .12700

IN2_O5          2.05870(6)       110-1 0-1     -.10000    .14200    .37300

Angle             Degrees         atom 1 loc  atom 3 loc

O4_IN2_O4          104.995(3)         1 0 0 0     9 0-1 0

O4_IN2_O4          107.009(2)         1 0 0 0   104-1-1 0

O4_IN2_O4          114.834(1)         1 0 0 0   106-1 0-1

O4_IN2_O5          165.176(0)         1 0 0 0    12 0-1 0

O4_IN2_O5           59.438(1)         1 0 0 0   110-1 0-1

O4_IN2_O4          114.834(1)         9 0-1 0   104-1-1 0

O4_IN2_O4          110.417(2)         9 0-1 0   106-1 0-1

O4_IN2_O5           77.976(3)         9 0-1 0    12 0-1 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  23

Angle             Degrees         atom 1 loc  atom 3 loc

O4_IN2_O5           76.626(2)         9 0-1 0   110-1 0-1

O4_IN2_O4          104.995(3)       104-1-1 0   106-1 0-1

O4_IN2_O5           59.438(1)       104-1-1 0    12 0-1 0

O4_IN2_O5          165.176(0)       104-1-1 0   110-1 0-1

O4_IN2_O5           76.626(2)       106-1 0-1    12 0-1 0

O4_IN2_O5           77.976(3)       106-1 0-1   110-1 0-1

O5_IN2_O5          134.683(1)        12 0-1 0   110-1 0-1

Vector         Length           Optr Cell        Neighbor atom coordinates

IN3_IN1         3.57434(13)        1 0 0 0      .25000    .25000    .25000

IN3_IN1         3.57637(13)        5 1-1 0      .75000   -.25000    .25000

IN3_IN1         3.57434(13)      104-1-1 0      .25000   -.25000    .25000

IN3_IN1         3.57637(13)      106 0 0-1      .75000    .25000    .25000

IN3_IN2         3.58100(9)         2 0 0 0      .25000   -.02158    .00000

IN3_IN2         3.42456(9)         6 0 0 0      .50000   -.25000    .47842

IN3_IN2         3.58100(9)         7 0 0 0      .25000    .02158    .50000

IN3_IN2         3.42456(9)         8 0 0 0      .50000    .25000    .02158

IN3_IN3         3.57637(9)         5 1-1 0      .75000   -.00014    .50000

IN3_IN3         3.57637(9)         6 0 0-1      .50000   -.25000   -.00014

IN3_IN3         3.57637(9)         8 0 0 1      .50000    .25000    .50014

IN3_IN3         3.57637(9)        11 0 0 0      .75000    .00014    .00000

IN3_O4          2.01861(6)         2 0 0 0      .39500    .12500    .13500

IN3_O4          2.01861(6)       111-1-1 0      .39500   -.12500    .36500

IN3_O5          1.96500(5)         2 0 0 0      .37300    .10000    .35800

IN3_O5          2.45288(7)         9 1-1 0      .64200   -.12700    .40000

IN3_O5          2.45288(7)       106 0 0-1      .64200    .12700    .10000

IN3_O5          1.96500(5)       111-1-1 0      .37300   -.10000    .14200

Angle             Degrees         atom 1 loc  atom 3 loc

O4_IN3_O4          116.622(1)         2 0 0 0   111-1-1 0

O4_IN3_O5           69.817(3)         2 0 0 0     2 0 0 0

O4_IN3_O5          172.746(0)         2 0 0 0     9 1-1 0

O4_IN3_O5           67.894(1)         2 0 0 0   106 0 0-1

O4_IN3_O5           70.069(1)         2 0 0 0   111-1-1 0

O4_IN3_O5           70.069(1)       111-1-1 0     2 0 0 0

O4_IN3_O5           67.894(1)       111-1-1 0     9 1-1 0

O4_IN3_O5          172.746(0)       111-1-1 0   106 0 0-1

O4_IN3_O5           69.817(3)       111-1-1 0   111-1-1 0

O5_IN3_O5          107.958(3)         2 0 0 0     9 1-1 0

O5_IN3_O5          117.184(1)         2 0 0 0   106 0 0-1

O5_IN3_O5           98.485(2)         2 0 0 0   111-1-1 0

O5_IN3_O5          108.250(2)         9 1-1 0   106 0 0-1

O5_IN3_O5          117.184(1)         9 1-1 0   111-1-1 0

O5_IN3_O5          107.958(3)       106 0 0-1   111-1-1 0

Vector         Length           Optr Cell        Neighbor atom coordinates

O4_IN1         2.25843(6)         1 0 0 0      .25000    .25000    .25000

O4_IN2         2.49219(7)         1 0 0 0     -.02158    .00000    .25000

O4_IN2         2.01024(6)         7 0 0 0      .25000    .02158    .50000

O4_IN3         2.01861(6)         3 0 0 0      .00000    .25000    .49986

Angle             Degrees         atom 1 loc  atom 3 loc

IN1_O4_IN2          103.472(3)         1 0 0 0     1 0 0 0

IN1_O4_IN2          106.548(2)         1 0 0 0     7 0 0 0

IN1_O4_IN3          113.260(1)         1 0 0 0     3 0 0 0

IN2_O4_IN2          111.852(1)         1 0 0 0     7 0 0 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  24

Angle             Degrees         atom 1 loc  atom 3 loc

IN2_O4_IN3          104.609(1)         1 0 0 0     3 0 0 0

IN2_O4_IN3          116.425(3)         7 0 0 0     3 0 0 0

Vector         Length           Optr Cell        Neighbor atom coordinates

O5_IN1         2.24521(6)         1 0 0 0      .25000    .25000    .25000

O5_IN2         2.05870(6)        12 0 0 0      .02158    .50000    .25000

O5_IN3         1.96500(5)         3 0 0 0      .00000    .25000    .49986

O5_IN3         2.45288(7)         7 0 1 0      .25000    .50014    .50000

Angle             Degrees         atom 1 loc  atom 3 loc

IN1_O5_IN2          105.358(3)         1 0 0 0    12 0 0 0

IN1_O5_IN3          116.041(1)         1 0 0 0     3 0 0 0

IN1_O5_IN3           99.052(1)         1 0 0 0     7 0 1 0

IN2_O5_IN3          125.724(1)        12 0 0 0     3 0 0 0

IN2_O5_IN3           98.385(2)        12 0 0 0     7 0 1 0

IN3_O5_IN3          107.586(3)         3 0 0 0     7 0 1 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  25

Space group I 4/mcm

The lattice is centric  I-centered tetragonal    Laue symmetry 4/mmm

Multiplicity of a general site is  32

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)    -Y      X      Z

( 3)    -X     -Y      Z  ( 4)     Y     -X      Z

( 5)    -X      Y  1/2+Z  ( 6)    -Y     -X  1/2+Z

( 7)     X     -Y  1/2+Z  ( 8)     Y      X  1/2+Z

GENLES was run on 2000-10-10T10:25:12     Total cycles run1064

The Current Least-Squares controls are

Maximum number of cycles is    6

I/SigI cut-off is  1.00

The atom type radii are

TYPE     BOND      ANGLE

BA       2.44000   2.24000

CU       1.48000   1.28000

IN       1.86000   1.66000

SC       1.84000   1.64000

O        1.09000    .89000

Lattice constants are   12.11764  12.11764   8.51388  .00000  .00000  .00000

Standard deviations     .00045    .00045    .00060  .00000  .00000  .00000

DMAX is    2.18000 DAGL is    1.78000 and IAGL is     0

The atoms read in are

BA1       .0000000(0)   .0000000(0)   .0000000(0) 4/M(001)  BA      1 1.000(0)

BA2       .2796150(0)   .7796170(0)   .0000000(0) MM2(110)  BA      2 1.000(0)

CU3       .5000000(0)   .0000000(0)   .2500000(0) -42M 001  CU      3 1.000(0)

CU4       .1056750(0)   .6056760(0)   .0000000(0) MM2(110)  CU      4 1.000(0)

IN5       .2424970(0)   .0000000(0)   .2500000(0)   2(100)  IN      5 1.000(0)

O6        .1084590(0)   .6084610(0)   .2362010(0)   M(+-0)  O       6 1.000(0)

O7        .1162440(0)   .1162440(0)   .2500000(0)   2(110)  O       7 1.000(0)

O8        .2222870(0)   .4949280(0)   .0000000(0)   M(001)  O       8 1.000(0)

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  26

Vector         Length           Optr Cell        Neighbor atom coordinates

BA1_BA1         4.25694(30)        5 0 0-1      .00000    .00000   -.50000

BA1_BA1         4.25694(30)        5 0 0 0      .00000    .00000    .50000

BA1_BA2         4.31417(16)        1 0-1 0      .27962   -.22038    .00000

BA1_BA2         4.31417(16)        2 1 0 0      .22038    .27962    .00000

BA1_BA2         4.31417(16)        3 0 1 0     -.27962    .22038    .00000

BA1_BA2         4.31417(16)        4-1 0 0     -.22038   -.27962    .00000

BA1_IN5         3.62838(12)        1 0 0 0      .24250    .00000    .25000

BA1_IN5         3.62838(12)        2 0 0 0      .00000    .24250    .25000

BA1_IN5         3.62838(12)        3 0 0 0     -.24250    .00000    .25000

BA1_IN5         3.62838(12)        4 0 0 0      .00000   -.24250    .25000

BA1_IN5         3.62838(12)        5 0 0-1     -.24250    .00000   -.25000

BA1_IN5         3.62838(12)        6 0 0-1      .00000   -.24250   -.25000

BA1_IN5         3.62838(12)        7 0 0-1      .24250    .00000   -.25000

BA1_IN5         3.62838(12)        8 0 0-1      .00000    .24250   -.25000

BA1_O7          2.91526(12)        1 0 0 0      .11624    .11624    .25000

BA1_O7          2.91526(12)        2 0 0 0     -.11624    .11624    .25000

BA1_O7          2.91526(12)        3 0 0 0     -.11624   -.11624    .25000

BA1_O7          2.91526(12)        4 0 0 0      .11624   -.11624    .25000

BA1_O7          2.91526(12)        5 0 0-1     -.11624    .11624   -.25000

BA1_O7          2.91526(12)        6 0 0-1     -.11624   -.11624   -.25000

BA1_O7          2.91526(12)        7 0 0-1      .11624   -.11624   -.25000

BA1_O7          2.91526(12)        8 0 0-1      .11624    .11624   -.25000

BA1_O8          3.36579(13)      105 0-1-1      .27771   -.00507    .00000

BA1_O8          3.36579(13)      106 0 0-1      .00507    .27771    .00000

BA1_O8          3.36579(13)      107-1 0-1     -.27771    .00507    .00000

BA1_O8          3.36579(13)      108-1-1-1     -.00507   -.27771    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_BA1_BA1         180.000(0)         5 0 0-1     5 0 0 0

BA1_BA1_BA2          90.000(0)         5 0 0-1     1 0-1 0

BA1_BA1_BA2          90.000(0)         5 0 0-1     2 1 0 0

BA1_BA1_BA2          90.000(0)         5 0 0-1     3 0 1 0

BA1_BA1_BA2          90.000(0)         5 0 0-1     4-1 0 0

BA1_BA1_IN5         125.917(2)         5 0 0-1     1 0 0 0

BA1_BA1_IN5         125.917(2)         5 0 0-1     2 0 0 0

BA1_BA1_IN5         125.917(2)         5 0 0-1     3 0 0 0

BA1_BA1_IN5         125.917(2)         5 0 0-1     4 0 0 0

BA1_BA1_IN5          54.083(2)         5 0 0-1     5 0 0-1

BA1_BA1_IN5          54.083(2)         5 0 0-1     6 0 0-1

BA1_BA1_IN5          54.083(2)         5 0 0-1     7 0 0-1

BA1_BA1_IN5          54.083(2)         5 0 0-1     8 0 0-1

BA1_BA1_O7          136.896(2)         5 0 0-1     1 0 0 0

BA1_BA1_O7          136.896(2)         5 0 0-1     2 0 0 0

BA1_BA1_O7          136.896(2)         5 0 0-1     3 0 0 0

BA1_BA1_O7          136.896(2)         5 0 0-1     4 0 0 0

BA1_BA1_O7           43.104(2)         5 0 0-1     5 0 0-1

BA1_BA1_O7           43.104(2)         5 0 0-1     6 0 0-1

BA1_BA1_O7           43.104(2)         5 0 0-1     7 0 0-1

BA1_BA1_O8           43.104(2)         5 0 0-1     8 0 0-1

BA1_BA1_BA2          90.000(0)         5 0 0 0     1 0-1 0

BA1_BA1_BA2          90.000(0)         5 0 0 0     2 1 0 0

BA1_BA1_BA2          90.000(0)         5 0 0 0     3 0 1 0

BA1_BA1_BA2          90.000(0)         5 0 0 0     4-1 0 0

BA1_BA1_IN5          54.083(2)         5 0 0 0     1 0 0 0

BA1_BA1_IN5          54.083(2)         5 0 0 0     2 0 0 0

BA1_BA1_IN5          54.083(2)         5 0 0 0     3 0 0 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  27

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_BA1_IN5          54.083(2)         5 0 0 0     4 0 0 0

BA1_BA1_IN5         125.917(2)         5 0 0 0     5 0 0-1

BA1_BA1_IN5         125.917(2)         5 0 0 0     6 0 0-1

BA1_BA1_IN5         125.917(2)         5 0 0 0     7 0 0-1

BA1_BA1_IN5         125.917(2)         5 0 0 0     8 0 0-1

BA1_BA1_O7           43.104(2)         5 0 0 0     1 0 0 0

BA1_BA1_O7           43.104(2)         5 0 0 0     2 0 0 0

BA1_BA1_O7           43.104(2)         5 0 0 0     3 0 0 0

BA1_BA1_O7           43.104(2)         5 0 0 0     4 0 0 0

BA1_BA1_O7          136.896(2)         5 0 0 0     5 0 0-1

BA1_BA1_O7          136.896(2)         5 0 0 0     6 0 0-1

BA1_BA1_O7          136.896(2)         5 0 0 0     7 0 0-1

BA1_BA1_O8          136.896(8)         5 0 0 0     8 0 0-1

BA2_BA1_BA2          90.000(0)         1 0-1 0     2 1 0 0

BA2_BA1_BA2         179.972(0)         1 0-1 0     3 0 1 0

BA2_BA1_BA2          90.000(0)         1 0-1 0     4-1 0 0

BA2_BA1_IN5          50.502(1)         1 0-1 0     1 0 0 0

BA2_BA1_IN5         120.087(1)         1 0-1 0     2 0 0 0

BA2_BA1_IN5         129.498(1)         1 0-1 0     3 0 0 0

BA2_BA1_IN5          59.913(1)         1 0-1 0     4 0 0 0

BA2_BA1_IN5         129.498(1)         1 0-1 0     5 0 0-1

BA2_BA1_IN5          59.913(1)         1 0-1 0     6 0 0-1

BA2_BA1_IN5          50.502(1)         1 0-1 0     7 0 0-1

BA2_BA1_IN5         120.087(1)         1 0-1 0     8 0 0-1

BA2_BA1_O7           85.389(0)         1 0-1 0     1 0 0 0

BA2_BA1_O7          132.733(2)         1 0-1 0     2 0 0 0

BA2_BA1_O7           94.611(0)         1 0-1 0     3 0 0 0

BA2_BA1_O7           47.267(2)         1 0-1 0     4 0 0 0

BA2_BA1_O7          132.733(2)         1 0-1 0     5 0 0-1

BA2_BA1_O7           94.611(0)         1 0-1 0     6 0 0-1

BA2_BA1_O7           47.267(2)         1 0-1 0     7 0 0-1

BA2_BA1_O8           85.389(2)         1 0-1 0     8 0 0-1

BA2_BA1_BA2          90.000(0)         2 1 0 0     3 0 1 0

BA2_BA1_BA2         179.972(0)         2 1 0 0     4-1 0 0

BA2_BA1_IN5          59.913(1)         2 1 0 0     1 0 0 0

BA2_BA1_IN5          50.502(1)         2 1 0 0     2 0 0 0

BA2_BA1_IN5         120.087(1)         2 1 0 0     3 0 0 0

BA2_BA1_IN5         129.498(1)         2 1 0 0     4 0 0 0

BA2_BA1_IN5         120.087(1)         2 1 0 0     5 0 0-1

BA2_BA1_IN5         129.498(1)         2 1 0 0     6 0 0-1

BA2_BA1_IN5          59.913(1)         2 1 0 0     7 0 0-1

BA2_BA1_IN5          50.502(1)         2 1 0 0     8 0 0-1

BA2_BA1_O7           47.267(2)         2 1 0 0     1 0 0 0

BA2_BA1_O7           85.389(0)         2 1 0 0     2 0 0 0

BA2_BA1_O7          132.733(2)         2 1 0 0     3 0 0 0

BA2_BA1_O7           94.611(0)         2 1 0 0     4 0 0 0

BA2_BA1_O7           85.389(0)         2 1 0 0     5 0 0-1

BA2_BA1_O7          132.733(2)         2 1 0 0     6 0 0-1

BA2_BA1_O7           94.611(0)         2 1 0 0     7 0 0-1

BA2_BA1_O8           47.267(2)         2 1 0 0     8 0 0-1

BA2_BA1_BA2          90.000(0)         3 0 1 0     4-1 0 0

BA2_BA1_IN5         129.498(1)         3 0 1 0     1 0 0 0

BA2_BA1_IN5          59.913(1)         3 0 1 0     2 0 0 0

BA2_BA1_IN5          50.502(1)         3 0 1 0     3 0 0 0

BA2_BA1_IN5         120.087(1)         3 0 1 0     4 0 0 0

BA2_BA1_IN5          50.502(1)         3 0 1 0     5 0 0-1

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  28

Angle             Degrees         atom 1 loc  atom 3 loc

BA2_BA1_IN5         120.087(1)         3 0 1 0     6 0 0-1

BA2_BA1_IN5         129.498(1)         3 0 1 0     7 0 0-1

BA2_BA1_IN5          59.913(1)         3 0 1 0     8 0 0-1

BA2_BA1_O7           94.611(0)         3 0 1 0     1 0 0 0

BA2_BA1_O7           47.267(2)         3 0 1 0     2 0 0 0

BA2_BA1_O7           85.389(0)         3 0 1 0     3 0 0 0

BA2_BA1_O7          132.733(2)         3 0 1 0     4 0 0 0

BA2_BA1_O7           47.267(2)         3 0 1 0     5 0 0-1

BA2_BA1_O7           85.389(0)         3 0 1 0     6 0 0-1

BA2_BA1_O7          132.733(2)         3 0 1 0     7 0 0-1

BA2_BA1_O8           94.611(2)         3 0 1 0     8 0 0-1

BA2_BA1_IN5         120.087(1)         4-1 0 0     1 0 0 0

BA2_BA1_IN5         129.498(1)         4-1 0 0     2 0 0 0

BA2_BA1_IN5          59.913(1)         4-1 0 0     3 0 0 0

BA2_BA1_IN5          50.502(1)         4-1 0 0     4 0 0 0

BA2_BA1_IN5          59.913(1)         4-1 0 0     5 0 0-1

BA2_BA1_IN5          50.502(1)         4-1 0 0     6 0 0-1

BA2_BA1_IN5         120.087(1)         4-1 0 0     7 0 0-1

BA2_BA1_IN5         129.498(1)         4-1 0 0     8 0 0-1

BA2_BA1_O7          132.733(2)         4-1 0 0     1 0 0 0

BA2_BA1_O7           94.611(0)         4-1 0 0     2 0 0 0

BA2_BA1_O7           47.267(2)         4-1 0 0     3 0 0 0

BA2_BA1_O7           85.389(0)         4-1 0 0     4 0 0 0

BA2_BA1_O7           94.611(0)         4-1 0 0     5 0 0-1

BA2_BA1_O7           47.267(2)         4-1 0 0     6 0 0-1

BA2_BA1_O7           85.389(0)         4-1 0 0     7 0 0-1

BA2_BA1_O8          132.733(3)         4-1 0 0     8 0 0-1

IN5_BA1_IN5          69.872(2)         1 0 0 0     2 0 0 0

IN5_BA1_IN5         108.165(4)         1 0 0 0     3 0 0 0

IN5_BA1_IN5          69.872(2)         1 0 0 0     4 0 0 0

IN5_BA1_IN5         180.000(0)         1 0 0 0     5 0 0-1

IN5_BA1_IN5         110.128(2)         1 0 0 0     6 0 0-1

IN5_BA1_IN5          71.835(4)         1 0 0 0     7 0 0-1

IN5_BA1_IN5         110.128(2)         1 0 0 0     8 0 0-1

IN5_BA1_O7           34.954(1)         1 0 0 0     1 0 0 0

IN5_BA1_O7           87.880(4)         1 0 0 0     2 0 0 0

IN5_BA1_O7           87.880(4)         1 0 0 0     3 0 0 0

IN5_BA1_O7           34.954(1)         1 0 0 0     4 0 0 0

IN5_BA1_O7          145.046(1)         1 0 0 0     5 0 0-1

IN5_BA1_O7          145.046(1)         1 0 0 0     6 0 0-1

IN5_BA1_O7           92.120(4)         1 0 0 0     7 0 0-1

IN5_BA1_O8           92.120(6)         1 0 0 0     8 0 0-1

IN5_BA1_IN5          69.872(2)         2 0 0 0     3 0 0 0

IN5_BA1_IN5         108.165(4)         2 0 0 0     4 0 0 0

IN5_BA1_IN5         110.128(2)         2 0 0 0     5 0 0-1

IN5_BA1_IN5         180.000(0)         2 0 0 0     6 0 0-1

IN5_BA1_IN5         110.128(2)         2 0 0 0     7 0 0-1

IN5_BA1_IN5          71.835(4)         2 0 0 0     8 0 0-1

IN5_BA1_O7           34.954(1)         2 0 0 0     1 0 0 0

IN5_BA1_O7           34.954(1)         2 0 0 0     2 0 0 0

IN5_BA1_O7           87.880(4)         2 0 0 0     3 0 0 0

IN5_BA1_O7           87.880(4)         2 0 0 0     4 0 0 0

IN5_BA1_O7           92.120(4)         2 0 0 0     5 0 0-1

IN5_BA1_O7          145.046(1)         2 0 0 0     6 0 0-1

IN5_BA1_O7          145.046(1)         2 0 0 0     7 0 0-1

IN5_BA1_O8           92.120(6)         2 0 0 0     8 0 0-1

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  29

Angle             Degrees         atom 1 loc  atom 3 loc

IN5_BA1_IN5          69.872(2)         3 0 0 0     4 0 0 0

IN5_BA1_IN5          71.835(4)         3 0 0 0     5 0 0-1

IN5_BA1_IN5         110.128(2)         3 0 0 0     6 0 0-1

IN5_BA1_IN5         180.000(0)         3 0 0 0     7 0 0-1

IN5_BA1_IN5         110.128(2)         3 0 0 0     8 0 0-1

IN5_BA1_O7           87.880(4)         3 0 0 0     1 0 0 0

IN5_BA1_O7           34.954(1)         3 0 0 0     2 0 0 0

IN5_BA1_O7           34.954(1)         3 0 0 0     3 0 0 0

IN5_BA1_O7           87.880(4)         3 0 0 0     4 0 0 0

IN5_BA1_O7           92.120(4)         3 0 0 0     5 0 0-1

IN5_BA1_O7           92.120(4)         3 0 0 0     6 0 0-1

IN5_BA1_O7          145.046(1)         3 0 0 0     7 0 0-1

IN5_BA1_O8          145.046(8)         3 0 0 0     8 0 0-1

IN5_BA1_IN5         110.128(2)         4 0 0 0     5 0 0-1

IN5_BA1_IN5          71.835(4)         4 0 0 0     6 0 0-1

IN5_BA1_IN5         110.128(2)         4 0 0 0     7 0 0-1

IN5_BA1_IN5         180.000(0)         4 0 0 0     8 0 0-1

IN5_BA1_O7           87.880(4)         4 0 0 0     1 0 0 0

IN5_BA1_O7           87.880(4)         4 0 0 0     2 0 0 0

IN5_BA1_O7           34.954(1)         4 0 0 0     3 0 0 0

IN5_BA1_O7           34.954(1)         4 0 0 0     4 0 0 0

IN5_BA1_O7          145.046(1)         4 0 0 0     5 0 0-1

IN5_BA1_O7           92.120(4)         4 0 0 0     6 0 0-1

IN5_BA1_O7           92.120(4)         4 0 0 0     7 0 0-1

IN5_BA1_O8          145.046(8)         4 0 0 0     8 0 0-1

IN5_BA1_IN5          69.872(2)         5 0 0-1     6 0 0-1

IN5_BA1_IN5         108.165(4)         5 0 0-1     7 0 0-1

IN5_BA1_IN5          69.872(2)         5 0 0-1     8 0 0-1

IN5_BA1_O7          145.046(1)         5 0 0-1     1 0 0 0

IN5_BA1_O7           92.120(4)         5 0 0-1     2 0 0 0

IN5_BA1_O7           92.120(4)         5 0 0-1     3 0 0 0

IN5_BA1_O7          145.046(1)         5 0 0-1     4 0 0 0

IN5_BA1_O7           34.954(1)         5 0 0-1     5 0 0-1

IN5_BA1_O7           34.954(1)         5 0 0-1     6 0 0-1

IN5_BA1_O7           87.880(4)         5 0 0-1     7 0 0-1

IN5_BA1_O8           87.880(2)         5 0 0-1     8 0 0-1

IN5_BA1_IN5          69.872(2)         6 0 0-1     7 0 0-1

IN5_BA1_IN5         108.165(4)         6 0 0-1     8 0 0-1

IN5_BA1_O7          145.046(1)         6 0 0-1     1 0 0 0

IN5_BA1_O7          145.046(1)         6 0 0-1     2 0 0 0

IN5_BA1_O7           92.120(4)         6 0 0-1     3 0 0 0

IN5_BA1_O7           92.120(4)         6 0 0-1     4 0 0 0

IN5_BA1_O7           87.880(4)         6 0 0-1     5 0 0-1

IN5_BA1_O7           34.954(1)         6 0 0-1     6 0 0-1

IN5_BA1_O7           34.954(1)         6 0 0-1     7 0 0-1

IN5_BA1_O8           87.880(2)         6 0 0-1     8 0 0-1

IN5_BA1_IN5          69.872(2)         7 0 0-1     8 0 0-1

IN5_BA1_O7           92.120(4)         7 0 0-1     1 0 0 0

IN5_BA1_O7          145.046(1)         7 0 0-1     2 0 0 0

IN5_BA1_O7          145.046(1)         7 0 0-1     3 0 0 0

IN5_BA1_O7           92.120(4)         7 0 0-1     4 0 0 0

IN5_BA1_O7           87.880(4)         7 0 0-1     5 0 0-1

IN5_BA1_O7           87.880(4)         7 0 0-1     6 0 0-1

IN5_BA1_O7           34.954(1)         7 0 0-1     7 0 0-1

IN5_BA1_O8           34.954(1)         7 0 0-1     8 0 0-1

IN5_BA1_O7           92.120(4)         8 0 0-1     1 0 0 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  30

Angle             Degrees         atom 1 loc  atom 3 loc

IN5_BA1_O7           92.120(4)         8 0 0-1     2 0 0 0

IN5_BA1_O7          145.046(1)         8 0 0-1     3 0 0 0

IN5_BA1_O7          145.046(1)         8 0 0-1     4 0 0 0

IN5_BA1_O7           34.954(1)         8 0 0-1     5 0 0-1

IN5_BA1_O7           87.880(4)         8 0 0-1     6 0 0-1

IN5_BA1_O7           87.880(4)         8 0 0-1     7 0 0-1

IN5_BA1_O8           34.954(1)         8 0 0-1     8 0 0-1

O7_BA1_O7           57.787(3)         1 0 0 0     2 0 0 0

O7_BA1_O7           86.208(5)         1 0 0 0     3 0 0 0

O7_BA1_O7           57.787(3)         1 0 0 0     4 0 0 0

O7_BA1_O7          122.213(3)         1 0 0 0     5 0 0-1

O7_BA1_O7          180.000(0)         1 0 0 0     6 0 0-1

O7_BA1_O7          122.213(3)         1 0 0 0     7 0 0-1

O7_BA1_O8           93.792(7)         1 0 0 0     8 0 0-1

O7_BA1_O7           57.787(3)         2 0 0 0     3 0 0 0

O7_BA1_O7           86.208(5)         2 0 0 0     4 0 0 0

O7_BA1_O7           93.792(5)         2 0 0 0     5 0 0-1

O7_BA1_O7          122.213(3)         2 0 0 0     6 0 0-1

O7_BA1_O7          179.960(0)         2 0 0 0     7 0 0-1

O7_BA1_O8          122.213(7)         2 0 0 0     8 0 0-1

O7_BA1_O7           57.787(3)         3 0 0 0     4 0 0 0

O7_BA1_O7          122.213(3)         3 0 0 0     5 0 0-1

O7_BA1_O7           93.792(5)         3 0 0 0     6 0 0-1

O7_BA1_O7          122.213(3)         3 0 0 0     7 0 0-1

O7_BA1_O8          179.960(5)         3 0 0 0     8 0 0-1

O7_BA1_O7          179.960(0)         4 0 0 0     5 0 0-1

O7_BA1_O7          122.213(3)         4 0 0 0     6 0 0-1

O7_BA1_O7           93.792(5)         4 0 0 0     7 0 0-1

O7_BA1_O8          122.213(7)         4 0 0 0     8 0 0-1

O7_BA1_O7           57.787(3)         5 0 0-1     6 0 0-1

O7_BA1_O7           86.208(5)         5 0 0-1     7 0 0-1

O7_BA1_O8           57.787(1)         5 0 0-1     8 0 0-1

O7_BA1_O7           57.787(3)         6 0 0-1     7 0 0-1

O7_BA1_O8           86.208(2)         6 0 0-1     8 0 0-1

O7_BA1_O8           57.787(1)         7 0 0-1     8 0 0-1

Vector         Length           Optr Cell        Neighbor atom coordinates

BA2_BA1         4.31417(16)        1 0 1 0      .00000   1.00000    .00000

BA2_BA1         4.31421(16)      105 0 0-1      .50000    .50000    .00000

BA2_BA2         4.37629(29)        6 1 1-1      .22038    .72038   -.50000

BA2_BA2         4.37629(29)        6 1 1 0      .22038    .72038    .50000

BA2_CU4         2.98081(11)        1 0 0 0      .10567    .60568    .00000

BA2_IN5         3.44447(12)        1 0 1 0      .24250   1.00000    .25000

BA2_IN5         4.01031(13)        4 0 1 0      .00000    .75750    .25000

BA2_IN5         4.01031(13)        6 0 1-1      .00000    .75750   -.25000

BA2_IN5         3.44447(12)        7 0 1-1      .24250   1.00000   -.25000

BA2_IN5         3.44449(12)      102 0 0-1      .50000    .74250   -.25000

BA2_IN5         4.01033(13)      103 0 0-1      .25750    .50000   -.25000

BA2_IN5         4.01033(13)      105 0 0-1      .25750    .50000    .25000

BA2_IN5         3.44449(12)      108 0 0-1      .50000    .74250    .25000

BA2_O6          2.95350(13)        6 1 1-1      .39154    .89154   -.26380

BA2_O6          2.95350(13)       -8 1 1 1      .39154    .89154    .26380

BA2_O7          3.16890(12)        4 0 1 0      .11624    .88376    .25000

BA2_O7          3.16890(12)        7 0 1-1      .11624    .88376   -.25000

BA2_O7          3.16892(12)      102 0 0-1      .38376    .61624   -.25000

BA2_O7          3.16892(12)      105 0 0-1      .38376    .61624    .25000

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  31

Vector         Length           Optr Cell        Neighbor atom coordinates

BA2_O8          3.51901(13)        1 0 0 0      .22229    .49493    .00000

BA2_O8          2.60919(10)        4 0 1 0      .49493    .77771    .00000

BA2_O8          2.60916(10)      105 0 0-1      .27771    .99493    .00000

BA2_O8          3.51899(13)      108-1 0-1     -.00507    .72229    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_BA2_BA1         166.488(0)         1 0 1 0   105 0 0-1

BA1_BA2_BA2          88.436(0)         1 0 1 0     6 1 1-1

BA1_BA2_BA2          88.436(0)         1 0 1 0     6 1 1 0

BA1_BA2_CU4          83.244(0)         1 0 1 0     1 0 0 0

BA1_BA2_IN5          54.375(1)         1 0 1 0     1 0 1 0

BA1_BA2_IN5          54.375(1)         1 0 1 0     7 0 1-1

BA1_BA2_IN5         133.610(1)         1 0 1 0   102 0 0-1

BA1_BA2_IN5         133.610(2)         1 0 1 0   108 0 0-1

BA1_BA2_O6           94.382(0)         1 0 1 0     6 1 1-1

BA1_BA2_O8           94.382(2)         1 0 1 0    -8 1 1 1

BA1_BA2_O8          142.263(0)         1 0 1 0     4 0 1 0

BA1_BA2_O8           51.250(0)         1 0 1 0   105 0 0-1

BA1_BA2_BA2          88.436(0)       105 0 0-1     6 1 1-1

BA1_BA2_BA2          88.436(0)       105 0 0-1     6 1 1 0

BA1_BA2_CU4          83.244(0)       105 0 0-1     1 0 0 0

BA1_BA2_IN5         133.610(1)       105 0 0-1     1 0 1 0

BA1_BA2_IN5         133.610(2)       105 0 0-1     7 0 1-1

BA1_BA2_IN5          54.374(1)       105 0 0-1   102 0 0-1

BA1_BA2_IN5          54.374(1)       105 0 0-1   108 0 0-1

BA1_BA2_O6           94.382(0)       105 0 0-1     6 1 1-1

BA1_BA2_O8           94.382(2)       105 0 0-1    -8 1 1 1

BA1_BA2_O8           51.249(0)       105 0 0-1     4 0 1 0

BA1_BA2_O8          142.262(2)       105 0 0-1   105 0 0-1

BA2_BA2_BA2         153.177(2)         6 1 1-1     6 1 1 0

BA2_BA2_CU4          76.588(1)         6 1 1-1     1 0 0 0

BA2_BA2_IN5         134.977(3)         6 1 1-1     1 0 1 0

BA2_BA2_IN5          60.307(3)         6 1 1-1     7 0 1-1

BA2_BA2_IN5          60.308(3)         6 1 1-1   102 0 0-1

BA2_BA2_IN5         134.977(2)         6 1 1-1   108 0 0-1

BA2_BA2_O6           53.909(3)         6 1 1-1     6 1 1-1

BA2_BA2_O8          152.914(11)        6 1 1-1    -8 1 1 1

BA2_BA2_O8           99.355(1)         6 1 1-1     4 0 1 0

BA2_BA2_O8           99.355(1)         6 1 1-1   105 0 0-1

BA2_BA2_CU4          76.588(1)         6 1 1 0     1 0 0 0

BA2_BA2_IN5          60.307(3)         6 1 1 0     1 0 1 0

BA2_BA2_IN5         134.977(2)         6 1 1 0     7 0 1-1

BA2_BA2_IN5         134.977(3)         6 1 1 0   102 0 0-1

BA2_BA2_IN5          60.308(3)         6 1 1 0   108 0 0-1

BA2_BA2_O6          152.914(1)         6 1 1 0     6 1 1-1

BA2_BA2_O8           53.909(3)         6 1 1 0    -8 1 1 1

BA2_BA2_O8           99.355(1)         6 1 1 0     4 0 1 0

BA2_BA2_O8           99.355(1)         6 1 1 0   105 0 0-1

CU4_BA2_IN5         117.122(1)         1 0 0 0     1 0 1 0

CU4_BA2_IN5         117.122(1)         1 0 0 0     7 0 1-1

CU4_BA2_IN5         117.122(1)         1 0 0 0   102 0 0-1

CU4_BA2_IN5         117.122(1)         1 0 0 0   108 0 0-1

CU4_BA2_O6          130.497(2)         1 0 0 0     6 1 1-1

CU4_BA2_O8          130.497(4)         1 0 0 0    -8 1 1 1

CU4_BA2_O8          134.493(0)         1 0 0 0     4 0 1 0

CU4_BA2_O8          134.494(2)         1 0 0 0   105 0 0-1

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  32

Angle             Degrees         atom 1 loc  atom 3 loc

IN5_BA2_IN5          76.331(5)         1 0 1 0     7 0 1-1

IN5_BA2_IN5         125.756(4)         1 0 1 0   102 0 0-1

IN5_BA2_IN5          79.668(3)         1 0 1 0   108 0 0-1

IN5_BA2_O6          100.011(4)         1 0 1 0     6 1 1-1

IN5_BA2_O8           40.007(1)         1 0 1 0    -8 1 1 1

IN5_BA2_O8           97.899(1)         1 0 1 0     4 0 1 0

IN5_BA2_O8           39.065(3)         1 0 1 0   105 0 0-1

IN5_BA2_IN5          79.668(3)         7 0 1-1   102 0 0-1

IN5_BA2_IN5         125.756(2)         7 0 1-1   108 0 0-1

IN5_BA2_O6           40.007(1)         7 0 1-1     6 1 1-1

IN5_BA2_O8          100.011(7)         7 0 1-1    -8 1 1 1

IN5_BA2_O8           97.899(0)         7 0 1-1     4 0 1 0

IN5_BA2_O8           39.065(2)         7 0 1-1   105 0 0-1

IN5_BA2_IN5          76.331(5)       102 0 0-1   108 0 0-1

IN5_BA2_O6           40.008(1)       102 0 0-1     6 1 1-1

IN5_BA2_O8          100.011(7)       102 0 0-1    -8 1 1 1

IN5_BA2_O8           39.065(3)       102 0 0-1     4 0 1 0

IN5_BA2_O8           97.899(1)       102 0 0-1   105 0 0-1

IN5_BA2_O6          100.011(4)       108 0 0-1     6 1 1-1

IN5_BA2_O8           40.008(1)       108 0 0-1    -8 1 1 1

IN5_BA2_O8           39.065(2)       108 0 0-1     4 0 1 0

IN5_BA2_O8           97.899(1)       108 0 0-1   105 0 0-1

O6_BA2_O8           99.006(8)         6 1 1-1    -8 1 1 1

O6_BA2_O8           62.927(1)         6 1 1-1     4 0 1 0

O6_BA2_O8           62.927(2)         6 1 1-1   105 0 0-1

O8_BA2_O8           62.927(4)        -8 1 1 1     4 0 1 0

O8_BA2_O8           62.927(4)        -8 1 1 1   105 0 0-1

O8_BA2_O8           91.013(1)         4 0 1 0   105 0 0-1

Vector         Length           Optr Cell        Neighbor atom coordinates

CU3_CU4         2.79463(12)        2 1 0 0      .39432    .10567    .00000

CU3_CU4         2.79463(12)        4 0 0 0      .60568   -.10567    .00000

CU3_CU4         2.79463(12)        6 1 0 0      .39432   -.10567    .50000

CU3_CU4         2.79463(12)        8 0 0 0      .60568    .10567    .50000

CU3_IN5         3.12033(12)        1 0 0 0      .24250    .00000    .25000

CU3_IN5         3.12033(12)        3 1 0 0      .75750    .00000    .25000

CU3_IN5         3.12033(12)      106 0 0-1      .50000    .25750    .25000

CU3_IN5         3.12033(12)      108 0-1-1      .50000   -.25750    .25000

CU3_O6          1.86238(7)         2 1 0 0      .39154    .10846    .23620

CU3_O6          1.86238(7)         4 0 0 0      .60846   -.10846    .23620

CU3_O6          1.86238(7)        -6 0 0 1      .60846    .10846    .26380

CU3_O6          1.86238(7)        -8 1 0 1      .39154   -.10846    .26380

Angle             Degrees         atom 1 loc  atom 3 loc

O6_CU3_O6          172.766(1)         2 1 0 0     4 0 0 0

O6_CU3_O6           90.229(0)         2 1 0 0    -6 0 0 1

O6_CU3_O6           90.227(0)         2 1 0 0    -8 1 0 1

O6_CU3_O6           90.227(0)         4 0 0 0    -6 0 0 1

O6_CU3_O6           90.229(0)         4 0 0 0    -8 1 0 1

O6_CU3_O6          172.767(1)        -6 0 0 1    -8 1 0 1

Vector         Length           Optr Cell        Neighbor atom coordinates

CU4_BA2         2.98081(11)        1 0 0 0      .27962    .77962    .00000

CU4_CU3         2.79463(12)        2 0 0 0      .00000    .50000    .25000

CU4_CU3         2.79463(12)        6 0 1-1      .00000    .50000   -.25000

CU4_IN5         3.09111(12)        4 0 1 0      .00000    .75750    .25000

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  33

Vector         Length           Optr Cell        Neighbor atom coordinates

CU4_IN5         3.09111(12)        6 0 1-1      .00000    .75750   -.25000

CU4_IN5         3.09112(12)      103 0 0-1      .25750    .50000   -.25000

CU4_IN5         3.09112(12)      105 0 0-1      .25750    .50000    .25000

CU4_O6          2.01155(14)        1 0 0 0      .10846    .60846    .23620

CU4_O6          2.01155(14)       -3 0 0 0      .10846    .60846   -.23620

CU4_O8          1.94877(7)         1 0 0 0      .22229    .49493    .00000

CU4_O8          1.94876(7)       108-1 0-1     -.00507    .72229    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

IN5_CU4_O6           88.641(3)         1 0 0 0     1 0 0 0

IN5_CU4_O6           88.641(3)         1 0 0 0    -3 0 0 0

IN5_CU4_O8           88.523(3)         1 0 0 0     1 0 0 0

IN5_CU4_O8           88.522(3)         1 0 0 0   108-1 0-1

O6_CU4_O6          177.281(0)         1 0 0 0    -3 0 0 0

O6_CU4_O8           89.965(0)         1 0 0 0     1 0 0 0

O6_CU4_O8           89.965(0)         1 0 0 0   108-1 0-1

O6_CU4_O8           89.965(0)        -3 0 0 0     1 0 0 0

O6_CU4_O8           89.965(0)        -3 0 0 0   108-1 0-1

O8_CU4_O8          177.045(0)         1 0 0 0   108-1 0-1

Vector         Length           Optr Cell        Neighbor atom coordinates

IN5_BA1         3.62838(12)        1 0 0 0      .00000    .00000    .00000

IN5_BA1         3.62838(12)        5 0 0 0      .00000    .00000    .50000

IN5_BA2         3.44447(12)        1 0-1 0      .27962   -.22038    .00000

IN5_BA2         4.01031(13)        2 1 0 0      .22038    .27962    .00000

IN5_BA2         4.01031(13)        6 1 0 0      .22038   -.27962    .50000

IN5_BA2         3.44447(12)        7 0 1 0      .27962    .22038    .50000

IN5_CU3         3.12033(12)        1 0 0 0      .50000    .00000    .25000

IN5_CU4         3.09111(12)        2 1 0 0      .39432    .10567    .00000

IN5_CU4         3.09111(12)        6 1 0 0      .39432   -.10567    .50000

IN5_O6          2.23671(8)         2 1 0 0      .39154    .10846    .23620

IN5_O6          2.23671(8)        -8 1 0 1      .39154   -.10846    .26380

IN5_O7          2.07960(8)         1 0 0 0      .11624    .11624    .25000

IN5_O7          2.07960(8)         4 0 0 0      .11624   -.11624    .25000

IN5_O8          2.17170(15)      103 0 0 0      .27771    .00507    .50000

IN5_O8          2.17170(15)      105 0-1-1      .27771   -.00507    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_IN5_BA1          71.835(4)         1 0 0 0     5 0 0 0

BA1_IN5_BA2          75.123(2)         1 0 0 0     1 0-1 0

BA1_IN5_CU4         117.921(2)         1 0 0 0     7 0 1 0

BA1_IN5_O6          128.544(2)         1 0 0 0     2 1 0 0

BA1_IN5_O6          133.215(1)         1 0 0 0    -8 1 0 1

BA1_IN5_O7           53.431(1)         1 0 0 0     1 0 0 0

BA1_IN5_O7           53.431(1)         1 0 0 0     4 0 0 0

BA1_IN5_O8          137.229(1)         1 0 0 0   103 0 0 0

BA1_IN5_O8           65.430(3)         1 0 0 0   105 0-1-1

BA1_IN5_BA2         117.921(3)         5 0 0 0     1 0-1 0

BA1_IN5_CU4          75.123(3)         5 0 0 0     7 0 1 0

BA1_IN5_O6          133.215(1)         5 0 0 0     2 1 0 0

BA1_IN5_O6          128.544(2)         5 0 0 0    -8 1 0 1

BA1_IN5_O7           53.431(1)         5 0 0 0     1 0 0 0

BA1_IN5_O7           53.431(1)         5 0 0 0     4 0 0 0

BA1_IN5_O8           65.430(3)         5 0 0 0   103 0 0 0

BA1_IN5_O8          137.229(1)         5 0 0 0   105 0-1-1

BA2_IN5_CU4         164.994(2)         1 0-1 0     7 0 1 0

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  34

Angle             Degrees         atom 1 loc  atom 3 loc

BA2_IN5_O6          108.522(1)         1 0-1 0     2 1 0 0

BA2_IN5_O6           58.093(2)         1 0-1 0    -8 1 0 1

BA2_IN5_O7          128.405(1)         1 0-1 0     1 0 0 0

BA2_IN5_O7           64.590(1)         1 0-1 0     4 0 0 0

BA2_IN5_O8          127.008(4)         1 0-1 0   103 0 0 0

BA2_IN5_O8           49.214(2)         1 0-1 0   105 0-1-1

CU4_IN5_O6           58.093(1)         7 0 1 0     2 1 0 0

CU4_IN5_O6          108.522(2)         7 0 1 0    -8 1 0 1

CU4_IN5_O7           64.590(0)         7 0 1 0     1 0 0 0

CU4_IN5_O7          128.405(2)         7 0 1 0     4 0 0 0

CU4_IN5_O8           49.214(2)         7 0 1 0   103 0 0 0

CU4_IN5_O8          127.008(2)         7 0 1 0   105 0-1-1

O6_IN5_O6           72.304(0)         2 1 0 0    -8 1 0 1

O6_IN5_O7          101.304(0)         2 1 0 0     1 0 0 0

O6_IN5_O7          172.755(0)         2 1 0 0     4 0 0 0

O6_IN5_O8           82.888(1)         2 1 0 0   103 0 0 0

O6_IN5_O8           78.842(0)         2 1 0 0   105 0-1-1

O6_IN5_O7          172.755(0)        -8 1 0 1     1 0 0 0

O6_IN5_O7          101.304(0)        -8 1 0 1     4 0 0 0

O6_IN5_O8           78.842(0)        -8 1 0 1   103 0 0 0

O6_IN5_O8           82.888(1)        -8 1 0 1   105 0-1-1

O7_IN5_O7           85.273(0)         1 0 0 0     4 0 0 0

O7_IN5_O8           97.203(1)         1 0 0 0   103 0 0 0

O7_IN5_O8           99.423(1)         1 0 0 0   105 0-1-1

O7_IN5_O8           99.423(1)         4 0 0 0   103 0 0 0

O7_IN5_O8           97.203(1)         4 0 0 0   105 0-1-1

O8_IN5_O8          157.335(2)       103 0 0 0   105 0-1-1

Vector         Length           Optr Cell        Neighbor atom coordinates

O6_BA2         2.95350(13)        6 1 1 0      .22038    .72038    .50000

O6_CU3         1.86238(7)         2 0 0 0      .00000    .50000    .25000

O6_CU4         2.01155(14)        1 0 0 0      .10567    .60568    .00000

O6_IN5         2.23671(8)         4 0 1 0      .00000    .75750    .25000

O6_IN5         2.23674(8)       105 0 0-1      .25750    .50000    .25000

Angle             Degrees         atom 1 loc  atom 3 loc

BA2_O6_CU3          126.880(3)         6 1 1 0     2 0 0 0

BA2_O6_CU4          140.862(2)         6 1 1 0     1 0 0 0

BA2_O6_IN5           81.900(0)         6 1 1 0     4 0 1 0

BA2_O6_IN5           81.900(0)         6 1 1 0   105 0 0-1

CU3_O6_CU4           92.257(0)         2 0 0 0     1 0 0 0

CU3_O6_IN5           98.734(0)         2 0 0 0     4 0 1 0

CU3_O6_IN5           98.733(0)         2 0 0 0   105 0 0-1

CU4_O6_IN5           93.222(0)         1 0 0 0     4 0 1 0

CU4_O6_IN5           93.221(0)         1 0 0 0   105 0 0-1

IN5_O6_IN5          161.110(0)         4 0 1 0   105 0 0-1

Vector         Length           Optr Cell        Neighbor atom coordinates

O7_BA1         2.91526(12)        1 0 0 0      .00000    .00000    .00000

O7_BA1         2.91526(12)        5 0 0 0      .00000    .00000    .50000

O7_BA2         3.16890(12)        2 1 0 0      .22038    .27962    .00000

O7_BA2         3.16890(12)        7 0 1 0      .27962    .22038    .50000

O7_IN5         2.07960(8)         1 0 0 0      .24250    .00000    .25000

O7_IN5         2.07960(8)         2 0 0 0      .00000    .24250    .25000

1Ba3Cu3In2Sc2O12                                                    DISAGL   Version MS-DOS 2000-10-12T13:00:20  Page  35

Angle             Degrees         atom 1 loc  atom 3 loc

BA1_O7_BA2           93.792(5)         1 0 0 0     5 0 0 0

BA1_O7_IN5           91.615(0)         1 0 0 0     1 0 0 0

BA1_O7_IN5           91.615(0)         1 0 0 0     2 0 0 0

BA2_O7_IN5           91.615(0)         5 0 0 0     1 0 0 0

BA2_O7_IN5           91.615(0)         5 0 0 0     2 0 0 0

IN5_O7_IN5          175.273(0)         1 0 0 0     2 0 0 0

Vector         Length           Optr Cell        Neighbor atom coordinates

O8_BA1         3.36579(13)      105 0 0-1      .50000    .50000    .00000

O8_BA2         3.51901(13)        1 0 0 0      .27962    .77962    .00000

O8_BA2         2.60919(10)        2 1 0 0      .22038    .27962    .00000

O8_CU4         1.94877(7)         1 0 0 0      .10567    .60568    .00000

O8_IN5         2.17170(15)      103 0 0-1      .25750    .50000   -.25000

O8_IN5         2.17170(15)      105 0 0-1      .25750    .50000    .25000

Angle             Degrees         atom 1 loc  atom 3 loc

BA2_O8_CU4          133.016(0)         2 1 0 0     1 0 0 0

BA2_O8_IN5           91.721(0)         2 1 0 0   103 0 0-1

BA2_O8_IN5           91.721(0)         2 1 0 0   105 0 0-1

CU4_O8_IN5           97.065(1)         1 0 0 0   103 0 0-1

CU4_O8_IN5           97.065(1)         1 0 0 0   105 0 0-1

IN5_O8_IN5          157.098(2)       103 0 0-1   105 0 0-1

Supplementary Material (ESI) for Journal of Materials Chemistry

This journal is (c) The Royal Society of Chemistry 2001