--------------------------------------------------------------

Archiving C:/GSAS/phil/in2sc2/IN2SC2.EXP as C:/GSAS/phil/in2sc2/IN2SC2!326.EXP

--------------------------------------------------------------

1Ba3Cu3In2Sc2O12                                                             Version        2000-10-10T10:24:55  Page   1

|---------------------------------------------------------|

|              Program POWPREF Version MS-DOS             |

| Prepares powder histograms for least-squares refinement |

|         Distributed on 15/ 7/1999; 0:31:36              |

|---------------------------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY599 EXPEDT  MS-DOS 2000-10-10T10:24:50                          D  C

Data for bank  1 read from file c:\gsas\phil\in2sc2\in2sc2.dat

The powder pattern has  5739 channels with   1 bins per channel

No fixed background points for this powder pattern

The  2 excluded regions are (in deg):

Exclude    from:       to:     from:       to:     from:       to:     from:       to:

.0000     .0000  120.0000 1000.0000

Incident spectrum type  0 can be used in the region     .000 deg to  180.000 deg

The minimum possible weighted residual for this histogram is    .0305

Histogram no.  1 on file IN2SC2.P01

updated with new excluded regions, background and incident spectrum data.

CPU time =    .11 to update histogram

Lattice parameters for phase 1 are:

a,b,c  = 11.996930 11.996930  8.447299  angles =    90.000    90.000    90.000

volume =  1215.789

Lattice parameters for phase 2 are:

a,b,c  = 10.113310 10.113310 10.113310  angles =    90.000    90.000    90.000

volume =  1034.380

Lattice parameters for phase 3 are:

a,b,c  = 12.117780 12.117780  8.513771  angles =    90.000    90.000    90.000

volume =  1250.167

Profile function 3 for phase no. 1 has the coefficients p1-p19:

.769344E+03   -.923823E+02    .874152E+00    .135541E+02

.735617E+01    .000000E+00    .500000E-03    .500000E-03

-.462270E+01    .158866E+01    .134424E+02   -.153688E+01

.000000E+00   -.263286E-01   -.582296E-02   -.341331E+00

.000000E+00    .000000E+00    .000000E+00

cutoff on the wings at  .010 of maximum

Profile function 3 for phase no. 2 has the coefficients p1-p19:

.671019E+02   -.595524E+02    .196186E+02    .000000E+00

.362423E+01    .000000E+00    .500000E-03    .500000E-03

-.615572E+00    .182760E+00    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00

cutoff on the wings at  .010 of maximum

Profile function 3 for phase no. 3 has the coefficients p1-p19:

.467690E+03    .961304E+01    .864576E+01    .346032E+01

.261419E+01    .000000E+00    .500000E-03    .500000E-03

-.174447E+02    .271460E+01    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00

cutoff on the wings at  .010 of maximum

Minimum d-spacing used to generate reflections    .8796 for phase 1

Minimum d-spacing used to generate reflections    .8758 for phase 2

Minimum d-spacing used to generate reflections    .8695 for phase 3

Minimum d-spacing used to generate reflections    .9886 for phase 1

Minimum d-spacing used to generate reflections    .9848 for phase 2

Minimum d-spacing used to generate reflections    .9781 for phase 3

Minimum d-spacing for matching reflections    .8894

Estimated number of reflections to be generated is  1931

Number of reflections generated for phase 1 is   544

Number of reflections generated for phase 2 is   322

Number of reflections generated for phase 3 is   574

Total number of reflections generated for all phases is  1440

CPU time =    .06 sec. to generate reflections.

CPU time =   1.31 sec. to locate reflection limits.

CPU time =    .06 sec. to match reflection ranges to powder pattern

The maximum number of reflections contributing to any profile point is   88

CPU time =    .05 sec. to update file

1Ba3Cu3In2Sc2O12                                                             Version        2000-10-10T10:25:02  Page   1

|----------------------------------------------------|

|            Program GENLES Version MS-DOS           |

|    General crystal structure refinement program    |

| Magnetic structure refinement added by M. Yethiraj |

|   Revised and corrected by Larson and Von Dreele   |

|      Distributed on 15/ 7/1999; 0:28:26            |

|----------------------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The experiment file is: IN2SC2.EXP

The last history record is :

HSTRY600 POWPREF MS-DOS 2000-10-10T10:24:55

Maximum number of cycles is    6

I/SigI cut-off is  1.00

Structure factors will be extracted from histogram  1

using extraction method codes     0    0    0    0    0    0    0    0    0

The atomic and magnetic scattering factors for  5 types of atoms are:

Atom type   b-len   a(1)      b(1)      a(2)      b(2)      a(3)      b(3)      a(4)      b(4)      c

BA           .525  20.33610   3.21600  19.29700    .27560  10.88800  20.20730   2.69590 167.20200   2.77310

CU           .772  13.33800   3.58280   7.16760    .24700   5.61580  11.39660   1.67350  64.81260   1.19100

IN           .406  19.16240    .54760  18.55960   6.37760   4.29480  25.84990   2.03960  92.80290   4.93910

SC          1.230   9.18900   9.02130   7.36790    .57290   1.64090 136.10800   1.46800  51.35310   1.33290

O            .581   3.04850  13.27710   2.28680   5.70110   1.54630    .32390    .86700  32.90890    .25080

Atom type  CrKa f'      f"   FeKa f'      f"   CuKa f'      f"   MoKa f'      f"   AgKa f'      f"

BA         -11.460    9.980   -4.830   12.160   -1.330    8.460    -.610    2.280    -.980    1.500

CU           -.795    1.196   -1.129     .888   -2.019     .589     .263    1.266     .265     .826

IN          -1.788    9.627    -.626    7.356    -.126    5.045    -.936    1.310   -1.493     .854

SC           -.717    2.968    -.038    2.256     .285    1.533     .226     .372     .156     .235

O             .090     .073     .069     .052     .047     .032     .008     .006     .003     .004

Space group   I4/mcm

The lattice is centric  I-centered tetragonal    Laue symmetry 4/mmm

Multiplicity of a general site is  32

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)    -Y      X      Z

( 3)    -X     -Y      Z  ( 4)     Y     -X      Z

( 5)    -X      Y  1/2+Z  ( 6)    -Y     -X  1/2+Z

( 7)     X     -Y  1/2+Z  ( 8)     Y      X  1/2+Z

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:02  Page   2

The atom positions read in are

Type seq. At. name  mult   symm  frac   pn    X    pn    Y    pn    Z    pn  u11 pn  u22 pn  u33 pn  u12 pn  u13 pn  u23 pn

BA      1 BA1         44/M(001) 1.0000   0  .0000   0  .0000   0  .0000   0  .6   1

BA      2 BA2         8MM2(110) 1.0000   0  .2782   2  .7782   3  .0000   0  .6   4

CU      3 CU3         4-42M 001 1.0000   0  .5000   0  .0000   0  .2500   0  .7   5

CU      4 CU4         8MM2(110) 1.0000   0  .1059   6  .6059   7  .0000   0  .3   8

IN      5 IN5        16  2(100)  .4217   9  .2416  10  .0000   0  .2500   0  .2   0

SC      6 SC6        16  2(100)  .5783  11  .2416  12  .0000   0  .2500   0  .2   0

O       7 O7         16  M(+-0) 1.0000   0  .1171  13  .6171  14  .2258  15  .2   0

O       8 O8         16  2(110) 1.0000   0  .1266  16  .1266  17  .2500   0  .2   0

O       9 O9         16  M(001) 1.0000   0  .2359  18  .5019  19  .0000   0  .2   0

Space group   I 21 3

The lattice is acentric  I-centered cubic         Laue symmetry m 3

Multiplicity of a general site is  24

The equivalent positions are:

( 1)     X      Y      Z  ( 2)     Z      X      Y  ( 3)     Y      Z      X

( 4) 1/2+X  1/2-Y     -Z  ( 5)    -Z  1/2+X  1/2-Y  ( 6) 1/2-Y     -Z  1/2+X

( 7) 1/2-Z     -X  1/2+Y  ( 8) 1/2+Y  1/2-Z     -X  ( 9)    -Y  1/2+Z  1/2-X

(10) 1/2-X     -Y  1/2+Z  (11) 1/2+Z  1/2-X     -Y  (12)    -X  1/2+Y  1/2-Z

The atom positions read in are

Type seq. At. name  mult   symm  frac   pn    X    pn    Y    pn    Z    pn  u11 pn  u22 pn  u33 pn  u12 pn  u13 pn  u23 pn

IN      1 IN1         8  3(111) 1.0000   0  .2500   0  .2500   0  .2500   023.9   0

IN      2 IN2        12  2(100) 1.0000   0 -.0216   0  .0000   0  .2500   0 1.0   0

IN      3 IN3        12  2(100) 1.0000   0  .4999   0  .0000   0  .2500   014.6   0

O       4 O4         24    1    1.0000   0  .1250   0  .1350   0  .3950   0 1.8   0

O       5 O5         24    1    1.0000   0  .1000   0  .3580   0  .3730   0 1.8   0

Space group   I 4/mcm

The lattice is centric  I-centered tetragonal    Laue symmetry 4/mmm

Multiplicity of a general site is  32

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)    -Y      X      Z

( 3)    -X     -Y      Z  ( 4)     Y     -X      Z

( 5)    -X      Y  1/2+Z  ( 6)    -Y     -X  1/2+Z

( 7)     X     -Y  1/2+Z  ( 8)     Y      X  1/2+Z

The atom positions read in are

Type seq. At. name  mult   symm  frac   pn    X    pn    Y    pn    Z    pn  u11 pn  u22 pn  u33 pn  u12 pn  u13 pn  u23 pn

BA      1 BA1         44/M(001) 1.0000   0  .0000   0  .0000   0  .0000   0 1.2   0

BA      2 BA2         8MM2(110) 1.0000   0  .2796   0  .7796   0  .0000   0  .6   0

CU      3 CU3         4-42M 001 1.0000   0  .5000   0  .0000   0  .2500   0 2.2   0

CU      4 CU4         8MM2(110) 1.0000   0  .1057   0  .6057   0  .0000   0  .2   0

IN      5 IN5        16  2(100) 1.0000   0  .2425   0  .0000   0  .2500   0  .2   0

O       6 O6         16  M(+-0) 1.0000   0  .1085   0  .6085   0  .2362   0  .6   0

O       7 O7         16  2(110) 1.0000   0  .1162   0  .1162   0  .2500   0  .6   0

O       8 O8         16  M(001) 1.0000   0  .2223   0  .4949   0  .0000   0  .6   0

Constraints read are LNCN   1 1  5X     1.0000 1  6X     1.0000

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:02  Page   3

LNCN   2 1  5UISO  1.0000 1  6UISO  1.0000

Parameter missing - 1  5UISO

Parameter missing - 1  6UISO

LNCN   3 1  5FRAC -1.0000 1  6FRAC  1.0000

LNCN   4 1  8UISO  1.0000 1  9UISO  1.0000

Parameter missing - 1  8UISO

Parameter missing - 1  9UISO

Lattice parameters for phase 1 are:

a         b         c          alpha      beta     gamma

11.996930 11.996930  8.447299   90.0000   90.0000   90.0000

These cell parameters will be refined

Reciprocal metric tensor elements:          damp= 0

Element :          g11   pn          g22   pn          g33   pn        2*g12   pn        2*g13   pn        2*g23   pn

Value   :   6.94800E-03  20   6.94800E-03  21   1.40141E-02  22  -1.69086E-10   0  -2.40137E-10   0  -2.40137E-10   0

Constr. :          1.000  1          1.000  1          1.000  2           .000  0           .000  0           .000  0

Lattice parameters for phase 2 are:

a         b         c          alpha      beta     gamma

10.113310 10.113310 10.113310   90.0000   90.0000   90.0000

These cell parameters will be refined

Reciprocal metric tensor elements:          damp= 0

Element :          g11   pn          g22   pn          g33   pn        2*g12   pn        2*g13   pn        2*g23   pn

Value   :   9.77718E-03  23   9.77718E-03  24   9.77718E-03  25  -2.37937E-10   0  -2.37937E-10   0  -2.37937E-10   0

Constr. :          1.000  3          1.000  3          1.000  3           .000  0           .000  0           .000  0

Lattice parameters for phase 3 are:

a         b         c          alpha      beta     gamma

12.117780 12.117780  8.513771   90.0000   90.0000   90.0000

These cell parameters will be refined

Reciprocal metric tensor elements:          damp= 0

Element :          g11   pn          g22   pn          g33   pn        2*g12   pn        2*g13   pn        2*g23   pn

Value   :   6.81011E-03  26   6.81011E-03  27   1.37961E-02  28  -1.65730E-10   0  -2.35886E-10   0  -2.35886E-10   0

Constr. :          1.000  4          1.000  4          1.000  5           .000  0           .000  0           .000  0

Phase/element fractions for phase no.  1

Hist Elm:    PXC   1 1   nc

Fraction:    .17401      29

Dmp/Cnst:    0     1.000  6

Phase/element fractions for phase no.  2

Hist Elm:    PXC   1 1   nc

Fraction:    .46435E-02  30

Dmp/Cnst:    0     1.000  7

Phase/element fractions for phase no.  3

Hist Elm:    PXC   1 1   nc

Fraction:    .26886E-01  31

Dmp/Cnst:    0     1.000  8

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:02  Page   4

Histogram scale factors:

Hist.   :        1  PXC  pn

Scale   :    67.391      32

Dmp/Cnst:    0     1.000  9

Absorption coefficients for powder data:

Hist/Typ:    1  PXC    0 pn

Absc 1. :    .00000       0

Dmp/Cnst:    0      .000  0

Absc 2. :    .00000       0

Dmp/Cnst:    0      .000  0

Diffractometer constants for powder data:

No. Type    Lam 1        Lam 2      Polariz.  pn Cnstr cn type    Zero  pn Cnstr cn    Kratio  pn Cnstr cn Damp

1  PXC  1.5405000    1.5443000       .50000   0  .000  0  0    -2.215  33 1.000 10     .5000   0  .000  0    0

Extinction coefficients for phase no.  1:

Hist.   :        1  PXC  pn

Extinct.:    .00000       0

Dmp/Cnst:    0      .000  0

Extinction coefficients for phase no.  2:

Hist.   :        1  PXC  pn

Extinct.:    .00000       0

Dmp/Cnst:    0      .000  0

Extinction coefficients for phase no.  3:

Hist.   :        1  PXC  pn

Extinct.:    .00000       0

Dmp/Cnst:    0      .000  0

Orientation distribution coefficients for powder data:

No ODF data for phase  1

No ODF data for phase  2

No ODF data for phase  3

Preferred orientation coeffs. for phase no.  1 histogram no.  1:

Axis    :        1       pn

Dir./typ:     .0  .0 1.0  0

PO ratio:        1.0000   0

Dmp/Cnst:    0      .000  0

PO frac.:        1.0000   0

Dmp/Cnst:    0      .000  0

Preferred orientation coeffs. for phase no.  2 histogram no.  1:

Axis    :        1       pn

Dir./typ:     .0  .0 1.0  0

PO ratio:        1.0000   0

Dmp/Cnst:    0      .000  0

PO frac.:        1.0000   0

Dmp/Cnst:    0      .000  0

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:02  Page   5

Preferred orientation coeffs. for phase no.  3 histogram no.  1:

Axis    :        1       pn

Dir./typ:     .0  .0 1.0  0

PO ratio:        1.0000   0

Dmp/Cnst:    0      .000  0

PO frac.:        1.0000   0

Dmp/Cnst:    0      .000  0

Profile coeff. for function type  3, phase no.  1 and histogram no.  1; aniso. axis   0.   0.   1.; damp= 0:

Coeff.  :      GU    pn      GV    pn      GW    pn      GP    pn      LX    pn      LY    pn     S/L    pn     H/L    pn

Value   : 7.693E+02   0-9.238E+01   0 8.742E-01   0 1.355E+01   0 7.356E+00   0 0.000E+00   0 5.000E-04   0 5.000E-04   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     trns   pn     shft   pn     stec   pn     ptec   pn     sfec   pn     L11    pn     L22    pn     L33    pn

Value   :-4.623E+00   0 1.589E+00   0 1.344E+01   0-1.537E+00   0 0.000E+00   0-2.633E-02   0-5.823E-03   0-3.413E-01   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     L12    pn     L13    pn     L23    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0

Profile coeff. for function type  3, phase no.  2 and histogram no.  1; aniso. axis   0.   0.   1.; damp= 0:

Coeff.  :      GU    pn      GV    pn      GW    pn      GP    pn      LX    pn      LY    pn     S/L    pn     H/L    pn

Value   : 6.710E+01   0-5.955E+01   0 1.962E+01   0 0.000E+00   0 3.624E+00   0 0.000E+00   0 5.000E-04   0 5.000E-04   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     trns   pn     shft   pn     stec   pn     ptec   pn     sfec   pn     L11    pn     L22    pn     L33    pn

Value   :-6.156E-01   0 1.828E-01   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     L12    pn     L13    pn     L23    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0

Profile coeff. for function type  3, phase no.  3 and histogram no.  1; aniso. axis   0.   0.   1.; damp= 0:

Coeff.  :      GU    pn      GV    pn      GW    pn      GP    pn      LX    pn      LY    pn     S/L    pn     H/L    pn

Value   : 4.677E+02   0 9.613E+00   0 8.646E+00   0 3.460E+00   0 2.614E+00   0 0.000E+00   0 5.000E-04   0 5.000E-04   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     trns   pn     shft   pn     stec   pn     ptec   pn     sfec   pn     L11    pn     L22    pn     L33    pn

Value   :-1.744E+01   0 2.715E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     L12    pn     L13    pn     L23    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0

Diffuse scattering coefficients for powder data:

No diffuse scattering coefficients for histogram    1

Background coefficients for powder data:

Histogram no.:    1 Damping factor:    0 Use all points: Y

Power series in Q**2n/n! and n!/Q**2n

Param.  :          1   pn          2   pn          3   pn          4   pn          5   pn          6   pn

Coeff.  :  .74904E+03  34 -.57456E+01  35  .39364E+02  36  .23824E+00  37 -.24918E+01  38 -.48815E-02  39

The constraint matrix has   39 terms

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:02  Page   6

Restraint data statistics:

Powder data statistics                Fitted         All               Average

Bank Ndata Sum(w*d**2)  wRp     Rp    wRp     Rp     DWd  Integral

Hstgm  1 PXC   1  5739  12183.      .0445  .0343  .0445  .0343   1.009    .967

Powder totals     5739  12183.      .0445  .0343  .0445  .0343   1.009

No serial correlation in fit at 90% confidence for 1.928 < DWd < 2.072

Cycle1063 There were  5739 observations. Total before-cycle CHI**2 = 1.2183E+04

Reduced CHI**2 =  2.134     for   29 variables

Reflection data statistics

Histogram  1  Type PXC   Nobs= 1405 R(F**2) =   .0340

1 Columns of the    29 Column matrix are 0.0

Variable    1HSCL was not refined

The value of the determinant is   .1041*10.0**(    -9)

Atom parameters for phase no. 1

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

BA    (  1) Values  : 1.000   .000000   .000000   .000000     .568

Sigmas  :                                         .049

Shft/esd:                                          .17

BA1      moved   .00A     sum(shift/e.s.d)**2 :     .03

BA    (  2) Values  : 1.000   .278205   .778205   .000000     .563

Sigmas  :         .000079   .000079               .043

Shft/esd:            -.02      -.02               -.12

BA2      moved   .00A     sum(shift/e.s.d)**2 :     .01

CU    (  3) Values  : 1.000   .500000   .000000   .250000     .669

Sigmas  :                                         .162

Shft/esd:                                          .02

CU3      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  4) Values  : 1.000   .105895   .605895   .000000     .306

Sigmas  :         .000167   .000167               .119

Shft/esd:             .11       .11                .08

CU4      moved   .00A     sum(shift/e.s.d)**2 :     .03

IN    (  5) Values  :  .421   .241647   .000000   .250000     .160

Sigmas  :  .003   .000109

Shft/esd:  -.33       .12

IN5      moved   .00A     sum(shift/e.s.d)**2 :     .12

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:07  Page   7

SC    (  6) Values  :  .579   .241647   .000000   .250000     .160

Sigmas  :  .003   .000109

Shft/esd:   .33       .12

SC6      moved   .00A     sum(shift/e.s.d)**2 :     .12

O     (  7) Values  : 1.000   .117166   .617164   .226078     .200

Sigmas  :         .000607   .000607   .001071

Shft/esd:             .07       .07       .26

O7       moved   .00A     sum(shift/e.s.d)**2 :     .08

O     (  8) Values  : 1.000   .126565   .126565   .250000     .200

Sigmas  :         .000651   .000651

Shft/esd:             .00       .00

O8       moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  9) Values  : 1.000   .236064   .501969   .000000     .200

Sigmas  :         .001100   .000606

Shft/esd:             .13       .19

O9       moved   .00A     sum(shift/e.s.d)**2 :     .05

Maximum atom shift:    .00

Atomic parameter sum(shift/error)**2 for phase 1 :       .44

Calculated unit cell formula weight:  4367.944, density:  5.966gm/cm**3

Atom parameters for phase no. 2

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

Calculated unit cell formula weight:  4442.192, density:  7.131gm/cm**3

Atom parameters for phase no. 3

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

Calculated unit cell formula weight:  5015.632, density:  6.662gm/cm**3

Phase/element fractions for phase no.  1

Hist Elem:      1 1 PXC

Fraction :    .174144

Sigmas   :    .630189E-03

Shift/esd:        .21

Wt. Frac.:     .83077

Sigmas   :    .508758E-03

Phase/element fractions for phase no.  2

Hist Elem:      1 1 PXC

Fraction :    .453898E-02

Sigmas   :    .769630E-04

Shift/esd:      -1.36

Wt. Frac.:     .22022E-01

Sigmas   :    .365178E-03

Phase/element fractions for phase no.  3

Hist Elem:      1 1 PXC

Fraction :    .268719E-01

Sigmas   :    .178265E-03

Shift/esd:       -.08

Wt. Frac.:     .14720

Sigmas   :    .832786E-03

Phase/element fraction sum(shift/error)**2 :      1.90

Histogram scale factors:

Histogram:    1  PXC

Scale    :    67.3910

Sigmas   :    .000000

Shift/esd:        .00

Histogram scale factor sum(shift/error)**2 :       .00

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:07  Page   8

Lattice parameters for powder data:

Phase  1

a         b         c       alpha     beta      gamma     volume

Value    :  11.99690  11.99690   8.44728    90.000    90.000    90.000    1215.780

Sigmas   :    .00028    .00028    .00022      .000      .000      .000        .075

Recprocal metric tensor shift factor = 100%

Phase  2

a         b         c       alpha     beta      gamma     volume

Value    :  10.11263  10.11263  10.11263    90.000    90.000    90.000    1034.172

Sigmas   :    .00036    .00036    .00036      .000      .000      .000        .112

Recprocal metric tensor shift factor = 100%

Phase  3

a         b         c       alpha     beta      gamma     volume

Value    :  12.11764  12.11764   8.51393    90.000    90.000    90.000    1250.162

Sigmas   :    .00045    .00045    .00060      .000      .000      .000        .119

Recprocal metric tensor shift factor = 100%

Recprocal metric tensor sum(shift/error)**2 :     10.56

Diffractometer coefficients for powder data:

Hist.    :   1  PXC

Zero       :     -2.23

Sigmas     :       .08

Shift/esd  :      -.27

Dif. Cons. Sum(shift/error)**2 :       .07

Background coefficients for histogram no.  1:

Param.   :           1              2              3              4              5              6

Coeff.   :   7.464295E+02  -5.476028E+00   4.112818E+01   2.221670E-01  -2.600243E+00  -4.423849E-03

Sigmas   :   3.075737E+00   4.943911E-01   2.723563E+00   4.458966E-02   2.025488E-01   1.739663E-03

Shift/esd:           -.85            .55            .65           -.36           -.54            .26

Background coef. sum(shift/error)**2 :      1.92

Final variable sum((shift/esd)**2) for cycle1063:       7.80 Time:    5.77 sec

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:07  Page   9

Restraint data statistics:

Powder data statistics                Fitted         All               Average

Bank Ndata Sum(w*d**2)  wRp     Rp    wRp     Rp     DWd  Integral

Hstgm  1 PXC   1  5739  12167.      .0445  .0343  .0445  .0343   1.010    .967

Powder totals     5739  12167.      .0445  .0343  .0445  .0343   1.010

No serial correlation in fit at 90% confidence for 1.928 < DWd < 2.072

Cycle1064 There were  5739 observations. Total before-cycle CHI**2 = 1.2167E+04

Reduced CHI**2 =  2.131     for   29 variables

Reflection data statistics

Histogram  1  Type PXC   Nobs= 1405 R(F**2) =   .0341

1 Columns of the    29 Column matrix are 0.0

Variable    1HSCL was not refined

The value of the determinant is   .1044*10.0**(    -9)

Atom parameters for phase no. 1

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

BA    (  1) Values  : 1.000   .000000   .000000   .000000     .568

Sigmas  :                                         .049

Shft/esd:                                         -.01

BA1      moved   .00A     sum(shift/e.s.d)**2 :     .00

BA    (  2) Values  : 1.000   .278206   .778206   .000000     .563

Sigmas  :         .000078   .000078               .043

Shft/esd:             .01       .01                .00

BA2      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  3) Values  : 1.000   .500000   .000000   .250000     .669

Sigmas  :                                         .162

Shft/esd:                                          .00

CU3      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  4) Values  : 1.000   .105895   .605895   .000000     .305

Sigmas  :         .000167   .000167               .119

Shft/esd:             .00       .00               -.01

CU4      moved   .00A     sum(shift/e.s.d)**2 :     .00

IN    (  5) Values  :  .421   .241647   .000000   .250000     .160

Sigmas  :  .003   .000109

Shft/esd:   .01       .01

IN5      moved   .00A     sum(shift/e.s.d)**2 :     .00

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:12  Page  10

SC    (  6) Values  :  .579   .241647   .000000   .250000     .160

Sigmas  :  .003   .000109

Shft/esd:  -.01       .01

SC6      moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  7) Values  : 1.000   .117168   .617166   .226069     .200

Sigmas  :         .000607   .000607   .001071

Shft/esd:             .00       .00      -.01

O7       moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  8) Values  : 1.000   .126565   .126565   .250000     .200

Sigmas  :         .000651   .000651

Shft/esd:             .00       .00

O8       moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  9) Values  : 1.000   .236055   .501974   .000000     .200

Sigmas  :         .001100   .000605

Shft/esd:            -.01       .01

O9       moved   .00A     sum(shift/e.s.d)**2 :     .00

Maximum atom shift:    .00

Atomic parameter sum(shift/error)**2 for phase 1 :       .00

Calculated unit cell formula weight:  4367.986, density:  5.966gm/cm**3

Atom parameters for phase no. 2

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

Calculated unit cell formula weight:  4442.192, density:  7.133gm/cm**3

Atom parameters for phase no. 3

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

Calculated unit cell formula weight:  5015.632, density:  6.662gm/cm**3

Phase/element fractions for phase no.  1

Hist Elem:      1 1 PXC

Fraction :    .174125

Sigmas   :    .629256E-03

Shift/esd:       -.03

Wt. Frac.:     .83071

Sigmas   :    .508212E-03

Phase/element fractions for phase no.  2

Hist Elem:      1 1 PXC

Fraction :    .454066E-02

Sigmas   :    .768987E-04

Shift/esd:        .02

Wt. Frac.:     .22030E-01

Sigmas   :    .364879E-03

Phase/element fractions for phase no.  3

Hist Elem:      1 1 PXC

Fraction :    .268811E-01

Sigmas   :    .178042E-03

Shift/esd:        .05

Wt. Frac.:     .14726

Sigmas   :    .831713E-03

Phase/element fraction sum(shift/error)**2 :       .00

Histogram scale factors:

Histogram:    1  PXC

Scale    :    67.3910

Sigmas   :    .000000

Shift/esd:        .00

Histogram scale factor sum(shift/error)**2 :       .00

1Ba3Cu3In2Sc2O12                                                    GENLES   Version MS-DOS 2000-10-10T10:25:12  Page  11

Lattice parameters for powder data:

Phase  1

a         b         c       alpha     beta      gamma     volume

Value    :  11.99690  11.99690   8.44728    90.000    90.000    90.000    1215.779

Sigmas   :    .00028    .00028    .00022      .000      .000      .000        .075

Recprocal metric tensor shift factor = 100%

Phase  2

a         b         c       alpha     beta      gamma     volume

Value    :  10.11264  10.11264  10.11264    90.000    90.000    90.000    1034.173

Sigmas   :    .00037    .00037    .00037      .000      .000      .000        .114

Recprocal metric tensor shift factor = 100%

Phase  3

a         b         c       alpha     beta      gamma     volume

Value    :  12.11764  12.11764   8.51388    90.000    90.000    90.000    1250.156

Sigmas   :    .00045    .00045    .00060      .000      .000      .000        .119

Recprocal metric tensor shift factor = 100%

Recprocal metric tensor sum(shift/error)**2 :       .01

Diffractometer coefficients for powder data:

Hist.    :   1  PXC

Zero       :     -2.23

Sigmas     :       .08

Shift/esd  :       .00

Dif. Cons. Sum(shift/error)**2 :       .00

Background coefficients for histogram no.  1:

Param.   :           1              2              3              4              5              6

Coeff.   :   7.464324E+02  -5.476768E+00   4.112626E+01   2.221828E-01  -2.600130E+00  -4.423298E-03

Sigmas   :   3.073778E+00   4.940647E-01   2.721792E+00   4.456037E-02   2.024167E-01   1.738495E-03

Shift/esd:            .00            .00            .00            .00            .00            .00

Background coef. sum(shift/error)**2 :       .00

Final variable sum((shift/esd)**2) for cycle1064:        .01 Time:    4.77 sec

Convergence was achieved

1Ba3Cu3In2Sc2O12                                                    PUBTABLE Version MS-DOS 2000-10-10T10:26:21  Page   1

|-----------------------------------------|

|     Program PUBTABLES Version MS-DOS    |

|  Generate crystal structure data tables |

| Distributed on 15/ 7/1999; 0:32:10      |

|-----------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY601 GENLES  MS-DOS 2000-10-10T10:25:07  Sdsq=  .122E+05 S/E=  .104E-01

--------------------------------------------------------------

Archiving C:/GSAS/phil/in2sc2/IN2SC2.EXP as C:/GSAS/phil/in2sc2/IN2SC2!327.EXP

--------------------------------------------------------------

--------------------------------------------------------------

Archiving C:/GSAS/phil/in2sc2/IN2SC2.EXP as C:/GSAS/phil/in2sc2/IN2SC2!328.EXP

--------------------------------------------------------------

--------------------------------------------------------------

Archiving C:/GSAS/phil/in2sc2/IN2SC2.EXP as C:/GSAS/phil/in2sc2/IN2SC2!329.EXP

--------------------------------------------------------------

Supplementary Material (ESI) for Journal of Materials Chemistry

This journal is (c) The Royal Society of Chemistry 2001