1Ba3Cu3In2Sc2O12                                                    PUBTABLE Version MS-DOS 2000-10-10T10:26:21  Page   1

|-----------------------------------------|

|     Program PUBTABLES Version MS-DOS    |

|  Generate crystal structure data tables |

| Distributed on 15/ 7/1999; 0:32:10      |

|-----------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

GENLES was run on 2000-10-10T10:25:12     Total cycles run1064

The Current Least-Squares controls are

Maximum number of cycles is    6

I/SigI cut-off is  1.00

Anisotropic thermal factors are defined by

T = exp(h**2*astr**2*u11+... +2*h*k*astr*bstr*u12+... )

Space group I4/mcm

The lattice is centric  I-centered tetragonal    Laue symmetry 4/mmm

Multiplicity of a general site is  32

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)    -Y      X      Z

( 3)    -X     -Y      Z  ( 4)     Y     -X      Z

( 5)    -X      Y  1/2+Z  ( 6)    -Y     -X  1/2+Z

( 7)     X     -Y  1/2+Z  ( 8)     Y      X  1/2+Z

Lattice constants are

a =  11.99690(28)  b = A  c =  8.44728(22)

Alpha =  90     Beta =  90    Gamma =  90

Cell volume = 1215.78(5)

Name         X             Y             Z         Ui/Ue*100    Site sym Mult Type Seq Fractn

BA1       .000000       .000000       .000000        .57(5)     4/M(001)   4   BA    1 1.0000

BA2       .27821(8)     .77821(8)     .000000        .56(4)     MM2(110)   8   BA    2 1.0000

CU3       .500000       .000000       .250000        .67(16)    -42M 001   4   CU    3 1.0000

CU4       .10589(17)    .60589(17)    .000000        .31(12)    MM2(110)   8   CU    4 1.0000

IN5       .24165(11)    .000000       .250000        .16          2(100)  16   IN    5  .421(3)

SC6       .24165(11)    .000000       .250000        .16          2(100)  16   SC    6  .579(3)

O7        .1172(6)      .6172(6)      .2261(11)      .20          M(+-0)  16   O     7 1.0000

O8        .1266(7)      .1266(7)      .250000        .20          2(110)  16   O     8 1.0000

O9        .2361(11)     .5020(6)      .000000        .20          M(001)  16   O     9 1.0000

1Ba3Cu3In2Sc2O12                                                    PUBTABLE Version MS-DOS 2000-10-10T10:26:22  Page   2

Thermal parameters multiplied by 100.0 are

Name        U11          U22          U33          U12          U13          U23

BA1        .57(5)       .57          .57          .00          .00          .00

BA2        .56(4)       .56          .56          .00          .00          .00

CU3        .67(16)      .67          .67          .00          .00          .00

CU4        .31(12)      .31          .31          .00          .00          .00

IN5        .16          .16          .16          .00          .00          .00

SC6        .16          .16          .16          .00          .00          .00

O7         .20          .20          .20          .00          .00          .00

O8         .20          .20          .20          .00          .00          .00

O9         .20          .20          .20          .00          .00          .00

1Ba3Cu3In2Sc2O12                                                    PUBTABLE Version MS-DOS 2000-10-10T10:26:22  Page   3

Space group I 21 3

The lattice is acentric  I-centered cubic         Laue symmetry m 3

Multiplicity of a general site is  24

The equivalent positions are:

( 1)     X      Y      Z  ( 2)     Z      X      Y  ( 3)     Y      Z      X

( 4) 1/2+X  1/2-Y     -Z  ( 5)    -Z  1/2+X  1/2-Y  ( 6) 1/2-Y     -Z  1/2+X

( 7) 1/2-Z     -X  1/2+Y  ( 8) 1/2+Y  1/2-Z     -X  ( 9)    -Y  1/2+Z  1/2-X

(10) 1/2-X     -Y  1/2+Z  (11) 1/2+Z  1/2-X     -Y  (12)    -X  1/2+Y  1/2-Z

Lattice constants are

a =  10.1126(4)  b = A  c = A

Alpha =  90     Beta =  90    Gamma =  90

Cell volume = 1034.17(7)

Name         X             Y             Z         Ui/Ue*100    Site sym Mult Type Seq Fractn

IN1       .250000       .250000       .250000      23.94          3(111)   8   IN    1 1.0000

IN2      -.021575       .000000       .250000       1.04          2(100)  12   IN    2 1.0000

IN3       .499858       .000000       .250000      14.56          2(100)  12   IN    3 1.0000

O4        .125000       .135000       .395000       1.77            1     24   O     4 1.0000

O5        .100000       .358000       .373000       1.77            1     24   O     5 1.0000

Thermal parameters multiplied by 100.0 are

Name        U11          U22          U33          U12          U13          U23

IN1      23.94        23.94        23.94          .00          .00          .00

IN2       1.04         1.04         1.04          .00          .00          .00

IN3      14.56        14.56        14.56          .00          .00          .00

O4        1.77         1.77         1.77          .00          .00          .00

O5        1.77         1.77         1.77          .00          .00          .00

1Ba3Cu3In2Sc2O12                                                    PUBTABLE Version MS-DOS 2000-10-10T10:26:22  Page   4

Space group I 4/mcm

The lattice is centric  I-centered tetragonal    Laue symmetry 4/mmm

Multiplicity of a general site is  32

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)    -Y      X      Z

( 3)    -X     -Y      Z  ( 4)     Y     -X      Z

( 5)    -X      Y  1/2+Z  ( 6)    -Y     -X  1/2+Z

( 7)     X     -Y  1/2+Z  ( 8)     Y      X  1/2+Z

Lattice constants are

a =  12.1176(5)  b = A  c =  8.5139(6)

Alpha =  90     Beta =  90    Gamma =  90

Cell volume = 1250.15(11)

Name         X             Y             Z         Ui/Ue*100    Site sym Mult Type Seq Fractn

BA1       .000000       .000000       .000000       1.22        4/M(001)   4   BA    1 1.0000

BA2       .279615       .779617       .000000        .58        MM2(110)   8   BA    2 1.0000

CU3       .500000       .000000       .250000       2.24        -42M 001   4   CU    3 1.0000

CU4       .105675       .605676       .000000        .20        MM2(110)   8   CU    4 1.0000

IN5       .242497       .000000       .250000        .20          2(100)  16   IN    5 1.0000

O6        .108459       .608461       .236201        .63          M(+-0)  16   O     6 1.0000

O7        .116244       .116244       .250000        .63          2(110)  16   O     7 1.0000

O8        .222287       .494928       .000000        .63          M(001)  16   O     8 1.0000

Thermal parameters multiplied by 100.0 are

Name        U11          U22          U33          U12          U13          U23

BA1       1.22         1.22         1.22          .00          .00          .00

BA2        .58          .58          .58          .00          .00          .00

CU3       2.24         2.24         2.24          .00          .00          .00

CU4        .20          .20          .20          .00          .00          .00

IN5        .20          .20          .20          .00          .00          .00

O6         .63          .63          .63          .00          .00          .00

O7         .63          .63          .63          .00          .00          .00

O8         .63          .63          .63          .00          .00          .00

Supplementary Material (ESI) for Journal of Materials Chemistry

This journal is (c) The Royal Society of Chemistry 2001