1bA3cU3In4O12                                                                Version        2000-10-09T12:29:19  Page   1

|---------------------------------------------------------|

|              Program POWPREF Version MS-DOS             |

| Prepares powder histograms for least-squares refinement |

|         Distributed on 15/ 7/1999; 0:31:36              |

|---------------------------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY358 GENLES  MS-DOS 2000-10-09T12:28:48  Sdsq=  .109E+05 S/E=  .970E-03

Data for bank  1 read from file in4sjb.dat

The powder pattern has  5750 channels with   1 bins per channel

No fixed background points for this powder pattern

The  2 excluded regions are (in deg):

Exclude    from:       to:     from:       to:     from:       to:     from:       to:

.0000     .0000  120.0000 1000.0000

Incident spectrum type  0 can be used in the region     .000 deg to  180.000 deg

The minimum possible weighted residual for this histogram is    .0474

Histogram no.  1 on file IN4SJB.P01

updated with new excluded regions, background and incident spectrum data.

CPU time =    .05 to update histogram

Lattice parameters for phase 1 are:

a,b,c  = 12.123830 12.123830  8.510691  angles =    90.000    90.000    90.000

volume =  1250.963

Lattice parameters for phase 2 are:

a,b,c  =  4.042903  4.042903  4.042903  angles =    90.000    90.000    90.000

volume =    66.082

Lattice parameters for phase 3 are:

a,b,c  = 10.101910 10.101910 10.101910  angles =    90.000    90.000    90.000

volume =  1030.885

Profile function 3 for phase no. 1 has the coefficients p1-p19:

.372297E+02   -.516158E+02    .160828E+02    .649140E+01

.713231E+01    .000000E+00    .500000E-03    .500000E-03

-.616515E+01   -.931623E+01    .960520E+01   -.192380E+01

.000000E+00   -.109637E-01    .752313E-02   -.919461E-01

.000000E+00    .000000E+00    .000000E+00

cutoff on the wings at  .010 of maximum

Profile function 3 for phase no. 2 has the coefficients p1-p19:

.200000E+01   -.200000E+01    .100000E+00    .000000E+00

.103186E+02    .000000E+00    .500000E-03    .500000E-03

.000000E+00    .000000E+00    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00

cutoff on the wings at  .010 of maximum

Profile function 3 for phase no. 3 has the coefficients p1-p19:

.937246E+03    .238984E+03    .258181E+03    .000000E+00

.391643E+01    .000000E+00    .500000E-03    .500000E-03

.000000E+00    .000000E+00    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00

cutoff on the wings at  .010 of maximum

Minimum d-spacing used to generate reflections    .8849 for phase 1

Minimum d-spacing used to generate reflections    .8797 for phase 2

Minimum d-spacing used to generate reflections    .8700 for phase 3

Minimum d-spacing used to generate reflections    .9944 for phase 1

Minimum d-spacing used to generate reflections    .9876 for phase 2

Minimum d-spacing used to generate reflections    .9759 for phase 3

Minimum d-spacing for matching reflections    .8894

Estimated number of reflections to be generated is  1221

Number of reflections generated for phase 1 is   552

Number of reflections generated for phase 2 is    16

Number of reflections generated for phase 3 is   336

Total number of reflections generated for all phases is   904

CPU time =    .06 sec. to generate reflections.

CPU time =    .66 sec. to locate reflection limits.

CPU time =    .05 sec. to match reflection ranges to powder pattern

The maximum number of reflections contributing to any profile point is   61

CPU time =    .06 sec. to update file

1bA3cU3In4O12                                                                Version        2000-10-09T12:29:25  Page   1

|----------------------------------------------------|

|            Program GENLES Version MS-DOS           |

|    General crystal structure refinement program    |

| Magnetic structure refinement added by M. Yethiraj |

|   Revised and corrected by Larson and Von Dreele   |

|      Distributed on 15/ 7/1999; 0:28:26            |

|----------------------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The experiment file is: IN4SJB.EXP

The last history record is :

HSTRY359 POWPREF MS-DOS 2000-10-09T12:29:19

Maximum number of cycles is    8

I/SigI cut-off is  1.00

Structure factors will be extracted from histogram  1

using extraction method codes     0    0    0    0    0    0    0    0    0

The atomic and magnetic scattering factors for  5 types of atoms are:

Atom type   b-len   a(1)      b(1)      a(2)      b(2)      a(3)      b(3)      a(4)      b(4)      c

BA           .525  20.33610   3.21600  19.29700    .27560  10.88800  20.20730   2.69590 167.20200   2.77310

CU           .772  13.33800   3.58280   7.16760    .24700   5.61580  11.39660   1.67350  64.81260   1.19100

IN           .406  19.16240    .54760  18.55960   6.37760   4.29480  25.84990   2.03960  92.80290   4.93910

O            .581   3.04850  13.27710   2.28680   5.70110   1.54630    .32390    .86700  32.90890    .25080

AL           .345   6.42020   3.03870   1.90020    .74260   1.59360  31.54720   1.96460  85.08860   1.11510

Atom type  CrKa f'      f"   FeKa f'      f"   CuKa f'      f"   MoKa f'      f"   AgKa f'      f"

BA         -11.460    9.980   -4.830   12.160   -1.330    8.460    -.610    2.280    -.980    1.500

CU           -.795    1.196   -1.129     .888   -2.019     .589     .263    1.266     .265     .826

IN          -1.788    9.627    -.626    7.356    -.126    5.045    -.936    1.310   -1.493     .854

O             .090     .073     .069     .052     .047     .032     .008     .006     .003     .004

AL            .318     .522     .269     .381     .204     .246     .056     .052     .032     .031

Space group   I4/mcm

The lattice is centric  I-centered tetragonal    Laue symmetry 4/mmm

Multiplicity of a general site is  32

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)    -Y      X      Z

( 3)    -X     -Y      Z  ( 4)     Y     -X      Z

( 5)    -X      Y  1/2+Z  ( 6)    -Y     -X  1/2+Z

( 7)     X     -Y  1/2+Z  ( 8)     Y      X  1/2+Z

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:25  Page   2

The atom positions read in are

Type seq. At. name  mult   symm  frac   pn    X    pn    Y    pn    Z    pn  u11 pn  u22 pn  u33 pn  u12 pn  u13 pn  u23 pn

BA      1 BA1         44/M(001) 1.0000   0  .0000   0  .0000   0  .0000   0 1.2   1

BA      2 BA2         8MM2(110) 1.0000   0  .2801   2  .7801   3  .0000   0  .4   4

CU      3 CU3         4-42M 001 1.0000   0  .5000   0  .0000   0  .2500   0  .7   5

CU      4 CU4         8MM2(110) 1.0000   0  .1057   6  .6057   7  .0000   0  .0   0

IN      5 IN5        16  2(100) 1.0000   0  .2426   8  .0000   0  .2500   0  .1   9

O       6 O6         16  M(+-0) 1.0000   0  .1183  10  .6183  11  .2323  12  .0   0

O       7 O7         16  2(110) 1.0000   0  .1288  13  .1288  14  .2500   0  .0   0

O       8 O8         16  M(001) 1.0000   0  .2328  15  .4986  16  .0000   0  .0   0

Space group   F m 3 m

The lattice is centric  F-centered cubic         Laue symmetry m3m

Multiplicity of a general site is 192

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)     Z      X      Y  ( 3)     Y      Z      X

( 4)     X      Y     -Z  ( 5)    -Z      X      Y  ( 6)     Y     -Z      X

( 7)    -Z      X     -Y  ( 8)    -Y     -Z      X  ( 9)     Y     -Z     -X

(10)    -X      Y     -Z  (11)    -Z     -X      Y  (12)     X     -Y     -Z

(13)     Y      X      Z  (14)     Z      Y      X  (15)     X      Z      Y

(16)     Y      X     -Z  (17)    -Z      Y      X  (18)     X     -Z      Y

(19)    -Z      Y     -X  (20)    -X     -Z      Y  (21)     X     -Z     -Y

(22)    -Y      X     -Z  (23)    -Z     -Y      X  (24)     Y     -X     -Z

The atom positions read in are

Type seq. At. name  mult   symm  frac   pn    X    pn    Y    pn    Z    pn  u11 pn  u22 pn  u33 pn  u12 pn  u13 pn  u23 pn

AL      1 AL1         4   M3M   1.0000   0  .0000   0  .0000   0  .0000   0 2.5   0

Space group   I 21 3

The lattice is acentric  I-centered cubic         Laue symmetry m 3

Multiplicity of a general site is  24

The equivalent positions are:

( 1)     X      Y      Z  ( 2)     Z      X      Y  ( 3)     Y      Z      X

( 4) 1/2+X  1/2-Y     -Z  ( 5)    -Z  1/2+X  1/2-Y  ( 6) 1/2-Y     -Z  1/2+X

( 7) 1/2-Z     -X  1/2+Y  ( 8) 1/2+Y  1/2-Z     -X  ( 9)    -Y  1/2+Z  1/2-X

(10) 1/2-X     -Y  1/2+Z  (11) 1/2+Z  1/2-X     -Y  (12)    -X  1/2+Y  1/2-Z

The atom positions read in are

Type seq. At. name  mult   symm  frac   pn    X    pn    Y    pn    Z    pn  u11 pn  u22 pn  u33 pn  u12 pn  u13 pn  u23 pn

IN      1 IN1         8  3(111) 1.0000   0  .2500   0  .2500   0  .2500   0 2.6   0

IN      2 IN2        12  2(100) 1.0000   0  .0210   0  .0000   0  .2500   038.0   0

IN      3 IN3        12  2(100) 1.0000   0  .4838   0  .0000   0  .2500   014.6   0

O       4 O4         24    1    1.0000   0  .1250   0  .1350   0  .3950   0 2.5   0

O       5 O5         24    1    1.0000   0  .1000   0  .3580   0  .3730   0 2.5   0

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:25  Page   3

Lattice parameters for phase 1 are:

a         b         c          alpha      beta     gamma

12.123830 12.123830  8.510691   90.0000   90.0000   90.0000

These cell parameters will be refined

Reciprocal metric tensor elements:          damp= 0

Element :          g11   pn          g22   pn          g33   pn        2*g12   pn        2*g13   pn        2*g23   pn

Value   :   6.80331E-03  17   6.80331E-03  18   1.38061E-02  19  -1.65565E-10   0  -2.35854E-10   0  -2.35854E-10   0

Constr. :          1.000  1          1.000  1          1.000  2           .000  0           .000  0           .000  0

Lattice parameters for phase 2 are:

a         b         c          alpha      beta     gamma

4.042903  4.042903  4.042903   90.0000   90.0000   90.0000

These cell parameters will be refined

Reciprocal metric tensor elements:          damp= 0

Element :          g11   pn          g22   pn          g33   pn        2*g12   pn        2*g13   pn        2*g23   pn

Value   :   6.11806E-02  20   6.11806E-02  21   6.11806E-02  22  -1.48889E-09   0  -1.48889E-09   0  -1.48889E-09   0

Constr. :          1.000  3          1.000  3          1.000  3           .000  0           .000  0           .000  0

Lattice parameters for phase 3 are:

a         b         c          alpha      beta     gamma

10.101910 10.101910 10.101910   90.0000   90.0000   90.0000

These cell parameters will be refined

Reciprocal metric tensor elements:          damp= 0

Element :          g11   pn          g22   pn          g33   pn        2*g12   pn        2*g13   pn        2*g23   pn

Value   :   9.79926E-03  23   9.79926E-03  24   9.79926E-03  25  -2.38474E-10   0  -2.38474E-10   0  -2.38474E-10   0

Constr. :          1.000  4          1.000  4          1.000  4           .000  0           .000  0           .000  0

Phase/element fractions for phase no.  1

Hist Elm:    PXC   1 1   nc

Fraction:    1.8978      26

Dmp/Cnst:    0     1.000  5

Phase/element fractions for phase no.  2

Hist Elm:    PXC   1 1   nc

Fraction:    1.6188      27

Dmp/Cnst:    0     1.000  6

Phase/element fractions for phase no.  3

Hist Elm:    PXC   1 1   nc

Fraction:    .78661E-01  28

Dmp/Cnst:    0     1.000  7

Histogram scale factors:

Hist.   :        1  PXC  pn

Scale   :    1.2521      29

Dmp/Cnst:    0     1.000  8

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:25  Page   4

Absorption coefficients for powder data:

Hist/Typ:    1  PXC    1 pn

Absc 1. :   -.45776E-01  30

Dmp/Cnst:    0     1.000  1

Absc 2. :    .00000       0

Dmp/Cnst:    0     1.000  1

Diffractometer constants for powder data:

No. Type    Lam 1        Lam 2      Polariz.  pn Cnstr cn type    Zero  pn Cnstr cn    Kratio  pn Cnstr cn Damp

1  PXC  1.5405000    1.5443000       .50000   0  .000  0  0    -7.341  31 1.000 10     .5000   0  .000  0    0

Extinction coefficients for phase no.  1:

Hist.   :        1  PXC  pn

Extinct.:    .00000       0

Dmp/Cnst:    0      .000  0

Extinction coefficients for phase no.  2:

Hist.   :        1  PXC  pn

Extinct.:    .00000       0

Dmp/Cnst:    0      .000  0

Extinction coefficients for phase no.  3:

Hist.   :        1  PXC  pn

Extinct.:    .00000       0

Dmp/Cnst:    0      .000  0

Orientation distribution coefficients for powder data:

No ODF data for phase  1

No ODF data for phase  2

No ODF data for phase  3

Preferred orientation coeffs. for phase no.  1 histogram no.  1:

Axis    :        1       pn

Dir./typ:     .0  .0 1.0  0

PO ratio:        1.0000   0

Dmp/Cnst:    0      .000  0

PO frac.:        1.0000   0

Dmp/Cnst:    0      .000  0

Preferred orientation coeffs. for phase no.  2 histogram no.  1:

Axis    :        1       pn

Dir./typ:     .0  .0 1.0  0

PO ratio:        1.0000   0

Dmp/Cnst:    0      .000  0

PO frac.:        1.0000   0

Dmp/Cnst:    0      .000  0

Preferred orientation coeffs. for phase no.  3 histogram no.  1:

Axis    :        1       pn

Dir./typ:     .0  .0 1.0  0

PO ratio:        1.0000   0

Dmp/Cnst:    0      .000  0

PO frac.:        1.0000   0

Dmp/Cnst:    0      .000  0

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:25  Page   5

Profile coeff. for function type  3, phase no.  1 and histogram no.  1; aniso. axis   0.   0.   1.; damp= 0:

Coeff.  :      GU    pn      GV    pn      GW    pn      GP    pn      LX    pn      LY    pn     S/L    pn     H/L    pn

Value   : 3.723E+01  32-5.162E+01  34 1.608E+01  35 6.491E+00  36 7.132E+00  37 0.000E+00   0 5.000E-04   0 5.000E-04   0

Constr. :      1.000 11      1.000 13      1.000 14      1.000 15      1.000 16       .000  0       .000  0       .000  0

Coeff.  :     trns   pn     shft   pn     stec   pn     ptec   pn     sfec   pn     L11    pn     L22    pn     L33    pn

Value   :-6.165E+00   0-9.316E+00   0 9.605E+00   0-1.924E+00   0 0.000E+00   0-1.096E-02   0 7.523E-03   0-9.195E-02   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     L12    pn     L13    pn     L23    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0

Profile coeff. for function type  3, phase no.  2 and histogram no.  1; aniso. axis   0.   0.   1.; damp= 0:

Coeff.  :      GU    pn      GV    pn      GW    pn      GP    pn      LX    pn      LY    pn     S/L    pn     H/L    pn

Value   : 2.000E+00   0-2.000E+00   0 1.000E-01   0 0.000E+00   0 1.032E+01   0 0.000E+00   0 5.000E-04   0 5.000E-04   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     trns   pn     shft   pn     stec   pn     ptec   pn     sfec   pn     L11    pn     L22    pn     L33    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     L12    pn     L13    pn     L23    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0

Profile coeff. for function type  3, phase no.  3 and histogram no.  1; aniso. axis   0.   0.   1.; damp= 0:

Coeff.  :      GU    pn      GV    pn      GW    pn      GP    pn      LX    pn      LY    pn     S/L    pn     H/L    pn

Value   : 9.372E+02  33 2.390E+02   0 2.582E+02   0 0.000E+00   0 3.916E+00   0 0.000E+00   0 5.000E-04   0 5.000E-04   0

Constr. :      1.000 12       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     trns   pn     shft   pn     stec   pn     ptec   pn     sfec   pn     L11    pn     L22    pn     L33    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     L12    pn     L13    pn     L23    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0

Diffuse scattering coefficients for powder data:

No diffuse scattering coefficients for histogram    1

Background coefficients for powder data:

Histogram no.:    1 Damping factor:    0 Use all points: Y

Power series in Q**2n/n! and n!/Q**2n

Param.  :          1   pn          2   pn          3   pn          4   pn          5   pn          6   pn

Coeff.  :  .34696E+03  38  .55534E+00  39 -.70698E+01  40 -.35815E-01  41  .59628E+00  42  .16247E-02  43

The constraint matrix has   43 terms

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:25  Page   6

Restraint data statistics:

Powder data statistics                Fitted         All               Average

Bank Ndata Sum(w*d**2)  wRp     Rp    wRp     Rp     DWd  Integral

Hstgm  1 PXC   1  5750  10902.      .0653  .0494  .0653  .0494   1.110    .953

Powder totals     5750  10902.      .0653  .0494  .0653  .0494   1.110

No serial correlation in fit at 90% confidence for 1.930 < DWd < 2.070

Cycle 622 There were  5750 observations. Total before-cycle CHI**2 = 1.0902E+04

Reduced CHI**2 =  1.907     for   34 variables

Reflection data statistics

Histogram  1  Type PXC   Nobs=  885 R(F**2) =   .1163

3 Columns of the    34 Column matrix are 0.0

Variable    1HSCL was not refined

Variable    1ABS1 was not refined

Variable 1  1PF 4 was not refined

The value of the determinant is   .1046*10.0**(   -10)

Atom parameters for phase no. 1

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

BA    (  1) Values  : 1.000   .000000   .000000   .000000    1.223

Sigmas  :                                         .108

Shft/esd:                                          .03

BA1      moved   .00A     sum(shift/e.s.d)**2 :     .00

BA    (  2) Values  : 1.000   .280082   .780086   .000000     .401

Sigmas  :         .000138   .000138               .079

Shft/esd:            -.02      -.02                .00

BA2      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  3) Values  : 1.000   .500000   .000000   .250000     .672

Sigmas  :                                         .262

Shft/esd:                                          .04

CU3      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  4) Values  : 1.000   .105673   .605671   .000000     .020

Sigmas  :         .000304   .000304

Shft/esd:             .02       .02

CU4      moved   .00A     sum(shift/e.s.d)**2 :     .00

IN    (  5) Values  : 1.000   .242643   .000000   .250000     .100

Sigmas  :         .000147                         .042

Shft/esd:            -.04                         -.05

IN5      moved   .00A     sum(shift/e.s.d)**2 :     .00

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:29  Page   7

O     (  6) Values  : 1.000   .118320   .618320   .232305     .020

Sigmas  :         .001084   .001084   .001998

Shft/esd:             .01       .01       .02

O6       moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  7) Values  : 1.000   .128866   .128866   .250000     .020

Sigmas  :         .001176   .001176

Shft/esd:             .06       .06

O7       moved   .00A     sum(shift/e.s.d)**2 :     .01

O     (  8) Values  : 1.000   .232767   .498610   .000000     .020

Sigmas  :         .001564   .001208

Shft/esd:             .00       .00

O8       moved   .00A     sum(shift/e.s.d)**2 :     .00

Maximum atom shift:    .00

Atomic parameter sum(shift/error)**2 for phase 1 :       .02

Calculated unit cell formula weight:  5015.632, density:  6.658gm/cm**3

Atom parameters for phase no. 2

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

Calculated unit cell formula weight:   107.928, density:  2.712gm/cm**3

Atom parameters for phase no. 3

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

Calculated unit cell formula weight:  4442.192, density:  7.155gm/cm**3

Phase/element fractions for phase no.  1

Hist Elem:      1 1 PXC

Fraction :    1.89794

Sigmas   :    .852091E-02

Shift/esd:        .02

Wt. Frac.:     .94789

Sigmas   :    .221762E-03

Phase/element fractions for phase no.  2

Hist Elem:      1 1 PXC

Fraction :    1.61134

Sigmas   :    .220255

Shift/esd:       -.03

Wt. Frac.:     .17317E-01

Sigmas   :    .232608E-02

Phase/element fractions for phase no.  3

Hist Elem:      1 1 PXC

Fraction :    .786592E-01

Sigmas   :    .570688E-02

Shift/esd:        .00

Wt. Frac.:     .34793E-01

Sigmas   :    .243650E-02

Phase/element fraction sum(shift/error)**2 :       .00

Histogram scale factors:

Histogram:    1  PXC

Scale    :    1.25210

Sigmas   :    .000000

Shift/esd:        .00

Histogram scale factor sum(shift/error)**2 :       .00

Lattice parameters for powder data:

Phase  1

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:29  Page   8

a         b         c       alpha     beta      gamma     volume

Value    :  12.12383  12.12383   8.51069    90.000    90.000    90.000    1250.962

Sigmas   :    .00019    .00019    .00015      .000      .000      .000        .052

Recprocal metric tensor shift factor = 100%

Phase  2

a         b         c       alpha     beta      gamma     volume

Value    :   4.04290   4.04290   4.04290    90.000    90.000    90.000      66.081

Sigmas   :    .00126    .00126    .00126      .000      .000      .000        .062

Recprocal metric tensor shift factor = 100%

Phase  3

a         b         c       alpha     beta      gamma     volume

Value    :  10.10192  10.10192  10.10192    90.000    90.000    90.000    1030.889

Sigmas   :    .00540    .00540    .00540      .000      .000      .000       1.654

Recprocal metric tensor shift factor = 100%

Recprocal metric tensor sum(shift/error)**2 :       .00

Absorption coefficients for powder data:

Hist.    :   1  PXC

Abscor. 1: -4.578E-02

Sigmas   :  0.000E+00

Shift/esd:        .00

Abscor. 2:  0.000E+00

Sigmas   :  0.000E+00

Shift/esd:        .00

Absorption coefficients sum(shift/error)**2 :       .00

Diffractometer coefficients for powder data:

Hist.    :   1  PXC

Zero       :     -7.34

Sigmas     :       .07

Shift/esd  :       .00

Dif. Cons. Sum(shift/error)**2 :       .00

Profile coefficients for histogram no.  1 and for phase no.  1:

Coeff.   :     GU         GV         GW         GP         LX         LY        S/L        H/L        trns       shft

Value    :  3.725E+01 -5.161E+01  1.607E+01  6.491E+00  7.135E+00  0.000E+00  5.000E-04  5.000E-04 -6.165E+00 -9.316E+00

Sigmas   :  5.235E+00  5.878E+00  1.679E+00  0.000E+00  1.133E-01

Shift/esd:        .00        .00       -.01        .00        .02

Coeff.   :    stec       ptec       sfec       L11        L22        L33        L12        L13        L23

Value    :  9.605E+00 -1.924E+00  0.000E+00 -1.096E-02  7.523E-03 -9.195E-02  0.000E+00  0.000E+00  0.000E+00

Sigmas   :

Shift/esd:

Profile coefficients for histogram no.  1 and for phase no.  3:

Coeff.   :     GU         GV         GW         GP         LX         LY        S/L        H/L        trns       shft

Value    :  9.370E+02  2.390E+02  2.582E+02  0.000E+00  3.916E+00  0.000E+00  5.000E-04  5.000E-04  0.000E+00  0.000E+00

Sigmas   :  8.827E+02

Shift/esd:        .00

Coeff.   :    stec       ptec       sfec       L11        L22        L33        L12        L13        L23

Value    :  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00

Sigmas   :

Shift/esd:

Profile coef. sum(shift/error)**2 :       .00

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:29  Page   9

Background coefficients for histogram no.  1:

Param.   :           1              2              3              4              5              6

Coeff.   :   3.469903E+02   5.523354E-01  -7.090316E+00  -3.595057E-02   5.975891E-01   1.636265E-03

Sigmas   :   1.908316E+00   3.036017E-01   1.679789E+00   2.760455E-02   1.266003E-01   1.077309E-03

Shift/esd:            .01           -.01           -.01            .00            .01            .01

Background coef. sum(shift/error)**2 :       .00

Final variable sum((shift/esd)**2) for cycle 622:        .01 Time:    3.63 sec

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:29  Page  10

Restraint data statistics:

Powder data statistics                Fitted         All               Average

Bank Ndata Sum(w*d**2)  wRp     Rp    wRp     Rp     DWd  Integral

Hstgm  1 PXC   1  5750  10902.      .0653  .0494  .0653  .0494   1.110    .953

Powder totals     5750  10902.      .0653  .0494  .0653  .0494   1.110

No serial correlation in fit at 90% confidence for 1.930 < DWd < 2.070

Cycle 623 There were  5750 observations. Total before-cycle CHI**2 = 1.0902E+04

Reduced CHI**2 =  1.907     for   34 variables

Reflection data statistics

Histogram  1  Type PXC   Nobs=  885 R(F**2) =   .1163

1 Columns of the    34 Column matrix are 0.0

Variable    1ABS1 was not refined

The value of the determinant is   .1421*10.0**(   -22)

Atom parameters for phase no. 1

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

BA    (  1) Values  : 1.000   .000000   .000000   .000000    1.222

Sigmas  :                                         .108

Shft/esd:                                          .00

BA1      moved   .00A     sum(shift/e.s.d)**2 :     .00

BA    (  2) Values  : 1.000   .280082   .780086   .000000     .401

Sigmas  :         .000138   .000138               .079

Shft/esd:             .00       .00                .00

BA2      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  3) Values  : 1.000   .500000   .000000   .250000     .671

Sigmas  :                                         .262

Shft/esd:                                          .00

CU3      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  4) Values  : 1.000   .105674   .605672   .000000     .020

Sigmas  :         .000304   .000304

Shft/esd:             .00       .00

CU4      moved   .00A     sum(shift/e.s.d)**2 :     .00

IN    (  5) Values  : 1.000   .242643   .000000   .250000     .100

Sigmas  :         .000147                         .042

Shft/esd:             .00                          .00

IN5      moved   .00A     sum(shift/e.s.d)**2 :     .00

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:32  Page  11

O     (  6) Values  : 1.000   .118323   .618323   .232296     .020

Sigmas  :         .001084   .001084   .001999

Shft/esd:             .00       .00       .00

O6       moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  7) Values  : 1.000   .128908   .128908   .250000     .020

Sigmas  :         .001176   .001176

Shft/esd:             .04       .04

O7       moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  8) Values  : 1.000   .232779   .498612   .000000     .020

Sigmas  :         .001564   .001208

Shft/esd:             .01       .00

O8       moved   .00A     sum(shift/e.s.d)**2 :     .00

Maximum atom shift:    .00

Atomic parameter sum(shift/error)**2 for phase 1 :       .00

Calculated unit cell formula weight:  5015.632, density:  6.658gm/cm**3

Atom parameters for phase no. 2

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

Calculated unit cell formula weight:   107.928, density:  2.712gm/cm**3

Atom parameters for phase no. 3

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

Calculated unit cell formula weight:  4442.192, density:  7.155gm/cm**3

Phase/element fractions for phase no.  1

Hist Elem:      1 1 PXC

Fraction :    2.31476

Sigmas   :    10.7055

Shift/esd:        .04

Wt. Frac.:     .94789

Sigmas   :    .228453

Phase/element fractions for phase no.  2

Hist Elem:      1 1 PXC

Fraction :    1.96535

Sigmas   :    9.09187

Shift/esd:        .04

Wt. Frac.:     .17318E-01

Sigmas   :    .787276E-01

Phase/element fractions for phase no.  3

Hist Elem:      1 1 PXC

Fraction :    .959349E-01

Sigmas   :    .443725

Shift/esd:        .04

Wt. Frac.:     .34794E-01

Sigmas   :    .155331

Phase/element fraction sum(shift/error)**2 :       .00

Histogram scale factors:

Histogram:    1  PXC

Scale    :    .977116

Sigmas   :    7.06258

Shift/esd:       -.04

Histogram scale factor sum(shift/error)**2 :       .00

Lattice parameters for powder data:

Phase  1

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:32  Page  12

a         b         c       alpha     beta      gamma     volume

Value    :  12.12383  12.12383   8.51069    90.000    90.000    90.000    1250.962

Sigmas   :    .00019    .00019    .00015      .000      .000      .000        .052

Recprocal metric tensor shift factor = 100%

Phase  2

a         b         c       alpha     beta      gamma     volume

Value    :   4.04290   4.04290   4.04290    90.000    90.000    90.000      66.081

Sigmas   :    .00126    .00126    .00126      .000      .000      .000        .062

Recprocal metric tensor shift factor = 100%

Phase  3

a         b         c       alpha     beta      gamma     volume

Value    :  10.10192  10.10192  10.10192    90.000    90.000    90.000    1030.889

Sigmas   :    .00540    .00540    .00540      .000      .000      .000       1.654

Recprocal metric tensor shift factor = 100%

Recprocal metric tensor sum(shift/error)**2 :       .00

Absorption coefficients for powder data:

Hist.    :   1  PXC

Abscor. 1: -4.578E-02

Sigmas   :  0.000E+00

Shift/esd:        .00

Abscor. 2:  0.000E+00

Sigmas   :  0.000E+00

Shift/esd:        .00

Absorption coefficients sum(shift/error)**2 :       .00

Diffractometer coefficients for powder data:

Hist.    :   1  PXC

Zero       :     -7.34

Sigmas     :       .07

Shift/esd  :       .01

Dif. Cons. Sum(shift/error)**2 :       .00

Profile coefficients for histogram no.  1 and for phase no.  1:

Coeff.   :     GU         GV         GW         GP         LX         LY        S/L        H/L        trns       shft

Value    :  3.771E+01 -5.163E+01  1.651E+01  6.050E+00  7.135E+00  0.000E+00  5.000E-04  5.000E-04 -6.165E+00 -9.316E+00

Sigmas   :  8.206E+01  5.882E+00  8.196E+01  8.196E+01  1.133E-01

Shift/esd:        .01        .00        .01       -.01        .00

Coeff.   :    stec       ptec       sfec       L11        L22        L33        L12        L13        L23

Value    :  9.605E+00 -1.924E+00  0.000E+00 -1.096E-02  7.523E-03 -9.195E-02  0.000E+00  0.000E+00  0.000E+00

Sigmas   :

Shift/esd:

Profile coefficients for histogram no.  1 and for phase no.  3:

Coeff.   :     GU         GV         GW         GP         LX         LY        S/L        H/L        trns       shft

Value    :  9.368E+02  2.390E+02  2.582E+02  0.000E+00  3.916E+00  0.000E+00  5.000E-04  5.000E-04  0.000E+00  0.000E+00

Sigmas   :  8.827E+02

Shift/esd:        .00

Coeff.   :    stec       ptec       sfec       L11        L22        L33        L12        L13        L23

Value    :  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00

Sigmas   :

Shift/esd:

Profile coef. sum(shift/error)**2 :       .00

1bA3cU3In4O12                                                       GENLES   Version MS-DOS 2000-10-09T12:29:32  Page  13

Background coefficients for histogram no.  1:

Param.   :           1              2              3              4              5              6

Coeff.   :   3.469930E+02   5.518389E-01  -7.092833E+00  -3.591137E-02   5.977593E-01   1.634918E-03

Sigmas   :   1.908297E+00   3.036029E-01   1.679769E+00   2.760485E-02   1.265989E-01   1.077319E-03

Shift/esd:            .00            .00            .00            .00            .00            .00

Background coef. sum(shift/error)**2 :       .00

Final variable sum((shift/esd)**2) for cycle 623:        .01 Time:    3.51 sec

Convergence was achieved

1bA3cU3In4O12                                                       PUBTABLE Version MS-DOS 2000-10-09T12:29:56  Page   1

|-----------------------------------------|

|     Program PUBTABLES Version MS-DOS    |

|  Generate crystal structure data tables |

| Distributed on 15/ 7/1999; 0:32:10      |

|-----------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY360 GENLES  MS-DOS 2000-10-09T12:29:29  Sdsq=  .109E+05 S/E=  .767E-02

1bA3cU3In4O12                                                       PUBTABLE Version MS-DOS 2000-10-10T10:39:29  Page   1

|-----------------------------------------|

|     Program PUBTABLES Version MS-DOS    |

|  Generate crystal structure data tables |

| Distributed on 15/ 7/1999; 0:32:10      |

|-----------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY360 GENLES  MS-DOS 2000-10-09T12:29:29  Sdsq=  .109E+05 S/E=  .767E-02

--------------------------------------------------------------

Archiving C:/GSAS/phil/in4/IN4SJB.EXP as C:/GSAS/phil/in4/IN4SJB!208.EXP

--------------------------------------------------------------

Supplementary Material (ESI) for Journal of Materials Chemistry

This journal is (c) The Royal Society of Chemistry 2001