1Ba3Cu3Sc3InO12                                                              Version        2000-10-10T23:15:39  Page   1

|---------------------------------------------------------|

|              Program POWPREF Version MS-DOS             |

| Prepares powder histograms for least-squares refinement |

|         Distributed on 15/ 7/1999; 0:31:36              |

|---------------------------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY257 GENLES  MS-DOS 2000-10-10T23:13:10  Sdsq=  .196E+05 S/E=  .185E-02

Data for bank  1 read from file insc3.dat

The powder pattern has  5739 channels with   1 bins per channel

No fixed background points for this powder pattern

The  7 excluded regions are (in deg):

Exclude    from:       to:     from:       to:     from:       to:     from:       to:

.0000     .0000   22.7000   23.0000   38.0000   38.6000   44.4000   45.5000

64.8000   65.5000   77.7500   78.7500  120.0000 1000.0000

Incident spectrum type  0 can be used in the region     .000 deg to  180.000 deg

The minimum possible weighted residual for this histogram is    .0294

Histogram no.  1 on file INSC3.P01

updated with new excluded regions, background and incident spectrum data.

CPU time =    .06 to update histogram

Lattice parameters for phase 1 are:

a,b,c  = 11.952920 11.952920  8.421080  angles =    90.000    90.000    90.000

volume =  1203.139

Profile function 3 for phase no. 1 has the coefficients p1-p19:

.680367E+03   -.206458E+03    .225153E+02    .151040E+02

.131058E+02    .000000E+00    .500000E-03    .500000E-03

-.176200E+01    .233097E+01    .000000E+00   -.964839E+01

.000000E+00   -.108484E-01   -.919656E-01    .196692E-01

.313215E-02    .559606E-01    .000000E+00

cutoff on the wings at  .015 of maximum

Minimum d-spacing used to generate reflections    .8795 for phase 1

Minimum d-spacing used to generate reflections    .9883 for phase 1

Minimum d-spacing for matching reflections    .8894

Estimated number of reflections to be generated is   710

Number of reflections generated for phase 1 is   544

Total number of reflections generated for all phases is   544

CPU time =    .00 sec. to generate reflections.

CPU time =    .39 sec. to locate reflection limits.

CPU time =    .05 sec. to match reflection ranges to powder pattern

The maximum number of reflections contributing to any profile point is   36

CPU time =    .06 sec. to update file

1Ba3Cu3Sc3InO12                                                              Version        2000-10-10T23:15:47  Page   1

|----------------------------------------------------|

|            Program GENLES Version MS-DOS           |

|    General crystal structure refinement program    |

| Magnetic structure refinement added by M. Yethiraj |

|   Revised and corrected by Larson and Von Dreele   |

|      Distributed on 15/ 7/1999; 0:28:26            |

|----------------------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The experiment file is: INSC3.EXP

The last history record is :

HSTRY258 POWPREF MS-DOS 2000-10-10T23:15:39

Maximum number of cycles is   10

I/SigI cut-off is  1.00

Structure factors will be extracted from histogram  1

using extraction method codes     0    0    0    0    0    0    0    0    0

The atomic and magnetic scattering factors for  5 types of atoms are:

Atom type   b-len   a(1)      b(1)      a(2)      b(2)      a(3)      b(3)      a(4)      b(4)      c

BA           .525  20.33610   3.21600  19.29700    .27560  10.88800  20.20730   2.69590 167.20200   2.77310

CU           .772  13.33800   3.58280   7.16760    .24700   5.61580  11.39660   1.67350  64.81260   1.19100

IN           .406  19.16240    .54760  18.55960   6.37760   4.29480  25.84990   2.03960  92.80290   4.93910

SC          1.230   9.18900   9.02130   7.36790    .57290   1.64090 136.10800   1.46800  51.35310   1.33290

O            .581   3.04850  13.27710   2.28680   5.70110   1.54630    .32390    .86700  32.90890    .25080

Atom type  CrKa f'      f"   FeKa f'      f"   CuKa f'      f"   MoKa f'      f"   AgKa f'      f"

BA         -11.460    9.980   -4.830   12.160   -1.330    8.460    -.610    2.280    -.980    1.500

CU           -.795    1.196   -1.129     .888   -2.019     .589     .263    1.266     .265     .826

IN          -1.788    9.627    -.626    7.356    -.126    5.045    -.936    1.310   -1.493     .854

SC           -.717    2.968    -.038    2.256     .285    1.533     .226     .372     .156     .235

O             .090     .073     .069     .052     .047     .032     .008     .006     .003     .004

Space group   I 4/mcm

The lattice is centric  I-centered tetragonal    Laue symmetry 4/mmm

Multiplicity of a general site is  32

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)    -Y      X      Z

( 3)    -X     -Y      Z  ( 4)     Y     -X      Z

( 5)    -X      Y  1/2+Z  ( 6)    -Y     -X  1/2+Z

( 7)     X     -Y  1/2+Z  ( 8)     Y      X  1/2+Z

1Ba3Cu3Sc3InO12                                                     GENLES   Version MS-DOS 2000-10-10T23:15:47  Page   2

The atom positions read in are

Type seq. At. name  mult   symm  frac   pn    X    pn    Y    pn    Z    pn  u11 pn  u22 pn  u33 pn  u12 pn  u13 pn  u23 pn

BA      1 BA1         44/M(001) 1.0000   0  .0000   0  .0000   0  .0000   0  .6   1

BA      2 BA2         8MM2(110) 1.0000   0  .2778   2  .7778   3  .0000   0  .5   4

CU      3 CU3         4-42M 001 1.0000   0  .5000   0  .0000   0  .2500   0  .9   5

CU      4 CU4         8MM2(110) 1.0000   0  .1060   6  .6060   7  .0000   0  .6   8

IN      5 IN5        16  2(100)  .2603   9  .2418  10  .0000   0  .2500   0  .1   0

SC      6 SC6        16  2(100)  .7397  11  .2418  12  .0000   0  .2500   0  .1   0

O       7 O7         16  M(+-0) 1.0000   0  .1168  13  .6168  14  .2298  15  .0  16

O       8 O8         16  2(110) 1.0000   0  .1297  17  .1297  18  .2500   0  .0  19

O       9 O9         16  M(001) 1.0000   0  .2423  20  .5005  21  .0000   0  .0  22

Constraints read are LNCN   1 1  5X     1.0000 1  6X     1.0000

LNCN   2 1  5UISO  1.0000 1  6UISO  1.0000

Parameter missing - 1  5UISO

Parameter missing - 1  6UISO

LNCN   3 1  5FRAC -1.0000 1  6FRAC  1.0000

LNCN   4 1  7UISO  1.0000 1  8UISO  1.0000 1  9UISO  1.0000

Lattice parameters for phase 1 are:

a         b         c          alpha      beta     gamma

11.952920 11.952920  8.421080   90.0000   90.0000   90.0000

These cell parameters will be refined

Reciprocal metric tensor elements:          damp= 0

Element :          g11   pn          g22   pn          g33   pn        2*g12   pn        2*g13   pn        2*g23   pn

Value   :   6.99926E-03  23   6.99926E-03  24   1.41015E-02  25  -1.70333E-10   0  -2.41772E-10   0  -2.41772E-10   0

Constr. :          1.000  1          1.000  1          1.000  2           .000  0           .000  0           .000  0

Phase/element fractions for phase no.  1

Hist Elm:    PXC   1 1   nc

Fraction:    1.4220      26

Dmp/Cnst:    0     1.000  3

Histogram scale factors:

Hist.   :        1  PXC  pn

Scale   :    11.068      27

Dmp/Cnst:    0     1.000  4

Absorption coefficients for powder data:

Hist/Typ:    1  PXC    0 pn

Absc 1. :    .00000       0

Dmp/Cnst:    0      .000  0

Absc 2. :    .00000       0

Dmp/Cnst:    0      .000  0

Diffractometer constants for powder data:

No. Type    Lam 1        Lam 2      Polariz.  pn Cnstr cn type    Zero  pn Cnstr cn    Kratio  pn Cnstr cn Damp

1  PXC  1.5405000    1.5443000       .50000   0  .000  0  0   -10.015  28 1.000  5     .5000   0  .000  0    0

Extinction coefficients for phase no.  1:

Hist.   :        1  PXC  pn

Extinct.:    .00000       0

Dmp/Cnst:    0      .000  0

1Ba3Cu3Sc3InO12                                                     GENLES   Version MS-DOS 2000-10-10T23:15:47  Page   3

Orientation distribution coefficients for powder data:

No ODF data for phase  1

Preferred orientation coeffs. for phase no.  1 histogram no.  1:

Axis    :        1       pn

Dir./typ:     .0  .0 1.0  0

PO ratio:        1.0000   0

Dmp/Cnst:    0      .000  0

PO frac.:        1.0000   0

Dmp/Cnst:    0      .000  0

Profile coeff. for function type  3, phase no.  1 and histogram no.  1; aniso. axis   0.   0.   1.; damp= 0:

Coeff.  :      GU    pn      GV    pn      GW    pn      GP    pn      LX    pn      LY    pn     S/L    pn     H/L    pn

Value   : 6.804E+02  29-2.065E+02  30 2.252E+01  31 1.510E+01  32 1.311E+01  33 0.000E+00   0 5.000E-04   0 5.000E-04   0

Constr. :      1.000  6      1.000  7      1.000  8      1.000  9      1.000 10       .000  0       .000  0       .000  0

Coeff.  :     trns   pn     shft   pn     stec   pn     ptec   pn     sfec   pn     L11    pn     L22    pn     L33    pn

Value   :-1.762E+00   0 2.331E+00   0 0.000E+00   0-9.648E+00   0 0.000E+00   0-1.085E-02   0-9.197E-02   0 1.967E-02   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     L12    pn     L13    pn     L23    pn

Value   : 3.132E-03   0 5.596E-02   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0

Diffuse scattering coefficients for powder data:

No diffuse scattering coefficients for histogram    1

Background coefficients for powder data:

Histogram no.:    1 Damping factor:    0 Use all points: Y

Power series in Q**2n/n! and n!/Q**2n

Param.  :          1   pn          2   pn          3   pn          4   pn          5   pn          6   pn

Coeff.  :  .73288E+03  34  .52732E+01  35  .12142E+03  36 -.53999E+00  37 -.44484E+01  38  .21373E-01  39

Param.  :          7   pn

Coeff.  :  .13870E+00  40

The constraint matrix has   40 terms

1Ba3Cu3Sc3InO12                                                     GENLES   Version MS-DOS 2000-10-10T23:15:47  Page   4

Restraint data statistics:

Powder data statistics                Fitted         All               Average

Bank Ndata Sum(w*d**2)  wRp     Rp    wRp     Rp     DWd  Integral

Hstgm  1 PXC   1  5553  19776.      .0555  .0398  .0555  .0398    .617    .921

Powder totals     5553  19776.      .0555  .0398  .0555  .0398    .617

No serial correlation in fit at 90% confidence for 1.928 < DWd < 2.072

Cycle 413 There were  5553 observations. Total before-cycle CHI**2 = 1.9776E+04

Reduced CHI**2 =  3.581     for   31 variables

Reflection data statistics

Histogram  1  Type PXC   Nobs=  541 R(F**2) =   .0517

2 Columns of the    31 Column matrix are 0.0

Variable 1  1PF 4 was not refined

Variable    1HSCL was not refined

The value of the determinant is   .2135*10.0**(   -15)

Atom parameters for phase no. 1

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

BA    (  1) Values  : 1.000   .000000   .000000   .000000     .606

Sigmas  :                                         .056

Shft/esd:                                          .02

BA1      moved   .00A     sum(shift/e.s.d)**2 :     .00

BA    (  2) Values  : 1.000   .277774   .777772   .000000     .511

Sigmas  :         .000087   .000087               .048

Shft/esd:            -.06      -.06                .14

BA2      moved   .00A     sum(shift/e.s.d)**2 :     .03

CU    (  3) Values  : 1.000   .500000   .000000   .250000     .938

Sigmas  :                                         .197

Shft/esd:                                         -.03

CU3      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  4) Values  : 1.000   .106027   .606031   .000000     .607

Sigmas  :         .000198   .000198               .136

Shft/esd:             .06       .06                .00

CU4      moved   .00A     sum(shift/e.s.d)**2 :     .01

IN    (  5) Values  :  .260   .241776   .000000   .250000     .078

Sigmas  :  .003   .000169

Shft/esd:   .02      -.04

IN5      moved   .00A     sum(shift/e.s.d)**2 :     .00

1Ba3Cu3Sc3InO12                                                     GENLES   Version MS-DOS 2000-10-10T23:15:50  Page   5

SC    (  6) Values  :  .740   .241776   .000000   .250000     .078

Sigmas  :  .003   .000169

Shft/esd:  -.02      -.04

SC6      moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  7) Values  : 1.000   .116941   .616943   .229809     .031

Sigmas  :         .000774   .000774   .001122     .124

Shft/esd:             .13       .13       .00     -.03

O7       moved   .00A     sum(shift/e.s.d)**2 :     .03

O     (  8) Values  : 1.000   .129663   .129663   .250000     .031

Sigmas  :         .000806   .000806               .124

Shft/esd:            -.07      -.07               -.03

O8       moved   .00A     sum(shift/e.s.d)**2 :     .01

O     (  9) Values  : 1.000   .242197   .500489   .000000     .031

Sigmas  :         .001461   .000629               .124

Shft/esd:            -.06       .02               -.03

O9       moved   .00A     sum(shift/e.s.d)**2 :     .01

Maximum atom shift:    .00

Atomic parameter sum(shift/error)**2 for phase 1 :       .09

Calculated unit cell formula weight:  4188.877, density:  5.781gm/cm**3

Phase/element fractions for phase no.  1

Hist Elem:      1 1 PXC

Fraction :    1.42168

Sigmas   :    .534063E-02

Shift/esd:       -.06

Wt. Frac.:     1.0000

Sigmas   :   -.108710E-09

Phase/element fraction sum(shift/error)**2 :       .00

Histogram scale factors:

Histogram:    1  PXC

Scale    :    11.0680

Sigmas   :    .000000

Shift/esd:        .00

Histogram scale factor sum(shift/error)**2 :       .00

Lattice parameters for powder data:

Phase  1

a         b         c       alpha     beta      gamma     volume

Value    :  11.95297  11.95297   8.42105    90.000    90.000    90.000    1203.145

Sigmas   :    .00030    .00030    .00025      .000      .000      .000        .079

Recprocal metric tensor shift factor = 100%

Recprocal metric tensor sum(shift/error)**2 :       .07

Diffractometer coefficients for powder data:

Hist.    :   1  PXC

Zero       :    -10.01

Sigmas     :       .08

Shift/esd  :       .05

Dif. Cons. Sum(shift/error)**2 :       .00

1Ba3Cu3Sc3InO12                                                     GENLES   Version MS-DOS 2000-10-10T23:15:50  Page   6

Profile coefficients for histogram no.  1 and for phase no.  1:

Coeff.   :     GU         GV         GW         GP         LX         LY        S/L        H/L        trns       shft

Value    :  6.745E+02 -1.997E+02  2.143E+01  1.510E+01  1.306E+01  0.000E+00  5.000E-04  5.000E-04 -1.762E+00  2.331E+00

Sigmas   :  3.778E+01  2.909E+01  5.202E+00  0.000E+00  1.079E-01

Shift/esd:       -.15        .23       -.21        .00       -.44

Coeff.   :    stec       ptec       sfec       L11        L22        L33        L12        L13        L23

Value    :  0.000E+00 -9.648E+00  0.000E+00 -1.085E-02 -9.197E-02  1.967E-02  3.132E-03  5.596E-02  0.000E+00

Sigmas   :

Shift/esd:

Profile coef. sum(shift/error)**2 :       .32

Background coefficients for histogram no.  1:

Param.   :           1              2              3              4              5              6

Coeff.   :   7.333558E+02   5.255226E+00   1.208469E+02  -5.376233E-01  -4.360404E+00   2.129347E-02

Sigmas   :   6.126047E+00   8.435759E-01   8.934745E+00   7.099064E-02   1.624252E+00   2.677269E-03

Shift/esd:            .08           -.02           -.06            .03            .05           -.03

Param.   :           7

Coeff.   :   1.362077E-01

Sigmas   :   5.249711E-02

Shift/esd:           -.05

Background coef. sum(shift/error)**2 :       .02

Final variable sum((shift/esd)**2) for cycle 413:        .44 Time:    3.35 sec

1Ba3Cu3Sc3InO12                                                     GENLES   Version MS-DOS 2000-10-10T23:15:50  Page   7

Restraint data statistics:

Powder data statistics                Fitted         All               Average

Bank Ndata Sum(w*d**2)  wRp     Rp    wRp     Rp     DWd  Integral

Hstgm  1 PXC   1  5553  19773.      .0555  .0398  .0555  .0398    .617    .921

Powder totals     5553  19773.      .0555  .0398  .0555  .0398    .617

No serial correlation in fit at 90% confidence for 1.928 < DWd < 2.072

Cycle 414 There were  5553 observations. Total before-cycle CHI**2 = 1.9773E+04

Reduced CHI**2 =  3.581     for   31 variables

Reflection data statistics

Histogram  1  Type PXC   Nobs=  541 R(F**2) =   .0519

2 Columns of the    31 Column matrix are 0.0

Variable 1  1PF 4 was not refined

Variable    1HSCL was not refined

The value of the determinant is   .2152*10.0**(   -15)

Atom parameters for phase no. 1

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

BA    (  1) Values  : 1.000   .000000   .000000   .000000     .606

Sigmas  :                                         .056

Shft/esd:                                          .00

BA1      moved   .00A     sum(shift/e.s.d)**2 :     .00

BA    (  2) Values  : 1.000   .277774   .777772   .000000     .511

Sigmas  :         .000087   .000087               .048

Shft/esd:             .00       .00               -.01

BA2      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  3) Values  : 1.000   .500000   .000000   .250000     .938

Sigmas  :                                         .197

Shft/esd:                                          .00

CU3      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  4) Values  : 1.000   .106026   .606030   .000000     .607

Sigmas  :         .000198   .000198               .136

Shft/esd:            -.01      -.01                .00

CU4      moved   .00A     sum(shift/e.s.d)**2 :     .00

IN    (  5) Values  :  .260   .241776   .000000   .250000     .078

Sigmas  :  .003   .000169

Shft/esd:   .00       .00

IN5      moved   .00A     sum(shift/e.s.d)**2 :     .00

1Ba3Cu3Sc3InO12                                                     GENLES   Version MS-DOS 2000-10-10T23:15:53  Page   8

SC    (  6) Values  :  .740   .241776   .000000   .250000     .078

Sigmas  :  .003   .000169

Shft/esd:   .00       .00

SC6      moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  7) Values  : 1.000   .116937   .616939   .229830     .031

Sigmas  :         .000773   .000773   .001122     .123

Shft/esd:             .00       .00       .02      .00

O7       moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  8) Values  : 1.000   .129659   .129659   .250000     .031

Sigmas  :         .000805   .000805               .123

Shft/esd:            -.01      -.01                .00

O8       moved   .00A     sum(shift/e.s.d)**2 :     .00

O     (  9) Values  : 1.000   .242196   .500489   .000000     .031

Sigmas  :         .001459   .000629               .123

Shft/esd:             .00       .00                .00

O9       moved   .00A     sum(shift/e.s.d)**2 :     .00

Maximum atom shift:    .00

Atomic parameter sum(shift/error)**2 for phase 1 :       .00

Calculated unit cell formula weight:  4188.876, density:  5.781gm/cm**3

Phase/element fractions for phase no.  1

Hist Elem:      1 1 PXC

Fraction :    1.42167

Sigmas   :    .534073E-02

Shift/esd:        .00

Wt. Frac.:     1.0000

Sigmas   :   -.704026E-10

Phase/element fraction sum(shift/error)**2 :       .00

Histogram scale factors:

Histogram:    1  PXC

Scale    :    11.0680

Sigmas   :    .000000

Shift/esd:        .00

Histogram scale factor sum(shift/error)**2 :       .00

Lattice parameters for powder data:

Phase  1

a         b         c       alpha     beta      gamma     volume

Value    :  11.95297  11.95297   8.42106    90.000    90.000    90.000    1203.147

Sigmas   :    .00030    .00030    .00025      .000      .000      .000        .079

Recprocal metric tensor shift factor = 100%

Recprocal metric tensor sum(shift/error)**2 :       .00

Diffractometer coefficients for powder data:

Hist.    :   1  PXC

Zero       :    -10.01

Sigmas     :       .08

Shift/esd  :       .01

Dif. Cons. Sum(shift/error)**2 :       .00

1Ba3Cu3Sc3InO12                                                     GENLES   Version MS-DOS 2000-10-10T23:15:53  Page   9

Profile coefficients for histogram no.  1 and for phase no.  1:

Coeff.   :     GU         GV         GW         GP         LX         LY        S/L        H/L        trns       shft

Value    :  6.741E+02 -1.991E+02  2.130E+01  1.510E+01  1.306E+01  0.000E+00  5.000E-04  5.000E-04 -1.762E+00  2.331E+00

Sigmas   :  3.773E+01  2.905E+01  5.192E+00  0.000E+00  1.079E-01

Shift/esd:       -.01        .02       -.02        .00       -.01

Coeff.   :    stec       ptec       sfec       L11        L22        L33        L12        L13        L23

Value    :  0.000E+00 -9.648E+00  0.000E+00 -1.085E-02 -9.197E-02  1.967E-02  3.132E-03  5.596E-02  0.000E+00

Sigmas   :

Shift/esd:

Profile coef. sum(shift/error)**2 :       .00

Background coefficients for histogram no.  1:

Param.   :           1              2              3              4              5              6

Coeff.   :   7.333693E+02   5.252702E+00   1.208355E+02  -5.374812E-01  -4.358977E+00   2.129040E-02

Sigmas   :   6.125495E+00   8.435051E-01   8.933768E+00   7.098291E-02   1.624091E+00   2.676904E-03

Shift/esd:            .00            .00            .00            .00            .00            .00

Param.   :           7

Coeff.   :   1.361723E-01

Sigmas   :   5.249235E-02

Shift/esd:            .00

Background coef. sum(shift/error)**2 :       .00

Final variable sum((shift/esd)**2) for cycle 414:        .00 Time:    2.47 sec

Convergence was achieved

1Ba3Cu3Sc3InO12                                                     PUBTABLE Version MS-DOS 2000-10-10T23:16:29  Page   1

|-----------------------------------------|

|     Program PUBTABLES Version MS-DOS    |

|  Generate crystal structure data tables |

| Distributed on 15/ 7/1999; 0:32:10      |

|-----------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY259 GENLES  MS-DOS 2000-10-10T23:15:50  Sdsq=  .198E+05 S/E=  .302E-02

--------------------------------------------------------------

Archiving C:/GSAS/phil/insc3/INSC3.EXP as C:/GSAS/phil/insc3/INSC3!213.EXP

--------------------------------------------------------------

--------------------------------------------------------------

Archiving C:/GSAS/phil/insc3/INSC3.EXP as C:/GSAS/phil/insc3/INSC3!214.EXP

--------------------------------------------------------------

--------------------------------------------------------------

Archiving C:/GSAS/phil/insc3/INSC3.EXP as C:/GSAS/phil/insc3/INSC3!215.EXP

--------------------------------------------------------------

Supplementary Material (ESI) for Journal of Materials Chemistry

This journal is (c) The Royal Society of Chemistry 2001