--------------------------------------------------------------

Archiving C:/GSAS/phil/sc4012/SC4O12.EXP as C:/GSAS/phil/sc4012/SC4O12!169.EXP

--------------------------------------------------------------

1Ba3cu3sc4o12                                                                Version        2000-10-10T10:51:12  Page   1

|---------------------------------------------------------|

|              Program POWPREF Version MS-DOS             |

| Prepares powder histograms for least-squares refinement |

|         Distributed on 15/ 7/1999; 0:31:36              |

|---------------------------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY328 EXPEDT  MS-DOS 2000-10-10T10:51:07                          D  C

Data for bank  1 read from file sc4012.dat

The powder pattern has  5710 channels with   1 bins per channel

No fixed background points for this powder pattern

The  2 excluded regions are (in deg):

Exclude    from:       to:     from:       to:     from:       to:     from:       to:

.0000     .0000  119.2000 1000.0000

Incident spectrum type  0 can be used in the region     .000 deg to  180.000 deg

The minimum possible weighted residual for this histogram is    .0333

Histogram no.  1 on file SC4O12.P01

updated with new excluded regions, background and incident spectrum data.

CPU time =    .05 to update histogram

Lattice parameters for phase 1 are:

a,b,c  = 11.902100 11.902100  8.396251  angles =    90.000    90.000    90.000

volume =  1189.413

Lattice parameters for phase 2 are:

a,b,c  =  4.049120  4.049120  4.049120  angles =    90.000    90.000    90.000

volume =    66.387

Profile function 3 for phase no. 1 has the coefficients p1-p19:

.561905E+02   -.724267E+02    .471038E+01    .209305E+02

.836506E+01    .910557E+00    .500000E-03    .500000E-03

-.564865E+01   -.524510E+01    .183293E+02   -.488179E+01

.000000E+00   -.253358E-03   -.106641E+00   -.176976E+00

.000000E+00    .000000E+00    .000000E+00

cutoff on the wings at  .010 of maximum

Profile function 3 for phase no. 2 has the coefficients p1-p19:

.867931E+03   -.128682E+04    .482162E+03    .000000E+00

.000000E+00    .000000E+00    .500000E-03    .500000E-03

.000000E+00    .000000E+00    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00    .000000E+00

.000000E+00    .000000E+00    .000000E+00

cutoff on the wings at  .010 of maximum

Minimum d-spacing used to generate reflections    .8872 for phase 1

Minimum d-spacing used to generate reflections    .8821 for phase 2

Minimum d-spacing used to generate reflections    .9926 for phase 1

Minimum d-spacing used to generate reflections    .9886 for phase 2

Minimum d-spacing for matching reflections    .8931

Estimated number of reflections to be generated is   710

Number of reflections generated for phase 1 is   532

Number of reflections generated for phase 2 is    16

Total number of reflections generated for all phases is   548

CPU time =    .00 sec. to generate reflections.

CPU time =    .39 sec. to locate reflection limits.

CPU time =    .05 sec. to match reflection ranges to powder pattern

The maximum number of reflections contributing to any profile point is   32

CPU time =    .06 sec. to update file

1Ba3cu3sc4o12                                                                Version        2000-10-10T10:51:32  Page   1

|----------------------------------------------------|

|            Program GENLES Version MS-DOS           |

|    General crystal structure refinement program    |

| Magnetic structure refinement added by M. Yethiraj |

|   Revised and corrected by Larson and Von Dreele   |

|      Distributed on 15/ 7/1999; 0:28:26            |

|----------------------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The experiment file is: SC4O12.EXP

The last history record is :

HSTRY329 POWPREF MS-DOS 2000-10-10T10:51:12

Maximum number of cycles is    6

I/SigI cut-off is  1.00

Structure factors will be extracted from histogram  1

using extraction method codes     0    0    0    0    0    0    0    0    0

The atomic and magnetic scattering factors for  5 types of atoms are:

Atom type   b-len   a(1)      b(1)      a(2)      b(2)      a(3)      b(3)      a(4)      b(4)      c

BA           .525  20.33610   3.21600  19.29700    .27560  10.88800  20.20730   2.69590 167.20200   2.77310

CU           .772  13.33800   3.58280   7.16760    .24700   5.61580  11.39660   1.67350  64.81260   1.19100

SC          1.230   9.18900   9.02130   7.36790    .57290   1.64090 136.10800   1.46800  51.35310   1.33290

AL           .345   6.42020   3.03870   1.90020    .74260   1.59360  31.54720   1.96460  85.08860   1.11510

O-2          .581   3.76936  15.07970   2.53342   6.30430   1.91579  40.34450   1.55094    .31291    .22789

Atom type  CrKa f'      f"   FeKa f'      f"   CuKa f'      f"   MoKa f'      f"   AgKa f'      f"

BA         -11.460    9.980   -4.830   12.160   -1.330    8.460    -.610    2.280    -.980    1.500

CU           -.795    1.196   -1.129     .888   -2.019     .589     .263    1.266     .265     .826

SC           -.717    2.968    -.038    2.256     .285    1.533     .226     .372     .156     .235

AL            .318     .522     .269     .381     .204     .246     .056     .052     .032     .031

O-2           .090     .073     .069     .052     .047     .032     .008     .006     .003     .004

Space group   I 4/m c m

The lattice is centric  I-centered tetragonal    Laue symmetry 4/mmm

Multiplicity of a general site is  32

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)    -Y      X      Z

( 3)    -X     -Y      Z  ( 4)     Y     -X      Z

( 5)    -X      Y  1/2+Z  ( 6)    -Y     -X  1/2+Z

( 7)     X     -Y  1/2+Z  ( 8)     Y      X  1/2+Z

1Ba3cu3sc4o12                                                       GENLES   Version MS-DOS 2000-10-10T10:51:32  Page   2

The atom positions read in are

Type seq. At. name  mult   symm  frac   pn    X    pn    Y    pn    Z    pn  u11 pn  u22 pn  u33 pn  u12 pn  u13 pn  u23 pn

BA      1 BA1         44/M(001) 1.0000   0  .0000   0  .0000   0  .0000   0  .6   1

CU      2 CU2         4-42M 001 1.0000   0  .5000   0  .0000   0  .2500   0  .4   2

SC      3 SC3        16  2(100) 1.0000   0  .2420   3  .0000   0  .2500   0  .0   4

O-2     4 O4         16  M(+-0) 1.0000   0  .1201   5  .6201   6  .2315   7 1.2   8

O-2     5 O5         16  2(110) 1.0000   0  .1269   9  .1269  10  .2500   0  .1  11

O-2     6 O6         16  M(001) 1.0000   0  .2390  12  .5012  13  .0000   0 1.4  14

CU      7 CU7         8MM2(110) 1.0000   0  .1048  15  .6048  16  .0000   0 1.1  17

BA      8 BA8         8MM2(110) 1.0000   0  .2771  18  .7771  19  .0000   0  .5  20

Space group   F m 3 m

The lattice is centric  F-centered cubic         Laue symmetry m3m

Multiplicity of a general site is 192

The symmetry of the point 0,0,0 contains 1bar

The equivalent positions are:

( 1)     X      Y      Z  ( 2)     Z      X      Y  ( 3)     Y      Z      X

( 4)     X      Y     -Z  ( 5)    -Z      X      Y  ( 6)     Y     -Z      X

( 7)    -Z      X     -Y  ( 8)    -Y     -Z      X  ( 9)     Y     -Z     -X

(10)    -X      Y     -Z  (11)    -Z     -X      Y  (12)     X     -Y     -Z

(13)     Y      X      Z  (14)     Z      Y      X  (15)     X      Z      Y

(16)     Y      X     -Z  (17)    -Z      Y      X  (18)     X     -Z      Y

(19)    -Z      Y     -X  (20)    -X     -Z      Y  (21)     X     -Z     -Y

(22)    -Y      X     -Z  (23)    -Z     -Y      X  (24)     Y     -X     -Z

The atom positions read in are

Type seq. At. name  mult   symm  frac   pn    X    pn    Y    pn    Z    pn  u11 pn  u22 pn  u33 pn  u12 pn  u13 pn  u23 pn

AL      1 AL1         4   M3M   1.0000   0  .0000   0  .0000   0  .0000   0 2.5   0

Lattice parameters for phase 1 are:

a         b         c          alpha      beta     gamma

11.902100 11.902100  8.396251   90.0000   90.0000   90.0000

These cell parameters will be refined

Reciprocal metric tensor elements:          damp= 0

Element :          g11   pn          g22   pn          g33   pn        2*g12   pn        2*g13   pn        2*g23   pn

Value   :   7.05916E-03  21   7.05916E-03  22   1.41850E-02  23  -1.71791E-10   0  -2.43522E-10   0  -2.43522E-10   0

Constr. :          1.000  1          1.000  1          1.000  2           .000  0           .000  0           .000  0

Lattice parameters for phase 2 are:

a         b         c          alpha      beta     gamma

4.049120  4.049120  4.049120   90.0000   90.0000   90.0000

These cell parameters will be refined

Reciprocal metric tensor elements:          damp= 0

Element :          g11   pn          g22   pn          g33   pn        2*g12   pn        2*g13   pn        2*g23   pn

Value   :   6.09928E-02  24   6.09928E-02  25   6.09928E-02  26  -1.48432E-09   0  -1.48432E-09   0  -1.48432E-09   0

Constr. :          1.000  3          1.000  3          1.000  3           .000  0           .000  0           .000  0

Phase/element fractions for phase no.  1

1Ba3cu3sc4o12                                                       GENLES   Version MS-DOS 2000-10-10T10:51:32  Page   3

Hist Elm:    PXC   1 1   nc

Fraction:    1.5182      27

Dmp/Cnst:    0     1.000  4

Phase/element fractions for phase no.  2

Hist Elm:    PXC   1 1   nc

Fraction:    2.0232      28

Dmp/Cnst:    0     1.000  5

Histogram scale factors:

Hist.   :        1  PXC  pn

Scale   :    8.4503      29

Dmp/Cnst:    0     1.000  6

Absorption coefficients for powder data:

Hist/Typ:    1  PXC    1 pn

Absc 1. :    .00000       0

Dmp/Cnst:    0      .000  0

Absc 2. :    .00000       0

Dmp/Cnst:    0      .000  0

Diffractometer constants for powder data:

No. Type    Lam 1        Lam 2      Polariz.  pn Cnstr cn type    Zero  pn Cnstr cn    Kratio  pn Cnstr cn Damp

1  PXC  1.5405000    1.5443000       .50000   0  .000  0  0    -4.874  30 1.000  7     .5000   0  .000  0    0

Extinction coefficients for phase no.  1:

Hist.   :        1  PXC  pn

Extinct.:    .00000       0

Dmp/Cnst:    0      .000  0

Extinction coefficients for phase no.  2:

Hist.   :        1  PXC  pn

Extinct.:    .00000       0

Dmp/Cnst:    0      .000  0

Orientation distribution coefficients for powder data:

No ODF data for phase  1

No ODF data for phase  2

Preferred orientation coeffs. for phase no.  1 histogram no.  1:

Axis    :        1       pn

Dir./typ:     .0  .0  .0  0

PO ratio:        1.0000   0

Dmp/Cnst:    0      .000  0

PO frac.:        1.0000   0

Dmp/Cnst:    0      .000  0

Preferred orientation coeffs. for phase no.  2 histogram no.  1:

Axis    :        1       pn

Dir./typ:     .0  .0 1.0  0

PO ratio:        1.0000   0

Dmp/Cnst:    0      .000  0

PO frac.:        1.0000   0

Dmp/Cnst:    0      .000  0

1Ba3cu3sc4o12                                                       GENLES   Version MS-DOS 2000-10-10T10:51:32  Page   4

Profile coeff. for function type  3, phase no.  1 and histogram no.  1; aniso. axis   0.   0.   1.; damp= 0:

Coeff.  :      GU    pn      GV    pn      GW    pn      GP    pn      LX    pn      LY    pn     S/L    pn     H/L    pn

Value   : 5.619E+01  31-7.243E+01  33 4.710E+00  35 2.093E+01  37 8.365E+00  38 9.106E-01  39 5.000E-04   0 5.000E-04   0

Constr. :      1.000  8      1.000 10      1.000 12      1.000 14      1.000 15      1.000 16       .000  0       .000  0

Coeff.  :     trns   pn     shft   pn     stec   pn     ptec   pn     sfec   pn     L11    pn     L22    pn     L33    pn

Value   :-5.649E+00  40-5.245E+00  41 1.833E+01  42-4.882E+00  43 0.000E+00   0-2.534E-04   0-1.066E-01   0-1.770E-01   0

Constr. :      1.000 17      1.000 18      1.000 19      1.000 20       .000  0       .000  0       .000  0       .000  0

Coeff.  :     L12    pn     L13    pn     L23    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0

Profile coeff. for function type  3, phase no.  2 and histogram no.  1; aniso. axis   0.   0.   1.; damp= 0:

Coeff.  :      GU    pn      GV    pn      GW    pn      GP    pn      LX    pn      LY    pn     S/L    pn     H/L    pn

Value   : 8.679E+02  32-1.287E+03  34 4.822E+02  36 0.000E+00   0 0.000E+00   0 0.000E+00   0 5.000E-04   0 5.000E-04   0

Constr. :      1.000  9      1.000 11      1.000 13       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     trns   pn     shft   pn     stec   pn     ptec   pn     sfec   pn     L11    pn     L22    pn     L33    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0       .000  0

Coeff.  :     L12    pn     L13    pn     L23    pn

Value   : 0.000E+00   0 0.000E+00   0 0.000E+00   0

Constr. :       .000  0       .000  0       .000  0

Diffuse scattering coefficients for powder data:

No diffuse scattering coefficients for histogram    1

Background coefficients for powder data:

Histogram no.:    1 Damping factor:    0 Use all points: Y

Power series in Q**2n/n! and n!/Q**2n

Param.  :          1   pn          2   pn          3   pn          4   pn          5   pn          6   pn

Coeff.  :  .63336E+03  44 -.78069E+00  45  .63053E+01  46  .15471E-01  47  .18150E+01  48  .78078E-03  49

The constraint matrix has   49 terms

1Ba3cu3sc4o12                                                       GENLES   Version MS-DOS 2000-10-10T10:51:32  Page   5

Restraint data statistics:

Powder data statistics                Fitted         All               Average

Bank Ndata Sum(w*d**2)  wRp     Rp    wRp     Rp     DWd  Integral

Hstgm  1 PXC   1  5710  15300.      .0544  .0406  .0544  .0406    .847    .930

Powder totals     5710  15300.      .0544  .0406  .0544  .0406    .847

No serial correlation in fit at 90% confidence for 1.932 < DWd < 2.068

Cycle 482 There were  5710 observations. Total before-cycle CHI**2 = 1.5300E+04

Reduced CHI**2 =  2.699     for   42 variables

Reflection data statistics

Histogram  1  Type PXC   Nobs=  547 R(F**2) =   .0465

1 Columns of the    42 Column matrix are 0.0

Variable 1  1PF 4 was not refined

The value of the determinant is   .4146*10.0**(   -32)

Atom parameters for phase no. 1

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

BA    (  1) Values  : 1.000   .000000   .000000   .000000     .594

Sigmas  :                                         .054

Shft/esd:                                          .00

BA1      moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  2) Values  : 1.000   .500000   .000000   .250000     .414

Sigmas  :                                         .157

Shft/esd:                                         -.01

CU2      moved   .00A     sum(shift/e.s.d)**2 :     .00

SC    (  3) Values  : 1.000   .242025   .000000   .250000     .040

Sigmas  :         .000187                         .063

Shft/esd:             .00                          .00

SC3      moved   .00A     sum(shift/e.s.d)**2 :     .00

O-2   (  4) Values  : 1.000   .120107   .620107   .231505    1.198

Sigmas  :         .000672   .000672   .000998     .273

Shft/esd:            -.02      -.02       .01      .00

O4       moved   .00A     sum(shift/e.s.d)**2 :     .00

O-2   (  5) Values  : 1.000   .126867   .126867   .250000     .113

Sigmas  :         .000668   .000668               .249

Shft/esd:             .01       .01                .01

O5       moved   .00A     sum(shift/e.s.d)**2 :     .00

1Ba3cu3sc4o12                                                       GENLES   Version MS-DOS 2000-10-10T10:51:35  Page   6

O-2   (  6) Values  : 1.000   .238995   .501218   .000000    1.444

Sigmas  :         .001261   .000546               .439

Shft/esd:             .02       .00               -.01

O6       moved   .00A     sum(shift/e.s.d)**2 :     .00

CU    (  7) Values  : 1.000   .104788   .604788   .000000    1.098

Sigmas  :         .000167   .000167               .110

Shft/esd:             .00       .00                .00

CU7      moved   .00A     sum(shift/e.s.d)**2 :     .00

BA    (  8) Values  : 1.000   .277091   .777091   .000000     .503

Sigmas  :         .000075   .000075               .039

Shft/esd:             .00       .00                .00

BA8      moved   .00A     sum(shift/e.s.d)**2 :     .00

Maximum atom shift:    .00

Atomic parameter sum(shift/error)**2 for phase 1 :       .00

Calculated unit cell formula weight:  3897.808, density:  5.442gm/cm**3

Atom parameters for phase no. 2

frac       x         y         z     100*Uiso  100*U11  100*U22  100*U33  100*U12  100*U13  100*U23

Calculated unit cell formula weight:   107.928, density:  2.700gm/cm**3

Phase/element fractions for phase no.  1

Hist Elem:      1 1 PXC

Fraction :    1.51812

Sigmas   :    1.12012

Shift/esd:        .00

Wt. Frac.:     .96442

Sigmas   :    .253210E-01

Phase/element fractions for phase no.  2

Hist Elem:      1 1 PXC

Fraction :    2.02298

Sigmas   :    1.49516

Shift/esd:        .00

Wt. Frac.:     .35585E-01

Sigmas   :    .253643E-01

Phase/element fraction sum(shift/error)**2 :       .00

Histogram scale factors:

Histogram:    1  PXC

Scale    :    8.45290

Sigmas   :    6.23457

Shift/esd:        .00

Histogram scale factor sum(shift/error)**2 :       .00

Lattice parameters for powder data:

Phase  1

a         b         c       alpha     beta      gamma     volume

Value    :  11.90210  11.90210   8.39625    90.000    90.000    90.000    1189.412

Sigmas   :    .00060    .00060    .00044      .000      .000      .000        .180

Recprocal metric tensor shift factor = 100%

Phase  2

a         b         c       alpha     beta      gamma     volume

Value    :   4.04912   4.04912   4.04912    90.000    90.000    90.000      66.387

Sigmas   :    .00063    .00063    .00063      .000      .000      .000        .031

Recprocal metric tensor shift factor = 100%

Recprocal metric tensor sum(shift/error)**2 :       .00

1Ba3cu3sc4o12                                                       GENLES   Version MS-DOS 2000-10-10T10:51:35  Page   7

Diffractometer coefficients for powder data:

Hist.    :   1  PXC

Zero       :     -4.88

Sigmas     :      1.20

Shift/esd  :       .00

Dif. Cons. Sum(shift/error)**2 :       .00

Profile coefficients for histogram no.  1 and for phase no.  1:

Coeff.   :     GU         GV         GW         GP         LX         LY        S/L        H/L        trns       shft

Value    :  5.618E+01 -7.244E+01  4.713E+00  2.093E+01  8.363E+00  9.150E-01  5.000E-04  5.000E-04 -5.650E+00 -5.248E+00

Sigmas   :  4.905E+00  5.153E+00  1.363E+00  0.000E+00  3.254E-01  8.901E-01                        3.365E-01  1.163E+00

Shift/esd:        .00        .00        .00        .00       -.01        .00                             -.01        .00

Coeff.   :    stec       ptec       sfec       L11        L22        L33        L12        L13        L23

Value    :  1.833E+01 -4.881E+00  0.000E+00 -2.534E-04 -1.066E-01 -1.770E-01  0.000E+00  0.000E+00  0.000E+00

Sigmas   :  1.187E+00  4.763E-01

Shift/esd:        .00        .00

Profile coefficients for histogram no.  1 and for phase no.  2:

Coeff.   :     GU         GV         GW         GP         LX         LY        S/L        H/L        trns       shft

Value    :  8.682E+02 -1.287E+03  4.823E+02  0.000E+00  0.000E+00  0.000E+00  5.000E-04  5.000E-04  0.000E+00  0.000E+00

Sigmas   :  1.364E+02  1.868E+02  6.351E+01

Shift/esd:        .00        .00        .00

Coeff.   :    stec       ptec       sfec       L11        L22        L33        L12        L13        L23

Value    :  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00  0.000E+00

Sigmas   :

Shift/esd:

Profile coef. sum(shift/error)**2 :       .00

Background coefficients for histogram no.  1:

Param.   :           1              2              3              4              5              6

Coeff.   :   6.333606E+02  -7.808476E-01   6.305418E+00   1.546070E-02   1.814985E+00   7.819885E-04

Sigmas   :   3.226108E+00   5.180310E-01   2.897269E+00   4.699878E-02   2.227280E-01   1.847778E-03

Shift/esd:            .00            .00            .00            .00            .00            .00

Background coef. sum(shift/error)**2 :       .00

Final variable sum((shift/esd)**2) for cycle 482:        .00 Time:    2.64 sec

Convergence was achieved

1Ba3cu3sc4o12                                                       PUBTABLE Version MS-DOS 2000-10-10T10:52:00  Page   1

|-----------------------------------------|

|     Program PUBTABLES Version MS-DOS    |

|  Generate crystal structure data tables |

| Distributed on 15/ 7/1999; 0:32:10      |

|-----------------------------------------|

|---------------------------------------------------------------|

|            Allen C. Larson and Robert B. Von Dreele           |

|      Manuel Lujan, Jr. Neutron Scattering Center, MS-H805     |

|      Los Alamos National Laboratory, Los Alamos, NM  87545    |

|                                                               |

| Copyright, 1999, The Regents of the University of California. |

|---------------------------------------------------------------|

The last history record is :

HSTRY330 GENLES  MS-DOS 2000-10-10T10:51:32  Sdsq=  .153E+05 S/E=  .103E-02