List of Tables in the Supplementary Material (29 pages)

Table S1.  Crystal data and structure refinement for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

Table S2.  Atomic coordinates ( x 10^4) and equivalent isotropic displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

Table S3.  Bond lengths [A] and angles [deg] for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

Table S4.  Anisotropic displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

Table S5.  Hydrogen coordinates ( x 10^4) and isotropic displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

Table S6.  Crystal data and structure refinement for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K.

Table S7.  Atomic coordinates ( x 10^4) and equivalent isotropic displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K.

Table S8.  Bond lengths [A] and angles [deg] for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K.

Table S9.  Anisotropic displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K

Table S10.  Hydrogen coordinates ( x 10^4) and isotropic displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K.

Table S11.  Crystal data and structure refinement for (SMeEt2)0.5[Pd(dmit)2]  (2) at 160 K.

Table S12.  Atomic coordinates ( x 10^4) and equivalent isotropic displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at 160 K.

Table S13.  Bond lengths [A] and angles [deg] for (SMeEt2)0.5[Pd(dmit)2]  (2)  at 160 K.

Table S14.  Anisotropic displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at 160 K

Table S15.  Hydrogen coordinates ( x 10^4) and isotropic displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at 160 K.

Table S16.  Crystal data and structure refinement for (SMeEt2)0.5[Pd(dmit)2]  (2) at room temperature.

Table S17.  Atomic coordinates ( x 10^4) and equivalent isotropic displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at room temperature

Table S18.  Bond lengths [A] and angles [deg] for (SMeEt2)0.5[Pd(dmit)2]  (2)  at room temperature.

Table S19.  Anisotropic displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at room temperature

Table S20.  Hydrogen coordinates ( x 10^4) and isotropic displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at room temperature.

Table S21 : Short S…S distances (< 3.70 Å) between the Pd(dmit)2 units in (SMeEt2)0.5[Pd(dmit)2] (2) at room temperature

Table S1.  Crystal data and structure refinement for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

Identification code               (SMeEt2)[Pd(dmit)2]2  (1)

Empirical formula                 C17 H13 Pd2 S21

Formula weight                    1103.58

Temperature                       293(2) K

Wavelength                        0.71073 A

Crystal system, space group       Triclinic,  P-1

Unit cell dimensions              a = 7.804(4) A   alpha = 91.68(4) deg.

b = 36.171(18) A    beta = 112.08(4) deg.

c = 6.284(2) A   gamma = 88.79(5) deg.

Volume                            1642.9(13) A^3

Z, Calculated density             2,  2.230 Mg/m^3

Absorption coefficient            2.446 mm^-1

F(000)                            1086

Crystal size                      0.30 x 0.25 x 0.05 mm

Theta range for data collection   1.13 to 22.5 deg.

Limiting indices                  -8<=h<=13, -38<=k<=38, 0<=l<=6

Reflections collected / unique    4698 / 4305 [R(int) = 0.2488]

Completeness to theta = 22.5      21.5 %

Absorption correction             Psi-scan

Max. and min. transmission        0.9902 and 0.5116

Refinement method                 Full-matrix least-squares on F^2

Data / restraints / parameters    4305 / 71 / 394

Goodness-of-fit on F^2            1.150

Final R indices [I>2sigma(I)]     R1 = 0.0651, wR2 = 0.1708

R indices (all data)              R1 = 0.1022, wR2 = 0.1987

Largest diff. peak and hole       1.701 and -1.224 e.A^-3

Table S2.  Atomic coordinates ( x 10^4) and equivalent isotropic

displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

U(eq) is defined as one third of the trace of the orthogonalized

Uij tensor.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

S(1)         4510(11)      2526(2)       7682(12)     106(2)

C(1A)        3360(50)      2331(11)      5060(30)      78(8)

C(1B)        4410(50)      2081(7)       6370(50)      68(8)

C(2)         4830(40)      2838(9)       5670(50)     130(9)

C(3A)        6590(90)      2760(20)      5250(170)    130(20)

C(3B)        6110(120)     2620(20)      4800(200)    160(20)

C(4)         2110(40)      2618(8)       7270(40)     112(8)

C(5A)        2020(110)     2427(19)      9300(90)     121(18)

C(5B)        1350(90)      2319(18)      8250(90)     107(17)

Pd(1)        1880(2)       4816(1)      10178(2)       31(1)

S(11)         370(6)       4344(1)       7701(6)       37(1)

S(12)        1981(6)       4474(1)      13228(6)       37(1)

S(13)        -659(6)       3592(1)       8588(7)       45(1)

S(14)         787(6)       3700(1)      13484(7)       45(1)

S(15)        -893(8)       2983(1)      11517(9)       69(1)

S(16)        3559(6)       5261(1)      12691(6)       38(1)

S(17)        1974(6)       5151(1)       7178(6)       38(1)

S(18)        5042(6)       5978(1)      11968(7)       43(1)

S(19)        3638(6)       5879(1)       7048(7)       42(1)

S(20)        5617(7)       6566(1)       9137(9)       60(1)

C(11)         279(18)      4024(4)       9570(30)      33(3)

C(12)        1000(20)      4075(4)      11940(20)      33(3)

C(13)        -300(30)      3396(4)      11230(30)      50(4)

C(14)        3823(19)      5565(4)      10920(30)      35(4)

C(15)        3160(20)      5530(4)       8580(20)      35(4)

C(16)        4810(20)      6171(4)       9400(30)      38(4)

Pd(2)        1851(2)        189(1)      10214(2)       31(1)

S(21)        1970(5)       -144(1)       7116(6)       37(1)

S(22)        3587(5)       -257(1)      12604(6)       38(1)

S(23)        3729(6)       -872(1)       6780(7)       42(1)

S(24)        5151(6)       -972(1)      11667(7)       41(1)

S(25)        5770(7)      -1561(1)       8651(9)       59(1)

S(26)        1909(5)        534(1)      13351(6)       37(1)

S(27)         295(6)        660(1)       7861(6)       38(1)

S(28)         602(6)       1306(1)      13803(7)       47(1)

S(29)        -848(6)       1412(1)       8923(7)       49(1)

S(30)       -1167(8)       2023(1)      12012(10)      77(2)

C(21)        3250(20)      -517(4)       8440(20)      33(3)

C(22)        3879(17)      -567(4)      10710(20)      31(3)

C(23)        4890(20)     -1159(4)       9020(30)      42(4)

C(24)         813(18)       929(4)      12120(20)      32(3)

C(25)         169(19)       981(4)       9830(20)      35(4)

C(26)        -550(20)      1602(4)      11580(30)      48(4)

________________________________________________________________

Table S3.  Bond lengths [A] and angles [deg] for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

_____________________________________________________________

S(1)-C(1A)                    1.692(19)

S(1)-C(1B)                    1.777(18)

S(1)-C(2)                     1.81(3)

S(1)-C(4)                     1.82(3)

C(2)-C(3B)                    1.52(2)

C(2)-C(3A)                    1.51(2)

C(4)-C(5A)                    1.50(2)

C(4)-C(5B)                    1.50(2)

Pd(1)-S(16)                   2.279(4)

Pd(1)-S(12)                   2.287(4)

Pd(1)-S(17)                   2.295(4)

Pd(1)-S(11)                   2.297(4)

Pd(1)-Pd(1)#1                 3.130(3)

S(11)-C(11)                   1.694(15)

S(12)-C(12)                   1.681(15)

S(13)-C(11)                   1.736(14)

S(13)-C(13)                   1.747(16)

S(14)-C(13)                   1.724(17)

S(14)-C(12)                   1.736(13)

S(15)-C(13)                   1.610(17)

S(16)-C(14)                   1.659(15)

S(17)-C(15)                   1.697(16)

S(18)-C(16)                   1.724(15)

S(18)-C(14)                   1.760(15)

S(19)-C(15)                   1.738(14)

S(19)-C(16)                   1.751(16)

S(20)-C(16)                   1.609(15)

C(11)-C(12)                   1.39(2)

C(14)-C(15)                   1.37(2)

Pd(2)-S(22)                   2.285(4)

Pd(2)-S(26)                   2.287(4)

Pd(2)-S(21)                   2.290(4)

Pd(2)-S(27)                   2.296(4)

Pd(2)-Pd(2)#2                 3.139(3)

S(21)-C(21)                   1.701(13)

S(22)-C(22)                   1.684(14)

S(23)-C(23)                   1.722(15)

S(23)-C(21)                   1.754(12)

S(24)-C(23)                   1.721(15)

S(24)-C(22)                   1.740(14)

S(25)-C(23)                   1.640(15)

S(26)-C(24)                   1.701(14)

S(27)-C(25)                   1.700(15)

S(28)-C(26)                   1.733(17)

S(28)-C(24)                   1.742(14)

S(29)-C(26)                   1.723(18)

S(29)-C(25)                   1.743(14)

S(30)-C(26)                   1.633(16)

C(21)-C(22)                   1.340(19)

C(24)-C(25)                   1.35(2)

C(1A)-S(1)-C(1B)             43.6(17)

C(1A)-S(1)-C(2)              75.0(15)

C(1B)-S(1)-C(2)             104.3(15)

C(1A)-S(1)-C(4)              77.7(16)

C(1B)-S(1)-C(4)             102.7(15)

C(2)-S(1)-C(4)              101.4(13)

C(3B)-C(2)-C(3A)             24(6)

C(3B)-C(2)-S(1)             102(5)

C(3A)-C(2)-S(1)             113(4)

C(5A)-C(4)-C(5B)             30(3)

C(5A)-C(4)-S(1)             100(4)

C(5B)-C(4)-S(1)             111(3)

S(16)-Pd(1)-S(12)            89.12(14)

S(16)-Pd(1)-S(17)            89.73(14)

S(12)-Pd(1)-S(17)           176.37(16)

S(16)-Pd(1)-S(11)           176.11(15)

S(12)-Pd(1)-S(11)            90.01(14)

S(17)-Pd(1)-S(11)            90.91(14)

S(16)-Pd(1)-Pd(1)#1          92.50(12)

S(12)-Pd(1)-Pd(1)#1          91.55(12)

S(17)-Pd(1)-Pd(1)#1          91.94(12)

S(11)-Pd(1)-Pd(1)#1          91.31(12)

C(11)-S(11)-Pd(1)           101.0(5)

C(12)-S(12)-Pd(1)           102.3(5)

C(11)-S(13)-C(13)            98.7(8)

C(13)-S(14)-C(12)            99.4(8)

C(14)-S(16)-Pd(1)           101.4(6)

C(15)-S(17)-Pd(1)           101.5(5)

C(16)-S(18)-C(14)            99.3(7)

C(15)-S(19)-C(16)            97.3(7)

C(12)-C(11)-S(11)           124.0(11)

C(12)-C(11)-S(13)           115.4(11)

S(11)-C(11)-S(13)           120.5(9)

C(11)-C(12)-S(12)           122.5(10)

C(11)-C(12)-S(14)           115.0(11)

S(12)-C(12)-S(14)           122.5(8)

S(15)-C(13)-S(14)           124.6(10)

S(15)-C(13)-S(13)           123.9(10)

S(14)-C(13)-S(13)           111.5(9)

C(15)-C(14)-S(16)           125.6(12)

C(15)-C(14)-S(18)           113.4(11)

S(16)-C(14)-S(18)           121.0(9)

C(14)-C(15)-S(17)           121.8(11)

C(14)-C(15)-S(19)           117.9(12)

S(17)-C(15)-S(19)           120.3(8)

S(20)-C(16)-S(18)           125.1(10)

S(20)-C(16)-S(19)           122.9(9)

S(18)-C(16)-S(19)           111.9(8)

S(22)-Pd(2)-S(26)            89.42(14)

S(22)-Pd(2)-S(21)            89.87(14)

S(26)-Pd(2)-S(21)           176.55(15)

S(22)-Pd(2)-S(27)           175.97(16)

S(26)-Pd(2)-S(27)            89.98(14)

S(21)-Pd(2)-S(27)            90.49(13)

S(22)-Pd(2)-Pd(2)#2          91.84(12)

S(26)-Pd(2)-Pd(2)#2          91.68(12)

S(21)-Pd(2)-Pd(2)#2          91.71(12)

S(27)-Pd(2)-Pd(2)#2          92.16(12)

C(21)-S(21)-Pd(2)           100.7(5)

C(22)-S(22)-Pd(2)           101.4(5)

C(23)-S(23)-C(21)            96.7(7)

C(23)-S(24)-C(22)            97.5(7)

C(24)-S(26)-Pd(2)           101.8(5)

C(25)-S(27)-Pd(2)           100.9(5)

C(26)-S(28)-C(24)            97.5(7)

C(26)-S(29)-C(25)            98.0(7)

C(22)-C(21)-S(21)           124.0(10)

C(22)-C(21)-S(23)           116.5(10)

S(21)-C(21)-S(23)           119.4(8)

C(21)-C(22)-S(22)           123.9(11)

C(21)-C(22)-S(24)           115.7(10)

S(22)-C(22)-S(24)           120.4(8)

S(25)-C(23)-S(24)           123.6(9)

S(25)-C(23)-S(23)           122.9(9)

S(24)-C(23)-S(23)           113.4(8)

C(25)-C(24)-S(26)           122.8(11)

C(25)-C(24)-S(28)           116.1(11)

S(26)-C(24)-S(28)           120.9(9)

C(24)-C(25)-S(27)           124.5(11)

C(24)-C(25)-S(29)           115.7(11)

S(27)-C(25)-S(29)           119.8(8)

S(30)-C(26)-S(29)           124.3(11)

S(30)-C(26)-S(28)           123.0(11)

S(29)-C(26)-S(28)           112.6(9)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x,-y+1,-z+2    #2 -x,-y,-z+2

Table S4.  Anisotropic displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

The anisotropic displacement factor exponent takes the form:

-2 pi^2 [ h^2 a*^2 U11 + ... + 2 h k a* b* U12 ]

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

S(1)    100(5)     132(6)      79(4)       2(4)      27(4)      -1(4)

C(1A)    40(20)    180(30)     18(11)     60(11)     12(12)     -9(16)

C(1B)    28(18)    161(15)     12(15)    -33(16)      4(15)    -53(16)

C(2)    120(20)    170(20)     97(19)     17(15)     34(17)    -27(18)

C(3A)   100(30)    150(50)    120(40)     50(40)     30(30)    -10(30)

C(3B)   150(50)    230(60)    110(40)     30(40)     60(30)    -10(40)

C(4)     98(12)    150(20)     86(17)      0(15)     30(14)     -2(15)

C(5A)   110(40)    160(40)    100(40)     20(30)     50(30)     40(30)

C(5B)    70(30)    150(40)     70(30)     30(30)      0(30)     10(30)

Pd(1)    32(1)      32(1)      29(1)       2(1)      11(1)      -3(1)

S(11)    40(2)      38(2)      32(2)       0(2)      12(2)      -8(2)

S(12)    45(2)      35(2)      31(2)       1(2)      12(2)      -9(2)

S(13)    50(3)      36(2)      46(2)      -1(2)      14(2)      -6(2)

S(14)    58(3)      37(2)      43(2)       7(2)      23(2)      -5(2)

S(15)    86(4)      40(2)      78(3)       9(2)      26(3)     -18(2)

S(16)    39(2)      41(2)      33(2)       3(2)       9(2)      -8(2)

S(17)    47(3)      35(2)      32(2)       1(2)      15(2)     -10(2)

S(18)    41(2)      40(2)      40(2)      -2(2)       9(2)      -8(2)

S(19)    47(3)      42(2)      39(2)       4(2)      18(2)      -8(2)

S(20)    62(3)      40(2)      79(3)       4(2)      28(3)     -14(2)

C(11)    11(7)      40(8)      48(10)    -11(7)      12(7)      -8(6)

C(12)    35(9)      34(8)      36(9)      15(6)      21(7)      10(7)

C(13)    68(12)     36(9)      53(10)      2(7)      32(10)      7(8)

C(14)    16(8)      43(9)      49(10)      8(7)      15(7)       2(6)

C(15)    37(9)      37(8)      40(9)       6(7)      24(8)       2(7)

C(16)    27(9)      37(8)      48(9)       8(7)      10(8)      -9(7)

Pd(2)    29(1)      33(1)      31(1)       1(1)      11(1)       5(1)

S(21)    40(2)      38(2)      32(2)       3(2)      13(2)      11(2)

S(22)    39(2)      42(2)      31(2)      -2(2)      10(2)       6(2)

S(23)    46(3)      42(2)      42(2)      -1(2)      21(2)      11(2)

S(24)    38(2)      42(2)      38(2)       3(2)       9(2)       8(2)

S(25)    63(3)      42(2)      74(3)      -3(2)      29(3)      16(2)

S(26)    34(2)      40(2)      34(2)       1(2)      10(2)       6(2)

S(27)    41(2)      39(2)      34(2)       1(2)      14(2)       6(2)

S(28)    55(3)      37(2)      56(3)      -9(2)      28(2)       2(2)

S(29)    48(3)      37(2)      55(3)       4(2)      13(2)       8(2)

S(30)    87(4)      41(3)     101(4)      -9(3)      37(3)      14(3)

C(21)    34(9)      32(8)      34(9)      -4(6)      14(7)      13(7)

C(22)     8(7)      51(9)      32(8)       4(6)       5(6)       0(6)

C(23)    45(10)     36(9)      42(9)       1(7)      14(8)       3(7)

C(24)    16(7)      38(8)      43(9)       0(6)      15(7)       7(6)

C(25)    16(8)      44(9)      38(9)      10(7)       4(7)      12(7)

C(26)    31(9)      43(9)      73(12)      0(8)      21(9)      -2(7)

_______________________________________________________________________

Table S5.  Hydrogen coordinates ( x 10^4) and isotropic

displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at room temperature.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H(1A1)       3891          2411          4002         118

H(1A2)       2082          2404          4532         118

H(1A3)       3459          2066          5168         118

H(1B1)       3151          2023          5449         103

H(1B2)       4911          1900          7535         103

H(1B3)       5126          2080          5411         103

H(2A)        3778          2818          4224         156

H(2B)        4854          3090          6256         156

H(3A1)       7624          2854          6519         190

H(3A2)       6513          2877          3865         190

H(3A3)       6737          2497          5087         190

H(3B1)       6244          2370          5351         236

H(3B2)       7300          2733          5330         236

H(3B3)       5604          2611          3145         236

H(4A)        1851          2881          7321         135

H(4B)        1265          2511          5835         135

H(5A1)       1138          2230          8789         182

H(5A2)       1637          2601         10230         182

H(5A3)       3213          2328         10198         182

H(5B1)       2352          2186          9357         160

H(5B2)        635          2152          7041         160

H(5B3)        575          2427          8988         160

________________________________________________________________

Table S6.  Crystal data and structure refinement for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K

Identification code               (SMeEt2)[Pd(dmit)2]2  (1)

Empirical formula                 C17 H13 Pd2 S21

Formula weight                    1103.58

Temperature                       160(2) K

Wavelength                        0.71073 A

Crystal system, space group       Triclinic,  P-1

Unit cell dimensions              a = 7.7888(9) A   alpha = 92.112(11) deg.

b = 36.181(3) A    beta = 112.169(12) deg.

c = 6.2573(6) A   gamma = 88.740(12) deg.

Volume                            1631.8(3) A^3

Z, Calculated density             2,  2.246 Mg/m^3

Absorption coefficient            2.463 mm^-1

F(000)                            1086

Crystal size                      0.5 x 0.35 x 0.05 mm

Theta range for data collection   2.82 to 21.03 deg.

Limiting indices                  -7<=h<=7, -33<=k<=35, 0<=l<=6

Reflections collected / unique    9065 / 3336 [R(int) = 0.0585]

Completeness to theta = 21.03     95.2 %

Absorption correction             Empirical (DIFABS)

Max. and min. transmission        0.5464 and 0.2078

Refinement method                 Full-matrix least-squares on F^2

Data / restraints / parameters    3336 / 22 / 364

Goodness-of-fit on F^2            1.175

Final R indices [I>2sigma(I)]     R1 = 0.0861, wR2 = 0.2233

R indices (all data)              R1 = 0.0962, wR2 = 0.2292

Largest diff. peak and hole       1.757 and -0.984 e.A^-3

Table S7.  Atomic coordinates ( x 10^4) and equivalent isotropic

displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K

U(eq) is defined as one third of the trace of the orthogonalized

Uij tensor.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

S(1)         4437(12)      2531(3)       7689(15)      91(2)

C(1)         4330(60)      2097(11)      6330(70)     132(14)

C(2)         4720(50)      2843(12)      5580(60)     114(10)

C(3)         6390(50)      2717(12)      5050(60)     123(13)

C(4)         2080(40)      2623(10)      7280(60)      96(8)

C(5)         1500(50)      2360(11)      8730(60)     110(11)

Pd(1)        1882(2)       4816(1)      10166(3)       47(1)

S(11)         361(8)       4343(2)       7638(10)      49(2)

S(12)        1991(8)       4474(2)      13227(10)      49(2)

S(13)        -697(9)       3588(2)       8493(11)      56(2)

S(14)         774(9)       3697(2)      13461(11)      58(2)

S(15)        -942(10)      2980(2)      11453(12)      70(2)

S(16)        3583(9)       5266(2)      12734(10)      51(2)

S(17)        1977(8)       5146(2)       7164(10)      49(2)

S(18)        5077(9)       5982(2)      12049(10)      54(2)

S(19)        3661(9)       5883(2)       7070(11)      54(2)

S(20)        5637(10)      6575(2)       9209(12)      65(2)

C(11)         300(30)      4007(6)       9550(40)      38(5)

C(12)         960(30)      4074(6)      11830(40)      49(6)

C(13)        -300(30)      3398(6)      11180(40)      49(6)

C(14)        3860(30)      5581(6)      10810(50)      53(7)

C(15)        3150(30)      5535(6)       8580(40)      37(5)

C(16)        4790(30)      6174(7)       9410(40)      53(6)

Pd(2)        1850(2)        191(1)      10218(3)       48(1)

S(21)        1973(8)       -142(2)       7086(10)      50(2)

S(22)        3596(9)       -257(2)      12625(10)      51(2)

S(23)        3748(9)       -875(2)       6712(10)      53(2)

S(24)        5180(9)       -976(2)      11650(10)      54(2)

S(25)        5795(10)     -1564(2)       8587(12)      66(2)

S(26)        1911(8)        537(2)      13405(10)      51(2)

S(27)         286(8)        661(2)       7857(10)      50(2)

S(28)         567(9)       1311(2)      13876(11)      57(2)

S(29)        -903(9)       1415(2)       8924(11)      59(2)

S(30)       -1233(11)      2026(2)      12088(14)      72(2)

C(21)        3210(30)      -528(6)       8390(40)      43(6)

C(22)        3910(30)      -578(7)      10590(50)      55(6)

C(23)        4920(30)     -1168(7)       8920(40)      58(7)

C(24)         830(30)       937(6)      12130(50)      55(7)

C(25)         160(30)       990(6)       9830(40)      43(6)

C(26)        -540(30)      1613(7)      11710(40)      56(6)

________________________________________________________________

Table S8.  Bond lengths [A] and angles [deg] for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K

_____________________________________________________________

S(1)-C(1)                     1.74(3)

S(1)-C(4)                     1.78(3)

S(1)-C(2)                     1.85(4)

C(2)-C(3)                     1.52(5)

C(4)-C(5)                     1.53(4)

Pd(1)-S(17)                   2.289(6)

Pd(1)-S(12)                   2.291(6)

Pd(1)-S(16)                   2.299(6)

Pd(1)-S(11)                   2.303(6)

Pd(1)-Pd(1)#1                 3.132(4)

S(11)-C(11)                   1.75(2)

S(12)-C(12)                   1.71(2)

S(13)-C(11)                   1.71(2)

S(13)-C(13)                   1.75(2)

S(14)-C(13)                   1.71(2)

S(14)-C(12)                   1.77(2)

S(15)-C(13)                   1.64(2)

S(16)-C(14)                   1.76(2)

S(17)-C(15)                   1.72(2)

S(18)-C(14)                   1.74(2)

S(18)-C(16)                   1.75(2)

S(19)-C(16)                   1.72(2)

S(19)-C(15)                   1.74(2)

S(20)-C(16)                   1.63(3)

C(11)-C(12)                   1.34(3)

C(14)-C(15)                   1.30(3)

Pd(2)-S(21)                   2.295(6)

Pd(2)-S(22)                   2.299(6)

Pd(2)-S(26)                   2.300(6)

Pd(2)-S(27)                   2.301(6)

Pd(2)-Pd(2)#2                 3.138(4)

S(21)-C(21)                   1.72(2)

S(22)-C(22)                   1.77(3)

S(23)-C(23)                   1.73(3)

S(23)-C(21)                   1.75(2)

S(24)-C(22)                   1.73(3)

S(24)-C(23)                   1.76(2)

S(25)-C(23)                   1.61(3)

S(26)-C(24)                   1.72(3)

S(27)-C(25)                   1.71(2)

S(28)-C(26)                   1.72(3)

S(28)-C(24)                   1.76(2)

S(29)-C(25)                   1.74(2)

S(29)-C(26)                   1.78(2)

S(30)-C(26)                   1.62(3)

C(21)-C(22)                   1.30(3)

C(24)-C(25)                   1.35(3)

C(1)-S(1)-C(4)              102.9(17)

C(1)-S(1)-C(2)              102(2)

C(4)-S(1)-C(2)              100.4(17)

C(3)-C(2)-S(1)              109(3)

C(5)-C(4)-S(1)              109(2)

S(17)-Pd(1)-S(12)           176.1(2)

S(17)-Pd(1)-S(16)            90.0(2)

S(12)-Pd(1)-S(16)            89.0(2)

S(17)-Pd(1)-S(11)            90.4(2)

S(12)-Pd(1)-S(11)            90.4(2)

S(16)-Pd(1)-S(11)           176.1(2)

S(17)-Pd(1)-Pd(1)#1          92.19(18)

S(12)-Pd(1)-Pd(1)#1          91.57(17)

S(16)-Pd(1)-Pd(1)#1          92.35(18)

S(11)-Pd(1)-Pd(1)#1          91.47(17)

C(11)-S(11)-Pd(1)           101.3(7)

C(12)-S(12)-Pd(1)           100.9(9)

C(11)-S(13)-C(13)            96.5(11)

C(13)-S(14)-C(12)            97.2(12)

C(14)-S(16)-Pd(1)           100.4(9)

C(15)-S(17)-Pd(1)           101.7(7)

C(14)-S(18)-C(16)            94.6(12)

C(16)-S(19)-C(15)            97.5(11)

C(12)-C(11)-S(13)           118.6(17)

C(12)-C(11)-S(11)           121.5(17)

S(13)-C(11)-S(11)           119.9(12)

C(11)-C(12)-S(12)           125.9(18)

C(11)-C(12)-S(14)           114.4(17)

S(12)-C(12)-S(14)           119.7(15)

S(15)-C(13)-S(14)           123.8(14)

S(15)-C(13)-S(13)           122.9(13)

S(14)-C(13)-S(13)           113.3(13)

C(15)-C(14)-S(18)           120.1(18)

C(15)-C(14)-S(16)           123.6(18)

S(18)-C(14)-S(16)           116.2(16)

C(14)-C(15)-S(17)           124.2(17)

C(14)-C(15)-S(19)           114.5(17)

S(17)-C(15)-S(19)           121.0(12)

S(20)-C(16)-S(19)           123.9(15)

S(20)-C(16)-S(18)           123.0(14)

S(19)-C(16)-S(18)           113.0(14)

S(21)-Pd(2)-S(22)            90.1(2)

S(21)-Pd(2)-S(26)           176.4(2)

S(22)-Pd(2)-S(26)            89.2(2)

S(21)-Pd(2)-S(27)            90.3(2)

S(22)-Pd(2)-S(27)           176.1(2)

S(26)-Pd(2)-S(27)            90.2(2)

S(21)-Pd(2)-Pd(2)#2          91.87(18)

S(22)-Pd(2)-Pd(2)#2          91.50(18)

S(26)-Pd(2)-Pd(2)#2          91.63(17)

S(27)-Pd(2)-Pd(2)#2          92.38(17)

C(21)-S(21)-Pd(2)           101.2(7)

C(22)-S(22)-Pd(2)           100.7(9)

C(23)-S(23)-C(21)            97.6(12)

C(22)-S(24)-C(23)            95.2(13)

C(24)-S(26)-Pd(2)           100.8(9)

C(25)-S(27)-Pd(2)           101.5(8)

C(26)-S(28)-C(24)            98.0(13)

C(25)-S(29)-C(26)            97.2(12)

C(22)-C(21)-S(21)           125.3(17)

C(22)-C(21)-S(23)           114.7(19)

S(21)-C(21)-S(23)           119.8(13)

C(21)-C(22)-S(24)           119.9(19)

C(21)-C(22)-S(22)           123(2)

S(24)-C(22)-S(22)           117.4(15)

S(25)-C(23)-S(23)           124.9(15)

S(25)-C(23)-S(24)           122.8(16)

S(23)-C(23)-S(24)           112.3(14)

C(25)-C(24)-S(26)           124.3(18)

C(25)-C(24)-S(28)           116.1(19)

S(26)-C(24)-S(28)           119.6(17)

C(24)-C(25)-S(27)           123.2(18)

C(24)-C(25)-S(29)           116.6(18)

S(27)-C(25)-S(29)           120.3(13)

S(30)-C(26)-S(28)           125.2(15)

S(30)-C(26)-S(29)           122.6(15)

S(28)-C(26)-S(29)           112.1(14)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x,-y+1,-z+2    #2 -x,-y,-z+2

Table S9.  Anisotropic displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K

The anisotropic displacement factor exponent takes the form:

-2 pi^2 [ h^2 a*^2 U11 + ... + 2 h k a* b* U12 ]

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

S(1)     84(5)      97(7)      85(5)       0(4)      23(4)      -3(5)

C(1)    140(30)    143(18)    160(40)    -70(20)    120(30)    -40(20)

C(2)     90(20)    170(30)     80(20)     26(18)     27(17)      0(20)

C(3)    120(30)    170(40)     80(20)     50(20)     43(19)     30(20)

C(4)     86(13)    100(20)    100(20)    -11(17)     38(17)    -10(16)

C(5)     86(19)    130(30)    110(30)     30(20)     33(19)     10(20)

Pd(1)    46(1)      51(1)      45(1)       2(1)      16(1)      -3(1)

S(11)    50(4)      50(4)      46(3)      -1(3)      17(3)      -5(3)

S(12)    46(4)      52(4)      47(3)      -2(3)      15(3)      -5(3)

S(13)    54(4)      52(4)      56(4)       3(3)      15(3)      -5(3)

S(14)    65(4)      53(4)      55(4)       8(3)      23(3)      -1(3)

S(15)    77(5)      56(5)      73(5)       7(3)      25(4)     -10(4)

S(16)    56(4)      53(4)      41(3)       4(3)      13(3)      -3(3)

S(17)    50(4)      49(4)      46(3)       0(3)      16(3)      -5(3)

S(18)    50(4)      53(4)      55(4)      -1(3)      14(3)      -7(3)

S(19)    54(4)      48(4)      61(4)       6(3)      23(3)      -4(3)

S(20)    66(4)      54(5)      75(4)       4(3)      26(4)      -9(3)

C(11)    35(12)     39(14)     42(13)     -6(10)     18(10)      2(10)

C(12)    33(13)     40(15)     80(19)      8(12)     29(13)     16(10)

C(13)    49(14)     39(15)     47(13)      0(10)      5(11)      7(11)

C(14)    41(14)     25(14)    100(20)     20(12)     29(14)     14(10)

C(15)    45(13)     33(14)     40(13)      7(10)     25(11)      2(10)

C(16)    42(14)     63(17)     56(15)     -2(12)     20(12)     -7(12)

Pd(2)    46(1)      49(1)      48(1)       1(1)      18(1)       2(1)

S(21)    53(4)      46(4)      50(3)       4(3)      18(3)       6(3)

S(22)    54(4)      55(4)      40(3)       2(3)      14(3)       4(3)

S(23)    54(4)      50(4)      57(4)      -1(3)      25(3)      10(3)

S(24)    52(4)      58(4)      52(4)       6(3)      18(3)       9(3)

S(25)    66(4)      59(5)      75(4)       1(3)      30(4)       9(3)

S(26)    48(4)      53(4)      51(4)       4(3)      17(3)       4(3)

S(27)    49(4)      52(4)      50(3)       5(3)      20(3)       2(3)

S(28)    60(4)      53(4)      61(4)      -5(3)      25(3)      -1(3)

S(29)    53(4)      53(4)      66(4)       2(3)      19(3)       6(3)

S(30)    76(5)      51(5)      94(5)      -1(4)      37(4)       9(4)

C(21)    54(15)     33(14)     49(15)    -16(10)     30(12)      1(10)

C(22)    40(14)     61(18)     72(19)     -2(13)     31(13)      4(12)

C(23)    48(15)     66(18)     61(16)    -12(13)     23(13)     -8(13)

C(24)    33(13)     37(15)    110(20)    -11(13)     45(14)    -11(11)

C(25)    44(14)     38(15)     48(14)     19(11)     16(11)     -8(10)

C(26)    48(15)     58(17)     65(16)      2(12)     23(13)     -3(12)

_______________________________________________________________________

Table S10.  Hydrogen coordinates ( x 10^4) and isotropic

displacement parameters (A^2 x 10^3) for (SMeEt2)[Pd(dmit)2]2  (1) at 160 K

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H(1A)        3994          1911          7204         197

H(1B)        5542          2034          6275         197

H(1C)        3394          2102          4760         197

H(2A)        3594          2838          4141         137

H(2B)        4896          3100          6218         137

H(3A)        7371          2634          6473         184

H(3B)        6846          2924          4449         184

H(3C)        6039          2513          3903         184

H(4A)        1940          2883          7749         115

H(4B)        1282          2587          5625         115

H(5A)        2535          2191          9507         165

H(5B)         429          2217          7729         165

H(5C)        1180          2502          9888         165

________________________________________________________________

Table S11.  Crystal data and structure refinement for (SMeEt2)0.5[Pd(dmit)2]  (2) at 160 K

.

Identification code               (SMeEt2)0.5[Pd(dmit)2]  (2)

Empirical formula                 C17 H13 Pd2 S21

Formula weight                    1103.58

Temperature                       160(2) K

Wavelength                        0.71073 A

Crystal system, space group       Triclinic,  P-1

Unit cell dimensions              a = 7.7877(12) A   alpha = 96.80(2) deg.

b = 18.323(3) A    beta = 112.257(18) deg.

c = 6.2846(10) A   gamma = 84.17(2) deg.

Volume                            822.5(2) A^3

Z, Calculated density             1,  2.228 Mg/m^3

Absorption coefficient            2.443 mm^-1

F(000)                            543

Crystal size                      0.4 x 0.35 x 0.05 mm

Theta range for data collection   2.24 to 24.08 deg.

Limiting indices                  -8<=h<=8, -21<=k<=20, -7<=l<=7

Reflections collected / unique    6587 / 2415 [R(int) = 0.0420]

Completeness to theta = 24.08     93.0 %

Absorption correction             Empirical (DIFABS)

Max. and min. transmission        1.1389 and 0.5385

Refinement method                 Full-matrix least-squares on F^2

Data / restraints / parameters    2415 / 30 / 208

Goodness-of-fit on F^2            1.110

Final R indices [I>2sigma(I)]     R1 = 0.0346, wR2 = 0.0925

R indices (all data)              R1 = 0.0368, wR2 = 0.0939

Largest diff. peak and hole       0.901 and -1.198 e.A^-3

Table S12.  Atomic coordinates ( x 10^4) and equivalent isotropic

displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at 160 K .

U(eq) is defined as one third of the trace of the orthogonalized

Uij tensor.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

Pd(1)        1926(1)       4629(1)       5068(1)       20(1)

S(11)        1935(2)       5291(1)       2189(2)       25(1)

S(12)        3511(2)       5525(1)       7780(2)       26(1)

S(13)        3415(2)       6750(1)       2332(2)       29(1)

S(14)        4789(2)       6960(1)       7314(2)       30(1)

S(15)        5167(2)       8132(1)       4658(3)       45(1)

S(16)        2104(2)       3941(1)       7987(2)       24(1)

S(17)         540(2)       3690(1)       2366(2)       25(1)

S(18)        1073(2)       2398(1)       7874(2)       31(1)

S(19)        -302(2)       2181(1)       2906(2)       33(1)

S(20)        -342(3)        952(1)       5572(3)       56(1)

C(11)        3036(7)       6044(2)       3713(8)       22(1)

C(12)        3694(6)       6144(2)       6090(8)       22(1)

C(13)        4474(7)       7324(3)       4763(9)       30(1)

C(14)        1186(7)       3148(2)       6461(8)       24(1)

C(15)         538(7)       3044(2)       4101(8)       23(1)

C(16)         126(8)       1799(3)       5449(10)      36(1)

S(1)         5569(7)         -3(3)       1224(6)       81(1)

C(1)         5060(30)      -920(9)        -50(30)      76(4)

C(2)         6550(50)       320(9)       -690(40)     129(8)

C(3)         7170(50)      -210(13)     -2340(50)     179(15)

C(4)         3690(40)       521(16)       610(50)     150(9)

C(5)         2410(40)        50(30)      1110(50)     227(19)

________________________________________________________________

Table S13.  Bond lengths [A] and angles [deg] for (SMeEt2)0.5[Pd(dmit)2]  (2) at 160 K .

_____________________________________________________________

Pd(1)-S(11)                   2.2966(12)

Pd(1)-S(12)                   2.2966(14)

Pd(1)-S(16)                   2.3012(12)

Pd(1)-S(17)                   2.3043(13)

Pd(1)-Pd(1)#1                 3.1397(9)

S(11)-C(11)                   1.692(5)

S(12)-C(12)                   1.693(5)

S(13)-C(13)                   1.721(5)

S(13)-C(11)                   1.746(4)

S(14)-C(13)                   1.732(5)

S(14)-C(12)                   1.745(5)

S(15)-C(13)                   1.643(5)

S(16)-C(14)                   1.704(5)

S(17)-C(15)                   1.702(5)

S(18)-C(16)                   1.729(6)

S(18)-C(14)                   1.748(4)

S(19)-C(16)                   1.723(5)

S(19)-C(15)                   1.746(4)

S(20)-C(16)                   1.646(5)

C(11)-C(12)                   1.379(7)

C(14)-C(15)                   1.370(7)

S(1)-C(4)                     1.61(3)

S(1)-C(1)                     1.789(18)

S(1)-C(2)                     1.831(15)

C(2)-C(3)                     1.509(18)

C(4)-C(5)                     1.52(5)

S(11)-Pd(1)-S(12)            89.84(4)

S(11)-Pd(1)-S(16)           176.46(4)

S(12)-Pd(1)-S(16)            89.52(4)

S(11)-Pd(1)-S(17)            90.18(4)

S(12)-Pd(1)-S(17)           175.89(4)

S(16)-Pd(1)-S(17)            90.21(4)

S(11)-Pd(1)-Pd(1)#1          92.70(4)

S(12)-Pd(1)-Pd(1)#1          91.83(4)

S(16)-Pd(1)-Pd(1)#1          90.80(4)

S(17)-Pd(1)-Pd(1)#1          92.27(4)

C(11)-S(11)-Pd(1)           101.82(16)

C(12)-S(12)-Pd(1)           101.48(16)

C(13)-S(13)-C(11)            97.5(2)

C(13)-S(14)-C(12)            97.4(2)

C(14)-S(16)-Pd(1)           101.26(16)

C(15)-S(17)-Pd(1)           100.97(16)

C(16)-S(18)-C(14)            97.5(2)

C(16)-S(19)-C(15)            97.8(2)

C(12)-C(11)-S(11)           123.1(3)

C(12)-C(11)-S(13)           115.7(3)

S(11)-C(11)-S(13)           121.2(3)

C(11)-C(12)-S(12)           123.7(3)

C(11)-C(12)-S(14)           115.6(3)

S(12)-C(12)-S(14)           120.7(3)

S(15)-C(13)-S(13)           122.8(3)

S(15)-C(13)-S(14)           123.4(3)

S(13)-C(13)-S(14)           113.7(3)

C(15)-C(14)-S(16)           123.4(3)

C(15)-C(14)-S(18)           115.8(4)

S(16)-C(14)-S(18)           120.8(3)

C(14)-C(15)-S(17)           124.1(4)

C(14)-C(15)-S(19)           115.6(3)

S(17)-C(15)-S(19)           120.3(3)

S(20)-C(16)-S(19)           123.6(3)

S(20)-C(16)-S(18)           123.1(3)

S(19)-C(16)-S(18)           113.3(3)

C(4)-S(1)-C(1)              110.3(13)

C(4)-S(1)-C(2)               99.7(15)

C(1)-S(1)-C(2)              100.9(7)

C(3)-C(2)-S(1)              121.4(13)

C(5)-C(4)-S(1)              101(3)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x,-y+1,-z+1

Table S14.  Anisotropic displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at 160 K

The anisotropic displacement factor exponent takes the form:

-2 pi^2 [ h^2 a*^2 U11 + ... + 2 h k a* b* U12 ]

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

Pd(1)    22(1)      20(1)      18(1)       1(1)       5(1)      -3(1)

S(11)    33(1)      23(1)      18(1)       1(1)       7(1)      -7(1)

S(12)    30(1)      25(1)      19(1)       1(1)       4(1)      -7(1)

S(13)    33(1)      27(1)      29(1)       5(1)      11(1)      -7(1)

S(14)    31(1)      27(1)      29(1)      -1(1)       5(1)     -10(1)

S(15)    46(1)      29(1)      60(1)       7(1)      16(1)     -12(1)

S(16)    28(1)      23(1)      20(1)       2(1)       7(1)      -4(1)

S(17)    30(1)      23(1)      20(1)       0(1)       7(1)      -6(1)

S(18)    40(1)      24(1)      34(1)       7(1)      16(1)      -3(1)

S(19)    36(1)      23(1)      34(1)      -1(1)       7(1)      -7(1)

S(20)    71(1)      28(1)      64(1)       8(1)      17(1)     -16(1)

C(11)    19(3)      19(2)      27(2)       5(2)       8(2)      -2(2)

C(12)    15(3)      21(2)      27(2)      -2(2)       4(2)      -2(2)

C(13)    22(3)      29(3)      35(3)       3(2)       7(2)       1(2)

C(14)    22(3)      24(2)      29(2)       8(2)      10(2)       2(2)

C(15)    20(3)      18(2)      30(2)      -1(2)       8(2)      -2(2)

C(16)    33(3)      27(3)      43(3)       6(2)       9(3)      -3(2)

S(1)     80(3)     104(3)      34(2)       0(2)      -2(2)      10(2)

C(1)     88(13)     91(8)      68(9)      32(7)      42(9)     -14(8)

C(2)    250(30)     57(10)     94(15)     16(9)      66(17)    -34(12)

C(3)    340(40)    148(18)    130(20)    -83(16)    160(20)   -190(20)

C(4)    140(17)    140(16)    112(16)     -6(15)      1(14)     47(13)

C(5)     66(14)    490(60)     77(19)     20(30)    -32(16)    -60(20)

_______________________________________________________________________

Table S15.  Hydrogen coordinates ( x 10^4) and isotropic

displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at 160 K .

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H(1A)        6223         -1225           242          91

H(1B)        4388          -911         -1721          91

H(1C)        4290         -1128           621          91

H(2A)        5622           680         -1635         154

H(2B)        7645           598           297         154

H(3A)        7760            59         -3105         215

H(3B)        6084          -444         -3494         215

H(3C)        8056          -588         -1474         215

H(4A)        3881           989          1604         180

H(4B)        3190           628         -1031         180

H(5A)        1156           284           635         272

H(5B)        2883           -15          2763         272

H(5C)        2376          -438           244         272

________________________________________________________________

Table S16.  Crystal data and structure refinement for (SMeEt2)0.5[Pd(dmit)2]  (2) at room temperature

Identification code               (SMeEt2)0.5[Pd(dmit)2]  (2)

Empirical formula                 C17 H13 Pd2 S21

Formula weight                    1103.58

Temperature                       293(2) K

Wavelength                        0.71069 A

Crystal system, space group       Triclinic,  P -1

Unit cell dimensions              a = 7.844(5) A   alpha = 97.654(5) deg.

b = 18.397(5) A    beta = 112.076(5) deg.

c = 6.320(5) A   gamma = 83.572(5) deg.

Volume                            835.7(9) A^3

Z, Calculated density             1,  2.193 Mg/m^3

Absorption coefficient            2.405 mm^-1

F(000)                            543

Crystal size                      0.30 x 0.25 x 0.05 mm

Theta range for data collection   1.12 to 29.96 deg.

Limiting indices                  -11<=h<=10, -25<=k<=25, 0<=l<=8

Reflections collected / unique    4847 / 4847 [R(int) = 0.0000]

Completeness to theta = 29.96     100.0 %

Absorption correction             Psi-scan

Max. and min. transmission        0.8863 and 0.5886

Refinement method                 Full-matrix least-squares on F^2

Data / restraints / parameters    4847 / 30 / 208

Goodness-of-fit on F^2            1.020

Final R indices [I>2sigma(I)]     R1 = 0.0312, wR2 = 0.0702

R indices (all data)              R1 = 0.0570, wR2 = 0.0790

Largest diff. peak and hole       0.556 and -0.884 e.A^-3

Table S17.  Atomic coordinates ( x 10^4) and equivalent isotropic

displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at .room temperature

U(eq) is defined as one third of the trace of the orthogonalized

Uij tensor.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

Pd(1)        1929(1)       4631(1)       5058(1)       29(1)

S(11)        1928(1)       5294(1)       2227(1)       36(1)

S(12)        3489(1)       5524(1)       7784(1)       37(1)

S(13)        3384(1)       6747(1)       2429(1)       41(1)

S(14)        4750(1)       6954(1)       7381(1)       43(1)

S(15)        5122(2)       8125(1)       4796(2)       63(1)

S(16)        2111(1)       3945(1)       7931(1)       35(1)

S(17)         564(1)       3694(1)       2342(1)       36(1)

S(18)        1120(1)       2405(1)       7764(2)       44(1)

S(19)        -246(1)       2186(1)       2822(2)       47(1)

S(20)        -275(2)        963(1)       5429(2)       78(1)

C(11)        3019(4)       6042(2)       3765(5)       31(1)

C(12)        3673(4)       6142(1)       6134(5)       30(1)

C(13)        4440(4)       7317(2)       4868(6)       40(1)

C(14)        1221(4)       3151(2)       6391(5)       32(1)

C(15)         564(4)       3051(2)       4036(5)       33(1)

C(16)         186(5)       1810(2)       5344(6)       47(1)

S(1)         5557(5)         55(2)       1207(5)      101(1)

C(1)         5150(20)      -941(8)        110(30)     122(5)

C(2)         5960(40)       449(12)      -630(40)     183(7)

C(3)         7590(30)       113(18)     -1090(40)     227(14)

C(4)         3270(20)       385(10)       580(30)     151(6)

C(5)         2960(40)        91(15)      2420(40)     220(12)

________________________________________________________________

Table S18.  Bond lengths [A] and angles [deg] for (SMeEt2)0.5[Pd(dmit)2]  (2) at .room temperature

.

_____________________________________________________________

Pd(1)-S(11)                   2.2954(14)

Pd(1)-S(12)                   2.2965(11)

Pd(1)-S(16)                   2.2990(14)

Pd(1)-S(17)                   2.3044(11)

Pd(1)-Pd(1)#1                 3.1534(18)

S(11)-C(11)                   1.689(3)

S(12)-C(12)                   1.694(3)

S(13)-C(13)                   1.722(3)

S(13)-C(11)                   1.741(3)

S(14)-C(13)                   1.726(4)

S(14)-C(12)                   1.742(3)

S(15)-C(13)                   1.647(3)

S(16)-C(14)                   1.706(3)

S(17)-C(15)                   1.698(3)

S(18)-C(16)                   1.722(4)

S(18)-C(14)                   1.742(3)

S(19)-C(16)                   1.723(4)

S(19)-C(15)                   1.749(3)

S(20)-C(16)                   1.652(3)

C(11)-C(12)                   1.382(4)

C(14)-C(15)                   1.373(4)

S(1)-C(2)                     1.587(19)

S(1)-C(4)                     1.745(17)

S(1)-C(1)                     1.888(15)

C(2)-C(3)                     1.472(18)

C(4)-C(5)                     1.452(17)

S(11)-Pd(1)-S(12)            89.78(5)

S(11)-Pd(1)-S(16)           176.57(3)

S(12)-Pd(1)-S(16)            89.47(5)

S(11)-Pd(1)-S(17)            90.32(5)

S(12)-Pd(1)-S(17)           175.93(3)

S(16)-Pd(1)-S(17)            90.19(5)

S(11)-Pd(1)-Pd(1)#1          92.58(3)

S(12)-Pd(1)-Pd(1)#1          92.16(4)

S(16)-Pd(1)-Pd(1)#1          90.80(3)

S(17)-Pd(1)-Pd(1)#1          91.90(4)

C(11)-S(11)-Pd(1)           101.92(11)

C(12)-S(12)-Pd(1)           101.63(11)

C(13)-S(13)-C(11)            97.62(15)

C(13)-S(14)-C(12)            97.32(15)

C(14)-S(16)-Pd(1)           101.34(11)

C(15)-S(17)-Pd(1)           101.05(11)

C(16)-S(18)-C(14)            97.57(16)

C(16)-S(19)-C(15)            97.57(16)

C(12)-C(11)-S(11)           123.2(2)

C(12)-C(11)-S(13)           115.4(2)

S(11)-C(11)-S(13)           121.37(17)

C(11)-C(12)-S(12)           123.5(2)

C(11)-C(12)-S(14)           115.8(2)

S(12)-C(12)-S(14)           120.74(17)

S(15)-C(13)-S(13)           122.8(2)

S(15)-C(13)-S(14)           123.4(2)

S(13)-C(13)-S(14)           113.75(18)

C(15)-C(14)-S(16)           123.2(2)

C(15)-C(14)-S(18)           115.9(2)

S(16)-C(14)-S(18)           120.89(18)

C(14)-C(15)-S(17)           124.2(2)

C(14)-C(15)-S(19)           115.3(2)

S(17)-C(15)-S(19)           120.47(18)

S(20)-C(16)-S(18)           123.2(2)

S(20)-C(16)-S(19)           123.2(2)

S(18)-C(16)-S(19)           113.60(18)

C(2)-S(1)-C(4)               98.2(11)

C(2)-S(1)-C(1)              109.3(9)

C(4)-S(1)-C(1)               98.2(8)

C(3)-C(2)-S(1)              112.6(17)

C(5)-C(4)-S(1)               98.2(15)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x,-y+1,-z+1

Table S19.  Anisotropic displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at .room temperature

.

The anisotropic displacement factor exponent takes the form:

-2 pi^2 [ h^2 a*^2 U11 + ... + 2 h k a* b* U12 ]

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

Pd(1)    28(1)      30(1)      29(1)       3(1)      11(1)      -1(1)

S(11)    43(1)      35(1)      30(1)       1(1)      13(1)      -7(1)

S(12)    41(1)      39(1)      30(1)       3(1)       9(1)      -7(1)

S(13)    44(1)      40(1)      44(1)       8(1)      19(1)      -6(1)

S(14)    41(1)      40(1)      44(1)      -2(1)      11(1)     -11(1)

S(15)    65(1)      42(1)      88(1)       7(1)      30(1)     -16(1)

S(16)    39(1)      34(1)      31(1)       5(1)      12(1)      -3(1)

S(17)    41(1)      35(1)      31(1)       2(1)      13(1)      -5(1)

S(18)    54(1)      36(1)      50(1)      10(1)      24(1)      -1(1)

S(19)    49(1)      35(1)      50(1)       0(1)      12(1)      -8(1)

S(20)    99(1)      41(1)      91(1)      13(1)      24(1)     -21(1)

C(11)    26(1)      31(1)      36(1)       4(1)      12(1)      -1(1)

C(12)    25(1)      29(1)      36(1)       1(1)      12(1)       1(1)

C(13)    29(1)      38(2)      55(2)       5(1)      17(1)      -3(1)

C(14)    30(1)      31(1)      40(2)       9(1)      17(1)       3(1)

C(15)    29(1)      27(1)      42(2)       1(1)      14(1)       1(1)

C(16)    42(2)      36(2)      63(2)       8(1)      18(2)      -2(1)

S(1)     96(2)     128(3)      55(1)       3(2)       4(1)       4(2)

C(1)    152(14)     99(7)     128(12)     34(8)      70(11)     35(8)

C(2)    247(19)    167(16)    144(14)     41(13)     61(15)    -61(16)

C(3)    147(16)    440(40)     97(14)     50(20)     16(10)   -118(19)

C(4)    155(11)    153(15)    103(11)      5(10)     22(10)     65(12)

C(5)    260(30)    280(30)    175(19)    -95(18)    140(20)   -140(20)

_______________________________________________________________________

Table S20.  Hydrogen coordinates ( x 10^4) and isotropic

displacement parameters (A^2 x 10^3) for (SMeEt2)0.5[Pd(dmit)2]  (2) at .room temperature

.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H(1A)        4086          -969         -1289         183

H(1B)        4938         -1184          1237         183

H(1C)        6207         -1176          -172         183

H(2A)        4893           426         -2050         220

H(2B)        6137           963           -76         220

H(3A)        8328          -181           127         340

H(3B)        8307           492         -1165         340

H(3C)        7210          -192         -2518         340

H(4A)        3127           918           703         182

H(4B)        2463           187          -918         182

H(5A)        2577          -401          1931         330

H(5B)        2020           393          2810         330

H(5C)        4085            85          3745         330

________________________________________________________________

Table S21 : Short S…S distances (< 3.70 Å) between the Pd(dmit)2 units in (SMeEt2)0.5[Pd(dmit)2] (2) at room temperature

Atoms		Symmetry operation	Distance (Å)

S11	S11	-x,-y+1,-z	3.4299(18)

S11	S12	x,+y,+z-1	3.5461(25)

S11	S16	x,+y,+z-1	3.4592(19)

S11	S16	-x,-y+1,-z+1	3.2885(22)

S11	S17	-x,-y+1,-z	3.4645(19)

S12	S12	-x+1,-y+1,-z+2	3.5502(18)

S12	S13	x,+y,+z+1	3.4738(21)

S12	S16	-x+1,-y+1,-z+2	3.6368(20)

S12	S17	-x,-y+1,-z+1	3.3162(22)

Atoms		Symmetry operation	Distance (Å)

S13	S16	-x+1,-y+1,-z+1	3.6989(25)

S13	S17	-x,-y+1,-z	3.4975(19)

S13	S18	-x,-y+1,-z+1	3.6636(24)

S14	S16	-x+1,-y+1,-z+2	3.5340(19)

S14	S17	-x+1,-y+1,-z+1	3.6817(25)

S14	S19	-x,-y+1,-z+1	3.6694(24)

S16	S17	x,+y,+z+1	3.5313(25)

S17	S18	x,+y,+z-1	3.6157(21)

S20	S20	-x,-y,-z+1	3.5134(18)