a

b

Figure S2 (a) XRD pattern of silver nanocomposite. In the 2 range of 2~15, the interlayer spacing distance of lamellar structures is ca. 4.5 nm. The reflection peaks are indexed as 100, 110, 111 and 200 planes for Ag phase in the 2 range of 15-60, (b) EDX pattern for single silver phase.