# Electronic supplementary information

M. Wiebcke: “Hydrothermal synthesis and structural characterization of a new layered zincophosphate co-templated by diprotonated 1,6-diaminohexane and orthoboric acid molecules”

Paper Ref.: B105057B

Powder X-ray diffraction data for [Zn3(PO4)2(HPO4)].H3N(CH2)6NH3.H3BO3 (I)

|  |  |  | P21/c a= 12.959(8) Å, b = 8.286(4) Å, c = 18.839(13) Å,  = 91.30(5) ° |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| h |  |  |  | k | l | 2obs [°] | 2calc [°] | (2)a [°] | dcalc [Å] | Irelb |  |  |  |  |
| 1 |  |  |  | 0 | 0 | 6.744 | 6.815 | -0.071 | 12.955 | 100.0 |  |  |  |  |
| 0 |  |  |  | 0 | 2 | 9.348 | 9.380 | -0.032 | 9.417 | 48.4 |  |  |  |  |
| -1 |  |  |  | 0 | 2 | 11.442 | 11.477 | -0.035 | 7.701 | 35.1 |  |  |  |  |
| 0 |  |  |  | 1 | 1 | 11.607 | 11.654 | -0.047 | 7.584 | 42.3 |  |  |  |  |
| -1 |  |  |  | 1 | 0 | 12.616 | 12.666 | -0.050 | 6.980 | 1.7 |  |  |  |  |
| -1 |  |  |  | 1 | 1 | 13.406 | 13.458 | -0.052 | 6.571 | 25.0 |  |  |  |  |
| 1 |  |  |  | 1 | 2 | 15.843 | 15.877 | -0.034 | 5.575 | 2.4 |  |  |  |  |
| 2 |  |  |  | 0 | 2 | 16.745 | 16.767 | -0.022 | 5.281 | 1.3 |  |  |  |  |
| -2 |  |  |  | 1 | 0 | 17.309 | 17.356 | -0.047 | 5.103 | 3.1 |  |  |  |  |
| 0 |  |  |  | 1 | 3 | 17.687 | 17.703 | -0.016 | 5.004 | 1.5 |  |  |  |  |
| 0 |  |  |  | 0 | 4 | 18.839 | 18.824 | 0.015 | 4.709 | 3.1 |  |  |  |  |
| 1 |  |  |  | 1 | 3 | 19.097 | 19.106 | -0.009 | 4.640 | 1.5 |  |  |  |  |
| -2 |  |  |  | 1 | 2 | 19.565 | 19.613 | -0.048 | 4.521 | 1.7 |  |  |  |  |
| -1 |  |  |  | 0 | 4 | 19.891 | 19.892 | -0.001 | 4.458 | 2.9 |  |  |  |  |
| 3 |  |  |  | 0 | 0 | 20.517 | 20.542 | -0.025 | 4.318 | 13.6 |  |  |  |  |
| 0 |  |  |  | 2 | 0 | 21.373 | 21.422 | -0.049 | 4.143 | 14.9 |  |  |  |  |
| -2 |  |  |  | 1 | 3 | 22.199 | 22.224 | -0.025 | 3.995 | 37.6 |  |  |  |  |
| 2 |  |  |  | 1 | 3 | 22.624 | 22.622 | 0.002 | 3.926 | 12.2 |  |  |  |  |
| 1 |  |  |  | 1 | 4 | 22.924 | 22.884 | 0.040 | 3.881 | 38.9 |  |  |  |  |
| -1 |  |  |  | 2 | 1 | 22.983 | 22.967 | 0.016 | 3.867 | 45.6 |  |  |  |  |
| -3 |  |  |  | 1 | 0 | 23.171 | 23.199 | -0.028 | 3.829 | 20.2 |  |  |  |  |
| 0 |  |  |  | 2 | 2 | 23.445 | 23.431 | 0.014 | 3.792 | 22.3 |  |  |  |  |
| -3 |  |  |  | 1 | 1 | 23.588 | 23.585 | 0.003 | 3.768 | 64.8 |  |  |  |  |
| -1 |  |  |  | 2 | 2 | 24.345 | 24.367 | -0.022 | 3.648 | 12.1 |  |  |  |  |
| -3 |  |  |  | 1 | 2 | 24.862 | 24.893 | -0.037 | 3.573 | 2.8 |  |  |  |  |
| 3 |  |  |  | 1 | 2 | 25.263 | 25.251 | 0.012 | 3.523 | 1.7 |  |  |  |  |
| -2 |  |  |  | 2 | 0 | 25.506 | 25.491 | 0.015 | 3.490 | 2.5 |  |  |  |  |
| 0 |  |  |  | 2 | 3 | 25.734 | 25.733 | 0.001 | 3.458 | 20.5 |  |  |  |  |
| 2 |  |  |  | 2 | 1 | 25.975 | 25.990 | -0.015 | 3.424 | 31.0 |  |  |  |  |
| -1 |  |  |  | 2 | 3 | 26.560 | 26.565 | -0.005 | 3.351 | 42.7 |  |  |  |  |
| 1 |  |  |  | 2 | 3 | 26.747 | 26.734 | 0.013 | 3.330 | 30.0 |  |  |  |  |
| -3 |  |  |  | 1 | 3 | 27.038 | 26.995 | 0.043 | 3.299 | 25.1 |  |  |  |  |
| 4 |  |  |  | 0 | 0 | 27.512 | 27.506 | 0.006 | 3.239 | 19.3 |  |  |  |  |
| -3 |  |  |  | 0 | 4 | 27.686 | 27.677 | 0.009 | 3.219 | 3.0 |  |  |  |  |
| 3 |  |  |  | 0 | 4 | 28.467 | 28.324 | 0.143 | 3.147 | 2.4 |  |  |  |  |
| -2 |  |  |  | 2 | 3 | 29.101 | 29.086 | 0.015 | 3.066 | 32.2 |  |  |  |  |
| 2 |  |  |  | 2 | 3 | 29.428 | 29.396 | 0.032 | 3.035 | 11.2 |  |  |  |  |
| -4 |  |  |  | 1 | 0 | 29.586 | 29.577 | 0.005 | 3.016 | 3.5 |  |  |  |  |
| -4 |  |  |  | 1 | 1 | 29.880 | 29.862 | 0.016 | 2.988 | 4.8 |  |  |  |  |
| -3 |  |  |  | 2 | 1 | 30.145 | 30.157 | -0.012 | 2.960 | 20.7 |  |  |  |  |
| 3 |  |  |  | 2 | 1 | 30.314 | 30.308 | 0.006 | 2.945 | 6.7 |  |  |  |  |
| 3 |  |  |  | 2 | 2 | 31.399 | 31.501 | -0.102 | 2.837 | 5.3 |  |  |  |  |
| 2 |  |  |  | 2 | 4 | 32.105 | 32.070 | 0.035 | 2.788 | 7.1 |  |  |  |  |
| 0 |  |  |  | 3 | 1 | 32.749 | 32.732 | 0.017 | 2.733 | 18.4 |  |  |  |  |
| -3 |  |  |  | 2 | 3 | 32.997 | 32.941 | 0.056 | 2.716 | 7.9 |  |  |  |  |
| -1 |  |  |  | 3 | 1 | 33.408 | 33.450 | -0.042 | 2.676 | 16.6 |  |  |  |  |
| 0 |  |  |  | 3 | 2 | 33.741 | 33.780 | -0.039 | 2.650 | 2.3 |  |  |  |  |
| 5 |  |  |  | 0 | 0 | 34.603 | 34.576 | 0.027 | 2.591 | 3.3 |  |  |  |  |
| -4 |  |  |  | 1 | 4 | 34.811 | 34.941 | -0.130 | 2.565 | 6.6 |  |  |  |  |
| -4 |  |  |  | 2 | 0 | 35.110 | 35.127 | -0.017 | 2.552 | 6.5 |  |  |  |  |
| -2 |  |  |  | 3 | 0 | 35.293 | 35.284 | 0.009 | 2.541 | 12.8 |  |  |  |  |
| -2 |  |  |  | 3 | 1 | 35.572 | 35.571 | 0.001 | 2.521 | 10.0 |  |  |  |  |
| -5 |  |  |  | 0 | 2 | 35.712 | 35.687 | 0.025 | 2.513 | 6.5 |  |  |  |  |
| 1 |  |  |  | 3 | 3 | 36.214 | 36.221 | -0.007 | 2.477 | 0.9 |  |  |  |  |
| 5 |  |  |  | 1 | 1 | 36.733 | 36.711 | 0.022 | 2.445 | 5.1 |  |  |  |  |
| -4 |  |  |  | 2 | 3 | 37.791 | 37.773 | 0.018 | 2.379 | 4.1 |  |  |  |  |
| -2 |  |  |  | 3 | 3 | 38.135 | 38.044 | 0.091 | 2.362 | 3.7 |  |  |  |  |
| 2 |  |  |  | 3 | 3 | 38.301 | 38.290 | 0.011 | 2.348 | 3.0 |  |  |  |  |
| -5 |  |  |  | 1 | 3 | 38.766 | 38.800 | -0.034 | 2.318 | 12.6 |  |  |  |  |
| -2 |  |  |  | 3 | 4 | 40.125 | 40.131 | -0.006 | 2.244 | 1.1 |  |  |  |  |
| 4 |  |  |  | 2 | 4 | 40.469 | 40.460 | 0.009 | 2.227 | 5.1 |  |  |  |  |
| -5 |  |  |  | 1 | 4 | 40.784 | 40.796 | -0.012 | 2.209 | 1.7 |  |  |  |  |
| -3 |  |  |  | 3 | 3 | 41.165 | 41.160 | 0.005 | 2.190 | 3.0 |  |  |  |  |
| 5 |  |  |  | 2 | 1 | 41.422 | 41.423 | -0.001 | 2.177 | 7.1 |  |  |  |  |
| -5 |  |  |  | 2 | 2 | 42.007 | 42.001 | 0.006 | 2.148 | 3.6 |  |  |  |  |
| -6 |  |  |  | 0 | 2 | 42.717 | 42.698 | 0.019 | 2.115 | 1.0 |  |  |  |  |
| 4 |  |  |  | 3 | 1 | 43.333 | 43.340 | -0.007 | 2.085 | 7.5 |  |  |  |  |
| 0 |  |  |  | 4 | 0 | 43.661 | 43.643 | 0.018 | 2.071 | 2.2 |  |  |  |  |
| 4 |  |  |  | 3 | 2 | 44.288 | 44.244 | 0.044 | 2.045 | 1.8 |  |  |  |  |
| 0 |  |  |  | 4 | 2 | 44.750 | 44.742 | 0.008 | 2.023 | 8.2 |  |  |  |  |
| -1 |  |  |  | 4 | 2 | 45.302 | 45.279 | 0.023 | 2.000 | 5.4 |  |  |  |  |
| -6 |  |  |  | 1 | 3 | 45.420 | 45.390 | 0.030 | 1.996 | 4.8 |  |  |  |  |
| -6 |  |  |  | 0 | 4 | 45.814 | 45.774 | 0.040 | 1.980 | 1.0 |  |  |  |  |
| 0 |  |  |  | 4 | 3 | 46.126 | 46.087 | 0.039 | 1.967 | 3.2 |  |  |  |  |
| 2 |  |  |  | 4 | 1 | 46.254 | 46.243 | 0.011 | 1.961 | 3.0 |  |  |  |  |
| 1 |  |  |  | 4 | 3 | 46.705 | 46.698 | 0.007 | 1.943 | 2.9 |  |  |  |  |
| -6 |  |  |  | 1 | 4 | 47.169 | 47.140 | 0.025 | 1.926 | 2.9 |  |  |  |  |
| -5 |  |  |  | 3 | 1 | 48.326 | 48.264 | 0.062 | 1.883 | 3.0 |  |  |  |  |
| 5 |  |  |  | 3 | 1 | 48.417 | 48.434 | -0.017 | 1.877 | 6.0 |  |  |  |  |
| 1 |  |  |  | 4 | 4 | 48.586 | 48.531 | 0.055 | 1.874 | 1.7 |  |  |  |  |
| 7 |  |  |  | 0 | 0 | 49.174 | 49.170 | 0.004 | 1.851 | 2.3 |  |  |  |  |
| -6 |  |  |  | 2 | 3 | 49.504 | 49.423 | 0.081 | 1.842 | 1.0 |  |  |  |  |
| -3 |  |  |  | 4 | 2 | 49.575 | 49.607 | -0.032 | 1.835 | 1.1 |  |  |  |  |
| 3 |  |  |  | 4 | 2 | 49.830 | 49.806 | 0.024 | 1.828 | 4.3 |  |  |  |  |

a (2) = (2obs - 2calc); b Irel = 100.(Iobs/Imax)