Supplementary information for

Structural aspects of a series of cation radical salts of tetrathiotetracene (TTT) with 2-alkoxy-1,1,3,3-tetracyanoallylide anions (RO-TCA–; R = Me, Et, Prn, Bun)

Shuichi Sekizaki, Chiyoko Tada, Hideki Yamochi, Gunzi Saito

-----------------------------------------------------------------------------------------------------------------------

Synthetic scheme of RO-TCA

Synthesis of TBA•PrO-TCA

Dicyanoketendipropylacetal. (DCKDPA)

A mixture of 8.0 g (63 mmol) of tetracyanoethylene (TCNE) and 3.7 g (62 mmol) of urea in 60 mL of n-propanol was warmed in water bath (ca. 90 °C) for 5 min until deep purple colour had faded to give brown solution. The solution was cooled to room temperature and poured into 100 mL of water, then extracted with ether. The ether solution, dried with MgSO4, was evaporated and dried in vacuum for a day. 9.1 g (47 mmol, 76%) of crude dicyanoketendipropylacetal (DCKDPA) was obtained as brown liquid, which was used for the next reaction without purification, max(film)/cm–1 2974s(C-H st.), 2225vs(CN st.), 1552s(C=C st.); H(200 MHz; CDCl3) 1.03 (6 H, t, J = 7 Hz, Me), 1.84 (4 H, q-like, CH2), 4.46(4 H, t, J = 7 Hz, OCH2)

Sodium 2-Propoxy-1,1,3,3-tetracyanopropenide. (Na•PrO-TCA)

DCKDPA (9.1 g, 47 mmol) was added to dispersion of sodiomalononitriles16 (4.1 g, 47 mmol) in THF (60 mL) with cooling in ice bath. The reaction mixture was stirred for 5 hours until almost all solids were reacted, to which ether (200 mL) was added. The resulting precipitates were collected by filtration and dried. 7.4 g (34 mmol, 72%) of Na•PrO-TCA was yielded as yellow powder, mp 250 ºC (decomp.); max(KBr)/cm–1 2926w(C-H st.), 2203s(CN st.), 1492m(C=C st.).

Tetrabutylammonium 2-Propoxy-1,1,3,3-tetracyanopropenide. (TBA•PrO-TCA)

A solution of 30 g (92 mmol) of tetrabutylammonium bromide (TBA•Br) in 50 mL of water was added to a solution of 7.4 g (34 mmol) of Na•PrO-TCA in 50 mL of water with stirring in ice bath.s17 The resulting precipitates were collected by filtration. Reprecipitation from ethanol-water gave 11.7 g (26 mmol, 83 %) of TBA•PrO-TCA as light yellow powder, mp 38.3-39.7 ºC (Found: C, 70.81; H, 9.95; N 15.85. Calc. For C26H43N5O: C, 70.71; H, 9.81; N 15.86 %); max(KBr)/cm–1 2966m, 2937m and 2878m(C-H st.), 2193vs(CN st.), 1503s(C=C st.); H(200 MHz; CDCl3) 1.04 (15 H, t, J = 7 Hz, Me), 1.36–1.83 (18 H, m, CH2), 3.18 (8 H, t, J = 8 Hz, NCH2), 4.25 (2 H, t, J = 6 Hz, OCH2).

Synthesis of TPA•BuO-TCA

BuO-TCA salt was prepared by the similar way to PrO-TCA salt with the following data for each material.

Dicyanoketendibutylacetal (DCKDBA): brown liquid (51% yield), max(film)/cm–1 2974s(C-H st.), 2225vs(CN st.), 1552s(C=C st.); H(200 MHz; CDCl3) 0.98(6 H, t, J = 7 Hz, Me), 1.40–1.81(8 H, m, CH2), 4.49(4 H, t, J = 6 Hz, OCH2)

Na•BuO-TCA: brown powder (100% yield), max(KBr)/cm-1 2926w(C-H st.), 2203vs(CN st.) 1491s(C=C st.).

TPA•BuO-TCA: white fine needles (79% yield), mp 74.7-75.3 ºC (Found C 69.25 %; H 9.24 %; N 17.45. Calc. for C23H37N5O: C, 69.14; H, 9.33; N, 17.53%.); max(KBr)/cm-1 2977m, 2943m and 2882m(C-H st.), 2194vs(CN st.), 1492s(C=C st.); H(200 MHz; CDCl3) 0.91–1.77 (27 H, m, Me, CH2), 3.16 (8 H, t, J = 9 Hz, NCH2), 4.29 (2 H, t, J = 7 Hz, OCH2).

-----------------------------------------------------------------------------------------------------------------------

Table S1. Overlap patterns of TTT molecules in reported salts.

| Counter anion (Acceptor) | D:A |  | overlap mode | x / Å | y / Å | interplanar distance / Å | Number of atomic contacts a) | overlap integral /10-3 | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Hg2Br62- | 3:1 | Intradimer | B | 0.15 | 2.18 | 3.37 | 0+4+0 | -10.30 | s1 |
|  |  | Interdimer b) | C | 1.54 | 0.83 | 3.48 | 0+0+0 | -9.28 |  |
| I3- | 2:1 | Uniform | A | 3.68 | 0.00 | 3.32 | 0+0+8 | 18.13 | s2 |
| [(C2B9H11)2Ni]- | 2:1 | Uniform | D | 0.17 | 0.09 | 3.41 | 0+0+0 | -7.97 | s3 |
| Br- | 1:1 | Uniform | D | 0.08 | 0.03 | 3.44 | 0+0+0 | 9.66 | s4 |
| TCNQ | 1:2 | Uniform | C | 1.09 | 0.71 | 3.52 | 0+0+0 | -6.55 | s5 |
| OCNAQ | 2:1:1 | Intradimer | A | 3.80 | 0.25 | 3.26 | 2+0+6 | -25.41 | s6 |
|  |  | Interdimer | B | 0.22 | 2.21 | 3.38 | 0+2+0 | -8.66 |  |
| Cu2Br42- | 2:1 | Intradimer | B | 0.09 | 2.28 | 3.37 | 0+8+2 | -10.48 | s7 |
|  |  | Interdimer | C' | 2.77 | 2.94 | 3.45 | 0+0+0 | 4.93 |  |
| Hg2I5- | 1.25:1 | Uniform | A | ? | ? | 3.32 | ? | ? | s8 |

a) Three numbers separated by "+" mean the number of atomic contacts between S∙∙∙S, S∙∙∙C and C∙∙∙C, respectively.

b) Between TTT+ and TTT0.

Table S2. Atomic coordinate of TTT0 molecule optimized by RHF/6-31G*.

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

x / Å	y / Å	 z / Å

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

S	 0.000000	 1.045805	 3.165844

S	 0.000000	-1.045805	 3.165844

S	 0.000000	-1.045805	-3.165844

S	 0.000000	 1.045805	-3.165844

C	 0.000000	 1.215624	 1.398521

C	 0.000000	 0.000000	 0.704242

C	 0.000000	-1.215624	 1.398521

C	 0.000000	-2.420446	 0.722268

C	 0.000000	-3.691528	 1.401219

C	 0.000000	-4.848158	 0.717882

C	 0.000000	-4.848158	-0.717882

C	 0.000000	-3.691528	-1.401219

C	 0.000000	-2.420446	-0.722268

C	 0.000000	-1.215624	-1.398521

C	 0.000000	 0.000000	-0.704242

C	 0.000000	 1.215624	-1.398521

C	 0.000000	 2.420446	-0.722268

C	 0.000000	 3.691528	-1.401219

C	 0.000000	 4.848158	-0.717882

C	 0.000000	 4.848158	 0.717882

C	 0.000000	 3.691528	 1.401219

C	 0.000000	 2.420446	 0.722268

H	 0.000000	-3.704456	 2.475674

H	 0.000000	-5.786273	 1.242328

H	 0.000000	-5.786273	-1.242328

H	 0.000000	-3.704456	-2.475674

H	 0.000000	 3.704456	-2.475674

H	 0.000000	 5.786273	-1.242328

H	 0.000000	 5.786273	 1.242328

H	 0.000000	 3.704456	 2.475674

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

Table S3. Atomic coordinate of TTT+• molecule optimized by ROHF/6-31G*.

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

x / Å	y / Å	 z / Å

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

S	 0.000000	 1.034424	 3.136392

S	 0.000000	-1.034424	 3.136392

S	 0.000000	-1.034424	-3.136392

S	 0.000000	 1.034424	-3.136392

C	 0.000000	 1.203219	 1.405400

C	 0.000000	 0.000000	 0.708578

C	 0.000000	-1.203219	 1.405400

C	 0.000000	-2.441588	 0.713702

C	 0.000000	-3.684450	 1.395415

C	 0.000000	-4.856391	 0.706835

C	 0.000000	-4.856391	-0.706835

C	 0.000000	-3.684450	-1.395415

C	 0.000000	-2.441588	-0.713702

C	 0.000000	-1.203219	-1.405400

C	 0.000000	 0.000000	-0.708578

C	 0.000000	 1.203219	-1.405400

C	 0.000000	 2.441588	-0.713702

C	 0.000000	 3.684450	-1.395415

C	 0.000000	 4.856391	-0.706835

C	 0.000000	 4.856391	 0.706835

C	 0.000000	 3.684450	 1.395415

C	 0.000000	 2.441588	 0.713702

H	 0.000000	-3.702000	 2.469545

H	 0.000000	-5.790299	 1.236729

H	 0.000000	-5.790299	-1.236729

H	 0.000000	-3.702000	-2.469545

H	 0.000000	 3.702000	-2.469545

H	 0.000000	 5.790299	-1.236729

H	 0.000000	 5.790299	 1.236729

H	 0.000000	 3.702000	 2.469545

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

Table S4. Atomic coordinate of TTT2+ molecule optimized by RHF/6-31G*.

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

x / Å	y / Å	 z / Å

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

S	 0.000000	 1.022922	 3.114486

S	 0.000000	-1.022922	 3.114486

S	 0.000000	-1.022922	-3.114486

S	 0.000000	 1.022922	-3.114486

C	 0.000000	 1.195455	 1.416804

C	 0.000000	 0.000000	 0.712626

C	 0.000000	-1.195455	 1.416804

C	 0.000000	-2.463507	 0.713132

C	 0.000000	-3.680425	 1.391290

C	 0.000000	-4.874151	 0.694992

C	 0.000000	-4.874151	-0.694992

C	 0.000000	-3.680425	-1.391290

C	 0.000000	-2.463507	-0.713132

C	 0.000000	-1.195455	-1.416804

C	 0.000000	 0.000000	-0.712626

C	 0.000000	 1.195455	-1.416804

C	 0.000000	 2.463507	-0.713132

C	 0.000000	 3.680425	-1.391290

C	 0.000000	 4.874151	-0.694992

C	 0.000000	 4.874151	 0.694992

C	 0.000000	 3.680425	 1.391290

C	 0.000000	 2.463507	 0.713132

H	 0.000000	-3.707648	 2.465515

H	 0.000000	-5.803527	 1.232458

H	 0.000000	-5.803527	-1.232458

H	 0.000000	-3.707648	-2.465515

H	 0.000000	 3.707648	-2.465515

H	 0.000000	 5.803527	-1.232458

H	 0.000000	 5.803527	 1.232458

H	 0.000000	 3.707648	 2.465515

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

Table S5. Atomic coordinate of MeO-TCA- anion optimized in Z-matrix by RHF/6-31G*.

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

x / Å	y / Å	 z / Å

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

C	 0.000000	 0.000000	 0.000000

C	 0.000000	 0.000000	 1.392515

C	 1.059402	 0.000000	 2.296519

C	 0.774939	 0.023539	 3.694900

N	 0.568953	 0.029162	 4.817426

C	 2.442596	-0.009169	 1.951505

N	 3.564513	-0.021726	 1.748310

C	 1.159678	-0.004095	-0.829154

N	 2.041334	-0.010773	-1.552185

C	-1.248900	 0.015983	-0.690846

N	-2.236648	 0.012885	-1.262543

O	-1.228955	 0.030640	 1.958136

C	-1.828348	-1.217098	 2.242314

H	-2.794681	-0.991180	 2.666437

H	-1.238172	-1.771918	 2.960112

H	-1.957473	-1.796303	 1.337103

––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––––

Table S6. Averaged Bond Length of TTT

| Formal Charge of TTT | Salt (Counter Anion or calc. Method) | Ratio | S-S | S-C | 1-1' | 3-3' | 5-5' | 1-2 | 2-3 | 3-4 | 4-5 | R | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | - | - | 2.092(2) | 1.763(3) | 1.429(4) | 1.456(9) | 1.415(5) | 1.397(6) | 1.398(5) | 1.423(6) | 1.356(6) | 0.028 | This Work, s9 |
|  |  |  | 2.091(2) | 1.764(3) | 1.423(4) | 1.449(4) | 1.416(5) | 1.399(5) | 1.399(5) | 1.424(6) | 1.358(5) |  |  |
| 0 | 6 (PrO-TCA-) | 3:2 | 2.090(3) | 1.758(6) | 1.416(8) | 1.451(8) | 1.402(11) | 1.403(8) | 1.403(13) | 1.426(10) | 1.354(10) | 0.050 | This Work |
| +1 | 6 (PrO-TCA-) | 3:2 | 2.069(3) | 1.734(7) | 1.426(8) | 1.438(9) | 1.398(10) | 1.392(12) | 1.423(10) | 1.413(9) | 1.362(15) | 0.050 | This Work |
| +1 | 1 (MeO-TCA-) | 1:1 | 2.074(3) | 1.743(5) | 1.417(6) | 1.438(6) | 1.400(8) | 1.397(7) | 1.422(8) | 1.415(7) | 1.366(8) | 0.041 | This Work |
| +1 | 2 (EtO-TCA-) | 1:1 | 2.075(2) | 1.737(5) | 1.428(5) | 1.441(5) | 1.399(7) | 1.395(5) | 1.424(5) | 1.415(6) | 1.369(8) | 0.039 | This Work |
|  |  |  | 2.071(2) | 1.731(7) | 1.416(5) | 1.432(5) | 1.390(8) | 1.397(5) | 1.426(6) | 1.421(6) | 1.374(7) |  |  |
| +1 | 4 (PrO-TCA-) | 1:1 | 2.067(5) | 1.732(13) | 1.422(12) | 1.435(13) | 1.398(15) | 1.393(12) | 1.422(12) | 1.409(13) | 1.366(14) | 0.083 | This Work |
| +1 | 8 (BuO-TCA-) | 1:1 | 2.067(6) | 1.734(8) | 1.432(6) | 1.446(8) | 1.399(8) | 1.388(7) | 1.423(7) | 1.408(8) | 1.362(8) | 0.048 | This Work |
| +2 | 3 (EtO-TCA-) | 1:2 | 2.040(2) | 1.707(4) | 1.409(5) | 1.433(5) | 1.382(7) | 1.391(6) | 1.446(6) | 1.398(6) | 1.375(7) | 0.049 | This Work |
| +2 | 7 (PrO-TCA-) | 1:2 | 2.040(2) | 1.710(4) | 1.416(5) | 1.437(5) | 1.377(7) | 1.391(6) | 1.445(5) | 1.399(6) | 1.373(6) | 0.050 | This Work |
| 0 | - | - | 2.100(3) | 1.786(13) | 1.415(17) | 1.454(13) | 1.429(15) | 1.407(16) | 1.37(3) | 1.437(15) | 1.36(3) | 0.13 | s10 |
|  |  |  | 2.100(3) | 1.778(11) | 1.429(20) | 1.457(12) | 1.412(16) | 1.41(3) | 1.380(14) | 1.463(15) | 1.372(14) |  |  |
| 0 | Hg2Br62- | 3:1 | 2.094(6) | 1.77(1) | 1.48 | 1.48 | 1.43 | 1.42 | 1.40 | 1.41 | 1.36 | 0.062 | s1 |
| +0.5 | I3- | 2:1 | 2.078(2) | 1.738(3) | 1.429(8) | 1.444(6) | 1.404(8) | 1.390(4) | 1.414(4) | 1.410(5) | 1.358(5) | 0.042 | s2 |
| +0.5 | I3- | 2:1 | 2.087(18) | 1.735(22) | 1.43(1) | 1.44(1) | 1.42(2) | 1.41(2) | 1.41(5) | 1.42(2) | 1.37(2) | 0.059 | s11 |
| +0.5 | I3- | 2:1 | 2.081(6) | 1.754(10) | 1.435(16) | 1.460(17) | 1.431(23) | 1.390(13) | 1.408(16) | 1.412(17) | 1.349(19) | 0.082 | s12 |
| +0.5 | I3- | 2:1 | 2.077(5) | 1.749(7) | 1.431(11) | 1.456(12) | 1.427(15) | 1.395(8) | 1.404(10) | 1.411(11) | 1.350(12) | 0.082 | s12 |
| +0.5 | I3- | 2:1 | 2.080(2) | 1.746(4) | 1.422(10) | 1.455(8) | 1.438(10) | 1.387(7) | 1.413(6) | 1.412(6) | 1.349(7) | 0.054 | s13 |
| +0.5 | I3- | 2:1 | 2.067 | 1.744 | 1.430 | 1.445 | 1.410 | 1.383 | 1.411 | 1.423 | 1.370 | 0.085 | s13 |
| +0.5 | [(C2B9H11)2Ni]- | 2:1 | 2.070(2) | 1.739(4) | 1.423 | 1.443 | 1.394 | 1.391 | 1.405(10) | 1.415 | 1.364 | 0.038 | s3 |
|  |  |  | 2.082(2) | 1.742(4) | 1.416 | 1.438 | 1.396 | 1.396 | 1.406(8) | 1.426 | 1.359 |  |  |
| +0.5 ? | I3-, I- | 4:1(I3):1(1) | 2.035(10) |  |  |  |  |  |  |  |  | 0.160 | s14, s15 |
| +0.8 ? | Hg2I52- | 1.25:1 | 2.066(3) |  |  |  |  |  |  |  |  | ? | s15, s8 |
| +1 | TCNQ | 2:1 | 2.083(2) | 1.732(7) | 1.375(15) | 1.431(12) | 1.401(12) | 1.401(8) | 1.431(8) | 1.426(8) | 1.360(8) | 0.125 | s5 |
| +1 | OCNAQ | 2:1 | 2.074(5) | 1.731(10) | 1.420(9) | 1.439(14) | 1.398(16) | 1.403(13) | 1.421(13) | 1.427(16) | 1.372(15) | 0.063 | s6 |
| +1 | Hg2Br6 | 3:1 | 2.077(6) | 1.76(1) | 1.45 | 1.45 | 1.44 | 1.40 | 1.41 | 1.41 | 1.41 | 0.062 | s1 |
| +1 | Br- | 1:1 | 2.075(1) | 1.744(4) | 1.441(6) | 1.442(6) | 1.382(8) | 1.392(6) | 1.415(6) | 1.425(6) | 1.361(7) | 0.038 | s4 |
| +1 | Cu2Br42- | 2:1 | 2.076(2) | 1.733(15) | 1.440 | 1.441 | 1.428 | 1.398 | 1.423 | 1.412 | 1.369 | 0.045 | s7 |
| 0 | PM3 | - | 2.1026 | 1.7611 | 1.4076 | 1.4328 | 1.4276 | 1.4169 | 1.3941 | 1.4364 | 1.3576 | - | This Work |
| +1 | PM3 | - | 2.0836 | 1.7296 | 1.4156 | 1.4238 | 1.4144 | 1.4130 | 1.4181 | 1.4213 | 1.3704 | - | This Work |
| +2 | PM3 | - | 2.0709 | 1.7053 | 1.4225 | 1.4263 | 1.3994 | 1.4132 | 1.4354 | 1.4066 | 1.3873 | - | This Work |
| 0 | RHF/6-31G* | - | 2.0916 | 1.7755 | 1.4085 | 1.4445 | 1.4358 | 1.3999 | 1.3816 | 1.4411 | 1.3434 | - | This Work |
| +1 | ROHF/6-31G* | - | 2.0688 | 1.7392 | 1.4172 | 1.4274 | 1.4137 | 1.3904 | 1.4185 | 1.4175 | 1.3593 | - | This Work |
| +2 | RHF/6-31G* | - | 2.0458 | 1.7064 | 1.4253 | 1.4263 | 1.3900 | 1.3871 | 1.4502 | 1.3931 | 1.3820 | - | This Work |

Table S7. Structural parameters of RO-TCA-.

| Salt (anion) or calc. Method | Torsion angle a) / ° | Dihedral angles c) / ° |  |  |  | Bond lengths / Å |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | C1-C5-C7-C4 | P1-P2 | P1-P3 | P2-P3 | P1-P4 | C5-C6 | C6-C7 | C6-O |
| 7 (PrO-TCA) | 13.7 | 5.3 | 3.6 | 8.3 | 73.0 | 1.410(6) | 1.376(6) | 1.364(5) |
| 3 (EtO-TCA) | 15.2 | 2.5 | 7.7 | 10.0 | 68.6 | 1.407(6) | 1.387(6) | 1.361(6) |
| 4 (PrO-TCA) | 34.7 | 9.9 | 13.2 | 20.9 | 66.5 | 1.394(11) | 1.404(13) | 1.356(10) |
| 8 (BuO-TCA) | 43.8 | 12.5 | 16.9 | 27.3 | 35.9 | 1.390(7) | 1.397(6) | 1.361(5) |
| 2 (EtO-TCA(a)) | 50.7 | 14.0 | 19.1 | 28.3 | 53.7 | 1.393(5) | 1.401(5) | 1.360(4) |
| 1 (MeO-TCA) | 51.7 | 13.5 | 20.8 | 30.0 | 50.9 | 1.394(6) | 1.394(6) | 1.359(6) |
| 2 (EtO-TCA(b)) | 52.2 | 19.0 | 18.5 | 36.0 | 51.0 | 1.401(6) | 1.398(5) | 1.354(5) |
| 6 (PrO-TCA) | 78.1 | 21.5 | 30.5 | 48.5 | 37.2 | 1.382(7) | 1.419(8) | 1.342(8) |
| RHF/6-31G* | 1.4 b) | 0.4 | 0.7 | 0.5 | 89.9 | 1.3925 | 1.3927 | 1.3532 |
| RHF/6-31G* | 15.0 | 5.1 | 6.4 | 11.2 | 83.5 | 1.3911 | 1.3941 | 1.3528 |
| RHF/6-31G* | 30.0 | 10.0 | 11.6 | 20.5 | 77.0 | 1.3897 | 1.3959 | 1.3516 |
| RHF/6-31G* | 45.0 | 13.7 | 17.0 | 28.4 | 66.4 | 1.3884 | 1.3985 | 1.3481 |
| RHF/6-31G* | 60.0 | 17.2 | 23.1 | 36.8 | 45.6 | 1.3891 | 1.4035 | 1.3383 |
| RHF/6-31G* | 75.0 | 20.8 | 27.2 | 41.5 | 38.6 | 1.3892 | 1.4056 | 1.3353 |
| RHF/6-31G* | 90.0 | 24.5 | 31.1 | 45.1 | 32.9 | 1.3893 | 1.4076 | 1.3330 |
| PM3 | 0.0 | 0.7 | 0.7 | 1.1 | 89.9 | 1.3978 | 1.3978 | 1.4051 |
| PM3 | 5.0 | 2.0 | 1.7 | 3.4 | 87.4 | 1.3976 | 1.3981 | 1.4050 |
| PM3 | 10.0 | 3.5 | 3.4 | 6.5 | 84.8 | 1.3974 | 1.3984 | 1.4048 |
| PM3 | 15.0 | 5.1 | 5.2 | 9.6 | 82.4 | 1.3972 | 1.3987 | 1.4045 |
| PM3 | 20.0 | 6.6 | 7.0 | 12.7 | 80.0 | 1.3970 | 1.3990 | 1.4041 |
| PM3 | 25.0 | 8.1 | 8.8 | 15.6 | 77.8 | 1.3969 | 1.3994 | 1.4036 |
| PM3 | 30.0 | 9.5 | 10.6 | 18.5 | 75.6 | 1.3968 | 1.3998 | 1.4030 |
| PM3 | 35.0 | 10.9 | 12.3 | 21.3 | 73.4 | 1.3967 | 1.4002 | 1.4023 |
| PM3 | 40.0 | 12.2 | 14.1 | 23.9 | 71.2 | 1.3966 | 1.4006 | 1.4016 |
| PM3 | 45.0 | 13.5 | 15.8 | 26.5 | 69.1 | 1.3965 | 1.4010 | 1.4007 |
| PM3 | 50.0 | 14.8 | 17.5 | 29.0 | 66.9 | 1.3964 | 1.4015 | 1.3998 |
| PM3 | 55.0 | 16.0 | 19.2 | 31.4 | 64.6 | 1.3964 | 1.4020 | 1.3988 |
| PM3 | 60.0 | 17.2 | 21.0 | 33.7 | 62.3 | 1.3963 | 1.4025 | 1.3977 |
| PM3 | 65.0 | 18.4 | 22.7 | 36.0 | 59.9 | 1.3963 | 1.4031 | 1.3965 |
| PM3 | 70.0 | 19.6 | 24.4 | 38.2 | 57.4 | 1.3963 | 1.4037 | 1.3952 |
| PM3 | 75.0 | 20.7 | 26.1 | 40.4 | 54.8 | 1.3963 | 1.4043 | 1.3937 |
| PM3 | 80.0 | 21.9 | 27.8 | 42.5 | 51.8 | 1.3963 | 1.4050 | 1.3921 |
| PM3 | 85.0 | 22.9 | 29.6 | 44.5 | 48.3 | 1.3964 | 1.4059 | 1.3901 |
| PM3 | 90.0 | 23.3 | 32.3 | 46.5 | 24.2 | 1.3983 | 1.4090 | 1.3800 |
| PM3 | 95.0 | 24.7 | 33.8 | 48.2 | 22.3 | 1.3982 | 1.4096 | 1.3790 |

a) Absolute values so as to be between 0-90°.

b) Fully optimaized strucuture of MeO-TCA–.

c) Taken as the angles are between 0-90°.

Table S8  Distances and angles of C–H∙∙∙X (X=N, O) weak hydrogen bonds between TTT and RO-TCA.

| Salts | Atom names | Distance (H∙∙∙X) / Å | Distance (C∙∙∙X) / Å | Angle (C–H∙∙∙X) / ° |
| --- | --- | --- | --- | --- |
| 1 | C14–H14∙∙∙O21 | 2.66(5) | 3.337(6) | 128.0 |
|  | C8–H8∙∙∙N23 | 2.74(4) | 3.677(6) | 174.1 |
| 2 | C8–H8∙∙∙N51 | 2.37(3) | 3.275(5) | 162.4 |
|  | C27–H27∙∙∙N51 | 2.67(4) | 3.388(6) | 131.1 |
|  | C28-H28∙∙∙N52 | 2.47(4) | 3.368(6) | 149.5 |
|  | C34–H34∙∙∙N41 | 2.54(4) | 3.374(5) | 139.0 |
|  | C6–H6∙∙∙N44 | 2.67(4) | 3.373(6) | 124.7 |
|  | C15–H15∙∙∙O41 | 2.71(4) | 3.620(5) | 164.5 |
| 4 | C8–H8∙∙∙N23 | 2.62(8) | 3.33(1) | 131.3 |
|  | C16–H16∙∙∙N23 | 2.75(8) | 3.41(1) | 129.1 |
| 8 | C14–H14∙∙∙N24 | 2.54(4) | 3.298(7) | 129.9 |
|  | C16–H16∙∙∙N22 | 2.75(5) | 3.543(6) | 143.6 |
|  | C8–H8∙∙∙N23 | 2.48(4) | 3.423(6) | 170.0 |
| 3 | C8–H8∙∙∙N11 | 2.58(5) | 3.486(6) | 176.5 |
|  | C5–H5∙∙∙N13 | 2.62(4) | 3.570(8) | 170.3 |
|  | C6–H6∙∙∙N14 | 2.69(4) | 3.353(6) | 133.1 |
| 7 | C6–H6∙∙∙N14 | 2.70(4) | 3.415(6) | 139.1 |

TableS9 Wave numbers of peaks in IR spectra of TTT salts with PrO-TCA

| 4 (1:1) | 5 (?) | TTT•Cl•H2O (TTT+•) | 6 (3:2) | TTT (TTT0) | 7 (1:2) | TTT(Br-)2 (TTT2+) |
| --- | --- | --- | --- | --- | --- | --- |
| 1601(m) 1551(m) 1465(s) 1432(m) 1362(m) 1313(s) 1285(s) 1274(s) 1168(m) 1058(m) 998(m) 974(m) 758(m) | 1597(m) 1552(m) 1465(s) 1420(w) 1362(m) 1313(m) 1284(s) 1273(s) 1166(m) 1058(m) 1000(m) 974(m) 755(m) | 1600(m) 1550(m) 1463(s) 1430(m) 1361(m) 1313(s) 1285(vs) 1273(vs) 1163(m) 1057(s) 997(s) 974(s) 752(m) | 1612(m) 1601(m) 1555(m) 1462(s) 1430(m) 1365(m) 1312(s) 1289(s) 1275(m) 1248(w) 1168(m) 1147(w) 1060(m) 1003(m) 974(m) 751(s) 714(w) | 1612(m) 1522(w) 1316(s) 1303(s) 1247(m) 1146(m) 1010(m) 967(m) 744(vs) 714(w) | 1596(m) 1449(s) 1318(m) 1303(m) 1173(br) 953(m) 775(s) | 1595(s) 1448(vs) 1320(m) 1299(m) 1162(m) 945(w) 775(s) |

References

s1	 R. P. Shibaeva, V.F. Kaminskii, Kristallografiya, 1983, 28, 296.

s2	 D. L. Smith, H. R. Luss, Acta Cryst., 1977, B33, 1744.

s3	 P.A. Chetcuti, W. Hofherr, A, Liégard, G. Rihs, H. Keller, D. Zech, Organometallics, 1995, 14, 666.

s4	 R.P. Shibaeva, V. F. Kaminskii, O. N. Eremenko, E. B. Yagbuskii, M. L. Khidekel, Kristallografiya, 1980, 25, 60.

s5	 R. P. Shibaeva, V.F. Kaminskii, Kristallografiya, 1975, 20, 943.

s6	 T. Inabe, T. Mitsuhashi, Y. Maruyama, Bull. Chem. Soc. Jpn., 1988, 61, 4215.

s7	 R.P. Shibaeva, V. F. Kaminskii, Kristallografiya, 1981, 26, 332.

s8	 V.F. Kaminskii, E. E. Kostuchenko, R. P. Shibaeva, E. B. Yagbuskii, A. V. Zvarykina, J. Phys. Colloque (Paris), 1983, C3, 1167.

s9	 Solved in our laboratory. a = 9.881(2), b = 18.212(2), c = 3.9620(3),  = 87.638(7),  = 79.597(8),  = 96.582(7), V = 695.2(2), which are identical within an experimental error to the data of ref. S10. No. of observed reflections 1959 (I > 3.00(I)), No. of refined parameters 231, R-value 0.028. Hydrogen atoms were determined by differential synthesis.

s10	 O. Dideberg, J. Toussaint, Acta Cryst., 1974, B30, 2481.

s11	 R. P. Shibaeva, V.F. Kaminskii, Kristallografiya, 1978, 23, 499.

s12	 P. A. Filhol, J. Gaultier, C. Hauw, B. Hilti, C. Mayer, Acta Cryst.,1982, B28, 2577.

s13	 C. Lowe-Ma, R. Williams, S. Samson, J. Chem. Phys., 1981, 74, 1966.

s14	 R. P. Shibaeva, Quasi One-Dimensional Conductors II, 1979, Springer-Verlag, Berlin, p. 167.

s15	 R. P. Shibaeva, personal communication; She mentioned that the stoichiometries of TTT4I3I and (TTT)1.25(Hg2I5) have some ambiguities.

s16   Na•CH(CN)2 was prepared by a reaction of sodium and malononitlile in ether with small amount of ethanol.; B. C. Hesse, Am. Chem. J., 1896, 18, 735.

s17  Use of a smaller excess of TBA•Br (e.g. 1.1 equivalent) makes the purification of TBA•PrO-TCA easy, however, results in a poorer yield.