Supporting Information Available: 1. XRD pattern of the PbS CNWs, 2. FTIR spectrum of the polymer, 3. TEM images of more PbS CNWs

#### Manuscript No. B111187F

1. XRD pattern of the PbS CNWs.

(a)

(b)

2. FTIR spectra: (a) the standard spectrum of polyacrylamide obtained from The Aldrich Library of Infrared Spectra, Edition Ⅲ, No. 18127-2, (b) the spectrum of poly[N-(2-Aminoethyl)acrylamide], its sample was obtained from the solvent after the synthetic process was carried out by fully separating the PbS CNWs and evaporating the small molecules (ethylenediamine, H2O).  Compared to (a), a characteristic peak of -CO-NH-R at 1566 cm-1 appeared in (b) resulting from the combination of the bending vibration of NH and the stretching vibration of C-N,* which was apparently different from that of –CO-NH2 [at ~1620 cm-1, δ(NH2)].** The wide peak at 3366-3261 cm-1 resulted from the stretching vibration of NH existing in the structure –CO-NH-CH2-CH2-NH2. The deformation vibration of the NH2 in  -CH2-CH2-NH2 was located at 1615 cm-1, which could not separated from that of the stretching vibration of C=O (1641.8 cm-1).

*L.C. Afremow, K. E. Isakson, D. A. Netzel, D. J. Tessari, J. T. Vandeberg, Infrared Spectroscopy Its Use in the Coating Inductry, Federation of Societies for Paint Technology, Philadelphia, 1969.

**N. B. Colthup, L. H. Daly, S. E. Wiberley, Introduction to Infrared and Raman Spectroscopy, Academic Press, New York, 1975.

3. TEM images of more PbS CNWs.

Notes The first number (X) in the photos ×103 shows the amplifications of the samples in this paper.