Strontium phosphates with (-Ca3(PO4)2-type structures: Sr9NiLi(PO4)7, Sr9.04Ni1.02Na0.88(PO4)7, and Sr9.08Ni1.04K0.76(PO4)7

Alexei A. Belik, Fujio Izumi, Takuji Ikeda, Artem P. Malakho and Bogdan I. Lazoryak

Journal of Materials Chemistry, Article No. B204808F

Table S2

Conditions of the XRD experiments and parts of refinement results for Sr9.04Ni1.02Na0.88(PO4)7 (Na-SNP) and Sr9.08Ni1.04K0.76(PO4)7 (K-SNP)

|  | Na-SNP | K-SNP |
| --- | --- | --- |
| Space group | R3c (No. 161) | R3c (No. 161) |
| Z | 6 | 6 |
| 2( range / ( | 10(140 | 10(140 |
| Step width / ( | 0.02 | 0.02 |
| Imax / counts | 99949 | 92134 |
| Lattice parameters: a / Å c / Å V / Å3 | 10.6755(1) 38.9339(3) 3842.69(5) | 10.7128(1) 38.9492(3) 3871.11(6) |
| Number of Bragg reflections | 821 | 826 |
| Variables: Structure/lattice Profile/background Scale/peak shifts PPP a | 63/2 10/12 1/2 40 | 63/2 10/12 1/2 40 |
| Rwp, Rp RB, RF S b | 4.94 %, 3.59 % 1.53 %, 0.70 % 2.01 | 4.86 %, 3.53 % 1.50 %, 0.70 % 1.97 |

a Refined primary profile parameters.17

b S = Rwp / Re.