Fig. S1. 	Rietveld refinement plots for VO(CH3COO)2 (a) and VO(OCH2CH2O) (b). The observed and calculated patterns are shown on the top as the circles and solid line respectively. Their difference is shown at the bottom. The vertical lines in the middle shows reflections positions.

(a)

(b)

Supporting information

Table 1

Reflection list for VO(CH3COO)2

h   k   l   d      Io/AT  I(c)

1   1   1  4.61028  7853  8410

3   1   0  3.87386 10000  9996

4   0   0  3.51635    34    25

0   0   2  3.46275   559   632

0   2   0  3.43854   111   104

3   1   1  3.38089  8312  8593

2   0   2  3.10659  3441  3979

2   2   0  3.08907  1210  1170

0   2   1  3.07982   256   218

1   1   2  3.02065  4742  5246

2   2   1  2.82116   302   318

5   1   0  2.60368   151   179

3   1   2  2.58169   927  1153

4   0   2  2.46727   457   439

4   2   0  2.45846  5845  6144

0   2   2  2.43993  1115  1129

5   1   1  2.43713  2345  2364

6   0   0  2.34423    66    94

4   2   1  2.31682  3383  3218

2   2   2  2.30514  1836  1832

1   3   0  2.26251   206   230

1   1   3  2.16247   790   924

1   3   1  2.15065  1356  1131

5   1   2  2.08103   767   955

3   3   0  2.05938   987   883

4   2   2  2.00461   923   931

3   1   3  1.98309   119   119

3   3   1  1.97396   463   381

6   0   2  1.94123   235   267

6   2   0  1.93693  1331  1498

7   1   0  1.92870   813   973

0   2   3  1.91663   896   904

1   3   2  1.89405   762   667

6   2   1  1.86535   792   917

7   1   1  1.85800   116   122

2   2   3  1.84918   100   107

5   3   0  1.77705  1697  1836

3   3   2  1.77001  1161  1159

8   0   0  1.75818   485   560

0   0   4  1.73138   270   322

5   1   3  1.72733   794   811

5   3   1  1.72129   209   156

0   4   0  1.71927    24    16

6   2   2  1.69044   860   968

7   1   2  1.68497   257   310

4   2   3  1.68288   187   231

2   0   4  1.68118   341   414

2   4   0  1.67009   117   111

0   4   1  1.66862   665   657

1   1   4  1.66715   800   814

2   4   1  1.62355   222   212

1   3   3  1.61585    81   108

5   3   2  1.58101  1018   965

3   1   4  1.58069   765   738

8   0   2  1.56768   150   188

8   2   0  1.56541    44    54

4   0   4  1.55330   331   359

0   2   4  1.54641   220   217

4   4   0  1.54454    29    27

0   4   2  1.53991   182   154

3   3   3  1.53676    55    52

8   2   1  1.52689     2     3

9   1   0  1.52397   379   471

7   3   0  1.51103   181   195

h   k   l   d      Io/AT  I(c)

2   2   4  1.51032   428   448

4   4   1  1.50750   113   109

2   4   2  1.50427   383   335

9   1   1  1.48836    54    44

6   2   3  1.48382   212   249

7   1   3  1.48011   105   130

7   3   1  1.47630   311   376

5   1   4  1.44172   231   432

8   2   2  1.42642   466   397

4   2   4  1.41557   356   352

4   4   2  1.41058   748   707

5   3   3  1.40816    64    69

10   0   0  1.40654   389   455

9   1   2  1.39486   265   300

6   0   4  1.39271   360   395

6   4   0  1.38638    88    84

7   3   2  1.38492   519   482

0   4   3  1.37888   260   213

1   3   4  1.37497   264   204

1   5   0  1.36889   297   252

6   4   1  1.35941    81    80

2   4   3  1.35312   293   257

1   1   5  1.35155    28    24

1   5   1  1.34291   170   152

3   3   4  1.32525    63   171

3   5   0  1.31980     1     5

3   1   5  1.30424   142   148

10   0   2  1.30314   123   128

10   2   0  1.30184    29    30

3   5   1  1.29646    81    82

8   2   3  1.29562    18    19

9   3   0  1.29129     3     3

6   2   4  1.29084   144   160

7   1   4  1.28840   321   344

6   4   2  1.28706   237   246

0   2   5  1.28478    11    10

4   4   3  1.28371    29    28

10   2   1  1.27943    20    15

1   5   2  1.27302   249   175

9   1   3  1.27183    74    57

9   3   1  1.26941    85    76

7   3   3  1.26428    47    54

2   2   5  1.26386    17    19

11   1   0  1.25713   133   202

5   3   4  1.24010   115   149

11   1   1  1.23692     6     7

5   5   0  1.23563     7     8

8   0   4  1.23363   155   171

3   5   2  1.23326   184   202

8   4   0  1.22923    55    60

5   1   5  1.22283    96    90

0   4   4  1.21997    33    30

10   2   2  1.21857    55    53

5   5   1  1.21642    35    39

8   4   1  1.21032    71   110

9   3   2  1.20990    37    58

4   2   5  1.20676   107   147

2   4   4  1.20201    49    50

6   4   3  1.18852    46    51

11   1   2  1.18167   142   120

1   3   5  1.18131   116   100

1   5   3  1.17744   340   292

12   0   0  1.17212    39    46

5   5   2  1.16376    52    45

h   k   l   d      Io/AT  I(c)

8   2   4  1.16117    77    69

8   4   2  1.15841    54    50

0   0   6  1.15425   171   155

4   4   4  1.15257   102    87

3   3   5  1.14933    34    29

0   6   0  1.14618    29    29

3   5   3  1.14576    21    22

9   1   4  1.14395   139   152

2   0   6  1.13901    49    51

7   3   4  1.13844    60    62

7   5   0  1.13498     1     1

1   1   6  1.13462   133   134

10   2   3  1.13396   128   128

2   6   0  1.13125    50    50

h   k   l   d      Io/AT  I(c)

0   6   1  1.13080    51    51

9   3   3  1.12696    22    21

6   2   5  1.12667    74    71

7   1   5  1.12504     6     6

7   5   1  1.12004    48    53

11   3   0  1.11670     1     1

2   6   1  1.11646    61    64

12   0   2  1.11024    75    76

12   2   0  1.10943    38    39

3   1   6  1.10619    64    77

11   1   3  1.10404   108   145

11   3   1  1.10246     9    13

11   3   1  1.10246     9    13

Table 2

Reflection list for VO(OCH2CH2O)

h   k   l   d       Iobs  Iclc

1   1   0  6.57261  9946 10000

1   1  -1  6.01285  3160  3223

1   1   1  4.95866  1173  1329

0   2   0  4.86727  1058  1199

0   0   2  4.76388   433   502

2   0   0  4.45511  1126  1173

0   2   1  4.33444  3896  4111

1   1  -2  4.29531   930   960

2   0  -2  3.82289   775   871

1   1   2  3.53063   166   111

0   2   2  3.40454   287   280

2   2  -1  3.32228   464   515

2   2   0  3.28631  1192  1139

1   1  -3  3.11929   873   699

1   3   0  3.04896   431   436

2   2  -2  3.00642     6     6

1   3  -1  2.98698   385   363

3   1  -1  2.94354   383   383

2   2   1  2.92828    83    82

2   0   2  2.88115  1062  1109

3   1   0  2.84079   218   224

1   3   1  2.82738   388   416

3   1  -2  2.78481    24    17

1   3  -2  2.68584   180   170

0   2   3  2.65978   561   595

1   1   3  2.65553   621   672

2   2  -3  2.55901   463   509

3   1   1  2.54455     1     1

2   2   2  2.47933    16    17

3   1  -3  2.46549   557   610

1   3   2  2.46448    33    36

0   4   0  2.43364    78    73

1   1  -4  2.40159    12    17

2   0  -4  2.39323    14    21

0   0   4  2.38194     1     2

0   4   1  2.35793    40   113

1   3  -3  2.31126     4    60

4   0  -2  2.27300     0    20

3   3  -1  2.23698    23    35

4   0   0  2.22755   168   233

3   1   2  2.19789    70   108

3   3   0  2.19087   117   161

0   4   2  2.16722    23    25

3   3  -2  2.16488    57    62

2   2  -4  2.14765     0     1

2   4  -1  2.14554    29    36

0   2   4  2.13949     2     3

2   4   0  2.13576   377   419

3   1  -4  2.12188   354   390

1   1   4  2.10621   123   125

1   3   3  2.10245   255   255

4   2  -1  2.09089   131   145

2   2   3  2.08167   657   754

4   2  -2  2.05949    88   104

2   4  -2  2.05295    23    27

3   3   1  2.04607     1     1

2   4   1  2.02754     0     0

4   2   0  2.02551    62    74

3   3  -3  2.00428    99    99

1   3  -4  1.96950   256   274

4   2  -3  1.94322   366   408

1   1  -5  1.93885    87    95

0   4   3  1.93171     1     1

4   0  -4  1.91144   216   217

1   5   0  1.90203   320   318

h   k   l   d       Iobs  Iclc

2   0   4  1.89430    65    64

2   4  -3  1.89206     0     0

1   5  -1  1.88670    91    90

4   2   1  1.88720     0     0

3   1   3  1.88443   284   284

2   4   2  1.85916    61    58

3   3   2  1.85239   142   132

1   5   1  1.84447     8     8

4   0   2  1.83297    70    85

3   1  -5  1.82049     1     2

2   2  -5  1.81687     3     4

5   1  -1  1.81388   102   138

5   1  -2  1.81233     1     2

3   3  -4  1.80620    87   115

1   5  -2  1.80343     7     9

1   3   4  1.79650    49    60

4   2  -4  1.77917    47    54

0   2   5  1.77441    44    50

2   2   4  1.76531    56    61

5   1   0  1.75291    10    11

5   1  -3  1.74872   163   187

1   1   5  1.73796    33    36

1   5   2  1.73164    47    48

4   2   2  1.71537    86    91

2   4  -4  1.70638   263   272

0   4   4  1.70227   152   157

1   3  -5  1.68924    17    18

4   4  -1  1.67748     0     0

1   5  -3  1.67590    73    74

2   4   3  1.67271    19    18

4   4  -2  1.66114    11    10

3   3   3  1.65289   184   184

3   5  -1  1.64692    45    47

2   0  -6  1.64646    24    25

5   1   1  1.64624     2     2

4   4   0  1.64315    55    59

5   1  -4  1.64046   207   222

3   5   0  1.62826    93    82

3   1   4  1.62600   140   121

0   6   0  1.62242     3     2

1   1  -6  1.62075   178   152

3   5  -2  1.61751    78    65

3   3  -5  1.60923    41    36

5   3  -1  1.60466    36    31

4   2  -5  1.60327    39    34

5   3  -2  1.60359     0     0

0   6   1  1.59940    58    48

4   4  -3  1.59830     6     5

1   5   3  1.59096    45    33

0   0   6  1.58796    82    60

3   1  -6  1.57448    21    18

4   4   1  1.56669     1     1

3   5   1  1.56611     2     2

5   3   0  1.56199   109    99

2   2  -6  1.55964     2     2

5   3  -3  1.55902    65    61

1   3   5  1.55138     3     3

3   5  -3  1.54713    72    76

6   0  -2  1.54405     1     1

4   2   3  1.54129   154   162

0   6   2  1.53580     1     1

1   5  -4  1.53096    21    23

2   6  -1  1.52803   164   176

2   4  -5  1.52575     1     1

2   6   0  1.52448    17    18

h   k   l   d       Iobs  Iclc

2   2   5  1.51962    10    11

5   1   2  1.51696    36    35

5   1  -5  1.51063     1     1

0   2   6  1.50965     6     6

4   0  -6  1.50418    35    36

4   4  -4  1.50321   168   172

0   4   5  1.50034    10    11

2   4   4  1.49483    85    86

2   6  -2  1.49349     2     2

6   0   0  1.48504    81    80

5   3   1  1.48509     0     0

2   6   1  1.48362     9     9

5   3  -4  1.48084    49    48

1   1   6  1.47643    34    35

3   5   2  1.47398   121   123

6   2  -2  1.47177    11    11

3   3   4  1.47019     6     6

1   3  -6  1.46630    72    77

4   4   2  1.46414   102   108

6   2  -1  1.46232   136   144

6   0  -4  1.45313    62    63

3   5  -4  1.45038    40    40

6   2  -3  1.44684    59    59

1   5   4  1.44535    12    12

0   6   3  1.44481    94    94

4   0   4  1.44057     5     5

4   2  -6  1.43712    15    14

3   3  -6  1.43177    80    77

2   6  -3  1.42799   130   122

6   2   0  1.42039    11     8

3   1   5  1.41863    18    13

2   6   2  1.41369    18    11

4   4  -5  1.39256     1     1

6   2  -4  1.39240    15    11

1   1  -7  1.39025    36    28

1   5  -5  1.38770     2     2

5   3   2  1.38811    34    28

5   3  -5  1.38325    35    32

5   1   3  1.38387    38    34

4   2   4  1.38134    18    17

2   0   6  1.38011    32    31

5   1  -6  1.37769    36    36

3   1  -7  1.37740    22    22

1   7   0  1.37401    65    70

1   7  -1  1.36820    59    63

3   5   3  1.36734    35    37

2   4  -6  1.36369   175   180

2   2  -7  1.35920   110   109

1   3   6  1.35685    59    57

6   2   1  1.35370     0     0

1   7   1  1.35184     8     8

4   4   3  1.35137     0     0

2   6  -4  1.34292     0     0

3   5  -5  1.34231     0     0

0   6   4  1.34092     6     6

5   5  -1  1.33965    23    24

5   5  -2  1.33903     3     4

2   4   5  1.33669     0     0

1   7  -2  1.33543    31    34

0   4   6  1.32989   122   131

4   6  -1  1.32870    36    39

2   2   6  1.32777    10    11

2   6   3  1.32633    71    76

4   6  -2  1.32054    16    17

6   2  -5  1.31773    16    16

6   0   2  1.31810    55    56

h   k   l   d       Iobs  Iclc

5   5   0  1.31452    67    65

5   5  -3  1.31275     8     8

7   1  -2  1.31223    13    12

4   6   0  1.31144     1     1

3   3   5  1.31158     1     1

0   2   7  1.31082    59    57

1   5   5  1.30818     0     0

1   7   2  1.30548    18    18

6   4  -2  1.30378     9     9

7   1  -3  1.30158    22    23

7   1  -1  1.29835    69    73

6   4  -1  1.29720     4     4

4   2  -7  1.28952    69    71

1   3  -7  1.28905    70    73

4   6  -3  1.28830    97    99

6   4  -3  1.28635     2     2

5   3   3  1.28396    19    20

1   1   7  1.28199     3     3

1   7  -3  1.28109    26    27

4   4  -6  1.27951    20    20

5   3  -6  1.27903     2     2

3   3  -7  1.27879    60    62

6   0  -6  1.27430     6     6

6   2   2  1.27228     0     0

4   6   1  1.27157     0     0

7   1  -4  1.26811    25    26

3   7  -1  1.26801    17    17

6   4   0  1.26766    41    44

5   5   1  1.26770     4     5

5   5  -4  1.26505    29    32

7   1   0  1.26214    63    69

3   7   0  1.25943    42    47

3   5   4  1.25839     3     3

5   1   4  1.25808     0     0

1   5  -6  1.25595    37    44

3   7  -2  1.25444     0     0

5   1  -7  1.25241     7     8

3   1   6  1.25237    45    56

2   6  -5  1.24939     7     8

6   4  -4  1.24764    54    68

1   7   3  1.24193    19    22

4   2   5  1.24107    14    16

2   0  -8  1.23910     6     6

4   4   4  1.23967    12    13

4   6  -4  1.23692     0     0

0   6   5  1.23532     4     5

3   5  -6  1.23404    25    27

6   2  -6  1.23275     0     0

2   6   4  1.23224     0     0

3   7   1  1.23000     1     1

7   3  -2  1.22613     5     7

2   4  -7  1.22359     0     0

3   7  -3  1.22074    48    68

3   1  -8  1.21915     3     5

6   4   1  1.21957     1     1

7   3  -3  1.21743     2     2

7   1  -5  1.21675     0     0

0   8   0  1.21682    38    55

1   1  -8  1.21615     5     7

7   3  -1  1.21478    31    45

4   6   2  1.21488    11    17

1   7  -4  1.21275     4     6

7   1   1  1.20886     0     0

0   8   1  1.20701     0     0

5   5   2  1.20576    23    31