Table 1. Crystal Data and Structure Refinement for (C4N2H11) ZrGe4O10F2 (FDZG-1)

|  | FDZG-1 |
| --- | --- |
| Empirical formula | (C4N2H12)ZrGe4O10F2 |
| Formula weight | 667.74 |
| Temperature | 293(2) K |
| Wavelength | 0.71073 Å |
| Crystal system | Monoclinic |
| Space group | C2/c |
| Unit cell dimensions | A = 17.725(5) Å α = 90° |
|  | B = 10.149(3) Å β= 120.720(2) ° |
|  | C = 9.547(3) Å γ = 90° |
| Volume, Z | 1476.4(7) Å3, 4 |
| Density(calculate) | 3.004 Mg/m3 |
| Absorption coefficient | 8.808 mm-1 |
| F(000) | 1264 |
| Crystal size | 0.08 x 0.05 x 0.05 mm |
| Θ range for data collection | 2.41 to 27.14° |
| Limiting indices | -22≤h≤22, -8≤k≤13, -12≤l≤12 |
| Reflections collected / unique | 3590 / 1619 （Rint = 0.0191） |
| Completeness to Θ= 27.14° | 98.8 % |
| Max. and min. transmission | 0.6671 and 0.5392 |
| Refinement method | Full-matrix least-squares on F2 |
| Data / restraints / parameters | 1619 / 0 / 123 |
| Goodness-of-fit on F2 | 1.171 |
| Final R indices [I>2sigma(I)] | R1a = 0.0284, wR2b = 0.0772 |
| R indices (all data) | R1 = 0.0298, wR2 = 0.0780 |
| Largest diff. peak and hole | 1.234 and -1.118 e. Å -3 |

aR1= Fo| – |Fc||/|Fo|.   bwR2=[w(Fo2 - Fc2)2/[w(Fo2)21/2, where w=1/[σ2(Fo2) +(0.0302P)2 + 5.74P] with P =(max Fo2 + 2Fc2)/3.

Table 2. Atomic Coordinates and Equivalent Isotropic Displacement Parameters for (C4N2H12) ZrGe4O10F2 (FDZG-1)

| atom | X | Y | Z | Ueqa |
| --- | --- | --- | --- | --- |
| Zr(1) | 0.5000 | 0.2184(1) | 0.7500 | 12(1) |
| Ge(1) | 0.3096(1) | 0.0683(1) | 0.4511(1) | 11(1) |
| Ge(2) | 0.2033(1) | 0.3167(1) | 0.2608(1) | 12(1) |
| O(1) | 0.2680(2) | 0.1779(3) | 0.2876(4) | 18(1) |
| O(2) | 0.2544(2) | 0.0961(3) | 0.5561(4) | 17(1) |
| O(3) | 0.2797(2) | -0.0912(3) | 0.3754(4) | 17(1) |
| O(4) | 0.4215(2) | 0.0815(3) | 0.5756(4) | 21(1) |
| O(5) | 0.4052(2) | 0.2236(3) | 0.8191(4) | 19(1) |
| F(1) | 0.4472(2) | 0.3621(4) | 0.5837(7) | 73(2) |
| C(1) | 0.4244(3) | 0.2248(5) | 0.2241(6) | 28(1) |
| C(2) | 0.4168(6) | 0.3642(10) | 0.1694(12) | 23(2) |
| C(3) | 0.5683(6) | 0.3747(10) | 0.2249(13) | 24(2) |
| N(1) | 0.5243(5) | 0.1915(8) | 0.3431(9) | 21(2) |
| N(2) | 0.4719(5) | 0.3982(7) | 0.1001(9) | 20(2) |

a Ueq (Å2103) is defined as third of the trace of the orthogonalized Uij tensor.

Table 3. Selected Bond Lengths (Å) and Angles (°) for (C4N2H12) ZrGe4O10F2

| Zr(1)-F(1) | 2.001(3) | Ge(2)-O(3)c | 1.749(3) |  |
| --- | --- | --- | --- | --- |
| Zr(1)-O(4) | 2.067(3) | Ge(2)-O(1) | 1.751(3) |  |
| Zr(1)-O(5) | 2.097(3) | C(1)-N(1) e | 1.396(9) |  |
| Ge(1)-O(4) | 1.719(3) | C(1)-C(2) | 1.490(11) |  |
| Ge(1)-O(3) | 1.741(3) | C(1)-N(1) | 1.576(9) |  |
| Ge(1)-O(1) | 1.744(3) | C(1)-C(3)e | 1.582(11) |  |
| Ge(1)-O(2) | 1.745(3) | C(2)-N(2) | 1.474(11) |  |
| Ge(2)-O(5)b | 1.716(3) | C(3)-N(2) | 1.522(11) |  |
| F(1)a-Zr(1)-F(1) | 86.4(4) | O(1)-Ge(1)-O(2) | 107.80(15) |  |
| F(1)a-Zr(1)-O(4) | 168.11(13) | O(5)b-Ge(2)-O(3)c |  | 112.08(15) |
| F(1)-Zr(1)-O(4) | 90.06(19) | O(5)b-Ge(2)-O(2)b | 112.08(14) |  |
| F(1)-Zr(1)-O(4)a | 168.11(13) | O(3)c-Ge(2)-O(2)b | 108.89(15) |  |
| O(4)-Zr(1)-O(4)a | 95.55(19) | O(5)b-Ge(2)-O(1) | 112.00(15) |  |
| F(1)a-Zr(1)-O(5) | 81.80(14) | O(3)c-Ge(2)-O(1) | 100.93(14) |  |
| F(1)-Zr(1)-O(5) | 96.08(14) | O(2)b-Ge(2)-O(1) | 110.29(14) |  |
| O(4)-Zr(1)-O(5) | 87.29(12) | Ge(1)-O(1)-Ge(2) | 126.16(17) |  |
| O(4)a-Zr(1)-O(5) | 94.65(12) | Ge(1)-O(2)-Ge(2)b | 125.17(17) |  |
| F(1)a-Zr(1)-O(5)a | 96.08(14) | Ge(1)-O(3)-Ge(2)d | 132.36(17) |  |
| F(1)-Zr(1)-O(5)a | 81.80(14) | Ge(1)-O(4)-Zr(1) | 132.36(18) |  |
| O(4)-Zr(1)-O(5)a | 94.65(12) | Ge(2)b-O(5)-Zr(1) | 138.56(17) |  |
| O(5)-Zr(1)-O(5)a | 177.12(18) | C(2)-C(1)-N(1) | 108.9(5) |  |
| O(4)-Ge(1)-O(3) | 111.03(15) | N(1) -C(1)e -C(3) | 113.9(6) |  |
| O(4)-Ge(1)-O(1) | 112.36(15) | N(2)-C(2)-C(1) | 114.6(7) |  |
| O(3)-Ge(1)-O(1) | 108.77(14) | N(2)-C(3)-C(1)e | 105.9(7) |  |
| O(4)-Ge(1)-O(2) | 112.16(15) | C(1)-N(1)-C(1)e | 111.8(5) |  |
| O(3)-Ge(1)-O(2) | 104.34(14) | C(2)-N(2)-C(3) | 110.4(7) |  |

Symmetry transformations used to generate equivalent atoms:

a (-x+1,y,-z+3/2)    b (-x+1/2,-y+1/2,-z+1)

c (-x+1/2,y+1/2,-z+1/2)    d (-x+1/2,y-1/2,-z+1/2)

e (-x+1,y,-z+1/2)

Figure 1. SEM image of FDZG-1 single crystals