Table S1 Amounts of propylammonium cations and phthalocyanines Pc intercalated into the interlayer space of Ti3O7

|  | C/wt% | N/wt% | amount of Pc mol/1 mol host | amount of PA mol/1 mol host |
| --- | --- | --- | --- | --- |
| H2Ti3O7 | — | — | — | — |
| PA/Ti3O7 | 6.55 | 2.43 | — | 0.544 |
| ABpy/Ti3O7 (pH=10.3) | 19.36 | 5.09 | 0.093 | 0.178 |
| FePc/Ti3O7 | 15.01 | 5.25 | 0.118 | 0.280 |

Fig. S1 XRD patterns of (a) H2Ti3O7, (b) PA/Ti3O7, (c) PA/Ti3O7 + ABpy(OH)4, and (d) PA/Ti3O7 + FePc(Cl).