Supplementary Information, Soler-Illia et al. Mixed Si-Zr MP Thin films

# Text boxes

SI Figure 2. TEM image and EDS spectra of an F127-templated ZrO2/SiO2 film (fSi=0.75; 150ºC); upper curve: mesostructured continuous background; lower curve: dense particles. The area ratio of the Si and Zr peaks is indicated in each spectrum.

SI Figure 1. EDS spectrum of an F127-templated ZrO2/SiO2 film (fSi=0.25; 150ºC); A ZrO2/SiO2 relationship of 74±1/26±1 is obtained.