Electronic supplementary information (ESI)

-Chromophore-functionalized SWNTs by covalent bonding: substantial change in the optical spectra proving strong electronic interaction

Weihong Zhu, Nobutsugu Minami,* Said Kazaoui and Yeji Kim

Nanotechnology Research Institute, National Institute of Advanced Industrial Science and Technology (AIST), 1-1-1 Higashi, Tsukuba, Ibaraki 305-8565, Japan. Fax: 81 298 61 6309; Tel: 81 298 61 9385; E-mail: n.minami@aist.go.jp

Fig. S1 UV-Vis-Near IR absorption spectra of a-SWNT-CO2H and b-SWNT-CO2H in DMF. While the van Hove absorption bands are almost completely lost for a-SWNT-CO2H, they remain nearly intact for b-SWNT-CO2H; absorption peaks due to the first (1236, 1320 and 1430 nm) and the second bandgaps (741, 815 and 890 nm) are observed.

Fig. S2 Near IR absorption spectra of the intermediate NI, a-SWNT-NI and b-SWNT-NI in CHCl3. The difference between a-SWNT-CO2H and b-SWNT-CO2H (shown in Fig. S1) are found to be preserved in the final products. Diffused spectra of a-SWNT-NI as compared with a-SWNT-CO2H (Fig. S1) imply the electronic perturbation due to the introduced -chromophores.

Fig. S3 Possible resonance structure formulas of SWNT-NI. Nitrogen's isolated electron pairs in the covalent bonding bridge (-NHNH-) can play a role in the -delocalization between SWNTs and moiety units, leading to a strong electronic interaction between the chromophore and SWNTs units, and thus resulting in the considerable change in the absorption and luminescence spectra.

Fig. S4 Luminescence excitation spectra monitored at 550 nm of a-SWNT-NI, b-SWNT-NI, the reference compounds NI-Ac, and NI.