Fabrication of poly(methyl methacrylate) capillary electrophoresis microchips by in situ surface polymerization

Supplementary Material (ESI) for Lab on a Chip

This journal is © The Royal Society of Chemistry 2006

Guoxi Xu,a Joseph Wang, b Yi Chen, a Luyan Zhang,a Derong Wang, a and Gang Chen* a

a Department of Chemistry, Fudan University, Shanghai 200433, China. Fax: 86 21 65641740; Email: gangchen@fudan.edu.cn

b Departments of Chemical & Materials Engineering and Chemistry, *Arizona State University, Tempe, AZ 85287-5001, USA

*To whom correspondence should be addressed.

Fax: 86-21-6564-1740. E-mail: gangchen@fudan.edu.cn

ESI-Fig. 1. Schematic of the sandwich molding process.  (A) casting the MMA prepolymer molding solution (a) on the nickel template (b); (B) sandwiching the molding solution between the PMMA plate (c) and the nickel template (b); (C) exposing the sandwich mold to the UV light (d); (D) demolding of the polymerized PMMA substrate with channels (e); (E) thermal sealing of the two PMMA plates to form the complete microchip (f). (g) cover plate. Dimensions are not in scale.

ESI-Fig. 2. Scanning electron micrographs (SEMs) of the cross sections of (A) an unsealed microchannel in the PMMA substrate and the channels in the complete PMMA electrophoresis microchips Conditions: accelerating voltage, 20 kV; magnification,  200.