Supplementary Material (ESI) for New Journal of Chemistry

This journal is © The Royal Society of Chemistry and the Centre National de la Recherche Scientifique 2002


   0.48

0.01

1.77

 0.05

The apparent order in [02] was found to be 0.5, (n=O.5). Therefore by plotting  (1-R)/R versus [O2]0.5 a linear dependence in oxygen quenching was displayed and the sensitivity of the film was denoted by the gradient

The data shown in figure 2 were treated according to equation 8. Plotting log( 1- R/R) versus log[O2] for each time interval gave a straight line of gradient 0.48 (:to.2). This value depended on time in a random scattered fashion. Data in the time interval 0.26 to O.56ms were used to determine the mean

Data Generated from Double Log plot

Time/ms 
 Gradient
      Intercept

0.01 0.06 0.11 0.16 0.21 0.26 0.31 0.36 0.41 0.46 0.51 0.56 0.61 0.66 0.71

0.45 0.48 0.49

0.5 

0.5

0.49

0.47

0.48

0.49

0.48

0.48

0.49

0.48

0.47

0.47

1.5 1.7 1.7 1.8 1.8 1.8 1.7 1.7 1.8 1.8 1.8 1;8 1.8 1.8 1.8

x

x

