# Supplementary Information

# for the manuscript

# Arene – Perfluoroarene Interactions in Crystal Engineering 8:

# Structures of 1:1 Complexes of Hexafluorobenzene with Fused-ring Polyaromatic Hydrocarbons

Jonathan C. Collings, Karl P. Roscoe, Edward G. Robins, Andrei S. Batsanov,

Lorna M. Stimson, Judith A.K. Howard, Stewart J. Clark, and Todd B. Marder

Contents:

Table S1. Components of T, L and S tensors in the inertial coordinate systems.

Table S2. Bond distances (Å) in HFB.

Table S3. Bond distances (Å) in arene molecules.

Table S4. Intermolecular H···F contacts.

Table S5. Calculated atomic coordinates in structure 1.

Table S6. Calculated atomic coordinates in structure 2.

Table S7. Calculated atomic coordinates in structure 4.

Table S8. Calculated atomic coordinates in structure 5.

Comment

All HFB molecules in each structure are rigorously parallel. However, the nearest arene molecules in a stack of 1 or 2 are not crystallographically parallel, in constrast with all other arene-perfluoroarene complexes (including 3–5) where these molecules are related by either translation or inversion. The planes of these molecules form an angle of 3.6º in 1 and 2.5º in 2, and their long axes, an angle of 64.5º and 10.0º respectively.

Table S1. Components of T (Å2 ×104), L (rad2 ×104) and S (rad·Å ×104) tensors in the inertial coordinate systems

| Complex/molecule | # T |  |  | # L |  |  | # S |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1, HFB | 336(15) | 0(13) | 0(16) | 66(6) | 0(3) | 0(4) |  |  |  |
|  |  | 421(15) | 2(16) |  | 51(6) | 2(4) |  |  |  |
|  |  |  | 226(25) |  |  | 63(3) |  |  |  |
| 1, naphthalene | 347(7) | –9(6) | 19(8) | 51(10) | 3(2) | 7(4) |  |  |  |
|  |  | 365(9) | –1(9) |  | 29(3) | –4(2) |  |  |  |
|  |  |  | 234(18) |  |  | 71(2) |  |  |  |
| 2, HFB | 179(14) | 0(12) | –12(15) | 54(5) | 0(3) | 3(4) |  |  |  |
|  |  | 291(14) | 0(15) |  | 26(5) | 0(4) |  |  |  |
|  |  |  | 207(23) |  |  | 42(3) |  |  |  |
| 2, anthracene | 197(3) | 14(3) | –9(3) | 37(5) | –1.0(7) | –3(1) |  |  |  |
|  |  | 218(5) | –3(5) |  | 12.4(6) | 0.0(5) |  |  |  |
|  |  |  | 195(8) |  |  | 15.8(5) |  |  |  |
| 3, HFB | 281(5) | 11(4) | 10(5) | 33(2) | 5(1) | 2(1) | –5(2) | 12(3) | –3(1) |
|  |  | 308(5) | –11(5) |  | 37(2) | 5(1) | 10(1) | 6(2) | 0(1) |
|  |  |  | 167(8) |  |  | 43(1) | 7(1) | –2(1) | –2(3) |
| 3, phenanthrene* | 258(3) | 13(3) | 2(4) | 23(2) | –1.9(7) | –1(1) | –2(2) | –4(3) | –1(1) |
|  |  | 221(4) | 6(5) |  | 13.3(8) | –2.5(7) | –3.2(7) | 3(1) | 0.1(7) |
|  |  |  | 158(7) |  |  | 22.5(6) | 5(1) | –11.6(7) | –1(2) |
| 4, HFB | 396(7) | 17(6) | –6(8) | 49(3) | 5(2) | 6(2) |  |  |  |
|  |  | 372(7) | 0(8) |  | 47(3) | 2(2) |  |  |  |
|  |  |  | 212(12) |  |  | 55(2) |  |  |  |
| 4, pyrene | 349(6) | -5(6) | 8(7) | 30(3) | -1(1) | 6(2) |  |  |  |
|  |  | 322(7) | -1(8) |  | 21(2) | 2(1) |  |  |  |
|  |  |  | 191(13) |  |  | 35(1) |  |  |  |
| 5, HFB | 318(10) | –6(9) | 31(11) | 34(4) | –4(2) | –4(3) | 13(4) | 12(6) | 3(3) |
|  |  | 307(10) | –8(11) |  | 30(4) | –2(3) | 6(3) | –8(4) | 4(3) |
|  |  |  | 104(17) |  |  | 41(2) | –20(3) | –1(3) | –5(6) |
| 5, triphenylene | 324(9) | –35(8) | 15(10) | 12(2) | 5(1) | 1(2) | –2(3) | 2(4) | –4(2) |
|  |  | 300(9) | –11(10) |  | 9(2) | 0(2) | 7(2) | 6(3) | –7(2) |
|  |  |  | 118(15) |  |  | 15(1) | 0(2) | –9(2) | –4(5) |

*Major position

Table S2. Bond distances (Å) in HFB, before (left) and after (right) correction for libration

|  | 1 |  | 2 |  | 3 |  | 4 |  | 5 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C(1)-F(1) | 1.345(3) | 1.353 | 1.346(3) | 1.352 | 1.342(2) | 1.348 | 1.338(2) | 1.345 | 1.333(7) | 1.337 |
| C(2)-F(2) | 1.342(2) | 1.351 | 1.340(2) | 1.345 | 1.339(2) | 1.344 | 1.341(2) | 1.348 | 1.347(8) | 1.352 |
| C(3)-F(3) | 1.338(2) | 1.346 | 1.335(2) | 1.340 | 1.340(2) | 1.345 | 1.338(2) | 1.345 | 1.347(8) | 1.352 |
| C(4)-F(4) | 1.344(3) | 1.351 | 1.344(2) | 1.350 | 1.341(1) | 1.346 |  |  | 1.336(7) | 1.341 |
| C(5)-F(5) |  |  |  |  | 1.344(1) | 1.350 |  |  | 1.340(7) | 1.345 |
| C(6)-F(6) |  |  |  |  | 1.339(2) | 1.344 |  |  | 1.354(7) | 1.359 |
| C-F, average | 1.342(3) | 1.350(3) | 1.341(4) | 1.347(5) | 1.341(2) | 1.346(2) | 1.339(1) | 1.346(1) | 1.343(7) | 1.348(7) |
| C(1)-C(2) | 1.371(2) | 1.380 | 1.371(2) | 1.376 | 1.383(2) | 1.388 | 1.379(3) | 1.386 | 1.378(9) | 1.383 |
| C(2)-C(3) | 1.381(3) | 1.389 | 1.384(3) | 1.391 | 1.382(2) | 1.388 | 1.375(3) | 1.383 | 1.383(9) | 1.388 |
| C(3)-C(4) | 1.378(2) | 1.387 | 1.373(2) | 1.379 | 1.382(2) | 1.388 |  |  | 1.374(9) | 1.379 |
| C(4)-C(5) |  |  |  |  | 1.385(2) | 1.391 |  |  | 1.380(9) | 1.385 |
| C(5)-C(6) |  |  |  |  | 1.382(2) | 1.387 |  |  | 1.381(9) | 1.386 |
| C(1)-C(6) |  |  |  |  | 1.382(2) | 1.388 | 1.376(3)* | 1.383 | 1.382(10) | 1.387 |
| C-C, average | 1.377(4) | 1.385(4) | 1.376(6) | 1.382(6) | 1.383(2) | 1.388(1) | 1.377(2) | 1.384(1) | 1.380(3) | 1.385(3) |

* Bond C(1)-C(3′)

Table S3. Bond distances (Å) in arene molecules, before (left) and after (right) correction for libration

|  | 1, naphthalene |  |  | 3, phenanthrene |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | observed | corrected |  | observed | corrected | minor* |
| C(11)-C(12) | 1.369(3) | 1.376 | C(7)-C(8) | 1.371(2) | 1.374 | 1.371(17) |
| C(11)-C(15) | 1.420(3) | 1.427 | C(7)-C(17) | 1.422(2) | 1.425 | 1.484(16) |
| C(12)-C(13) | 1.395(3) | 1.404 | C(8)-C(9) | 1.411(2) | 1.414 | 1.317(18) |
| C(13)-C(14) | 1.365(3) | 1.372 | C(9)-C(10) | 1.373(2) | 1.375 | 1.396(17) |
| C(14)-C(15) | 1.424(3) | 1.431 | C(10)-C(18) | 1.419(2) | 1.422 | 1.371(15) |
| C(15)-C(15′) | 1.420(3) | 1.429 | C(11)-C(12) | 1.384(2) | 1.386 | 1.373(17) |
|  | 2, anthracene |  | C(11)-C(19) | 1.417(2) | 1.420 | 1.423(16) |
| C(11)-C(12) | 1.400(2) | 1.402 | C(12)-C(13) | 1.406(3) | 1.409 | 1.41(2) |
| C(11)-C(17) | 1.393(2) | 1.396 | C(13)-C(14) | 1.372(3) | 1.375 | 1.339(18) |
| C(12)-C(13) | 1.431(2) | 1.433 | C(14)-C(20) | 1.421(2) | 1.424 | 1.473(16) |
| C(13)-C(14) | 1.358(3) | 1.360 | C(15)-C(16) | 1.353(2) | 1.356 | 1.339(14) |
| C(14)-C(15) | 1.420(3) | 1.424 | C(15)-C(20) | 1.436(2) | 1.439 | 1.432(14) |
| C(15)-C(16) | 1.357(3) | 1.360 | C(16)-C(17) | 1.439(2) | 1.442 | 1.417(14) |
| C(16)-C(17′) | 1.431(2) | 1.433 | C(17)-C(18) | 1.421(2) | 1.424 | 1.407(16) |
| C(17)-C(12′) | 1.445(2) | 1.449 | C(18)-C(19) | 1.462(2) | 1.465 | 1.526(14) |
|  |  |  | C(19)-C(20) | 1.418(2) | 1.421 | 1.368(15) |

* Minor position of the phenanthrene molecule was refined in isotropic approximation (no libration correction).

Table S3 (continued)

|  | 4, pyrene |  |  | 5, triphenylene |  |  | 5, triphenylene |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | observed | corr. |  | observed | corr. |  | observed | corr. |
| C(11)-C(12) | 1.405(3) | 1.409 | C(11)-C(12) | 1.358(9) | 1.360 | C(19)-C(27) | 1.421(9) | 1.423 |
| C(11)-C(16) | 1.415(2) | 1.419 | C(11)-C(23) | 1.420(9) | 1.422 | C(20)-C(21) | 1.417(10) | 1.418 |
| C(11)-C(17) | 1.434(3) | 1.438 | C(12)-C(13) | 1.390(10) | 1.392 | C(21)-C(22) | 1.375(10) | 1.377 |
| C(12)-C(13) | 1.371(3) | 1.375 | C(13)-C(14) | 1.371(9) | 1.373 | C(22)-C(28) | 1.412(10) | 1.414 |
| C(13)-C(14) | 1.389(3) | 1.393 | C(14)-C(24) | 1.404(9) | 1.406 | C(23)-C(24) | 1.408(9) | 1.410 |
| C(14)-C(15) | 1.390(3) | 1.394 | C(15)-C(16) | 1.382(9) | 1.384 | C(23)-C(28) | 1.471(9) | 1.473 |
| C(15)-C(16) | 1.442(3) | 1.446 | C(15)-C(25) | 1.407(9) | 1.409 | C(24)-C(25) | 1.496(8) | 1.497 |
| C(16)-C(18) | 1.434(3) | 1.438 | C(16)-C(17) | 1.390(10) | 1.392 | C(25)-C(26) | 1.395(9) | 1.397 |
| C(16)-C(16′) | 1.419(3) | 1.423 | C(17)-C(18) | 1.375(10) | 1.377 | C(26)-C(27) | 1.476(9) | 1.478 |
| C(17)-C(18′) | 1.349(3) | 1.353 | C(18)-C(26) | 1.418(9) | 1.419 | C(27)-C(28) | 1.403(8) | 1.405 |
|  |  |  | C(19)-C(20) | 1.365(10) | 1.367 |  |  |  |

Table S4. Intermolecular H···F contacts (Å) shorter than 2.67 Å (C–H bonds regularised to 1.08 Å)

| Compound | Contact | Symmetry transforma-tion for the F atom | Distance, Å |
| --- | --- | --- | --- |
| 1 | H(12)···F(3) | x – ½ , y – ½ , z | 2.52 |
|  | H(13)···F(4) | x – ½ , y – ½ , z | 2.61 |
| 2 | H(14)···F(3) | 1 – x, y, ½ – z | 2.64 |
|  | H(14)···F(4) | 1 – x, 1 – y, 1 – z | 2.49 |
|  | H(15)···F(2) | 1 – x, y, ½ – z | 2.45 |
|  | H(16)···F(2) | 1 – x, –y, 1 – z | 2.63 |
| 3 | H(8)···F(4) | 1 – x, 2 – y, 1 – z | 2.52 |
|  | H(9)···F(2) | x + 1, y + 1, z | 2.66 |
|  | H(9)···F(3) | 1 – x, 2 – y, 1 – z | 2.53 |
|  | H(12)···F(6) | 1 – x, 2 – y, 2 – z | 2.58 |
|  | H(13)···F(1) | 1 – x, 1 – y, 2 – z | 2.65 |
|  | H(13)···F(5) | 1 – x, 2 – y, 2 – z | 2.68 |
| 4 | H(13)···F(2) | 1 – x, 2 – y, –z | 2.64 |
|  | H(14)···F(2) | 1 – x, ½ + y, ½ – z | 2.63 |
| 5 | H(14)···F(2) | x, ½ – y, ½ + z | 2.65 |
|  | H(15)···F(1) | x, ½ – y, ½ + z | 2.51 |
|  | H(20)···F(5) | x, ½ – y, z – ½ | 2.57 |
|  | H(21)···F(4) | x, ½ – y, z – ½ | 2.57 |

Table S5. Calculated atomic coordinates in structure 1.

Atom		x/a		y/b		z/c

C(1)	0.50000000	0.11778826	0.75000000

C(2)	0.55740226	0.16920610	0.64586731

C(3)	0.55794841	0.27092914	0.64662205

C(4)	0.50000000	0.32241155	0.75000000

F(1)	0.50000000	0.01898256	0.75000000

F(2)	0.61298239	0.12022346	0.54294936

F(3)	0.61652787	0.31980172	0.54710055

F(4)	0.50000000	0.42120119	0.75000000

C(11)	0.27004878	0.11810321	0.44939334

C(12)	0.21144263	0.07220880	0.55624353

C(13)	0.15764461	0.12775094	0.66368566

C(14)	0.16312611	0.22836257	0.66261253

C(15)	0.22284376	0.27819235	0.55461214

H(11)	0.31185117	0.07606518	0.36466320

H(12)	0.20620032	–0.00760464	0.55891338

H(13)	0.11174476	0.09004337	0.74819905

H(14)	0.12192792	0.27058853	0.74722557

Table S6. Calculated atomic coordinates in structure 2.

Atom		x/a		y/b		z/c

C(1)	0.50000000	0.11716089	0.75000000

C(2)	0.53701099	0.17385103	0.66204155

C(3)	0.53692844	0.28726766	0.66177091

C(4)	0.50000000	0.34388742	0.75000000

F(1)	0.50000000	0.00681201	0.75000000

F(2)	0.57307657	0.11817236	0.57686186

F(3)	0.57257555	0.34272760	0.57573894

F(4)	0.50000000	0.45424679	0.75000000

C(11)	0.24829505	0.36449783	0.51242163

C(12)	0.28476158	0.31678974	0.41520110

C(13)	0.32159687	0.38151716	0.32969939

C(14)	0.35781930	0.33341539	0.23608959

C(15)	0.35938781	0.21790703	0.22247892

C(16)	0.32529040	0.15235359	0.30397984

C(17)	0.28684553	0.19929165	0.40225811

H(11)	0.24770621	0.45342389	0.52273074

H(13)	0.32137365	0.47031909	0.34186468

H(14)	0.38690105	0.38405349	0.17301895

H(15)	0.38844855	0.18210521	0.14678997

H(16)	0.32731250	0.06334096	0.29481785

Table S7. Calculated atomic coordinates in structure 4.

Atom		x/a		y/b		z/c

C(1)	1.01307469	0.39760518	0.51880421

C(2)	0.92209298	0.43769340	0.38077848

C(3)	0.90870344	0.53988904	0.36204290

F(1)	1.02491551	0.29823576	0.53726918

F(2)	0.84732906	0.37712213	0.26432611

F(3)	0.81843956	0.57842320	0.22792124

C(11)	0.38526348	0.42632943	0.32638174

C(12)	0.28635573	0.44451174	0.17730665

C(13)	0.24867530	0.54107984	0.12549883

C(14)	0.30794307	0.62156359	0.21976453

C(15)	0.40981243	0.60718682	0.36932012

C(16)	0.44924549	0.50837277	0.42411060

C(17)	0.42461705	0.32843675	0.38529331

C(18)	0.47670204	0.68757132	0.47007200

H(12)	0.23758682	0.38216389	0.10179959

H(13)	0.17118536	0.55373245	0.00954952

H(14)	0.27442261	0.69674339	0.17734269

H(17)	0.37346514	0.26536007	0.31219005

H(18)	0.44739405	0.76334526	0.42903800

Table S8. Calculated atomic coordinates in structure 5.

Atom		x/a		y/b		z/c

C(1)	0.20707862	0.45443343	0.49927186

C(2)	0.29952917	0.52006333	0.49840737

C(3)	0.34568111	0.57825625	0.56581125

C(4)	0.30001809	0.56643538	0.63401154

C(5)	0.20844556	0.49640404	0.63510849

C(6)	0.16160321	0.44167804	0.56758620

F(1)	0.16140644	0.40065892	0.43371050

F(2)	0.34435576	0.52801295	0.43208022

F(3)	0.43531267	0.64414674	0.56520603

F(4)	0.34460576	0.62398259	0.69932686

F(5)	0.16491467	0.48340922	0.70169350

F(6)	0.07157557	0.37788313	0.56826698

C(11)	0.43635759	0.16509566	0.60545720

C(12)	0.48140908	0.22318202	0.67262181

C(13)	0.43493661	0.20898854	0.74098829

C(14)	0.34465835	0.13567452	0.74068993

C(15)	0.15437466	-0.02614767	0.74181879

C(16)	0.06327139	-0.09525008	0.74248646

C(17)	0.01591092	-0.14499228	0.67387121

C(18)	0.06049142	-0.12512211	0.60611362

C(19)	0.15741046	-0.09291805	0.46205380

C(20)	0.20247906	-0.07954499	0.39399827

C(21)	0.29497982	-0.01100012	0.39387446

C(22)	0.34016787	0.04354131	0.46168562

C(23)	0.34400577	0.09006499	0.60326081

C(24)	0.29715692	0.07385393	0.67291182

C(25)	0.20154401	-0.00303168	0.67327827

C(26)	0.15377931	-0.05571487	0.60367755

C(27)	0.20174082	-0.03849403	0.53205974

C(28)	0.29569634	0.03227949	0.53187627

H(11)	0.47434114	0.18121017	0.55313355

H(12)	0.55261845	0.28168336	0.67204269

H(13)	0.47037674	0.25519436	0.79412926

H(14)	0.30982490	0.12670955	0.79469411

H(15)	0.19014011	0.01018912	0.79604670

H(16)	0.02798981	-0.11135461	0.79610579

H(17)	-0.05588888	-0.20087542	0.67398214

H(18)	0.02162744	-0.16468955	0.55351342

H(19)	0.08571031	 -0.14932924	0.46062758

H(20)	0.16528216	-0.12070756	0.34088642

H(21)	0.33191407	-0.00139210	0.34076759

H(22)	0.41199042	0.09844873	0.45993892