# Supplementary Material (ESI) for New Journal of Chemistry

# This journal is © The Royal Society of Chemistry and 

# The Centre National de la Recherche Scientifique, 2003


[image: image1.wmf]-10

-5

0

5

10

 

 

 

 

Relative Intensity

Velocity (mm s

-1

)

Supplementary information

Mössbauer spectrum of as-prepared (-Fe2O3 nanowires.

The hyperfine parameters in Mössbauer spectrum are ( = 0.328 mm/s, <QS> = 1.032 mm/s, which are typical of iron(III). No peak characteristic of Fe(II) is present in the spectrum.
� EMBED Origin50.Graph  ���








[image: image2.wmf]-10

-5

0

5

10

 

 

 

 

Relative Intensity

Velocity (mm s

-1

)

_1101541265.bin

