Supplementary material

A unique methoxo-fluoro-bridged triangular trinuclear Cu(II) species linked in a lattice via mononuclear Cu(II) units. Synthesis, X-ray structure and magnetism of [Cu4(2-aminopyrimidine)6(μ3-OCH3)2(μ-F)3(F)2](BF4).

G.A.van Albada, O. Roubeau, I. Mutikainen,  U. Turpeinen and J. Reedijk.

Supplementary fig.1

Fitting according to scheme 2A (Trimer (one J) +  monomer)

Result:  J = -54.9 cm-1, gtrimer = gmonomer = 2, p = 0

(O = observed parameters, solid line is fitting result)